## Slide 1
12/5/2022
Design of Precast, Prestressed Concrete Bridges
P r e s t r e s s e d C o n c r e t e B r i d g e D e s i g n W o r k s h o p
Richard Brice, PE
Washington State Department of Transportation December 7, 2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Participant Materials
Download from https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Slides
Design Example
Other supporting documents
2
1
10
2

## Slide 2: Introduction to Precast, Prestressed Concrete Design
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
3
Participant Materials
https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Prestressed Concrete
AASHTO LRFD Bridge Design Specifications
  Prestressed Concrete - Concrete components in which stresses and deformations are introduced by application of prestressing forces
  Post-Tensioning – A method of prestressing in which the tendons are tensioned after the concrete has reached a predetermined strength
  Pretensioning – A method of prestressing in which the strands are tensioned before the concrete is placed
ACI Committee on Prestressed Concrete
  Concrete in which there have been introduced internal stresses of such magnitude and distribution that the stresses resulting from given external loadings are counteracted to a desired degree. In reinforced-concrete members the prestress is commonly introduced by tensioning the steel reinforcement.
4
3
10
4

## Slide 3: Prestressed Concrete
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
5
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Post-tensioned Concrete
6
5
10
6

## Slide 4: Stress Distribution
12/5/2022
7
e
P/A
Pey/
I
My/I
P/A + Pey/I + My/I
+ + =
Direct prestress Eccentric prestress External load Resultant stress profile
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
M
P
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Load and Resistance Factor Design (LRFD)
8
7
10
8

## Slide 5: Applicable Limit States
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
AASHTO LRFD Bridge Design Specifications 9th Edition, 2020
– ∑ 𝛾i𝑄i = 𝑳𝒐𝒂𝒅, 𝑸 ≤ 𝑹𝒆𝒔𝒊𝒔𝒕𝒂𝒏𝒄𝒆, 𝑹 = 𝜙𝑅n
Service Limit State (Service I, Service III)
  Stresses
  Camber and Deflection
  Cracking
Strength Limit State (Strength I)
  Flexural Strength
  Shear Strength
Fatigue Limit State (Fatigue I)
  Cyclical stress range
9
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Materials
10
9
10
10

## Slide 6: Materials
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop 11
Reinforcing steel
Prestressing strand
Girder concrete
Epoxy coated reinforcing steel
CIP deck concrete
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Reinforcing Steel
LRFD 5.4.3
Deformed bars, welded wire mesh
ASTM A615, A706, A1035
Yield strength, 𝑓y, 60-100 ksi
Modulus of Elasticity, 𝐸e = 29000 𝑘𝑠𝑖, LRFD 5.4.3.2
12
11
10
12

## Slide 7: Prestressing strand
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
LRFD 5.4.4
Carbon Steel - ASTM A416
7-wire strand
Grade 250, 270, 300
Stress Relieved, Low Relaxation
0.375” - 0.6” + 0.62” & 0.70”
Modulus of Elasticity, 𝐸e = 28500 𝑘𝑠𝑖, LRFD 5.4.4.2
High yield and ultimate strength
Less ductility than reinforcing bars
– Fraction strain 3.5% compared to 9-11%
13
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Corrosion resistant strand
Stainless steel
  Grade 250 ksi
  Elongation 1.2%-2.0% (Compared to > 3.5% for A416)
  E = 24,500 ksi (compared to 28,500 ksi for A416)
Carbon fiber reinforced polymer (CFRP)
  Elongation 1.7%
– E = 17,000 ksi
Epoxy Coated
14
13
10
14

## Slide 8: Concrete
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
LRFD 5.4.2
Normal and Lightweight Concrete
e e
Modulus of elasticity 𝐸e = 120,000𝐾1𝑤2𝑓,o.33
– LRFD 5.4.2.4
Girder Concrete (HSC)
ei
– Initial strength, 𝑓, = 4 − 7.5 𝑘𝑠𝑖
– Final strength, 𝑓, = 5 − 15 𝑘𝑠𝑖
e
Deck Concrete (NSC)
– Initial strength, 𝑓, ≈ 0.8𝑓,
ei e
e
– Final strength, 𝑓, = 4 − 5 𝑘𝑠𝑖
fl
LRFD 5.4.2.8
Density Modification Factor
𝜆 = 4.7fct ≤ 1.0,
c
– 𝑓et splitting tensile strength
0.75 ≤ 𝜆 = 7.5𝑤e ≤ 1.0
et
– when 𝑓 is not specified
15
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Design Example
16
15
10
16

## Slide 9: Design Example
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Based on WSDOT’s BridgeLink::PGSuper validation example
“Hand” calculations that illustrate how the software is performing engineering analysis
Download BridgeLink™ from https://www.wsdot.wa.gov/eesc/bridge/software
Google “PGSuper Download” or “BridgeLink Download”
BridgeLink suite is Open Source Software
Jointly developed by WSDOT and TxDOT
Source code available on GitHub (https://github.com/WSDOT)
17
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Design Example
6-WF74G Girders – 7ft Spacing
165 ft nominal span
Horizontal & Vertical Curves
4% Superelevation
7.5” Deck, 𝑓, = 4 𝑘𝑠𝑖
e
42’ Out-to-Out
0.5” sac depth
35 psf future overlay
42” Single Slope Barrier
18
17
10
18

## Slide 10: Alignment/Profile
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
19
Length
PVI Elevation Grade in 𝐠𝟏
100.00 -2%
Grade out (𝐠𝟐)
-1.5%
600 ft
Alignment
PI Station Back Tangent Delta Radius
10+00 N 34° 45’ 32” W 12° 34’ 15” R 6000 ft
Profile
PVI
Station
9+00
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Bridge Layout
Back of Pavement Seat, Abutment 1, 7+00
Back of Pavement Seat, Abutment 2, 8+65
Abutments are oriented at S 58° 41, 13.47" W
Abutment 1, Skew Angle 0°
Abutment 2, Skew Angle 1° 34, 32.28" L
20
19
10
20

## Slide 11: Design Objectives
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Determine
ei e
Minimum required initial and 28-day design concrete strengths (𝑓, , 𝑓,)
Prestressing
Slab haunch build up (“A” Dimension)
Stirrup Arrangement
Perform load rating analysis
21
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Assumed Construction Sequence
22
21
10
22

## Slide 12: WSDOT Design Criteria
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Stress analysis based on gross section properties
Prestress losses – LRFD refined method + elastic gains
Envelope of simple span and simple span made continuous
Zero tension in Service III limit state
Service III Live Load Factor = 0.8
Design for lateral stability using PCI recommended practice
Flexural strength by strain compatibility analysis
Shear strength MCFT General Procedure
23
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
24
Item Compression Tension
Upward Deflection Downward Deflection Top Section Modulus Bottom Section Modulus
Strand Eccentricity above Centroid Strand Eccentricity below Centroid
Value
< 0
> 0
> 0
< 0
< 0
> 0
< 0
> 0
𝑓 = + +
𝑃 𝑃𝑒 𝑀
𝐴 𝑆 𝑆
Sign Convention
Based on “A simple sign convention for elastic analysis of prestressed concrete members”, Stanton, PCI Journal, Nov-Dec 2007
23
10
24

## Slide 13: Geometrics
12/5/2022
R n 6ooo n
Chord Length: 2𝑅 𝑠𝑖𝑛 8 = 2 6000 𝑠𝑖𝑛 1.575634 = 164.995 𝑓𝑡
2 2
s
2.7o83ft = 159.578𝑓𝑡
eo s 1.575634
Brg-to-Brg Span:𝐿 = 164.995𝑓𝑡 − 2.7083𝑓𝑡 −
Girder Length: 𝐿g = 159.577𝑓𝑡 + 1.7083𝑓𝑡 + (1.7083𝑓𝑡)/𝑐𝑜𝑠(1.575634) = 162.995𝑓𝑡
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop 25
q
BPS CL Brg CL Brg BPS
1.7083'
2.7083'
Radial at 8+65
Radial at 7+00
Parallel lines
164.995'
BPS-to-BPS Arc Length: 165 ft
Subtended angle: 𝛿 = L c 18o = 165 18o = 1.575634°
q
d2
d2 = d1/cosq q = 1.575634°
2' - 8.5"
1' - 8.5"
Back of Pavement Seat
CL Brg
Dimensions measured normal to BPS
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Section Properties
26
25
10
26

## Slide 14: Section Properties
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
LRFD 5.9.1.3 – Section properties may be based on either gross or transformed sections
Gross properties
  Concrete outline of bare girder
Composite Properties
  Deck concrete transformed to girder concrete
Transformed Properties
  Reinforcement is transformed to girder concrete
Transformed Composite Properties
  Deck and reinforcement transformed to girder concrete
27
38.343"
35.657"
74"
25.113"
CompositeCG
81"
NoncompositeCG
48.867"
83.99"
0.725(83.99")
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Effective Flange Width
LRFD 4.6.2.6.1
Effective Flange Width = Tributary Width
  Skew less that 75 degrees
– L/S > 2.0
  Overhang less than S/2
28
27
10
28

## Slide 15: Section Properties
12/5/2022
Participant Materials
https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
29
 | Girder | Composite Girder
Area, 𝐀 | 2 923.531 in | 2 1349.614 in
𝐈𝐱 | 4 734356.0 in | 4 1246570.6in
𝐈𝐲 | 4 72018.4 in | -
𝐘𝐭𝐨𝐩 𝐠𝐢𝐫𝐝𝐞𝐫 | 38.343 in | 25.113 in
𝐘𝐭𝐨𝐩 𝐬𝐥𝐚𝐛 | - | 32.116 in
𝐘𝐛 | 35.657 in | 48.867 in
𝐒𝐭𝐨𝐩 𝐠𝐢𝐫𝐝𝐞𝐫 | 3 -19152.5 in | 3 -49599.7 in
𝐒𝐭𝐨𝐩 𝐬𝐥𝐚𝐛 | - | 3 -53531.9 in
𝐒𝐛 | 3 20594.8 in | 3 25509.3 in
𝐐𝐬𝐥𝐚𝐛 | - | 3 12199.9 in
𝐖𝐞𝐟𝐟 | - | 83.992 in
Perimeter | 289.284 in | -
WSDOT: Deck is directly on top of girder (no haunch)
,
Assume 𝑓e = 8.7 𝑘𝑠𝑖
2 o.33
Deck: 𝐸e = 120,000 1.0 0.150 4.0 = 4266.2 𝑘𝑠𝑖
e
Beam: 𝐸 = 120,000 1.0 0.155 2 8.7 o.33 = 5886.9 𝑘𝑠𝑖
𝐸e beam
5886.9
𝐸e deek 4266.2
𝑛 = = = 0.725
83.99"
38.343"
35.657"
48.867"
74"
81"
NoncompositeCG
25.113"
CompositeCG
0.725(83.99")
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Loads and Load Distribution
30
29
10
30

## Slide 16: Load Analysis
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Approximate Method for Beam-Slab Bridges (LRFD 4.6.2.2)
  Girder Line Analysis
  2D Plane Frame Analysis
Dead Loads
  Distributed to individual girders
Live Load
  Distributed to girders with distribution factors, 𝑔
  𝑄per girder = 𝑔𝑄per lane
Key analysis points
Mid-span
Harping or Debonding Points
Prestress transfer 𝑙t = 60𝑑b
Lift & Bunk Points
Critical Section for Shear
Point loads
Cross section changes
31
Permanent Loads
Girder
  NWC 155 pcf (unreinforced), 165 pcf (reinforced)
  LWC 125 pcf (unreinforced), 135 pcf (reinforced)
Deck
  150 pcf (unreinforced), 155 pcf (reinforced)
  0.5” Sacrificial Wearing Surface
Intermediate and End Diaphragms
  155 pcf (reinforced)
Barriers
  42” Single Slope 690 plf, 42” F-Shape 730 plf
Future Overlay
  35 psf
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
32
31
10
32

## Slide 17: Permanent Load Distribution
12/5/2022
LRFD 4.6.2.2.1
  Where bridges meeting the conditions specified herein, permanent loads of and on the deck may be distributed uniformly among the beams
Slab, Haunch, and Diaphragms
  Tributary width
  Full haunch depth for DL
Barriers
  Equally to 3 exterior girders, or all girders if 6 or fewer
Overlay
  Uniform
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
33
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Live Loads
HL-93 Notional Live Load
  Design Truck + 0.640 klf lane load
  90% of 2-Design Trucks with min 50ft headway spacing + lane, for negative moment and interior pier reactions
Design Tandem
  2-25 kip axles at 4 ft apart + 0.640 klf lane load
  2-design tandems 26-40 ft spacing + lane for negative moment and interior pier reactions
Dynamic Load Allowance (Impact)
  Strength and Service, IM = 33%
  Fatigue, IM = 15%
34
0.640 KLF
8 KIP
32 KIP 32 KIP
14' - 30' 14'
0.640 KLF
4'
25 KIP
25 KIP
Design Truck + Lane Load
Design Tandem + Lane Load
33
10
34

## Slide 18: Live Load Distribution
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
LRFD 4.6.2.2
Live Load Distribution Factors
  Equations
    Section Type
    Interior & Exterior Girders
    Shear & Moment
  Lever Rule
  Skew Correction Factors
  Range of Applicability
Type (k) for design example
35
Participant Materials
https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Design Moments
36
Loading | Transfer Point | Harp Point | Mid-Span
Girder | 253.96 k · ft | 3373.66 k · ft | 3514.22 k · ft
Loading | 0.5Ls
Girder after erection | 3368.43 k · ft
Diaphragm | 140.14 k · ft
Slab | 2465.61 k · ft
Haunch | 760.28 k · ft
Traffic Barrier | 732.12 k · ft
Future Overlay | 739.63 k · ft
*Design LLIM (HL-93) | 5485.09 k · ft
*Fatigue LLIM | 2686.86 k · ft
At Release
At Bridge Site
*Live load moments are per lane
Distribution Factor | 1 Loaded Lane | 2+ Loaded Lanes | Controlling Factor
Moment (𝐠𝐌) | 0.694 | 0.648 | 0.694
Shear (𝐠𝐕) | 0.694 | 0.744 | 0.744
Distribution Factor | 1 Loaded Lane
Moment (𝐠𝐌) | 0.694
Shear (𝐠𝐕) | 0.694
Strength and Service Limit States
Fatigue Limit State
𝑀 =
𝑤𝐿2 8
𝑤𝑥
2
𝑀 = 𝑙 − 𝑥
35
10
36

## Slide 19: Flexure Design
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
37
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Flexure Design
Service Limit State
P
pe
pe
P e
M
nc
Anc snc snc
M
c
sc
– Concrete stresses less than limit, 𝑓 = + + + ≤ 𝑓
limit
P
pe
Aps
limit
Strand stress less than limit, 𝑓 = ≤ 𝑓
Anchorage zone criteria
Fatigue Limit State
  Cyclical stresses less than limit
Strength Limit State
  Sufficient strength
– 𝑀u ≤ 𝑀r = 𝜙𝑀n
38
37
10
38

## Slide 20: Concrete Stress Limits
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
39
Stage
Initial (5.9.4.1)
Limit State
Service I
Limit Type Limit
Tension
ei
0.0948𝜆 𝑓, ≤ 0.200 𝑘𝑠𝑖 w/o rebar
ei
0.24𝜆 𝑓, 𝑘𝑠𝑖 w/ rebar
ei
0.65𝑓,
Erection
(WSDOT)
Service I
0.19𝜆
e
𝑓,
e
0.45𝑓,
Final (5.9.4.2)
Service I
Compression Tension
Compression Compression
0.45𝑓, 𝑤𝑖𝑡ℎ𝑜𝑢𝑡 𝐿𝐿 ,
e
0.60𝑓,(𝑤𝑖𝑡ℎ 𝐿𝑖𝑣𝑒 𝐿𝑜𝑎𝑑)
Service III
Tension
e
0.0 𝑘𝑠𝑖 (𝑊𝑆𝐷𝑂𝑇)
e
0.19𝜆 𝑓, ≤ 0.6𝑘𝑠𝑖
e
0.0948𝜆 𝑓, ≤ 0.3𝑘𝑠𝑖
Fatigue (5.5.3.1)
Fatigue I + 0.5(Dead+PS)
Compression
e
0.40𝑓,
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Principal Tension Stress in Web
LRFD 5.9.2.3.3
Applicable to pretensioned concrete
e
when 𝑓, > 10.0 𝑘𝑠𝑖
e
𝑓 ≤ 0.100𝜆 𝑓, for the Service III load
combination
40
39
10
40

## Slide 21: PS Steel Stress Limits
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
LRFD 5.9.3
Immediately prior to transfer, 0.75𝑓pu
  Requires jacking beyond 0.75𝑓pu to compensate for relaxation
  WSDOT
    𝑓pj ≤ 0.75𝑓pu
    Relaxation between stressing and release
At service limit state after all losses, 0.80𝑓py
41
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
How much prestress?
Excessive prestress can develop high tension stresses in the top flange and compression stresses in the bottom flange leading to end region cracking and high initial strength requirements.
Insufficient prestressing can result in tension stresses in the bottom flange at mid-span leading to cracking under service loads and serviceability issues.
42
f’ci
Tension
Compression
f’c
Compression
Initial Conditions
Tension
Service Conditions
41
10
42

## Slide 22
12/5/2022
Design Procedure
1) Design for final service conditions Number of permanent strands
2) Design for initial lifting w/o TTS Lifting embedment locations
Arrangement of permanent strands Greatest strength at lifting (f’ci)
3) Design for hauling
Hauling setup & trucking requirements Temporary strand requirements Strength at hauling (f’c)
TTS
Required?
4) Design for initial lifting w/ TTS Lifting embedment locations Least strength at lifting (f’ci)
7) Check design for final strength and
service conditions
Yes
No
5) Refine hauling design
Check stress and FS limits using updated losses and fpe.
Revise as needed per Step 3 procedure
Based on Design optimization for fabrication of pretensioned concrete bridge girders: An example problem, Brice, et. al. PCI Journal Fall 2009
TTS = temporary top strands
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
6) Check erection stress (WSDOT)
43
Why design for stability?
AASHTO LRFD requirements
  2.5.3 – Constructability issues should include, but not be limited to, consideration of deflection, strength of steel and concrete, and stability during critical stages of construction.
  5.5.4.3 – Buckling and stability of precast members during handling, transportation, and erection shall be investigated.
Engineering for Constructability – not construction engineering
EOR should be reasonably satisfied that girders can be safety fabricated, lifted, transported, and erected.
Avoid design modifications under contract
Designing Precast, Prestressed Concrete Bridge Girders for Lateral Stability: An Owner’s Perspective, Brice, R., ASPIRE, Winter 2018
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
44
43
10
44

## Slide 23: Step 1 – Final Service Conditions
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Establish permanent prestressing
Stress due to loads on non-composite and composite section
– Girder, Diaphragms, Slab, Haunch, Barrier, Overlay, Live Load, Slab Shrinkage
– 𝑓ps + 𝑓servieelll = 0.0 𝑘𝑠𝑖
Slab Shrinkage
∆𝑓psD + ∆𝑓pCD + ∆𝑓pR2 − ∆𝑓pss df
– ∆𝑓pT = ∆𝑓pEs + ∆𝑓pLT
– ∆𝑓pLT = ∆𝑓psR + ∆𝑓pCR + ∆𝑓pR1 id +
E
p
Ec
pss edf df
𝐾 1 + 0.7𝜓 𝑡 , 𝑡
f d
– ∆𝑓 = ∆𝑓
– Δ𝑓edf=change in concrete stress at centroid of prestressing strands due to shrinkage of deck concrete
45
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Slab Shrinkage
∆𝑃ds =
Δ𝑓edf = change in concrete stress at centroid of prestressing strands due to shrinkage of deck concrete
Shrinkage of deck concrete also causes change in stress at bottom of girder
Treat as external load at CG of deck,
−𝜀ddf𝐴d𝐸edeek
1 + 0.7𝜓 𝑡 , 𝑡
d f d
Stress in girder concrete due to deck shrinkage,
𝑓ss = ∆𝑃ds
1 𝑒d
𝐴e + 𝑆e
46
45
10
46

## Slide 24: Creep [LRFD 5.4.2.3.2]
12/5/2022
i
V
s
Increase in strain due to a sustained stress
Creep coefficient = creep strain / initial strain
𝜓 𝑡, 𝑡i = 1.9𝑘s𝑘he𝑘td𝑡-o.118
𝑘s factor for effects of volume to surface area ratio, 𝑘s = 1.45 − 0.13 ≥ 1.0
𝑘he humidity factor for creep,𝑘he = 1.56 − 0.008𝐻
𝑘f factor for the effect of concrete strength, 𝑘f =
5
ci
1+fl
𝑘td time development factor, 𝑘td =
12
t
100-4 l
l
fci+20
ci +t
𝑡 mature of concrete = age of concrete between time of loading and time under consideration (duration load is applied)
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
47
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
e
,,
Age Adjusted Elastic Modulus
E
c
1+Xl/J
48
𝐸 =
Aging factor
  𝜒 = 0.7 for slowly developing loads
  𝜒 = 1.0 for instantaneous loads Ec
Stress
Strain, e
Initial (Elastic) Strain, e
Creep Strain, cye
Total Strain, e+cye=e(1+cy)
E’’c
47
10
48

## Slide 25: Slab Creep Coefficient
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
s
V
s s
ei e f
V = 4.15 𝑖𝑛, 𝑘 = 1.45 − 0.13 = 0.91 < 1.0 ∴ 1.0
𝑘he = 1.56 − 0.008𝐻 = 0.96 (𝐻 = 75%)
𝑓, = 0.8𝑓, = 0.8 4𝑘𝑠𝑖 = 3.2𝑘𝑠𝑖, 𝑘 =
5
ci
1+fl
= 1.19
𝑡 = 𝑡f − 𝑡d = 2000 − 120 = 1880 𝑑𝑎𝑦𝑠, 𝑘td =
t
12
100-4fl
l
fci+20
ci +t
= 0.978
𝑡i = 1 𝑑𝑎𝑦
𝜓d 𝑡f, 𝑡d = 1.9 1.0 0.96 (1.19) 0.978
1 -o.118 = 2.12
49
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Shrinkage [LRFD 5.4.2.3.3]
Volumetric change due to autogenous (chemical process of hydration) and drying shrinkage
𝜀sh = 𝑘s𝑘hs𝑘f𝑘td 0.48𝑥10-3
𝑘hs humidity factor for shrinkage, 𝑘hs = 2.00 − 0.014𝐻
Other parameters same as for creep
50
49
10
50

## Slide 26: Slab Shrinkage Strain
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
𝑘hs = 2.00 − 0.014𝐻 = 0.95 (𝐻 = 75%)
𝐾sh = 0.5 (WSDOT uses 50% slab shrinkage strain)
•
𝜀ddf =
0.5 1.0 0.95 1.19 0.978 0.48 × 10-3 = 0.265 × 10-3
51
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Deck shrinkage force
ds
1+o.71/d tf,td
ds
-3 2
1+o.7 2.12
∆𝑃 = -c:ddfAdEc deck
𝜀ddf= deck shrinkage between deck placement and final time
𝐴d= area of deck including sacrificial depth
𝐸e deek/ 1 + 0.7𝜓d 𝑡f, 𝑡d = age adjusted modulus of elasticity of deck concrete between time of deck casting and final time
𝐴d = 681.165 𝑖𝑛2
𝐸e deek = 4266.223 𝑘𝑠𝑖
Δ𝑃 = -o.265×1o 681.165i 4266.223ksi = −310.0 𝑘𝑖𝑝
52
ed
ComposteCGi
DPds
51
10
52

## Slide 27: Stress in girder concrete
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Stress in girder concrete due to deck shrinkage
1 + ed
Ac sc
– 𝑓ss = ∆𝑃ds
– 𝐴e = 1349.614 𝑖𝑛2, 𝑆tge = −49599.7 𝑖𝑛3, 𝑆be = 25509.3 𝑖𝑛3
– 𝑒d = − 𝑌tge
2 2
tgross slab depth
+ = − 25.133 + 7.5 = −28.883 𝑖𝑛
ss
Top of girder 𝑓 = (−310.0𝑘𝑖𝑝)
1 -28.883in
1349.614in2 -49599.7in3
+ = −0.410 𝑘𝑠𝑖
ss
Bottom of girder 𝑓 = −310.0𝑘𝑖𝑝
1
+ -2 .883in
1349.614in2 255o9.3in3
= 0.121 𝑘𝑠𝑖
53
Participant Materials
https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Dead & Live Load Stress
s
t b tge
𝑓 = M , 𝑆 = −19152.5𝑖𝑛3, 𝑆 = 20594.8 𝑖𝑛3, 𝑆 = −49599.7𝑖𝑛3, 𝑆
bg
= 25509.6𝑖𝑛3
54
Load | Moment (k-ft) | 𝒇𝒕 𝒌𝒔𝒊 | 𝒇𝒃 𝒌𝒔𝒊
Girder | 3368.43 | -2.110 | 1.963
Diaphragms | 140.17 | -0.088 | 0.082
Slab | 2465.61 | -1.545 | 1.437
Haunch | 760.28 | -0.476 | 0.443
Barrier | 732.12 | -0.177 | 0.344
Future Overlay | 739.63 | -0.179 | 0.348
Design (HL-93) | (0.694)(5485.09)=3804.05 per girder | -0.920 | 1.789
Fatigue | (0.694)(2686.86)=1863.40 per girder | -0.451 | 0.877
53
10
54

## Slide 28: Estimate Prestress
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
𝑆𝑒𝑟𝑣𝑖𝑐𝑒 𝐼𝐼𝐼 = 1.0𝐷𝐶 + 1.0𝐷𝑊 + 0.8(𝐿𝐿 + 𝐼𝑀)
𝑓b = 6.169𝑘𝑠𝑖
𝑓b + 𝑓ps = 0.0 𝑘𝑠𝑖 (0 ksi per WSDOT)
Assume resultant prestress force 3” above bottom of girder
– 𝑒 = 𝑌b − 3 𝑖𝑛 = 35.657 − 3 = 33.657 𝑖𝑛
ps
P P e P
pe pe pe
pe
P 33.657
A s 923.531 2o594.8
pe
+ = 0𝑘𝑠𝑖 − 6.169𝑘𝑠𝑖, 𝑃 = −2270.5 𝑘𝑖𝑝
𝑓 = + =
𝑃pe = 𝑁𝑎ps𝑓pe , 𝑓pe = 1 − 𝑙𝑜𝑠𝑠 𝑓pj = (1 − 𝑙𝑜𝑠𝑠)0.75𝑓pu , Assume 15% loss
– 2270.5 𝑘𝑖𝑝 = 𝑁 0.217𝑖𝑛2 1 − 0.15 0.75 270𝑘𝑠𝑖 , 𝑁 = 60.8 → 𝑁 = 61
– 𝑃 = 61 0.217 1 − 0.15 0.75 270 = 2278.4 𝑘𝑖𝑝
55
Check Concrete Strength
Top girder stress due to prestress
–
923.531in2 -2o594.8in3
𝑓ps = -2278.4kip + -22 .4kip 33.657in = 1.256𝑘𝑠𝑖
Top girder stress Service I with live load
– 𝑓t = −5.905 𝑘𝑠𝑖
e
o.6
– −0.6𝑓, = 1.256 − 5.905 = −4.649 𝑘𝑠𝑖 𝑓, = − 4.649 = 7.75 𝑘𝑠𝑖
e
Top girder stress Service I without live load
– 𝑓t = −4.985 𝑘𝑠𝑖
e e
Top girder stress Fatigue I 0.5𝐷𝐶 + 0.5𝐷𝐶 + 1.5𝐿𝐿𝐼𝑀
– 𝑓t = −3.282 𝑘𝑠𝑖
e
Participant Materials
e
https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
– −0.40𝑓, = 0.5 1.256 − 3.282 = −2.618 𝑓, = 6.55 𝑘𝑠𝑖
56
– −0.45𝑓, = 1.256 − 4.985 = −3.729 𝑘𝑠𝑖 𝑓, = 8.29 𝑘𝑠𝑖 < 8.7 𝑘𝑠𝑖
55
10
56

## Slide 29: Step 2 – Lifting without TTS
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
ei
ei
Proportion Strands
Start with 2 Straight : 1 Harped (40s : 21h)
Compute required 𝑓, at harp point
Reduce # harped and increase # straight until required 𝑓, at transfer length is equal
ei
to required 𝑓, at harp point
57
ee=-26.813in
eh=30.775in
CGGirder
Ns=44
e=31748ni.s
Nh=17
Harp point Transfer point
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Transfer Length
58
LRFD 5.9.4.3.1
The length over which the pretensioning force is transferred to the concrete by bond and friction in a pretensioned member
𝑙t = 60𝑑b
𝑓 linearly increases from 0 to 𝑓pe 𝑓 = 𝑓pe
𝑓 = 0
57
10
58

## Slide 30: Prestress Losses
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
59
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Prestress Losses
Initial jacking force is reduced over time due to losses
Initial and Long-Term Time Dependent
𝑓pe = 𝑓pj − ∆𝑓pF − ∆𝑓pAs − ∆𝑓pEs − ∆𝑓pLT
Friction
Anchor Set
Elastic Shortening
Creep of Concrete
Shrinkage of Concrete
Relaxation of Prestressing Steel
60
Prestress Losses (5.9.3)
Instantaneous (5.9.3.2)
Anchor Set (5.9.3.2.1)
Friction (5.9.3.2.2)
Elastic Shortening
(5.9.3.2.3)
Time Dependent
Creep
Shrinkage
Relaxation
Approximate (5.9.3.3)
Refined (5.9.3.4)
Time Step (5.9.3.5)
59
10
60

## Slide 31: Pretension Losses
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Initial Relaxation
Elastic Shortening
Creep & Shrinkage
Relaxation
61
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Initial Relaxation
pRo
𝑓pj = 0.75𝑓pu
𝑓pe = 𝑓pj − ∆𝑓pRo immediate before release
∆𝑓 =
4o.o
log(24.ot) f
pj
fpy
− 0.55 𝑓
pj
∆𝑓
pRo
4o 243.oksi
= log(24.o·1day) 2o2.5ksi − 0.55
202.5𝑘𝑠𝑖 = 1.980 𝑘𝑠𝑖
This is intrinsic relaxation – no reduction in length while stressed
– Other relaxation losses are for reduced relaxation
62
61
10
62

## Slide 32: Elastic Shortening
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
– 𝑓
egp = A
P + Pe
𝑓egp change in concrete stress at level of strands
2
l
−
Mge
l
𝑃 force in strands after elastic shortening
– 𝑃 =
𝑁strand 𝑎ps 𝑓pj − ∆𝑓pRo − ∆𝑓pEs
Change in strand stress
– ∆𝑓 = Ep 𝑓
pEs Eci egp
63
Participant Materials
https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Elastic Shortening
Assume 10% loss for first guess of P
𝑃 = 61 0.217 0.9 202.5 = 2412.4 𝑘𝑖𝑝
𝑓
egp
= 2412.4 kip + 2412.4kip 31.477in 923.531in2 734356.oi 4
−
2 3514.22k·ft
12in 1ft
31.477in
734356.oi 4
= 4.059 𝑘𝑠𝑖
pEs
285ooksi
558o.731ksi
4.059𝑘𝑠𝑖 = 20.68𝑘𝑠𝑖
∆𝑓 =
𝑃 = 61 0.217𝑖𝑛2 202.5𝑘𝑠𝑖 − 1.98𝑘𝑠𝑖 − 20.68𝑘𝑠𝑖 = 2380.5 𝑘𝑖𝑝
Try again with 𝑃 = 2380.5 𝑘𝑖𝑝 and repeat until converted
64
Location | Effective Prestress after release, P | ∆𝒇𝒑𝑬𝑺
PSXFR | 2423.16 𝑘𝑖𝑝 | 17.461ksi
HP | 2380.27 𝑘𝑖𝑝 | 20.701ksi
0.5Lg | 2384.47 𝑘𝑖𝑝 | 20.384ksi
11% loss
63
10
64

## Slide 33: Lifting Analysis
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Location of center of mass
Compute equilibrium roll angle
Compute stresses
Compute concrete strength to satisfy compression stress limit
Check FS cracking
Check FS failure
After many iterations
– Lift points at 11 ft
–
ei
𝑓,
= 7.4 𝑘𝑠𝑖
65
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Rigid body roll + increased roll due to lateral deflections
Equilibrium when resultant weight is directly beneath the roll axis
Girder Stability Basics
Hanging Girder Seated Girder
Rigid body roll + increased roll due to lateral deflections
Roll is resisted by rotational stiffness of support
66
65
10
66

## Slide 34: Lifting Stability Design Criteria
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Stress limits
ei
– Tension 0.24𝜆 𝑓, ,
– Compression 0.65𝑓, CL, 0.70𝑓, Corners
ei ei
Factor of Safety 1.0 Cracking & 1.5 Failure
67
Participant Materials
https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Horizontal Location Center of Mass
1
Lift device eccentricity 𝑒lift = 0.25 𝑖𝑛
Sweep Δsweep = 𝑖𝑛 𝑝𝑒𝑟 10 𝑓𝑡 = 2.037 𝑖𝑛
8
L
g
2
Ls 1
− = 0.415
3
Offset Factor, 𝐹o =
𝑒i = 0.25 + 0.415 2.037 = 1.095 𝑖𝑛
68
Dsw | eep
a
a
Ls
esweep=F
oDsweep
Centerline
RolAxsil
Plan View
Section at Lift Point
elift
esweep
ei
67
10
68

## Slide 35: Camber
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
69
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Camber – Girder Deflection
24Ecilx
g1 s
s
∆ = wga 3𝑎2 𝑎 + 2𝐿 − 𝐿3 =
-1.o58klf 11ft
24 558o.731ksi 734356.oi 4
[3 11𝑓𝑡 2(11𝑓𝑡 +
2 140.995𝑓𝑡 ) − 140.995𝑓𝑡 3]
3
17
1ft3
= 0.551 𝑖𝑛
g2
∆ =
5w L4 w a2L2
g s − g s = [
5 -1.o58klf 14o.995ft 4
384Ecilx 16Ecilx 384 558o.731ksi 734356.oin4
−
16 558o.731ksi 734356.oin4
-1.o58klf 11ft 2 14o.995ft 2]
1728i 3
1ft3 = −2.296𝑖𝑛 + 0.067𝑖𝑛 = −2.229𝑖𝑛
70
Dg1
Dg2
Self-weight Deflection
69
10
70

## Slide 36: Camber – Prestress Deflection
12/5/2022
71
Superimpose case (3) and (5) for harped strands
PCI Bridge Design Manual
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
C.G.
e?’
e
https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Straight Strands
44
61
– 𝑃 = 2384.47𝑘𝑖𝑝 = 1719.95𝑘𝑖𝑝
– ∆
ss
2
= PeL = 1719.95kip 31.447in 162.995ft
2
8Ecilx 8 558o.731ksi 734356.oin4
2
144i
1ft2 = 6.308𝑖𝑛
Harped Strands
17
61
– 𝑃 = 2384.47𝑘𝑖𝑝 = 664.52 𝑘𝑖𝑝
– 𝑒, = 𝑒hp − 𝑒e = 30.775𝑖𝑛 − (−26.813𝑖𝑛)) = 57.588 𝑖𝑛
– 𝑏 = 0.4
l
–
𝑁 = Pe = 664.52kip 57.588in
bL (o.4)(162.995ft)
1ft = 48.91𝑘𝑖𝑝
12in
– ∆
hs
2 3 2 2
= b 3-4b NL + PeeL = o.4 3-4 o.4 48.91kip 162.995ft
3
24 cilx 8Ecilx 24 558o.731ksi 734356.oin4
3
1728
1ft3 +
664.52kip -2 .813in 162.995ft 2 144in2
8 558o.731ksi 734356in4 1ft2
Participant Materials
= 3.513𝑖𝑛 − 1.973𝑖𝑛 = 1.540𝑖𝑛
72
Camber – Prestress Deflection
Dps
Prestress Deflection
71
10
72

## Slide 37: Camber at Lifting
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
For stability analysis, camber is measured relative to the ends of the girder
∆ps= 𝛥ss + 𝛥hs = 6.308𝑖𝑛 + 1.540𝑖𝑛 = 7.848𝑖𝑛
∆eamber= −∆g1 + 𝛥g2 + ∆ps= −0.551𝑖𝑛 − 2.229𝑖𝑛 + 7.848𝑖𝑛 = 5.068𝑖𝑛
73
Dcamber = -Dg1+Dg2+Dps
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Vertical Location Center of Mass
Distance from Center of Gravity to Roll Axis
Assume camber is a parabolic arc (elevation view)
𝑦r = 𝑌top + 𝑦lift − 𝐹o∆eamber= 38.343𝑖𝑛 + 0𝑖𝑛 − 0.415 5.068𝑖𝑛 = 36.24 𝑖𝑛
74
RollAxis
Ytop
ylift
yr
FoDcamber
a
Ytop a
RollAxis
yitfl
yr
FoDcamber
Centroid
Section at Lift Point
Dcamber
Ls
Elevation View
73
10
74

## Slide 38: Lateral Deflection of CG
12/5/2022
o
g
s
Lateral deflection of center of mass
– Not deflection of beam
S
Wg L
12EcilyyL2 1o
s
2 3 4
s
5
S
− 𝑎 𝐿 + 3𝑎 𝐿 + 6a = 12.187 𝑖𝑛
𝑧 =
𝑧 = 𝑧o𝜃
75
q
D
Wg=wgLg
Lg
Ls
a a
zo
Wgsin(q)=Wgq zoq=z
Plan View
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
q
Wg
Wgcos(q)=Wg
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Hanging Girder Equilibrium
𝑒i + 𝑧osin(𝜃)
≈ 𝑊g 𝑒i + 𝑧o𝜃
∑ 𝑀 = 0, 𝑀aeting = 𝑀resisting
Small angle theory, 𝑠𝑖𝑛𝜃 ≈ 𝑡𝑎𝑛𝜃 ≈ 𝜃, 𝑐𝑜𝑠𝜃 ≈ 1
𝑀aeting = 𝑊g𝑐𝑜𝑠 𝜃 𝑒i + 𝑧 = 𝑊g𝑐𝑜𝑠 𝜃
𝑀resisting = 𝑊g𝑠𝑖𝑛 𝜃 𝑦r ≈ 𝑊g𝜃𝑦r
𝑊g 𝑒i + 𝑧o𝜃 =𝑊g𝜃𝑦r
Solve for 𝜃
𝜃 = 𝜃
eq
= ei
yr-zo
𝜃
eq
= ei =
1.o95
yr-zo 36.24-1 .187
= 0.04552 𝑟𝑎𝑑 = 2.6°
76
q
Wgsin(q)=Wgq zoq=z
q
Wg Wgcos(q)=Wg
75
10
76

## Slide 39: Concrete Stress Limits Tension
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Stress due to PS and self weight
–
𝑓 = P + Pe + M
A s s
Stress due to self weight from tilt
– 𝑓tl =
2lyy
𝜃eq, 𝑓br = −
M W M W
g tf g bf
2lyy
𝜃eq
77
𝑓 ≤ 0.65𝑓′
𝑓 ≤ 0.70𝑓𝑐𝑖
′
𝑐𝑖
General Case
Peak Compressive Stress Case
Neutral Axis
Compression
f
f
 | PS |  | Girder |  |  | General Case |  | Tilt |  | Peak Case | 
Point | ftop(ksi) | fbot(ksi) | M(kft) | ftop(ksi) | fbot(ksi) | ftop(ksi) | fbot(ksi) | ftl(ksi) | fbr(ksi) | ftl(ksi) | fbr(ksi)
Lift, 11ft | -0.329 | -4.754 | -64.02 | 0.04 | -0.037 | -0.289 | -4.792 | -0.012 | 0.009 | -0.576 | -4.528
Harp, 0.4L | 1.335 | -6.215 | 2425 | -1.519 | 1.413 | -0.184 | -4.802 | 0.451 | -0.353 | 0.266 | -5.155
ei
General case, harp point, −0.65𝑓, = −4.802 𝑘𝑠𝑖 𝑓, = 7.39 𝑘𝑠𝑖
ei ei
Peak case, bottom left flange, harp point, −0.70𝑓, = −5.155𝑘𝑠𝑖 𝑓, = 7.36 𝑘𝑠𝑖
ei ei
Tension stress: 0.266 𝑘𝑠𝑖 < 0.24𝜆 𝑓, = 0.653 𝑘𝑠𝑖 OK
Controls
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Concrete Stress Limits
ei
ei
0.65𝑓, general case stress limit
0.70𝑓, peak case stress limit
Lateral stability and concrete strength requirements for precast, prestressed concrete components, Seguirant, et. al. PCI Journal March-April 2020
Currently WSDOT policy
Adopted by AASHTO for LRFD 10th Edition
78
77
10
78

## Slide 40: Cracking Factor of Safety
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Cracking, 𝐹𝑆 ≥ 1.0
Harp Point, Top Left Flange Tip
Calculate lateral moment that will cause cracking
er
– 𝑀 =
f -f 2l
r direct yy
Wtop
r ei
, 𝑓 = 0.24𝜆 𝑓, = 0.653 𝑘𝑠𝑖, 𝑓
= 𝑓 + 𝑓
direet ps girder
= −0.184𝑘𝑠𝑖
– 𝑀
er
= (o.653ksi- -o.184ksi )(2)(72o18.4i
4
49in
12in
) 1ft = 205.19 𝑘 · 𝑓𝑡
Calculate rotation that produces 𝑀er
er
Mg 2425.o
– 𝜃 = Mcr ≤ 0.4 𝑟𝑎𝑑 = 2o5.91 = 0.08461 𝑟𝑎𝑑 = 4.8°
Calculate factor of safety
– 𝐹𝑆
er
Macting
Mresisting r cr
= = y 0 =
36.24in o.o8461
ei+zo0cr 1.o95in (12.187in) o.o8461
= 1.4 > 1.0 OK
79
Participant Materials
https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Failure Factor of Safety
Failure, 𝐹𝑆 ≥ 1.5
Need adequate reserve capacity if the girder cracks
Lateral stiffness reduces for cracked girder
Calculate critical angle
– 𝜃max =
ei 1.o95
2.5zo 2.5 12.187
≤ 0.4 𝑟𝑎𝑑 = = 0.1896 𝑟𝑎𝑑 = 10.8°
Calculate factor of safety
– 𝐹𝑆
f
ei+ 1+2.50max
Macting zo0max
Mresisting
= = yr0max =
36.24in o.1896
1.o95in+ 1+2.5 o.1896 12.187in
o.1896
=
1.527 > 1.5 OK
80
 | Equilibrium | Cracking | Failure
Tilt Angle | 2.6° | 4.8° | 10.8°
FS | 1.0 | 1.4 | 1.5
79
10
80

## Slide 41: Step 3 – Design for Shipping
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
This step is based on assumed parameters
ei
– Losses depend on 𝑓, and prestress (including temporary strand)
ei
– This step estimates temporary top strand requirement, but based on 𝑓, without
TTS
ei
Numerous iterations are performed using the assumed 𝑓, for lifting w/o TTS
Number of TTS = 4
Bunk points at 13’-8”
These calculations will be updated in Step 5 using the results from Step 4
81
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Step 4 – Lifting with TTS
Same procedure as Step 2, except girder has temporary top strands
Prestress losses
Elastic shortening in TTS and Permanent Strands are very different
Estimate total prestress force after ES
Compute 𝑓egp for temporary and permanent strands
Compute ∆𝑓pEs for temporary and permanent strands
Update estimate of total prestress force
𝑓pj − ∆𝑓pRo − ∆𝑓pEs-perm
𝑃 = 𝑁p 𝑎ps +
𝑁t(𝑎ps)(𝑓pj − ∆𝑓pRo − ∆𝑓pEs-temp)
– Iterate until converged
ei
Lift point: Reduces from 11 ft to 8.25 ft
𝑓, : Reduces from 7.4 to 7.2 ksi
82
fcgp-temp
fcgp-perm
81
10
82

## Slide 42: Step 5 – Revise Shipping Design
12/5/2022
Participant Materials
https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
We now have number of TTS (Step 3) and corresponding 𝑓, (Step 4)
ei
Need to compute prestress losses and camber at time of hauling
  Effective prestress is greater at an earlier age (WSDOT: min. haul is 10 days)
  Camber is greater at a later age (WSDOT: max. haul is 90 days)
  What’s the critical combination of loss and camber?
  Conservative to take losses at day 10 and camber at day 90.
Losses at time of hauling
  Initial relaxation and elastic shortening – same as before
  Shrinkage, Creep, Relaxation that occur during storage
– ∆𝑓pLTH = ∆𝑓psRH + ∆𝑓pCRH + ∆𝑓pR1H
83
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Shrinkage of Girder Concrete
id
𝐾 =
LRFD 5.9.3.4.2a
Δ𝑓psRH = 𝜀bih𝐸p𝐾id
Δ𝑓ps = Δ𝜀ps𝐸p Hooke’s law
Δ𝜀ps = Δ𝜀e strain compatibility
1
1+
Ep Aps Eci Ag
1+
Age2g
p lg
1+o.71/b tf,ti
– transformed section coefficient that accounts for the time-dependent interaction between concrete and bonded steel
𝜀bih Unrestrained (free) shrinkage strain of girder concrete from initial to hauling
See NCHRP Report 496 for derivation
84
1.0
Strain due to internal restraining forces
Time-Dependent Strain, ebihKid
Free Shrinkage Strain, ebih
83
10
84

## Slide 43: Creep of Girder Concrete
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
CRH Eci egp b h i id
Eci
LRFD 5.9.3.4.2b
Δ𝑓 = Ep 𝑓 𝜓 𝑡 , 𝑡 𝐾
𝑓egp is the stress in the concrete at the level of the strand due to applied load
fcgp is the initial strain in the concrete
f
cgp
Eci
𝜓b(𝑡h, 𝑡i) is the unrestrained (free) creep strain from 𝑡i to 𝑡h
ps e
•
Δ𝜀 = Δ𝜀 strain compatibility
Δ𝑓ps = Δ𝜀ps𝐸p Hooke’s law
𝐾id transformed section coefficient
See NCHRP Report 496 for derivation
85
E
c
Stress
Strain, e
Initial (Elastic) Strain, e
Creep Strain, cye
Total Strain, e+cye=e(1+cy)
E’’c
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Relaxation of Strand
LRFD 5.9.3.4.2c
Δ𝑓
pR1H
3o
fpy
fpt fpt
= − 0.55
f
pt
fpy
pR1
≈ 1.2 𝑘𝑠𝑖, < 0.55, ∆𝑓 = 0 (doesn’t account for time)
pR1H
fpt log 24th 45 log 24 i
fpy
fpt − 0.55 1 −
3 ∆f +∆f
pSRH pCRH
fpt
ih
𝐾 (LRFD C5.9.3.4.2c)
∆𝑓 =
𝑓pt stress in strand immediately after transfer, 𝑓pt = 𝑓pj − ∆𝑓pRo − ∆𝑓pEs
This is a reduced relaxation – the length of the strand is shortening over time
86
85
10
86

## Slide 44: Prestress Losses
12/5/2022
Participant Materials
https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Strand | ∆𝒇𝒑𝑹𝟎 | ∆𝒇𝒑𝑬𝑺 | ∆𝒇𝒑𝑺𝑹𝑯 | ∆𝒇𝒑𝑪𝑹𝑯 | ∆𝒇𝒑𝑹𝟏𝑯 | 𝒇𝒑𝒆
Temporary | 1.980 ksi | 7.2 ksi | 1.414 ksi | 1.921 ksi | 0.920 ksi | 189.0 ksi
Permanent | 1.980 ksi | 20.53 ksi | 1.895 ksi | 4.033 ksi | 1.773 ksi | 172.5 ksi
87
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Camber at Hauling
Similar to camber for lifting analysis
Camber is measured relative to the ends of the girder with dead load deflection based on bunk locations
Increase in camber due to creep occurs based on storage conditions
∆ereep= ∆girder + ∆ps
– 𝜓b 𝑡h = 90, 𝑡i = 1
∆eamber= 7.338 𝑖𝑛
88
Dcamber = -Dg1+Dg2+Dps
87
10
88

## Slide 45: Hauling Analysis
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Assume bunk point location, 13’-8”
Assume truck rotational stiffness, 40,000 kip-in/rad, and other geometric parameters
Location of center of mass
Compute equilibrium roll angle
Compute stresses
Compute concrete strength to satisfy compression stress limit
Check FS cracking
Check FS rollover
89
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Hauling Stability Design Criteria
Stress limits
e
– Tension 0.24𝜆 𝑓,,
e e
– Compression 0.65𝑓, CL, 0.70𝑓, Corners
Factor of Safety 1.0 Cracking & 1.5 Rollover
Travel at typical 2% slope with +/-20% impact
6% Superelevation
90
89
10
90

## Slide 46: Haul Truck Parameters
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
𝐻re = 24 𝑖𝑛
𝐻bg = 72 𝑖𝑛
𝑊ee, 𝐾0 per BDM Table 5.6.3-1
– Use smallest 𝐾0 possible
91
ei
Wcc
Hbg
Hcr
Hg
Ytop
FoDcamber
yrc
yr
RollCenter
Section at Bunk Point
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
sweep
8
Bunk point eccentricity 𝑒bunk = 1.0 𝑖𝑛
Sweep Δ = 1 𝑖𝑛 𝑝𝑒𝑟 10 𝑓𝑡 = 2.037 𝑖𝑛
o
Ls
2
Lg 3
− 1 = 0.359
Offset Factor, 𝐹 =
𝑒i = 1.0 + 0.359 2.037 = 1.723 𝑖𝑛
92
Section at Bunk Point
Horizontal Location Center of Mass
ei
ebunk
esweep
91
10
92

## Slide 47: Vertical Location Center of Mass
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Height of roll center below top of girder
– 𝑦re = 𝐻bg + 𝐻g − 𝐻re = 72.0𝑖𝑛 + 74.0𝑖𝑛 − 24.0𝑖𝑛 = 122.0𝑖𝑛
Location of center of gravity above roll center
– Assume camber is a parabolic arc (elevation view)
–
93
D
a
camber
Ls
Elevation View
Ytop a
FoDcamber
𝑦r = 𝑦re − 𝑌top + 𝐹o ∆eamber
= 122.0𝑖𝑛 − 38.343𝑖𝑛 + 0.359 7.338𝑖𝑛
= 86.295𝑖𝑛
Centroid
ei
Hrc
Hbg
Hg
Ytop
FoDcamber
yrc
yr
RollCenter
Wcc
Section at Bunk Point
Participant Materials
https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
•
Hauling Equilibrium
∑ 𝑀 = 0, 𝑀aeting = 𝑀resisting
eq
K0-Wg yr+zo
𝜃 = K0a+Wgei
𝑊g = 172.48 𝑘𝑖𝑝
𝐾0 = 40,000 𝑘 · 𝑖𝑛/𝑟𝑎𝑑
𝑧o = 9.137 𝑖𝑛 (7.309 𝑖𝑛 𝐼𝑀 ↑, 10.3964 𝑖𝑛 𝐼𝑀 ↓)
94
q
Wg
Wgsin(q)=Wgq
Wg
a RolCenterl
Wgcos(q)=Wg
FBD at equilibrium
a | Impact | IM | 𝜽𝒆𝒒 (rad) | 𝜽𝒆𝒒 (deg)
2% | Up | 0.8 | 0.03836 | 2.19
2% | None | 1.0 | 0.04668 | 2.67
2% | Down | 1.2 | 0.05831 | 3.34
6% | None | 1.0 | 0.11465 | 6.57
93
10
94

## Slide 48: Concrete Stress Limits
12/5/2022
Stress due to PS and self weight
–
𝑓 = P + Pe + M
A s s
Stress due to self weight from tilt
– 𝑓tl =
MgWtf
2l
yy
𝜃eq, 𝑓br = −
MgWbf
2l
yy
𝜃eq
95
𝑓 ≤ 0.65𝑓𝑐𝑖
′
𝑐𝑖
𝑓 ≤ 0.70𝑓′
General Case
Peak Compressive Stress Case
Neutral Axis
Tension
Compression
f
f
Case | 𝒇𝒑𝒔 𝒌𝒔𝒊 | IM | 𝒇𝒈 𝒌𝒔𝒊 | 𝒇𝒅𝒊𝒓𝒆𝒄𝒕 = 𝒇𝒑𝒔 + 𝑰𝑴 𝒇𝒈 𝒌𝒔𝒊 | 𝒇, = 𝒇𝒅𝒊𝒓𝒆𝒄𝒕 𝒌𝒔𝒊 𝒄 𝟎. 𝟔𝟓 | 𝒇𝒕𝒊𝒍𝒕 𝒌𝒔𝒊 | 𝒇, = 𝒇𝒅𝒊𝒓𝒆𝒄𝒕 + 𝒇𝒕𝒊𝒍𝒕 (𝒌𝒔𝒊) 𝒄 𝟎. 𝟕𝟎
2% slope, impact up | -5.886 | 0.8 | 1.279 | -4.863 | 7.5 | -0.215 | 7.3
2% slope, no impact | -5.886 | 1.0 | 1.279 | -4.607 | 7.1 | -0.318 | 7.1
2% slope, impact down | -5.886 | 1.2 | 1.279 | -4.351 | 6.2 | -0.491 | 6.9
6% slope, no impact | -5.886 | 1.0 | 1.279 | -4.607 | 7.1 | -0.856 | 7.8
e
Max tension, harp point, top left flange tip, 6% slope
𝑓tl = 0.800 𝑘𝑠𝑖 − 1.375 𝑘𝑠𝑖 + 1.027 𝑘𝑠𝑖 = 0.452 𝑘𝑠𝑖 < 0.24𝜆 𝑓, = 0.708 𝑘𝑠𝑖
Requires sufficient bonded reinforcement with 𝑓s < 0.5𝑓y 30 𝑘𝑠𝑖 𝑚𝑎𝑥
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Participant Materials
https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Cracking Factor of Safety
Cracking, 𝐹𝑆 ≥ 1.0
er
At equilibrium, how close is tension stress to modulus of rupture?
No cracking is design objective
– 𝑀 = ±
f -f
2l
r direct yy
Wtop
, 𝑓r = 0.24𝜆 𝑓, = 0.653 𝑘𝑠𝑖, 𝑓direet = 𝑓ps + (𝐼𝑀)𝑓girder
ei
er
Mg
– 𝜃 = Mcr ≤ 0.4 𝑟𝑎𝑑
– 𝐹𝑆
er
Mresisting
=
Macting
K0 0cr-a
g o r cr i
≥ 1.0
– 𝐹𝑆er =
W z +y 0 +e
– Harp Point governs
96
Case | 𝒇𝒅𝒊𝒓𝒆𝒄𝒕 (𝒌𝒔𝒊) | 𝑴𝒄𝒓 (𝒌 · 𝒇𝒕) | 𝜽𝒄𝒓 (𝒓𝒂𝒅) | 𝜽𝒄𝒓 (𝐝𝐞𝐠) | 𝑭𝑺
2% slope, impact up | -0.300 | 246.88 | 0.14059 | 8.06 | 2.23
2% slope, no impact | -0.575 | 314.26 | 0.14323 | 8.21 | 1.86
2% slope impact down | -0.850 | 381.64 | 0.14489 | 8.30 | 1.53
6% slope, no impact | -0.575 | 314.26 | 0.14317 | 8.20 | 1.25
95
10
96

## Slide 49: Rollover Factor of Safety
12/5/2022
Participant Materials
https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Wcc
Wg -Hrca
K0
𝜃ro = 2 + 𝛼
𝐹𝑆
ro
Wg zo 1+2.50ro +yr 0ro+ei
= K0(0ro-a) ≥ 1.5
97
FBD at rollover
Case | 𝜽𝒓𝒐 (𝑟𝑎𝑑) | 𝜽𝒓𝒐 (𝐝𝐞𝐠) | 𝑭𝑺
2% slope, impact up | 0.14253 | 8.17 | 2.30
2% slope, no impact | 0.17316 | 9.92 | 1.87
2% slope impact down | 0.20380 | 11.68 | 1.56
6% slope, no impact | 0.20903 | 11.98 | 1.52
Step 6 – Check Erection Stress
WSDOT check – not required by AASHTO
Check girder stresses after temporary strand are removed
  Temporary top strands are removed shortly after erection (before diaphragms)
  Temporary strand removal causes a change in effective prestress
ptr
Ag
lg
𝑃tr = 𝐴t 𝑓pj − ∆𝑓pH force in prestressing strands at time of removal
𝑓 = − Ptr − Ptretep stress in girder concrete at level of permanent strands
ptr
E
p
Ec
ptr
change in stress in permanent strands
∆𝑓 = 𝑓
Removal of temporary strand also causes change in camber
Check girder stresses after deck casting
– Estimate prestress losses at day 120 using same process as before
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
98
97
10
98

## Slide 50: Check after deck placement
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
ed
lg
Placement of the wet deck concrete causes elongation of the strand and tension stress in the bottom of the girder
The elongation of the strand is called an “elastic gain”. It’s just strain compatibility
∆𝑓, = Madle change in concrete stress at level of strands due to added dead load
pED
E
p
Ec
ed
,
∆𝑓 = ∆𝑓 change in stress in strands
Effective prestress, 𝑃 = 𝐴ps 𝑓pj − ∆𝑓pRo − ∆𝑓pEs − ∆𝑓pLTid − ∆𝑓ptr + ∆𝑓pED
𝑓 = + +
P Pe Mgirder+Mdiaphragm+Mslab+Mhaunch
A s s
– −2.974 𝑘𝑠𝑖 𝑡𝑜𝑝 𝑎𝑡 ℎ𝑎𝑟𝑝 𝑝𝑡 , −3.892 𝑘𝑠𝑖 (𝑏𝑜𝑡𝑡𝑜𝑚 𝑎𝑡 𝑡𝑟𝑎𝑛𝑠𝑓𝑒𝑟 𝑝𝑡)
e
e
Compare to stress limit, 0.45𝑓,
This case governs for compression, 𝑓, = 8.65 𝑘𝑠𝑖
99
controlling strength 8.7 𝑘𝑠𝑖
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Step 7 – Check Final Conditions
Service Limit State
  Compute losses from time of deck placement to final time
    Shrinkage & Creep of Girder Concrete
    Relaxation of strand
    Slab Shrinkage
  Check Service I, Service III, and Fatigue I stresses
Strength Limit State
  Moment capacity
100
99
10
100

## Slide 51: Shrinkage
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
df
– 𝐾 =
LRFD 5.9.3.4.3a
Δ𝑓psD = 𝜀bdf𝐸p𝐾df
𝜀bdf shrinkage strand of beam from deck placement to final
𝐾df transformed section coefficient for composite deck/girder section
1
Eci Ac
1+ 1+
pc
Ep Aps Ace2
lc
1+o.71/b tf,ti
101
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Creep
pCD Eci egp b f i b d i df
E
p
Ec
+ Δ𝑓 𝜓 𝑡 , 𝑡 𝐾
∆𝑓 = − ∆𝑓 + ∆𝑓 + ∆𝑓
ed psR pCR pR1
LRFD 5.9.3.4.3b
Δ𝑓 = Ep 𝑓 𝜓 𝑡 , 𝑡 − 𝜓 𝑡 , 𝑡 𝐾
ed b f d df
First term is creep due to initial loads for the deck placement to final time period
Second term is creep due to initial to deck losses and loads applied to the girder at and after deck casting
2
Aps
Ag lg
ed ed
Age , ,,
1 + − ∆𝑓 + ∆𝑓
ed
lg
∆𝑓, = Mdiaphragm+Mslab+Mhaunch e change in stress due to loads at deck casting
ed
,,
∆𝑓 =
M +M
Y -Y +e
barrier overlay bc bg
lc
change in stress due to loads after deck casting
102
101
10
102

## Slide 52: Relaxation
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
LRFD 5.9.3.4.3c
Δ𝑓pR2 = Δ𝑓pR1
103
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Shrinkage of Deck Concrete
LRFD 5.9.3.4.3d
In Step 1, we computed stress in girder concrete due to deck shrinkage and indirectly included ∆𝑓pss in our guess of 15% prestress loss.
edf
Δ𝑓 = c:ddfAdEc deck
1 − epced
1+o.71/d tf,td Ac lc
ds
= ∆𝑃 −
1 e e
pc d
Ac lc
ds
, ∆𝑃 = −310.0 𝑘𝑖𝑝
edf
𝛥𝑓 = (−310.0𝑘𝑖𝑝)
1
− (44.687in)(28.883in)
1349.614in2 124657o.6i 4
= 0.091 𝑘𝑠𝑖
pss
E
p
Ec
∆𝑓 = ∆𝑓 𝐾
edf df b f d
1 + 0.7𝜓 𝑡 , 𝑡 =
285ooksi 0.091𝑘𝑠𝑖 0.777 1 + 0.7 0.644 = 0.498 𝑘𝑠𝑖
5886.891ksi
pss
E
p
Ec
E
p
Ec
∆𝑓 = ∆𝑓 𝐾 + ∆𝑓 𝐾
0.7𝜓 𝑡 , 𝑡
edf df edf df b f d
104
Elastic gain
Creep of girder concrete
103
10
104

## Slide 53: Elastic Gains
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Elastic gains are the change in strand stress due to externally applied loads
Added dead load to non-composite section
E
p
Ec
– ∆𝑓 = ∆𝑓
pED ed
,
Superimposed Dead Loads
E
p
Ec
– ∆𝑓 = ∆𝑓
slDL ed
,,
Slab Shrinkage
– Already included in ∆𝑓pss
Live Load
ed
,,,
– ∆𝑓 =
M Y -Y +e
llim bc bg
lc
, ∆𝑓
pLLlM
E
Ec
ed
p ,,,
= ∆𝑓 (HL-93)
edf
,,,
– ∆𝑓 =
M
Y -Y +e
fatigue bc bg
lc
, ∆𝑓
pFatigue
E
p
Ec
edf
,,,
= ∆𝑓 (Fatigue)
105
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Service I Compression Check
Service I Compression without Live Load, 0.45𝑓,
e
– 𝑃 = 𝐴ps 𝑓pj − Δ𝑓pRo − Δ𝑓pEs − ∆𝑓ptr − Δ𝑓pLT + Δ𝑓pED + Δ𝑓pslDL
A s
P Pe (M
girder+Mdiaphragm+Mslab+Mhaunch s
+
) M
+M
barrier overlay
sc
+ 𝑓
ss
e
– 𝑓 = + +
– 𝑓 = −3.709 𝑘𝑠𝑖 < −0.45𝑓, = −0.45(8.7𝑘𝑠𝑖) = −3.915 𝑘𝑠𝑖 OK
Service I Compression with Live Load, 0.60𝑓,
e
– 𝑃 = 𝐴ps 𝑓pj − Δ𝑓pRo − Δ𝑓pEs − ∆𝑓ptr − Δ𝑓pLT + Δ𝑓pED + Δ𝑓pslDL + Δ𝑓pLL
A s
P Pe (M
girder+Mdiaphragm+Mslab+Mhaunch s
+
) M
barrier+Moverlay+Mllim sc
+ 𝑓
ss
e
– 𝑓 = + +
– 𝑓 = −4.570 𝑘𝑠𝑖 < −0.60𝑓, = −0.60(8.7𝑘𝑠𝑖) = −5.220 𝑘𝑠𝑖 OK
106
105
10
106

## Slide 54
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Fatigue I Compression Check
Fatigue I Compression, 0.40𝑓,
e
– 𝑃 = 𝐴ps 𝑓pj − Δ𝑓pRo − Δ𝑓pEs − ∆𝑓ptr − Δ𝑓pLT + Δ𝑓pED + Δ𝑓pslDL + 1.5Δ𝑓pFatigue
– 𝑓 = 0.5 + +
P Pe (M
girder+Mdiaphragm+Mslab+Mhaunch s
+
) M
+M
barrier overlay
sc
ss
+ 𝑓 +
A s
1.5Mfatigue sc
e
– 𝑓 = −2.619 𝑘𝑠𝑖 < −0.40𝑓, = −0.40(8.7𝑘𝑠𝑖) = −3.480 𝑘𝑠𝑖 OK
107
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Service III Tension Check
Service III Tension, 0.0 𝑘𝑠𝑖
– 𝑃 = 𝐴ps 𝑓pj − Δ𝑓pRo − Δ𝑓pEs − ∆𝑓ptr − Δ𝑓pLT + Δ𝑓pED + Δ𝑓pslDL + 0.8Δ𝑓pLL
– 𝑃 = 13.237𝑖𝑛2(202.5𝑘𝑠𝑖 − 1.98𝑘𝑠𝑖 − 20.328𝑘𝑠𝑖 − 0.375𝑘𝑠𝑖 − 19.206𝑘𝑠𝑖 + 8.382𝑘𝑠𝑖 + 3.065𝑘𝑠𝑖 + (0.8)7.922 𝑘𝑠𝑖) = (13.237𝑖𝑛2)(178.397𝑘𝑠𝑖) = 2361.4 𝑘𝑖𝑝
A s
girder diaphragm slab haunch
s
+
P Pe (M +M +M +M ) M
barrier+Moverlay+o.8Mllim sc
+ 𝑓
ss
– 𝑓 = + +
– 𝑓 = 0.003 𝑘𝑠𝑖 ≈ 0.0 𝑘𝑠𝑖 OK
Verify assumed 15% prestress loss from Step 1
pe
P
Aps fpj
13.237 in2 2o2.5
– 𝑓 = = 2361.4 kip = 178.4 𝑘𝑠𝑖, fpe = 178.4 = 0.88
fpj
– 𝐿𝑜𝑠𝑠 = 1 − fpe = 1 − 0.88 = 0.12 = 12% ≈ 15%
108
107
10
108

## Slide 55: Strand Stress
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Prior to transfer
– 𝑓pe = 202.5𝑘𝑠𝑖 − 1.98 𝑘𝑠𝑖 = 200.52 𝑘𝑠𝑖 ≤ 0.75𝑓pu = 202.5 𝑘𝑠𝑖 OK
At service limit state
– 𝐿𝑖𝑚𝑖𝑡 = 0.8𝑓py , 𝑓py = 0.9𝑓pu, 𝐿𝑖𝑚𝑖𝑡 = 0.8 0.9 270 𝑘𝑠𝑖 = 194.4 𝑘𝑠𝑖
– 𝑓pe = 179.98 𝑘𝑠𝑖 < 194.4 𝑘𝑠𝑖 OK
109
110
Check Anchorage Zone
Anchorage Zones 5.9.4.4
Splitting Resistance 5.9.4.4.1
Confinement Reinforcement 5.9.4.2.2
Hoyer Effect
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
109
10
110

## Slide 56
12/5/2022
Anchorage Zone Reinforcement
Splitting Reinforcement within h/4 from end of beam (can also be used for shear)
Confinement of strand for 1.5d (some owners use full length)
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop 111
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Anchorage Zone Design
Splitting Resistance LRFD 5.9.4.4.1
𝑃r = 𝑓s𝐴s ≥ 0.04𝑃ps
– 𝑓s ≤ 20 𝑘𝑠𝑖
  𝐴s within ℎ/4 from beam end
  Vertical for I-Beams
  WSDOT BDM 5.6.2.F #5 @ 2.5” min, extend beyond h/4 at minimum spacing if needed
Confinement, LRFD 5.9.4.4.2
  #3 at 6” for 1.5d, confining prestressing strands
112
111
10
112

## Slide 57: Splitting
12/5/2022
Force at end of transfer length
𝑃 = 0.04𝐴ps 𝑓pj − Δ𝑓pRo − Δ𝑓pEs
– 𝑃perm = 0.04 13.237𝑖𝑛2 202.5 − 19.858𝑘𝑠𝑖 = 96.71 𝑘𝑖𝑝
– 𝑃temp = 0.04 0.868𝑖𝑛2 202.5 − 8.656𝑘𝑠𝑖 = 6.73 𝑘𝑖𝑝
– 𝑃 = 96.71 + 6.73 = 103.44 𝑘𝑖𝑝
1ft
4 4 12in
= 1.542𝑓𝑡.
s s s
2
Splitting zone h = 74in
Splitting resistance 𝑃r = 𝑓s𝐴s, 𝑓s = 20 𝑘𝑠𝑖,
Compute 𝐴 , 103.44 𝑘𝑖𝑝 = 20 𝑘𝑠𝑖 𝐴 , 𝐴 = 5.172 𝑖𝑛2, 5.172i = 3.62 in
2
1.542ft ft
2
2.Sin 12 in⁄ft
2
ft
2-Legs #5 at 2.5”, 2 o.31in = 2.976 in , WSDOT BDM permits extending beyond h/4
2
ft
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
5.172𝑖𝑛2 = 2.976 in 𝑋, 𝑋 = 1.74 𝑓𝑡, Use 2-legs #5 at 2.5” for 1’-9”
113
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Confinement Zone
LRFD 5.9.4.4.2
– For the distance of 1.5d from the ends of the girder, reinforcement shall be placed to confine the prestressing steel in the bottom flange. The reinforcement shall not be less than #3 deformed bars with spacing not exceeding 6 in.
Zone Length = 1.5𝑑 = 1.5 74𝑖𝑛 = 111𝑖𝑛 = 9.25 𝑓𝑡
Provide #3 bars spaced at 6” in the end 9’-3” of the girder
114
113
10
114

## Slide 58: End Zone Details
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
[G1] bars provide splitting resistance
[G7] bars provide confinement
Zone 1, 1’-9” (min) @ 2.5”
Zone 2, 9’-3” (min) @ 6”
WSDOT provides confinement bars full length of beam, 18” max
115
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Moment Capacity
LRFD 5.6.3.2. 𝑀u ≤ 𝑀r = 𝜙𝑀n
Strength I = 1.25DC + 1.5DW + 1.75(LL+IM)
– 𝑀u = 1.25 3368.43 + 140.17 + 2465.61 + 760.28 + 732.12 + 1.50 739.63 +
1.75 3804.05 = 17099.8𝑘 · 𝑓𝑡
n ps ps p
+ 𝐴 𝑓 𝑑 + 𝐴, 𝑓, 𝑑, − a + 𝛼 𝑓, 𝑏 − 𝑏 ℎ
s s s s s s 1 e w f
− a − a a − hf
2 2 2 2 2
𝑀 = 𝐴 𝑓 𝑑
Doesn’t account for higher strength of girder concrete or large top flange area
Often predicts a compression-controlled section, 𝜙 = 0.75
LRFD 5.6.3.2.5 – Strain Compatibility Approach
– PGSuper uses strain compatibility analysis
116
115
10
116

## Slide 59: Nominal Moment Capacity
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
𝑑p = 𝑌t + 𝑒 + 𝑡s = 38.343𝑖𝑛 + 31.477𝑖𝑛 + 7𝑖𝑛 = 76.82𝑖𝑛
𝑐 =
l
A f -a f b-b h
a fl/3 b +kA
ps pu 1 c w f
fpu
1 c 1 w ps dp
2
o.85 4ksi o.85 6.125in o.28 13.237i 2
= (13.237i )(27oksi)-o.85 4ksi 84in-6.125in 7in
270ksi
76.B2in
= 56.04𝑖𝑛
𝑘 = 2 1.04 − fpy
fpu
27o
= 2 1.04 − 243 = 0.28
ps pu
dp
𝑓 = 𝑓 1 − 𝑘 e = 270𝑘𝑠𝑖
1 − 0.28 56.o4in
76.82in
= 214.85𝑘𝑠𝑖
𝑎 = 𝛽1𝑐 = 0.85 56.04𝑖𝑛 = 47.63𝑖𝑛
𝑀 = 𝐴 𝑓 𝑑
n ps ps p
− a
2
+ 𝛼1𝑓, 𝑏 − 𝑏 ℎ
e w f
a − hf
2 2
= 13.237𝑖𝑛2 214.85𝑘𝑠𝑖 (76.82𝑖𝑛 −
2
47.63in) + 0.85 4𝑘𝑠𝑖 84𝑖𝑛 − 6.125𝑖𝑛 7𝑖𝑛
47.63in − 7in
2 2
= 188396.9𝑘 · 𝑖𝑛 = 15699.7𝑘 · 𝑓𝑡
117
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Moment Resistance
t
e 56.o4
𝑑t = 74𝑖𝑛 + 7𝑖𝑛 − 2𝑖𝑛 = 79𝑖𝑛
𝜀 = 0.003 dt-e = 0.003 79-5 .o4 = 0.00123
c:tl-c:cl
0.75 ≤ 𝜙 = 0.75 + 0.25 c:t-c:cl ≤ 1.0
•
𝜙 = 0.75 + 0.25 o.oo123-o.oo2
o.oo5-o.oo2
= 0.686, 𝑢𝑠𝑒 0.75
– Compression controlled section
𝑀r = 𝜙𝑀n = 0.75 15699.7𝑘 · 𝑓𝑡 = 11774.8𝑘 · 𝑓𝑡
𝑀r = 11774.8𝑘 · 𝑓𝑡 < 𝑀u = 17099.8𝑘 · 𝑓𝑡 No Good
118
117
10
118

## Slide 60: Strain Compatibility
12/5/2022
Participant Materials
https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Prestressing steel constitutive model
Modified Ramberg-Osgood model
– aka power formula
ps ps
𝑓 = 𝜀 877 +
27,613
1+ 112.4c:
ps
1
7.36 7.36
119
100
50
0
≤ 270𝑘𝑠𝑖 200
150
250
300
0
fps (ksi)
0.005 0.01 0.015 0.02 0.025 0.03 0.035 0.04
eps (in/in)
Strain Compatibility
Concrete constitutive model
Thorenfeldt-Popovics model
𝑓 = 𝑓
e e
n
Ecf
E
, c
l
n-1+
l
Ecf nk
Ec
𝑛 = 0.8 +
l
f (psi)
c
25oo
𝑘 = 0.67 +
l
f (psi)
c
9ooo
c:
cf
c
c:l
, 𝑖𝑓 < 1.0, 𝑘 = 1.0
,
e
𝜀 𝑥1000 =
l
f n
c
Ec n-1
𝐸e =
c
4o,ooo fl (psi)+1,ooo,ooo
1ooo
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
120
119
10
120

## Slide 61: Strain Compatibility
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Select strain profile
Get 𝜀i at CG of each slice
Compute stress for each slice using constitutive model
Compute 𝐹i = 𝐴i 𝑓i(𝜀i) for each slice
Adjust strain profile until ∑ 𝐹i = 0
𝑀n = ∑ 𝐹i𝑦i
121
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Moment Capacity
c = 15.124 in
C = -3464.24 kip
Depth to neutral axis,
Resultant compression,
Depth to compression resultant, dc =5.720 in
Tension resultant,
Depth to tension resultant,
Net tensile strain,
Nominal capacity,
Moment arm,
T = 3464.24 kip
de = 76.822 in
𝜀t = 12.7𝑥10-3
Mn = 20526.2 kip-ft de - dc = Mn/T = 71.102in
c:tl-c:cl
0.75 ≤ 𝜙 = 0.75 + 0.25 c:t-c:cl ≤ 1.0
•
𝜙 = 0.75 + 0.25 o.o127-o.oo2
o.oo5-o.oo2
= 1.64, 𝑢𝑠𝑒 1.0
– Tension controlled section
𝑀r = 𝜙𝑀n = 1.0 20526.2 𝑘 · 𝑓𝑡
𝑀r ≥ 𝑀u = 17099.8𝑘 · 𝑓𝑡 OK
122
121
10
122

## Slide 62: Minimum Reinforcement
12/5/2022
LRFD 5.6.3.3
Reinforcement required for minimum moment capacity
Ensures there is sufficient reinforcement to achieve ductile behavior
  Avoid fracture of reinforcement at first crack
  Avoid crushing of concrete at first crack
𝑀r,min = 𝑙𝑒𝑠𝑠𝑜𝑟 𝑜𝑓 𝑀er, 1.33𝑀u
  𝑀er = Sectional requirement
  1.33𝑀u = Overstrength Requirement
1 r 2 epe e dne
sb
𝑀 = 𝛾 𝛾 𝑓 + 𝛾 𝑓 𝑆 − 𝑀 sc − 1
er 3
“Making sense of minimum flexural reinforcement requirements for reinforced concrete members”, Seguirant, et. al., PCI Journal, Summer 2010
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
123
Minimum Moment Capacity
𝑓r = 0.24𝜆 𝑓, = 0.24 1.0 8.7𝑘𝑠𝑖 = 0.708𝑘𝑠𝑖
e
𝑓epe = 5.947𝑘𝑠𝑖
𝑆e = 25509.3𝑖𝑛3, 𝑆b = 20594.8𝑖𝑛3
𝑀dne = 𝑀girder + 𝑀diaphragms + 𝑀slab + 𝑀hauneh = 6734.48𝑘 ⋅ 𝑓𝑡
1ft
12in
𝑀 = 1.0 [ 1.6 · 0.708𝑘𝑠𝑖 + 1.0 · 5.947𝑘𝑠𝑖 25509.3𝑖𝑛3 − (6734.48𝑘 ·
𝑓𝑡)
er 255o9.3in
3
2o594.8in3
− 1 ] = 14707.1 𝑘 · 𝑓𝑡
𝑀u = 17099.8𝑘 · 𝑓𝑡
r min
𝑀 = 𝑙𝑒𝑠𝑠𝑒𝑟 𝑜𝑓 {
𝑀er = 14707.1𝑘 · 𝑓𝑡
1.33𝑀u = 1.33 · 17099.8𝑘 · 𝑓𝑡 = 22742.7𝑘 · 𝑓𝑡
= 14707.1𝑘 · 𝑓𝑡
123
10
𝑀r = 20526.2𝑘 · 𝑓𝑡 ≥ 𝑀r min = 14707.1𝑘 · 𝑓𝑡 OK
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop 124
124

## Slide 63: Shear Design
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
125
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Shear Design
Shear Strength
– Modified Compression Field Theory (MCFT) – Variable angle truss model
Longitudinal Tension Tie for Shear
Horizontal Interface Shear
126
125
10
126

## Slide 64: Sectional Design Model
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
127
Critical Section
Face of Support
Sections Near Supports
LRFD 5.7.3.2
  Where the reaction force in the direction of the applied shear introduces compression into the end region of a member, the location of the critical section for shear shall be taken as dv from the internal face of the support and the shear reinforcement required at the critical section shall be extended to the support.
Face of support
  0.5 width of bearing, from CL Bearing
CL Bearing
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Critical Section for Shear
dv from face of support
𝑑v = 𝑀𝑜𝑚𝑒𝑛𝑡 𝑎𝑟𝑚, 𝑏𝑢𝑡 𝑛𝑜𝑡 𝑙𝑒𝑠𝑠 𝑡ℎ𝑎𝑛 𝑡ℎ𝑒 𝑔𝑟𝑒𝑎𝑡𝑒𝑟 𝑜𝑓 0.9𝑑e 𝑜𝑟 0.72ℎ
Moment arm comes from moment capacity analysis and varies with location because of the harped strands
Critical section occurs where dv graph intersects a 45° line
128
127
10
128

## Slide 65: Critical Section for Shear
12/5/2022
Participant Materials
https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
From moment capacity analysis
– 𝑀𝑜𝑚𝑒𝑛𝑡 𝐴𝑟𝑚 = 59.470 𝑖𝑛
– 𝑑e = 77.094 𝑖𝑛
– ℎ = 81 𝑖𝑛
Critical Section
– 𝑑 =
v
𝑀𝑎𝑥 𝑀𝑜𝑚𝑒𝑛𝑡 𝐴𝑟𝑚, 0.9𝑑e, 0.72ℎ =
𝑀𝑎𝑥 59.470 𝑖𝑛, 69.384𝑖𝑛, 58.320 𝑖𝑛 = 69.384 𝑖𝑛 𝑓𝑟𝑜𝑚 𝑓𝑎𝑐𝑒 𝑜𝑓 𝑠𝑢𝑝𝑝𝑜𝑟𝑡
From CL Bearing
12
– 69.384in + 0.5𝑓𝑡 = 6.282 𝑓𝑡
129
Location from Left Support (ft) | Assumed C.S. Location (in) | dv (in) | CS Intersects?
(FoS) 0.500 | 0.000 | 69.382 | No
(Bar Develop.) 0.834 | 4.011 | 69.382 | No
(PSXFR) 1.292 | 9.498 | 69.382 | No
4.625 | 49.500 | 69.384 | No
6.282 | 69.384 | 69.384 | *Yes
6.542 | 72.498 | 69.384 | No
(H) 6.667 | 74.000 | 69.384 | No
(1.5H) 9.750 | 111.000 | 69.384 | No
11.958 | 137.498 | 69.384 | No
(SZB) 12.170 | 140.037 | 69.384 | No
(SZB) 12.920 | 149.037 | 69.384 | No
14.591 | 169.092 | 69.384 | No
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Shear Stress
LRFD 5.7.2.8
u
cpbvdv
Vu
= Vu-cpVp =
-Vp
bvdv
e
𝑣
When 𝑣u > 0.18𝑓, and beam not integral with support, design end region using strut-
u
(o.9)(6.125)(69.384)
𝑣 = = 0.98 𝑘𝑠𝑖 < 0.18 8.7𝑘𝑠𝑖 = 1.566 𝑘𝑠𝑖
and-tie method, LRFD 5.7.3.2
𝑏v = 6.125 𝑖𝑛. , 𝑑v = 69.384 𝑖𝑛.
𝑉u = 413.73 𝑘𝑖𝑝, 𝑉p = 43.18 𝑘𝑖𝑝, 𝜙 = 0.9
413.73-o.9 43.18
Strut and tie design not required
130
129
10
130

## Slide 66: Shear Resistance
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
𝑉n = 𝑉e + 𝑉s + 𝑉p
– Eq 5.7.3.3-1
– Strength of concrete, stirrups, prestress
𝑉n = 0.25𝑓,𝑏 𝑑 + 𝑉
e v v p
– Eq 5.7.3.3-2
– Upper limit to ensure the concrete in the web of the beam will not crush prior to yielding of the transverse reinforcement (ductility requirement)
Minimum of Equation -1 & -2
Capacity Reduction Factor 𝜙 = 0.9, LRFD 5.5.4.2
𝑉r = 𝜙𝑉n
131
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Shear strength
𝑉n = 𝑉e + 𝑉s + 𝑉p
Concrete
e
– 𝑉e = 0.0316𝛽𝜆 𝑓,𝑏v𝑑v
Stirrups
s
– 𝑉 =
A f d cot 0
v y v
s
𝜆duet, 𝜆duet
= 1 − 𝛿
bw
cpduct 2 = 1.0 𝑓𝑜𝑟 𝑝𝑟𝑒𝑡𝑒𝑛𝑠𝑖𝑜𝑛𝑒𝑑 𝑠𝑡𝑟𝑎𝑛𝑑
Prestressing
– 𝑉p = 𝑃pe sin 𝑠𝑙𝑜𝑝𝑒
132
𝑃pe
𝑉p
e
𝑓, 𝑝𝑠𝑖 =
𝑓,𝑘𝑠𝑖
e
1000
=
1
1000
e
𝑓,𝑘𝑠𝑖 = 0.0316 𝑓,𝑐 𝑘𝑠𝑖
131
10
132

## Slide 67: Shear Parameters, band q
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
b= factor indicating ability of diagonally crack concrete to transmit tension and shear
q= inclination of diagonal compression strut
𝛽 and 𝜃 are related by the longitudinal strain in the concrete, 𝜀x
133
𝑑v cot 𝜃
𝑑v
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Shear Parameters, band q
𝛽 =
LRFD 5.7.3.4
b= factor indicating ability of diagonally crack concrete to transmit tension and shear
q= inclination of diagonal compression strut
General Procedure 5.7.3.4.2
4.8
1+75o s
𝜃 = 29 + 3500𝜀s
𝜀
s
= dv
Mu +o.5Nu+ Vu-Vp -Apsfpo
EsAs+EpAps
Mu +o.5Nu+ Vu-Vp -Apsfpo
EsAs+EpAps+EcAct
s s
𝜀 = dv 𝑓𝑜𝑟 𝜀 < 0
134
133
10
134

## Slide 68: Longitudinal Strain
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Mu +o.5Nu+ Vu-Vp -Apsfpo
EsAs+EpAps+EcAct
s s
2603.9Bk·f
𝜀 = dv 𝑓𝑜𝑟 𝜀 < 0
𝑀u = 2603.98 𝑘 ⋅ 𝑓𝑡
𝑑v = 69.384 𝑖𝑛
𝑉u = 431.73 𝑘𝑖𝑝, 𝑉p = 43.18 𝑘𝑖𝑝
𝐸ps = 28500 𝑘𝑠𝑖, 𝐴ps = 9.143 𝑖𝑛2
𝐸e = 5886.9 𝑘𝑠𝑖, 𝐴et = 507.406 𝑖𝑛2
12in
1f
+o.5 o +37o.54ki 9.143in2 189ksi
29oooksi oin2 + 285ooksi 9.143in2 + 5886.891ksi 5o7.4o6in2
𝜀s = 69.3B4in = −0.279𝑥10-3
135
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
band q
4.8
1+75o s
4.8
1+ 75o -o.279x1o-3 = 6.07
𝛽 = =
𝜃 = 29 + 3500𝜀s = 29 + 3500 −0.279𝑥10-3 = 28.02°
136
135
10
136

## Slide 69: Shear strength
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Concrete
e
– 𝑉e = 0.0316𝛽𝜆 𝑓,𝑏v𝑑v = 0.0316 6.07 (1.0) 8.7𝑘𝑠𝑖 6.125𝑖𝑛 69.384𝑖𝑛 =
240.51 𝑘𝑖𝑝
Stirrups (2 - #5 @ 6”)
s
– 𝑉 =
A f d cot 0
𝜆duet, 𝜆duet
v y v
s bw
2
= 1 − 𝛿 cpduct = 1.0 𝑓𝑜𝑟 𝑝𝑟𝑒𝑡𝑒𝑛𝑠𝑖𝑜𝑛𝑒𝑑 𝑠𝑡𝑟𝑎𝑛𝑑
s
2
6 in
– 𝑉 = 2 o.31 in 6o ksi 69.384in cot 28.o2 (1.0) = 808.29 𝑘𝑖𝑝
Prestressing
– 𝑉p = 43.18 𝑘𝑖𝑝
137
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Shear Resistance
𝑉n = 𝑉e + 𝑉s + 𝑉p = 240.51 𝑘𝑖𝑝 + 808.29 𝑘𝑖𝑝 + 43.18 𝑘𝑖𝑝 = 1091.99 𝑘𝑖𝑝
𝑉n = 0.25𝑓,𝑏 𝑑 + 𝑉
e v v p
138
= 0.25 8.7 𝑘𝑠𝑖 6.125 𝑖𝑛 69.384 𝑖𝑛 + 43.18 𝑘𝑖𝑝 = 967.51𝑘𝑖𝑝 Controls
𝑉r = 𝜙𝑉n = 0.9 967.51 𝑘𝑖𝑝 = 870.76 𝑘𝑖𝑝
𝑉u = 413.73 𝑘𝑖𝑝 ≤ 𝑉r = 870.76 𝑘𝑖𝑝
137
10
138

## Slide 70: Check Stirrup Requirement
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
LRFD 5.8.2.4 – Stirrups required when 𝑉u> 0.5𝜙 𝑉e + 𝑉p
0.5𝜙 𝑉e + 𝑉p = 0.5 0.9 240.51 𝑘𝑖𝑝 + 43.18 𝑘𝑖𝑝 = 127.66 𝑘𝑖𝑝 < 413.73 𝑘𝑖𝑝
Stirrups are required at this section and stirrups are provided
139
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Check Min Stirrup Requirement
e fy
6o ksi
LRFD 5.8.2.4
Minimum spacing controls shear cracking and ensures ductility
𝐴v min = 0.0316 𝑓, bvs = 0.0316 8.7 𝑘𝑠𝑖 6.125 in 6 in = 0.057 𝑖𝑛2 < 0.62 𝑖𝑛2
OK
Sometimes it is more convenient to represent this check as Area/Length
e fy
Av 𝑚𝑖𝑛 = 0.0316 𝑓, bv = 0.0316
8.7 𝑘𝑠𝑖 6.125 in 12in
6o ksi 1ft
= 0.114 in2 < 1.24 in2
ft ft
s
OK
140
139
10
140

## Slide 71: Check Max Stirrup Spacing
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
LRFD 5.7.2.6
– Maximum spacing ensures reinforcement crosses shear cracks for large theta angles (areas where moment is large, and shear is small)
– 𝑣u < 0.125𝑓,, 𝑠 = 0.8𝑑 ≤ 24 𝑖𝑛
e max v
– 𝑣u ≥ 0.125𝑓,, 𝑠 = 0.4𝑑 ≤ 12 𝑖𝑛
e max v
– WSDOT: 𝑠max = 18 𝑖𝑛
e
e
0.125𝑓, = 0.125 8.7 𝑘𝑠𝑖 = 1.09 𝑘𝑠𝑖
𝑣u = 0.98 𝑘𝑠𝑖 < 0.125𝑓, = 1.09 𝑘𝑠𝑖
𝑠max = 0.8𝑑v = 0.8 69.384 𝑖𝑛 = 55.5 𝑖𝑛 ≤ 24 𝑖𝑛 (18 𝑖𝑛. 𝑝𝑒𝑟 𝑊𝑆𝐷𝑂𝑇)
𝑠max = 18 𝑖𝑛 > 6 𝑖𝑛. 𝑝𝑟𝑜𝑣𝑖𝑑𝑒𝑑 OK
141
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Longitudinal Tension Tie
LRFD 5.7.3.5
General
ps ps s y
– 𝐴 𝑓 + 𝐴 𝑓 ≥
M
u
o.5N
u
dvcpf cpc
+ +
V
u
cpv
p
− 𝑉 − 0.5𝑉
s
cot 𝜃
s y ps ps
– 𝐴 𝑓 + 𝐴 𝑓 ≥
Face of bearing to Critical Section
V
u
cpv
− 0.5𝑉 − 𝑉
s p
cot 𝜃
•
𝐴ps𝑓ps > 𝐴s𝑓y
142
𝐹y
𝐹x
𝜃
𝐹y
𝐹x
tan 𝜃 = , 𝐹x =
𝐹y
= 𝐹y cot 𝜃
tan 𝜃
141
10
142

## Slide 72: Longitudinal Tension Tie
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
143
At face of support
FOS = 2.208 ft
d
l = 3.943 ft
V
u
cpv
s p
cot 𝜃 = 413.73kip − 0.5 459.7𝑘𝑖𝑝 − 43.18𝑘𝑖𝑝 cot 28.02° = 350.7𝑘𝑖𝑝
– 𝐴ps = 9.548 𝑖𝑛2,
– 𝑓ps = 126.855 𝑘𝑠𝑖, reduced due to lack of full development per LRFD 5.9.4.3.2
– 𝑉u = 413.73 𝑘𝑖𝑝
– 𝑉s = 459.7 𝑘𝑖𝑝
– 𝑉p = 43.18 𝑘𝑖𝑝
– 𝜃 = 28.02°
– Demand: − 0.5𝑉 − 𝑉
o.9
– Capacity: 𝐴ps𝑓ps = 9.548𝑖𝑛2 126.885𝑘𝑠𝑖 = 1211.5𝑘𝑖𝑝
– 1211.5 𝑘𝑖𝑝 > 350.7 𝑘𝑖𝑝, 𝑂𝐾
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Development Length
LRFD 5.9.4.3.2
The distance required to develop the specified strength of a reinforcing bar or prestressing strand at nominal resistance
𝑙 ≥ 𝑘 𝑓 − 2 𝑓 𝑑
d ps 3 pe b
144
143
10
144

## Slide 73: Interface Shear
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
145
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Interface Shear
Horizontal shear force develops at the deck/girder interface
Shear force is resisted by cohesion (bond between concrete), aggregate interlock, shear friction
Adequate interface shear resistance is required for composite action
146
145
10
146

## Slide 74: Interface Shear Resistance
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
LRFD 5.7.4.3
𝑉ui ≤ 𝑉ri = 𝜙𝑉ni
𝑉ni = 𝑐𝐴ev + 𝜇 𝐴vf𝑓y + 𝑃e but not to exceed
e
– 𝑉ni ≤ 𝐾1𝑓,𝐴ev - concrete strength available to resist interface shear
– 𝑉ni ≤ 𝐾2𝐴ev - limiting interface shear
Cohesion 𝑐𝐴ev
Friction 𝜇(𝐴vf𝑓y + 𝑃e)
  Use minimum load factors for 𝑃e when it increases resistance
  𝑃e is conservatively taken as zero
147
Participant Materials
https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Cohesion and Fraction Factors
LRFD 5.7.4.4
148
 | 𝒄 (𝒌𝒔𝒊) | 𝝁 | 𝑲𝟏 | 𝑲𝟐 (𝒌𝒔𝒊)
Cast-in-place concrete slab on clear girder surface, free of laitance with surface roughened to an amplitude of 0.25 in | 0.28 | 1.0 | 0.3 | 1.8 NWC 1.3 LWC
For concrete placed against a clean concrete surface, free of laitance, but not intentionally roughened: | 0.075 | 0.6 | 0.2 | 0.8
147
10
148

## Slide 75: Interface Shear Force
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
LRFD 5.7.4.5
•
𝑉ui = 𝑣ui𝐴ev = 𝑣ui
12 in
1 ft
vi
𝑏 where 𝑣
ui
= VuQ
lbvi
ui
l
= VuQ kip ft
𝑉
These calculations are most easily carried out on a per-foot basis
149
𝐴ev
𝐴vf
𝑏vi
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Parameters at Critical Section
= 588 in
2
12 in
1 ft ft
vf
𝐾1 = 0.3, 𝐾2 = 0.8, 𝑐 = 0.280 𝑘𝑠𝑖, 𝜇 = 10.0
𝐴ev = 49𝑖𝑛
2 - #5 @ 3.5” extending from top flange into deck
𝐴 = 2 o.31in
2
3.5in
12 in
1 ft
= 2.216 in
2
ft
150
149
10
150

## Slide 76: Capacity
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Conservatively take 𝑃e = 0
𝑉ni = 𝑐𝐴ev + 𝜇 𝐴vf𝑓y + 𝑃e
= 0.280 𝑘𝑠𝑖 588in2
ft
+ 1.0 2.126in2
ft
1 e ev
ft
𝐾 𝑓,𝐴 = 0.3 4𝑘𝑠𝑖 588in2 = 705.6 𝑘𝑖𝑝⁄𝑓𝑡,
2 ev
ft
ri ni
𝐾 𝐴 = 1.8 588in2 = 1058.4 𝑘𝑖𝑝⁄𝑓𝑡
𝑉ni = 292.183 𝑘𝑖𝑝⁄𝑓𝑡
𝑉 = 𝜙𝑉 = 0.9 292.183 kip = 262.965 kip
ft ft
151
60𝑘𝑠𝑖 = 292.183 𝑘𝑖𝑝⁄𝑓𝑡 Controls
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
𝑉
ui
= VuQ =
Demand
413.73kip 12199.9i 3
l 124657o.6i 4
= 48.589 k
ft
ui ri
ft ft
𝑉 = 48.6 k ≤ 𝑉 = 262.965 kip OK
152
151
10
152

## Slide 77: Required Reinforcement
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
vf
fy
Minimum 𝐴 ≥ o.o5Acv, LRFD 5.7.4.2
vf
𝐴 need not exceed requirement for 1.33 ui
cp
– 1.33𝑉ui/𝜙 = 𝑐𝐴ev + 𝜇 𝐴vf𝑓y + 𝑃e , Solve for 𝐴vf
Minimum required waived for Girder/Slab interfaces roughened to 0.25” amplitude and 𝑣ui < 0.210 𝑘𝑠𝑖
– 𝑣
ui
bvidv Acv
= Vu1 = Vu1 = 48.589 = 0.083 ksi < 0.210 ksi
588 ft ft
– Minimum reinforcement required is waived
Maximum spacing = 24”, Max provided is 18” per WSDOT
153
𝐴ev
𝐴
vf
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Slab Haunch Build-up
154
153
10
154

## Slide 78: Slab Haunch
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
155
“A”
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
“A” Dimension (Slab Offset)
•
𝐴hauneh = 𝐴slab+fillet + 𝐴profile effeet + 𝐴girder orientation effeet + 𝐴exeess eamber
156
155
10
156

## Slide 79: Slab + Fillet
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
157
Minimum build-up
𝐴slab+fille = 𝑡slab + 𝑡fillet
WSDOT: 𝑡fillet = 3/4“
𝐴slab+fillet = 7.5 𝑖𝑛 + 0.75 𝑖𝑛 = 8.25 𝑖𝑛
Location of minimum haunch
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
ve
𝐴 = 1.5 g2-g1 Lg
Profile Effect – Vertical Curve
2
Lvc
ve
2
1oo 6ooft
= 0.194 𝑖𝑛
𝐴 = 1.5 -1.5%- -2% 124.58ft
Positive for sag curves
Negative for crest curves
158
Vertical Curve Effect
157
10
158

## Slide 80: Profile Effect – Horizontal Curve
12/5/2022
𝐴
he
2
= 1.5s m
R
=
1.5 827.42 − 702.71𝑓𝑡 2 0.04 𝑓𝑡
𝑓𝑡
6000 𝑓𝑡
= 0.156𝑖𝑛
•
𝐴profile = 𝐴ve + 𝐴he
= 0.194𝑖𝑛 + 0.156𝑖𝑛 = 0.350𝑖𝑛
159
Horizontal Curve Effect
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Girder Orientation Effect
go
𝐴 = 𝑚 W, plumb girder
go
𝐴 =
d 2
W 2
g
1+m2
md-mg , tilted girder
Varies along girder in regions of superelevation transition
2
𝐴go = 0.04 49in = 0.980𝑖𝑛
160
159
10
160

## Slide 81: Excess Camber
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Camber that remains after all loads are applied
Δ1 = Δgirder + Δps
Δ2 = Δ1 + Δereep1
– Δereep1 = 𝜓b 𝑡e, 𝑡i Δ1
Δ1& Δ2 are computed based on storage then adjusted for erection
Δ3 = Δ2 + Δtpr + Δdiaphragm
Δ4 = Δ3 + Δereep2
– 𝜓b 𝑡d, 𝑡i − 𝜓b 𝑡e, 𝑡i Δ1 + 𝜓b 𝑡d, 𝑡e
Δereep2 = Δtpr + Δdiaphragm + 𝛿girder
– 𝛿girder = change in dead load deflection between storage and erection
Δ5 = Δ4 + Δdeek + Δhauneh
Δ6 = Δ5 + Δbarrier = Δexeess (Assumes no creep deflection after deck is composite)
161
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Creep Coefficients
Prestress release until erection 𝜓b 𝑡h, 𝑡i = 𝜓b 𝑡e = 90, 𝑡i = 1 = 0.852
Prestress release until deck casting 𝜓b 𝑡d = 120, 𝑡e = 1 = 0.912
Compute creep coefficient for erection to deck casting
ei
f
– 𝑓, = 7.4 𝑘𝑠𝑖
– 𝑘 = 5 = 0.610
1+7.4
12o-9
td 12 100-4(7.4) +(12o-9 )
– 𝑘 = = 0.488
7.4+20
– 𝜓b 𝑡d = 120, 𝑡e = 90 = 1.9 1.04 0.96 0.610 0.488 90 -o.118 = 0.331
162
161
10
162

## Slide 82: Excess Camber
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Δgirder = −3.802 𝑖𝑛
Δps = 6.897 𝑖𝑛
Δereep1 = 2.639 𝑖𝑛
Δtpr = 0.628 𝑖𝑛
Δdiaphragm = −0.141 𝑖𝑛
Δslab = −2.610 𝑖𝑛
Δhauneh = −0.808 𝑖𝑛
Δereep2 = 0.347 𝑖𝑛
Δbarrier = −0.457 𝑖𝑛
Δ1 = −3.802 + 6.897 = 3.096𝑖𝑛
Δ2 = 3.096 + 2.639 = 5.735 𝑖𝑛
Δ3 = 5.735 + 0.628 − 0.141 = 6.222 𝑖𝑛
Δ4 = 6.222 + 0.347 = 6.569 𝑖𝑛 = 𝐷12o
Δ5 = 6.569 − 2.610 − 0.808 = 3.150 𝑖𝑛
Δ6 = 3.150 − 0.457 = 2.693𝑖𝑛
Δexeess = Δ6 = 2.693 𝑖𝑛
120
D = Camber at deck casting
163
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Required Slab Haunch
𝐴hauneh = 𝐴slab+fill + 𝐴profile effeet + 𝐴girder orientation effeet + 𝐴exeess eamber
𝛢hauneh = 8.25𝑖𝑛 + 0.98𝑖𝑛 + 0.35𝑖𝑛 + 2.693𝑖𝑛 = 12.27 𝑖𝑛
𝐴provided = 12.5 𝑖𝑛
164
“A”
163
10
164

## Slide 83: Camber Range
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Camber variation
  Construction Timing
    40-120 days
  Natural
    ±25% variation from average
AASHTO Equations result in an upper bound camber prediction
WSDOT provides range of camber
  D40 = lower bound at 40 days
  D120 = upper bound at 120 days
165
Also see, “A Probabilistic Comparison of Prestress Loss Methods in Prestressed Concrete Beams”, Gilbertson, et. al., PCI Journal, Sept-Oct 2004
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Lower Bound Camber (D40)
Creep coefficients
– ψb td = 10, ti = 1 = 0.257
– ψb tf = 40, t1 = 1 = 0.638
– ψb td = 40, te = 10 = 0.429
Creep during storage
– ∆creep1= 0.638 6.897in − 3.802in = 0.795in
Creep between diaphragm and deck casting
–
∆creep2=
0.638 − 0.257 6.897in − 3.802in + 0.429 −0.141in = 1.391in
Δ4 = Δgirder + Δps + Δereep1 + Δtpr + Δdiaphragm + Δereep2 = 5.769 𝑖𝑛 = 𝐷4o
Lower Bound 0.5𝐷4o = 2.88 𝑖𝑛
Expected range of camber is 2.9 𝑖𝑛. 𝑎𝑡 40 𝑑𝑎𝑦𝑠 − 6.6 𝑖𝑛. 𝑎𝑡 120 𝑑𝑎𝑦𝑠
166
165
10
166

## Slide 84: Girder Sag Check
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Lower Bound 0.5𝐷4o = 2.88 𝑖𝑛
𝐷4o = ∆4= 5.796 𝑖𝑛
Δ5 = 5.796 − 2.610 − 0.808 = 2.351 𝑖𝑛 (after deck casting)
Δ6 = 2.351 − 0.457 = 1.894𝑖𝑛 = ∆exeess (after all loads)
Screed camber (downward deflection due to deck and superimposed loads)
– ∆exeess= ∆6= 𝐷 − 𝐶 = ∆4 − 𝐶
– 𝐶 = ∆4 − ∆6= 5.769 − 1.894 = 3.875 𝑖𝑛
𝐶 > 0.50𝐷4o - Girder may have a sag
The average camber at 40 days is 75%𝐷4o = 4.327 𝑖𝑛
𝐶 < 0.75𝐷4o -Sag unlikely
167
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Load Rating
168
167
10
168

## Slide 85: Load Rating
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Load Rating – The determination of the live-load carrying capacity of an existing bridge
Live Load
𝑅𝐹 = Capaeity -Dea Load ≥ 1.0
•
Criteria
  AASHTO “The manual for bridge evaluation” (MBE), 3rd Edition, 2018 + 2020 interims
  WSDOT Bridge Design Manual, Chapter 13
169
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Load Rating Types
Design Load Rating
  Inventory Rating (evaluation at design reliability, 𝛽 = 3.5)
  Operating Rating (evaluation at operating reliability, 𝛽 = 2.5)
  HL-93 Live Load
Legal Load Rating
  Safe load capacity of AASHTO and state legal loads
  Routine Commercial Traffic, Specialized Hauling Vehicles, Emergency Vehicles
Permit Load Rating
  Check safety and serviceability in review of permit applications
  Routine (Annual) Permits, Special (Limited Crossing) Permits
170
169
10
170

## Slide 86: WSDOT Criteria
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
All Ratings
  Rate for Flexure and Shear at the Strength I limit state
  Rate for Tension Stress at the Service III limit state
    Live Load Factor, 𝛾LL = 1.0
    0.19𝜆 𝑓, ≤ 0.600 ksi tension limit
e
Permit Ratings - Check optional reinforcement yield strain limit in pretensioned members
171
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Inventory Rating - Moment
𝑅𝐹 = cpccpscpnKMn-yDCMDC-yDWMDW
yLLMLLlM
LLlM
•
𝜙e𝜙s ≥ 0.85
𝜙e = 𝜙s = 𝜙n = 1.0
𝑀n = 20526.2𝑘 · 𝑓𝑡
𝑀DC = 7466.6𝑘 · 𝑓𝑡
𝑀DW = 0.0𝑘 · 𝑓𝑡
𝑀 = 3804.05 k·ft
girder
min
𝑀 = 𝑚𝑖𝑛 {
𝑀er 1.33𝑀u
= 14707.13𝑘 · 𝑓𝑡
Mmin
147o7.13k·ft
𝐾 = Mr = 1.o 2o526.2k·ft = 1.39 ≤ 1.0 ∴ 1.0
𝑅𝐹 =
(1.75)(38o4.o5k· )
𝑀er = 14707.13𝑘 · 𝑓𝑡
𝑀u = 17099.79𝑘 · 𝑓𝑡
•
𝛾DC = 1.25, 𝛾DW = 1.50, 𝛾LL = 1.75
2o526.2k· 1.25 7466.6k·ft -(1.5)(ok·ft)
𝑅𝐹 = 1.68
172
171
10
172

## Slide 87: Inventory Rating – Service III
12/5/2022
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
𝑅𝐹 = fR-yDCfDC-yDWfDW
•
yLLfLLlM
𝑓R = 𝑓limit − 𝑓ps = 0.19𝜆 𝑓, − 𝑓ps
e
𝑓R = 0.19 1.0 8.7𝑘𝑠𝑖 − (−6.221𝑘𝑠𝑖) = 0.560𝑘𝑠𝑖 − (−6.221𝑘𝑠𝑖) = 6.781𝑘𝑠𝑖
𝛾LL = 1.0
•
(1.o)(1.789ksi)
𝑅𝐹 = 6.78 1.o 4.268ksi -1.o(oksi) = 1.40
173
Participant Materials https://ftp.wsdot.wa.gov/incoming/PSCBridgeDesignWorkshop
Design Summary
ei
𝑓, = 7.2 𝑘𝑠𝑖, 𝑓, = 8.7 𝑘𝑠𝑖
e
Prestressing: 44 Straight, 17 Harped, 4 Temporary
Stirrups per WSDOT standard
Slab Offset (“A”) = 12.5”
Pick point: 8’-3”
Bunk point: 13’-8”
Minimum Truck Stiffness: 40,000 kip-in/rad with 72” wheelbase
Load Rating:
  Inventory: Service III RF = 1.4,
  Operating: +M RF = 2.18
174
173
10
174

## Slide 88: Precast, Prestress Bridge Girder Design Example
PGSuper Training
WSDOT Bridge and Structures Office

## Slide 90
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Title | Precast, prestressed bridge girder design example – PGSuper Training |  |  |  |  |  |  |  | Publication No. |  | 
Abstract This document is a detailed design example of a 165 ft long, WF74G precast-prestressed concrete bridge girder. The example illustrates design, analysis, and load rating of a typical exterior girder in a horizontally curved structure. The primary design elements include alignment and bridge geometrics, loads and load distribution, flexure design for optimized fabrication, shear design, deflections and camber, slab haunch build-up, lateral stability during initial lifting of the girder from the casting bed and hauling the girder from the fabrication facility to the bridge site, treatment of prestress losses, and load rating. This example is intended to illustrate the calculations performed by the BridgeLink::PGSuper computer program. |  |  |  |  |  |  |  |  |  |  | 
Notes |  |  |  |  |  |  |  |  |  |  | 
Author |  | Richard Brice, PE |  |  |  | Sponsor | WSDOT |  |  |  | 
Specification |  | AASHTO LRFD Bridge Design Specifications, 9th Edition, 2020 WSDOT Bridge Design Manual (M 23-50.21), June 2022 |  |  |  |  |  |  |  |  | 
Original Publication Date |  |  |  | 10/18/2018 | Date of Latest Revision |  |  | 11/16/2022 |  | Version | 3.2
Notice of Copyright |  |  | Copyright © 2018-2022, Washington State Department of Transportation, All rights reserved |  |  |  |  |  |  |  | 

## Slide 92
1
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Table of Contents
1 Introduction..........................................................................................................................................................................1
1.1 Sign Convention ..........................................................................................................................................................1
2 Bridge Description ...............................................................................................................................................................1
2.1 Site Conditions............................................................................................................................................................. 1
2.2 Roadway ......................................................................................................................................................................1
2.3 Bridge Layout ..............................................................................................................................................................2
3 Design Preliminaries............................................................................................................................................................ 4
3.1 Construction Sequence.................................................................................................................................................4
3.2 Girder Length...............................................................................................................................................................5
3.3 Section Properties ........................................................................................................................................................6
3.3.1 Effective Flange Width ........................................................................................................................................6
3.3.2 Composite Girder Properties................................................................................................................................6
3.3.3 First Moment of Area of deck slab, .....................................................................................................................8
3.3.4 Section Property Summary ..................................................................................................................................8
3.4 Structural Analysis....................................................................................................................................................... 9
3.4.1 Girder Fabrication ................................................................................................................................................9
3.4.2 Erected Girder.................................................................................................................................................... 10
3.4.3 Analysis Results Summary ................................................................................................................................ 14
3.4.4 Limit State Responses........................................................................................................................................ 15
3.4.5 Live Load Distribution Factors .......................................................................................................................... 15
4 Flexure Design................................................................................................................................................................... 18
4.1 Step 1 Design for Final Service Conditions ............................................................................................................... 21
4.1.1 Stresses due to loads on non-composite section................................................................................................. 21
4.1.2 Stresses due to loads on the composite section .................................................................................................. 21
4.1.3 Check Estimate of Final Concrete Strength ....................................................................................................... 24
4.2 Step 2 - Design for Lifting without Temporary Top Strands ..................................................................................... 25
4.2.1 Proportion Strands ............................................................................................................................................. 25
4.2.2 Prestress losses................................................................................................................................................... 26
4.2.3 Concrete strength for form stripping.................................................................................................................. 27
4.2.4 Check girder stability ......................................................................................................................................... 28
4.3
4.4
Step 3 - Design for Shipping...................................................................................................................................... 35 Step 4 - Design for Lifting with Temporary Top Strands .......................................................................................... 36
4.4.1 Prestress losses................................................................................................................................................... 36
4.4.2 Check girder stability ......................................................................................................................................... 37
4.5 Step 5 – Revise Shipping Design ............................................................................................................................... 42
4.5.1 Estimate Prestress Losses at Shipping ............................................................................................................... 42

## Slide 93
2
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
4.5.2 Check Girder Stability ....................................................................................................................................... 44
4.5.3 Check concrete strength ..................................................................................................................................... 54
4.6 Step 6 – Check Erection Stresses ............................................................................................................................... 55
4.6.1 Losses between Transfer to Deck Placement ..................................................................................................... 55
4.6.2 Stresses .............................................................................................................................................................. 57
4.7 Step 7 – Check Final Conditions................................................................................................................................ 58
4.7.1 Losses from Deck Placement to Final................................................................................................................ 58
4.7.2 Stresses .............................................................................................................................................................. 60
4.7.3 Moment Capacity............................................................................................................................................... 63
4.8 Check Splitting Resistance ........................................................................................................................................ 68
4.9 Check Confinement Zone Reinforcement.................................................................................................................. 69
5 Shear Design ...................................................................................................................................................................... 69
5.1 Locate Critical Section for Shear ............................................................................................................................... 69
5.2 Check Ultimate Shear Capacity ................................................................................................................................. 70
5.2.1 Compute Nominal Shear Resistance .................................................................................................................. 70
5.2.2 Check Requirement for Transverse Reinforcement ........................................................................................... 73
5.2.3 Check Minimum Transverse Reinforcement ..................................................................................................... 73
5.2.4 Check Maximum Spacing of Transverse Reinforcement................................................................................... 73
5.3
5.4
Check Longitudinal Reinforcement for Shear ........................................................................................................... 74
Check Horizontal Interface Shear .............................................................................................................................. 74
5.4.1 Check Nominal Capacity ................................................................................................................................... 75
5.4.2 Check Minimum Reinforcement........................................................................................................................ 76
6 Check the “A” Dimension ................................................................................................................................................. 76
6.1 Slab and Fillet ............................................................................................................................................................ 76
6.2 Profile Effect.............................................................................................................................................................. 77
6.2.1 Vertical Curve .................................................................................................................................................... 78
6.2.2 Horizontal Curve................................................................................................................................................ 79
6.2.3 Profile Effect...................................................................................................................................................... 79
6.3
6.4
Girder Orientation Effect ........................................................................................................................................... 79
Excess Camber........................................................................................................................................................... 80
6.4.1
6.4.2
Compute Creep Coefficients .............................................................................................................................. 82
Compute Deflections ......................................................................................................................................... 82
6.5
6.6
Check Required Haunch ............................................................................................................................................ 83
Compute Lower Bound Camber at 40 days ............................................................................................................... 83
6.6.1 Creep Coefficients ............................................................................................................................................. 83
6.6.2 Compute Deflections ......................................................................................................................................... 83
6.7 Check for Possible Girder Sag ................................................................................................................................... 83

## Slide 94
3
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
7 Bearing Seat Elevations ..................................................................................................................................................... 83
8 Design Summary ............................................................................................................................................................... 84
9 Load Rating ....................................................................................................................................................................... 84
9.1 Inventory Rating ........................................................................................................................................................ 84
9.1.1 Moment .............................................................................................................................................................. 84
9.1.2 Shear .................................................................................................................................................................. 85
9.1.3 Bending Stress – Service III limit state .............................................................................................................. 85
9.2 Operating Rating........................................................................................................................................................ 85
9.2.1 Moment .............................................................................................................................................................. 85
9.2.2 Shear .................................................................................................................................................................. 86
9.3 Legal Loads................................................................................................................................................................ 86
9.3.1 Moment .............................................................................................................................................................. 87
9.3.2 Shear .................................................................................................................................................................. 87
9.3.3 Bending Stress – Service III limit state .............................................................................................................. 87
9.3.4 Special Hauling Vehicles (SHV) ....................................................................................................................... 88
9.4 Permit Loads .............................................................................................................................................................. 88
10 Software ......................................................................................................................................................................... 89
11 References...................................................................................................................................................................... 90

## Slide 95
4
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
List of Figures
Figure 2-1: Bridge Plan................................................................................................................................................................ 2
Figure 2-2: Bridge Section at Station 7+82.50 ............................................................................................................................2
Figure 2-3: Girder Dimensions ....................................................................................................................................................3
Figure 2-4: Slab Detail................................................................................................................................................................. 3
Figure 3-1 Assumed Construction Sequence ...............................................................................................................................5
Figure 3-2 Connection Geometry ................................................................................................................................................5
Figure 3-3 Effective Flange Width ..............................................................................................................................................6
Figure 3-4 Centroid of Non-composte and Composite Section ...................................................................................................8
Figure 3-5 Main slab section for slab loading............................................................................................................................ 11
Figure 3-5: Slab Haunch ............................................................................................................................................................ 12
Figure 3-6: HL93 Live Load Model .......................................................................................................................................... 14
Figure 3-7: eg Detail................................................................................................................................................................... 15 Figure 4-1: Optimized Fabrication Girder Design Procedure .................................................................................................... 20
Figure 4-2: Optimum Strand Arrangement ................................................................................................................................ 25
Figure 4-3: Equilibrium of Hanging Girder ............................................................................................................................... 29
Figure 4-4: Girder Self-Weight Deflection during Lifting......................................................................................................... 29 Figure 4-5: Offset Factor ........................................................................................................................................................... 31
Figure 4-6: Equilibrium during Hauling .................................................................................................................................... 45
Figure 4-7: Prestress induced Deflection based on Storage Datum ........................................................................................... 46
Figure 4-8: Girder Self-Weight Deflection during Storage ....................................................................................................... 46
Figure 4-9: Discretized Girder Section for Strain Compatibility Analysis ................................................................................ 65
Figure 5-1: Graphical method to Determine Critical Section Location ..................................................................................... 70 Figure 5-2: Flexural Tension Side of Beam with Area of Concrete and Area of Steel Identified ............................................. 72 Figure 6-1: Slab + Fillet Effect .................................................................................................................................................. 77
Figure 6-2: General Method for Profile Effect .......................................................................................................................... 77
Figure 6-3: Vertical Curve Effect .............................................................................................................................................. 78
Figure 6-4: Horizontal Curve Effect .......................................................................................................................................... 79
Figure 6-5: Top Flange Effect ................................................................................................................................................... 80
Figure 6-6: Camber Effect ......................................................................................................................................................... 80
Figure 6-7: Camber Diagram ..................................................................................................................................................... 81

## Slide 96
5
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Revisions
Date | Version | Name | Revision
10/8/2018 | 1.0 | Brice | Original example
03/09/2022 | 2.0 | Brice | Updated calculations of capacity reduction factor for flexure
03/18/2022 | 3.0 | Brice | Changed bridge configuration and girder type so design includes temporary top strands for shipping.
06/02/2022 | 3.1 | Brice | Evaluation of total reinforcement strain from moment capacity analysis did not include the initial strain. The calculation is updated to show the total strain is the sum of the net tensile strain and the initial strain.
10/19/2022 | 3.2 | Brice | Editorial and format revisions

## Slide 98
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Introduction
The purpose of this document is to illustrate how the PGSuper computer program performs its computations. PGSuper is a computer program for the design, analysis, and load rating of precast, prestressed concrete girder bridges.
A design example followed by a load rating analysis illustrates the engineering computations performed by PGSuper. PGSuper uses a state-of-the-art iterative design algorithm and other iterative computational procedures. Only the final iterative steps are of interest. To avoid lengthy iterations in this document, trial variables are “guessed” based on the final iterations produced by the software.
PGSuper uses 16 decimals of precision. There will be minor differences between these “hand” calculations and numbers reported by PGSuper. When noted, these calculations adopt numeric values reported by PGSuper.
  Sign Convention
This document and PGSuper use the following sign convention.
Item Value
Compression < 0
Tension > 0
Upward Deflection > 0
Downward Deflection < 0
Top Section Modulus < 0
Bottom Section Modulus > 0
Strand Eccentricity above Centroid < 0
Strand Eccentricity below Centroid > 0
Bridge Description
  Site Conditions
Normal Exposure
Average Ambient Relative Humidity: 75%
  Roadway
Alignment
PI Station | Back Tangent | Delta | Radius | 
10+00 | N 34° 45’ 32” W | 12° 34’ 15” R | 6000 ft | 
Profile |  |  |  | 
PVI Station | PVI Elevation | Grade in (𝐠𝐠𝟏𝟏) | Grade out (𝐠𝐠𝟐𝟐) | Length
9+00 | 100.00 | -2% | -1.5% | 600 ft
Superelevations
Left
Right
ft
0.04
ft
ft
−0.04
ft

## Slide 99
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
2.3 Bridge Layout
Back of Pavement Seat, Abutment 1, 7+00
Back of Pavement Seat, Abutment 2, 8+65 Abutments are oriented at S 58° 41′ 13.47" W Abutment 1, Skew Angle 0°
Abutment 2, Skew Angle 1° 34′ 32.28" L
Figure 2-1: Bridge Plan
Figure 2-2: Bridge Section at Station 7+82.50

## Slide 100
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Girders
6 WF74G @ 7’-0”
measured radial at BPS
A = 923.531 in2 Ix = 734356.0 in4 Iy = 72018.4 in4 Yt = 38.343 in Yb = 35.657 in St = 19152.5 in3 Sb = 20594.8 in3
Perimeter = 289.284 in
Wtf = 49.0 in Wbf = 38.375 in tweb = 6.125 in
f’ci = to be determined f’c = to be determined wc = 155 lb/ft3
wc = 165 lb/ft3 (including rebar)
Prestressing = to be determined
49.000in.
38.375in.
74.000in.
6.125in.
Figure 2-3: Girder Dimensions
Harping points at 0.4L from the end of the girder.
Interior Diaphragms |  | 
Rectangular – Between girders only. | H = 62.875 in T = 8.00 in | Located at 0.25Ls, 0.50Ls and 0.75Ls.
Slab
Gross Depth = 7.5 in Overhang Edge Depth = 7.0 in Overhang = Varies Edge Offset = 21’-0” Overall width = 42’-0” Slab Offset (“A” Dimension) = To be determined Fillet = ¾” Sacrificial Depth = ½” f’c = 4 ksi wc = 150 lb/ft3 wc = 155 lb/ft3 (including rebar) Future Wearing Surface, 0.035 k/ft2
Figure 2-4: Slab Detail
Strands

## Slide 101
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
0.6” Diameter Grade 270 Low Relaxation | fpu = 270.0 ksi fpy = 243.0 ksi Eps = 28500 ksi aps = 0.217 in2/per strand
Traffic Barrier
42” Single Slope Design weight = 0.690 kip/ft/barrier Load is distributed to 3 exterior girders
Load Modifiers |  | 
Ductility D = 1.0 | Redundancy R = 1.0 | Importance I = 1.0
Criteria
Design in accordance with the AASHTO LRFD Bridge Design Specification, Ninth Edition, 2020 and the WSDOT Bridge Design Manual Load Rate in accordance with AASHTO, The Manual for Bridge Evaluation, Third Edition, 2018 with 2020 interim revisions and the WSDOT Bridge Design Manual WSDOT policy is to design using gross section properties (BDM 5.6.2.I) using refined estimate of prestress losses (BDM 5.4.1.C) and elastic gains. PGSuper supports stress analysis with transformed section properties, the LRFD approximate method for estimating prestress losses, and a non-linear time-step analysis.
Design Preliminaries
The framing of this bridge results in girders that are all the same length. The left exterior girder (Girder A) has the largest overhang at mid-span. Design and load rate Girder A.
  Construction Sequence
Figure 3-1 shows the assumed construction sequence. PGSuper models the various construction stages with Construction Events.

## Slide 102
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Event 1 – Construct Girders and Erect Piers
Event 2 – Erect Girders
Event 3 – Remove Temporary Strands and Cast Diaphragms
Event 4 – Cast Deck
Event 5 – Construct Traffic Barriers Event 6 & 7– Open to Traffic
Figure 3-1 Assumed Construction Sequence
3.2 Girder Length
For a typical stub abutment with a Type A connection, the centerline of bearing is located 2’-8.5” from, and measured normal to, the back of pavement seat (BPS). The distance from the centerline bearing to the end of the girder is 1’-8.5” measured normal to the CL Bearing, which is parallel to the back of pavement seat.

BPS CL Brg CL Brg BPS
1.7083'
2.7083'
Radial at 8+65
Radial at
7+00
Parallel lines

d2
d2 = d1/cos
 = 1.575634°
164.995'
Figure 3-2 Connection Geometry

## Slide 103
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
The BPS-to-BPS distance of 165 ft is measured along the arc of the horizontal curve. The angle subtended by the girder is
𝛿𝛿
𝛿𝛿 = 𝐿𝐿𝑐 𝑐 180 = 165 180 = 1.575634°. The chord length of the girder is 2𝑅𝑅 𝑠𝑠𝑠𝑠𝑠𝑠 = 2 6000 𝑠𝑠𝑠𝑠𝑠𝑠
𝑅𝑅 𝜋𝜋 6000 𝜋𝜋 2 2
( ) 1.575634 = 164.995 𝑓𝑓𝑓𝑓 .
The bearing-to-bearing span length is 𝐿𝐿𝑠𝑠 = 164.995𝑓𝑓𝑓𝑓 − 2.7083𝑓𝑓𝑓𝑓 − (2.7083𝑓𝑓𝑓𝑓)/𝑐𝑐𝑐𝑐𝑠𝑠 (1.575634) = 159.578𝑓𝑓𝑓𝑓. The overall girder length is 𝐿𝐿𝑔𝑔 = 159.577𝑓𝑓𝑓𝑓 + 1.7083𝑓𝑓𝑓𝑓 + (1.7083𝑓𝑓𝑓𝑓)/𝑐𝑐𝑐𝑐𝑠𝑠 (1.575634) = 162.995𝑓𝑓𝑓𝑓.
  Section Properties
Compute the composite section properties. The basic (non-composite) girder section properties are given in the bridge description.
    Effective Flange Width
The effective flange width of a composite concrete deck slab is the tributary width of the member (LRFD 4.6.2.6.1). LRFD C4.6.2.6.1 states “These provisions are considered applicable for skew angles less than or equal to 75 degrees, L/S greater than or equal to 2.0 and overhang widths less than or equal to 0.5S”. The maximum overhang is approximately 4 ft which exceeds S/2 = 3.5ft. For this reason, the overhang portion of the effective flange width is taken to be equal to S/2.
Varies 3.5ft - 4.07'ft
S=7'-0"
7'-0"
S/2 =3.5'
S/2 =3.5'
A
B
Figure 3-3 Effective Flange Width
The effective flange width is measured perpendicular to the centerline of the girder.
12𝑠𝑠𝑠𝑠
𝑤𝑤𝑒𝑒𝑒𝑒𝑒𝑒 = (3.5𝑓𝑓𝑓𝑓 + 3.5𝑓𝑓𝑓𝑓) � 1𝑓𝑓𝑓𝑓 � 𝑐𝑐𝑐𝑐𝑠𝑠1.575634 = 83.97𝑠𝑠𝑠𝑠
3.3.2 Composite Girder Properties
Transform the slab to equivalent girder material and use the parallel axis theorem to compute the composite girder properties. At mid-span the bottom of the slab is above the top of the girder by the fillet amount (¾”). If the actual camber exceeds the predicted camber, the ¾” fillet can be easily lost. Assume the bottom of the slab is directly on top of the girder. This provides the least stiff section where the maximum demand occurs. For simplicity, use this section model at all locations (BDM 5.6.2.B.1).
PGSuper has options to include the haunch depth in the section properties calculations. Each section can use the minimum haunch depth (fillet dimension) or the actual haunch depth. Using the actual

## Slide 104
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
haunch depth means there is a different set of section properties at every cross section. Using more precise section properties may be desirable for load rating.
Modulus of elasticity of slab concrete
𝐸𝐸 = 120,000𝐾𝐾 𝑤𝑤2𝑓𝑓′0.33 = (120,000)(1.0)(0.150)2(4.0)0.33 = 4266.223 𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐 1 𝑐𝑐 𝑐𝑐
𝑐𝑐
Modulus of elasticity of girder concrete assuming a concrete strength of 𝑓𝑓′ = 8.7𝑘𝑘𝑠𝑠𝑠𝑠
𝐸𝐸 = 120,000𝐾𝐾 𝑤𝑤2𝑓𝑓′0.33 = (120,000)(1.0)(0.155)2(8.7)0.33 = 5886.891 𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐 1 𝑐𝑐 𝑐𝑐
The overall controlling 28-day design concrete strength is 8.7 ksi after multiple design iterations and refinements. See Section 4.6.2.
𝐸𝐸𝑐𝑐 𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠
𝐸𝐸𝑐𝑐 𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔
𝑠𝑠 = =
4266.223𝑘𝑘𝑠𝑠𝑠𝑠
5886.891𝑘𝑘𝑠𝑠𝑠𝑠
= 0.725
The sacrificial wearing surface is not part of the structural section. Use the structural slab depth for computing section properties.
𝑓𝑓𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 = 𝑓𝑓𝑔𝑔𝑔𝑔𝑔𝑔𝑠𝑠𝑠𝑠 𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 𝑔𝑔𝑒𝑒𝑑𝑑𝑑𝑑ℎ − 𝑓𝑓𝑠𝑠𝑠𝑠𝑐𝑐𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔𝑐𝑐𝑠𝑠𝑠𝑠 𝑔𝑔𝑒𝑒𝑑𝑑𝑑𝑑ℎ = 7.5𝑠𝑠𝑠𝑠 − 0.5𝑠𝑠𝑠𝑠 = 7.0𝑠𝑠𝑠𝑠
 | Area | Yb | (Area)(Yb)
Slab | (0.725)(83.9𝑠𝑠𝑠𝑠)(7.0𝑠𝑠𝑠𝑠) = 425.793𝑠𝑠𝑠𝑠2 | 7.0𝑠𝑠𝑠𝑠 74.0𝑠𝑠𝑠𝑠 + = 77.5𝑠𝑠𝑠𝑠 2 | 32998.958𝑠𝑠𝑠𝑠3
Girder | 923.531𝑠𝑠𝑠𝑠2 | 35.657𝑠𝑠𝑠𝑠 | 32930.345𝑠𝑠𝑠𝑠3
Total | 𝐴𝐴𝑐𝑐 = 1349.324𝑠𝑠𝑠𝑠2 |  | 65929.303𝑠𝑠𝑠𝑠3
𝑌𝑌𝑠𝑠𝑐𝑐 =
∑(𝐴𝐴𝐴𝐴𝐴𝐴𝐴𝐴)
∑(𝐴𝐴𝐴𝐴𝐴𝐴𝐴𝐴)(𝑌𝑌𝑠𝑠 ) 65929.303𝑠𝑠𝑠𝑠3
= = 48.861𝑠𝑠𝑠𝑠
1349.324𝑠𝑠𝑠𝑠2
𝑌𝑌𝑑𝑑𝑐𝑐 𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 = 𝐻𝐻𝑔𝑔 − 𝑌𝑌𝑠𝑠𝑐𝑐 = 74.0𝑠𝑠𝑠𝑠 − 48.861𝑠𝑠𝑠𝑠 = 25.139𝑠𝑠𝑠𝑠
 | Area | d | (Area)(d2) | Io | Io + (Area)(d2 )
Slab | 425.793𝑠𝑠𝑠𝑠2 | 7.0𝑠𝑠𝑠𝑠 74.0𝑠𝑠𝑠𝑠 + 2 − 48.861𝑠𝑠𝑠𝑠 = 28.639𝑠𝑠𝑠𝑠 | 349207.761𝑠𝑠𝑠𝑠4 | 1 (0.725)(83.9𝑠𝑠𝑠𝑠)(7.0𝑠𝑠𝑠𝑠) 12 = 1738.653𝑠𝑠𝑠𝑠4 | 350946.414𝑠𝑠𝑠𝑠4
Girder | 923.531𝑠𝑠𝑠𝑠2 | 35.657𝑠𝑠𝑠𝑠 − 48.861𝑠𝑠𝑠𝑠 = −13.204𝑠𝑠𝑠𝑠 | 161013.58𝑠𝑠𝑠𝑠4 | 734356.0𝑠𝑠𝑠𝑠4 | 895369.58𝑠𝑠𝑠𝑠4
 |  |  |  |  | 𝐼𝐼𝑥𝑥 = 1246315.994𝑠𝑠𝑠𝑠4
𝐼𝐼𝑥𝑥
𝑌𝑌𝑠𝑠𝑐𝑐
𝑆𝑆𝑠𝑠𝑐𝑐 = − = −
1246315.994𝑠𝑠𝑠𝑠4
48.861𝑠𝑠𝑠𝑠
= −25507.378𝑠𝑠𝑠𝑠3

## Slide 105
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝑆𝑆𝑑𝑑𝑐𝑐 𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 =
𝐼𝐼𝑥𝑥
𝑌𝑌𝑑𝑑𝑐𝑐 𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔
=
1246315.994𝑠𝑠𝑠𝑠4
25.113𝑠𝑠𝑠𝑠
= 49628.319𝑠𝑠𝑠𝑠3
3.3.3 First Moment of Area of deck slab,
𝑄𝑄𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 = 𝐴𝐴𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 �𝑌𝑌𝑑𝑑𝑐𝑐 𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔
𝑓𝑓𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 7𝑠𝑠𝑠𝑠
+ � = 425.793𝑠𝑠𝑠𝑠2 �25.113𝑠𝑠𝑠𝑠 + � = 12183.2125 𝑠𝑠𝑠𝑠3
2 2
3.3.4 Section Property Summary
Below are the section properties from PGSuper. They are slightly different then the properties computed above. Use the section properties reported by PGSuper for better agreement between these calculations and the software.
83.99"
38.343"
35.657"
48.867"
74"
81"
Noncomposite CG
25.113"
Composite CG
Figure 3-4 Centroid of Non-composte and Composite Section
Table 3-1: Section Properties from PGSuper
 | Girder | Composite Girder
Area, 𝐀𝐀 | 923.531 in2 | 1349.614 in2
𝐈𝐈𝐱𝐱 | 734356.0 in4 | 1246570.6in4
𝐈𝐈𝐲𝐲 | 72018.4 in4 | -
𝐘𝐘𝐭𝐭𝐭𝐭𝐭𝐭 𝐠𝐠𝐠𝐠𝐠𝐠𝐠𝐠𝐠𝐠𝐠𝐠 | 38.343 in | 25.113 in
𝐘𝐘𝐭𝐭𝐭𝐭𝐭𝐭 𝐬𝐬𝐬𝐬𝐬𝐬𝐬𝐬 | - | 32.116 in
𝐘𝐘𝐬𝐬 | 35.657 in | 48.867 in
𝐒𝐒𝐭𝐭𝐭𝐭𝐭𝐭 𝐠𝐠𝐠𝐠𝐠𝐠𝐠𝐠𝐠𝐠𝐠𝐠 | −19152.5 in3 | −49599.7 in3
𝐒𝐒𝐭𝐭𝐭𝐭𝐭𝐭 𝐬𝐬𝐬𝐬𝐬𝐬𝐬𝐬 | - | −53531.9 in3
𝐒𝐒𝐬𝐬 | 20594.8 in3 | 25509.3 in3
𝐐𝐐𝐬𝐬𝐬𝐬𝐬𝐬𝐬𝐬 | - | 12199.9 in3
Effective Flange Width, 𝐖𝐖𝐠𝐠𝐞𝐞𝐞𝐞 | - | 83.992 in
Perimeter | 289.284 in | -

## Slide 106
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
3.4 Structural Analysis
There are several significant stages during the life of a prestressed girder. PGSuper automatically models these stages as Construction Events. The events, and the related construction activities, are:
Fabricate girders
  Tension strands, place reinforcement, form girders, cast concrete, concrete curing. Initial relaxation of the prestressing strand occurs.
  Strip forms and impart the precompression force into the girder (aka Release)
  Move girders into storage area (Initial lifting)
  Elapsed time during storage (creep, shrinkage, and relaxation losses occur)
Erect girders
  Prior to erection, the girders must be transported from the fabrication facility to the bridge site
  Erect and brace girders
  De-tension temporary strands (if applicable)
Cast diaphragms and deck (dead load is applied to non-composite girder section)
Install railing system (traffic barriers, sidewalks, etc.) (dead load is applied to composite section)
Final without Live Load (includes future overlay if applicable)
Final with Live Load
PGSuper models the individual steps within a Construction Event with Analysis Intervals. For example, Event 1 – Construct Girders, models five analysis intervals: Tension Strands and Cast Concrete, Elapsed Time during Curing, Prestress Release, Lifting, Placement into Storage, and Elapsed Time during Storage.
The analysis intervals are a general modelling approach associated with time-step analysis. Precast girder design normally uses a 2-step time-step analysis. However, PGSuper can perform a refined non-linear time-step analysis. PGSplice uses the non-linear time-step analysis as well.
3.4.1 Girder Fabrication
Girder fabrication consists of tensioning strands, placing mild reinforcement, installing girder forms, and placing concrete. Stripping of girder forms occurs after the concrete reaches adequate strength to accommodate the stresses and stability of the girder. The strands are then detensioned but because of bond with the girder concrete, the tension force is transferred into the girder concrete, compressing it. If the prestress force is eccentric to the centroid of the girder and it is sufficient to overcome the self-weight of the girder, the girder cambers upwards. In this condition, the girder bears on its ends and bending stresses develop.
𝑤𝑤
𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 𝑐𝑐 𝑔𝑔
144𝑔𝑔𝑖𝑖2
2
= 𝑤𝑤 𝐴𝐴 = (0.165𝑘𝑘𝑐𝑐𝑓𝑓)(923.531𝑠𝑠𝑠𝑠2) � 1𝑒𝑒𝑑𝑑 � = 1.058 𝑘𝑘𝑘𝑘𝑓𝑓
where:
Ag | = | Gross cross-sectional area of the girder
c | = | Unit weight of concrete
𝑤𝑤𝑤𝑤
𝑀𝑀𝑔𝑔 = 2 (𝑘𝑘 − 𝑤𝑤)
Moment at point of prestress transfer
Prestress transfer occurs over 60 strand diameters (LRFD 5.9.4.3.1)
𝑘𝑘𝑑𝑑 = 60𝑑𝑑𝑠𝑠 = (60)(0.6𝑠𝑠𝑠𝑠) = 36𝑠𝑠𝑠𝑠 = 3𝑓𝑓𝑓𝑓 (1.058𝑘𝑘𝑘𝑘𝑓𝑓)(3𝑓𝑓𝑓𝑓)
2
𝑀𝑀𝑔𝑔 = (162.995𝑓𝑓𝑓𝑓 − 3𝑓𝑓𝑓𝑓) = 253.912 𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓

## Slide 107
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Moment at harp point (HP)
Harp point is 0.4L from the end of the girder (0.4)(162.995𝑓𝑓𝑓𝑓) = 65.198𝑓𝑓𝑓𝑓
(1.058𝑘𝑘𝑘𝑘𝑓𝑓)(65.198𝑓𝑓𝑓𝑓)
2
𝑀𝑀𝑔𝑔 = (162.995𝑓𝑓𝑓𝑓 − 65.198𝑓𝑓𝑓𝑓) = 3372.99𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
Moment at mid-span (0.5L)
𝑔𝑔
𝑀𝑀 =
2
162.995𝑓𝑓𝑓𝑓
(1.058𝑘𝑘𝑘𝑘𝑓𝑓) � �
162.995𝑓𝑓𝑓𝑓
2 2
�162.995𝑓𝑓𝑓𝑓 − � = 3513.534𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
    Erected Girder
Substructure elements support the girder at permanent bearing locations once erected. Bracing stabilizes the girder. Temporary top strands are detensioned, followed by diaphragm and roadway slab casting. Installation of the railing system occurs after the roadway slab gains adequate strength.
      Diaphragm and Deck Placement
In this stage, the girder supports its self-weight along with the weight of the diaphragms and slab.
        Diaphragm Loads
The diaphragm load for an interior girder is 𝑃𝑃 = 𝐻𝐻𝐻𝐻𝑤𝑤𝑐𝑐 (𝑆𝑆 − 𝑓𝑓𝑤𝑤𝑒𝑒𝑠𝑠 ), where:
H = Height of interior diaphragm
W = Width of interior diaphragm
tweb = Width of girder web
S = Spacing of girders
𝑃𝑃 = 𝐻𝐻𝐻𝐻𝑤𝑤𝑐𝑐 (𝑆𝑆 − 𝑓𝑓𝑤𝑤𝑒𝑒𝑠𝑠 ) = (62.875𝑠𝑠𝑠𝑠)(8𝑠𝑠𝑠𝑠)(0.155𝑘𝑘𝑐𝑐𝑓𝑓)
2
(83.99𝑠𝑠𝑠𝑠 − 6.125𝑠𝑠𝑠𝑠) 1𝑓𝑓𝑓𝑓3
� � = 1.76 𝑘𝑘𝑠𝑠𝑘𝑘
1728𝑠𝑠𝑠𝑠3
Diaphragms are located at 39.894𝑓𝑓𝑓𝑓 (0.25𝐿𝐿), 79.789𝑓𝑓𝑓𝑓 (0.5𝐿𝐿) and 119.683 𝑓𝑓𝑓𝑓 (0.75𝐿𝐿) from the left bearing. Slab Loads The slab load consists of the main slab and the slab haunch.
3.4.2.1.1.1 Main Slab Load
The slab overhang varies along the length of the girder. Also, the thickness of the slab varies from 7” at the edge of deck to 7.5” at the edge of the girder top flange. The basic loading of the main slab is 𝑤𝑤𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 = 𝑤𝑤𝑐𝑐 𝐻𝐻𝑑𝑑𝑔𝑔𝑔𝑔𝑠𝑠 𝑓𝑓𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 for interior beams and
𝑤𝑤𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 = 𝑤𝑤𝑐𝑐 �𝑓𝑓𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠
2
� � + �𝐻𝐻
𝑔𝑔𝑜𝑜𝑒𝑒𝑔𝑔ℎ𝑠𝑠𝑖𝑖𝑔𝑔
𝑡𝑡𝑡𝑡 𝑡𝑡𝑡𝑡
2
− �
𝑆𝑆+𝑊𝑊 𝑊𝑊 �𝑑𝑑
+𝐴𝐴�
𝑒𝑒𝑒𝑒𝑒𝑒𝑒𝑒
2
� for exterior beams.

## Slide 108
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Wtf
tedge
tslab
Woverhang
S/2
“A”
Slab haunch
Figure 3-5 Main slab section for slab loading
Woverhang varies along the length of the span.
Assume a slab offset (“A” dimension) of 12.5in. This assumption will be verified in Section 6.5. The main slab weight computed by PGSuper is:
Location (ft) | 𝐖𝐖𝐭𝐭𝐨𝐨𝐠𝐠𝐠𝐠𝐨𝐨𝐬𝐬𝐨𝐨𝐠𝐠(𝐠𝐠𝐨𝐨) | Main Slab weight (klf)
0.000 | 42.440 | 0.725
15.958 | 44.732 | 0.747
31.916 | 46.518 | 0.764
47.873 | 47.795 | 0.775
63.831 | 48.564 | 0.782
79.789 | 48.826 | 0.785
95.747 | 48.580 | 0.782
111.704 | 47.826 | 0.776
127.662 | 46.564 | 0.764
143.620 | 44.794 | 0.748
159.578 | 42.516 | 0.726
3.4.2.1.1.2 Slab Haunch Load
The slab haunch load accounts for the buildup of concrete between the top of the girder and the bottom of the main slab. This concrete element has a width equal to the top flange width (Wtf) and varies in depth along the length of the girder because of camber and variations in the roadway surface.

## Slide 109
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Figure 3-6: Slab Haunch
WSDOT’s design policy is to assume the top of the girder is flat (no camber) for purposes of determining the slab haunch load (BDM 5.6.2.D.3.iv).
PGSuper provides the option to consider excess camber when determining loading. This option may be desirable for load rating as it reduces the haunch dead load.
The basic haunch dead load at any given section is
𝑤𝑤ℎ𝑠𝑠𝑎𝑎𝑖𝑖𝑐𝑐ℎ = 𝐻𝐻𝑑𝑑𝑒𝑒 𝑓𝑓ℎ𝑠𝑠𝑎𝑎𝑖𝑖𝑐𝑐ℎ 𝑤𝑤𝑐𝑐
Assuming a slab offset (“A” dimension) of 12.5in, the slab haunch load at the start of the span is
𝑓𝑓ℎ𝑠𝑠𝑎𝑎𝑖𝑖𝑐𝑐ℎ = A − 𝑓𝑓𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 = 12.5𝑠𝑠𝑠𝑠 − 7.5𝑠𝑠𝑠𝑠 = 5.0𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓2
𝑤𝑤ℎ𝑠𝑠𝑎𝑎𝑖𝑖𝑐𝑐ℎ = (49𝑠𝑠𝑠𝑠)(5𝑠𝑠𝑠𝑠)(0.155𝑘𝑘𝑐𝑐𝑓𝑓) �144𝑠𝑠𝑠𝑠2� = 0.264 𝑘𝑘𝑘𝑘𝑓𝑓
The vertical curve causes the haunch depth to vary along the length of the girder. The table below lists the haunch loading for half the span. This load is modeled as linear load segments.
Location | 𝐭𝐭𝐨𝐨𝐬𝐬𝐡𝐡𝐨𝐨𝐡𝐡𝐨𝐨(𝐠𝐠𝐨𝐨) | 𝐰𝐰𝐨𝐨𝐬𝐬𝐡𝐡𝐨𝐨𝐡𝐡𝐨𝐨(𝐤𝐤𝐬𝐬𝐞𝐞)
0.0L | 5.0 | 0.264
0.1L | 4.795 | 0.253
0.2L | 4.635 | 0.244

## Slide 110
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
0.3L | 4.524 | 0.238
0.4L | 4.453 | 0.235
0.5L | 4.430 | 0.234
      Superimposed Dead Loads
Application of superimposed dead loads occurs after the deck has reached adequate strength. The superimposed dead loads consist of the traffic barrier and the overlay if present. The composite section is resisting these loads.
        Traffic Barrier
The traffic barrier weight is distributed over n exterior girders, if there are 2n or more girders, otherwise the weight of the
𝑑𝑑𝑠𝑠
𝑁𝑁
traffic barrier per girders is 𝑤𝑤 = 𝑊𝑊𝑡𝑡𝑡𝑡 𝑙𝑙𝑒𝑒𝑡𝑡𝑡 𝑡 +𝑊𝑊𝑡𝑡𝑡𝑡 𝑟𝑟𝑟𝑟𝑒𝑒ℎ𝑡𝑡, where N is the number of girders in the span. From BDM 5.6.3.2.B.2.d,
𝑠𝑠 = 3.
2𝑠𝑠 = 6, 𝑁𝑁 = 6, 2𝑠𝑠 = 𝑁𝑁
𝑤𝑤𝑑𝑑𝑠𝑠 =
𝐻𝐻𝑑𝑑𝑠𝑠
0.690𝑘𝑘𝑘𝑘𝑓𝑓 𝑘𝑘𝑘𝑘𝑓𝑓
= = 0.230
𝑠𝑠 3 𝑔𝑔𝑠𝑠𝐴𝐴𝑑𝑑𝐴𝐴𝐴𝐴𝑠𝑠 𝑔𝑔𝑠𝑠𝐴𝐴𝑑𝑑𝐴𝐴𝐴𝐴
AASHTO permits equal distribution for barrier loads to all girders.
      Open to Traffic
        Future Overlay
Evenly distribute the weight of the future wearing surface to all girders. The curb-to-curb width of the deck is 39.833ft.
𝑤𝑤𝑔𝑔 =
(39.833𝑓𝑓𝑓𝑓)(0.035𝑘𝑘𝑠𝑠𝑓𝑓)
6 𝑔𝑔𝑠𝑠𝐴𝐴𝑑𝑑𝐴𝐴𝐴𝐴
𝑘𝑘𝑘𝑘𝑓𝑓
= 0.232
𝑔𝑔𝑠𝑠𝐴𝐴𝑑𝑑𝐴𝐴𝐴𝐴
Take care when applying the future overlay loading. Certain stress conditions are worse before the overlay is applied and others are worse after it is applied.
3.4.2.3.2 Live Load
The design live load is the HL93 notional model defined in the AASHTO LRFD BDS.
The vehicular live loading is the combination of the:
design truck or design tandem (LRFD 3.6.1.1)
design lane load (LRFD 3.6.1.2.1)
The design truck consists of three axles. Axle weights and spacing are, 8.0 kip, 14.0 ft, 32.0 kip, 14.0 to 30.0 ft, 32.0 kip. See Figure 3-6 below.
The design tandem consists of a pair of 25.0 kip axles spaced 4.0 ft apart.
The design lane load is 0.640 klf, uniformly distributed along the length of the span.

## Slide 111
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
8 KIP
32 KIP
14'
32 KIP
14' - 30'
4'
25 KIP
25 KIP
0.640 KLF
Design Truck + Lane Load
0.640 KLF
Design Tandem + Lane Load
Figure 3-7: HL93 Live Load Model
Apply a dynamic load allowance (impact) of 33% to the design truck and design tandem portions of the live load response.
The fatigue live load is the design truck with the rear axle spacing fixed at 30 ft. The dynamic load allowance for fatigue is 15%.
    Analysis Results Summary
The following load responses are computed by PGSuper.
      At Release
Loading | Transfer Point | Harp Point | Mid-Span
Girder | 253.96 k ∙ ft | 3373.66 k ∙ ft | 3514.22 k ∙ ft
3.4.3.2 At Bridge Site
Loading | 0.5Ls
Girder after erection | 3368.43 k ∙ ft
Diaphragm | 140.14 k ∙ ft
Slab | 2465.61 k ∙ ft
Haunch | 760.28 k ∙ ft
Traffic Barrier | 732.12 k ∙ ft
Future Overlay | 739.63 k ∙ ft
*Design LLIM (HL-93) | 5485.09 k ∙ ft
*Fatigue LLIM | 2686.86 k ∙ ft
*Live load moments are per lane

## Slide 112
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
    Limit State Responses
Group the structural responses into load cases and compute limit state responses. The total factored load, or limit state response, is 𝑄𝑄 = ∑ 𝜂𝜂𝑔𝑔 𝛾𝛾𝑔𝑔𝑞𝑞𝑔𝑔 . (LRFD Eqn. 3.4.1-1)
LRFD Table 3.4.1-1 gives the load factors. The limit states of importance are:
      Service I, Q = 1.0DC + 1.0DW + 1.0(LL+IM)
      Service III, Q = 1.0DC + 1.0DW + 0.8(LL+IM)
      Strength I, Q = 1.25DC + 1.50DW + 1.75(LL+IM)
      Fatigue I, Q = 0.5DC + 0.5DW + 1.5(LL+IM)
WSDOT specifies the live load factor for Service III is 0.8 for design and 1.0 for load rating. See BDM 3.5.2
    Live Load Distribution Factors
Compute the live load distribution factors. Select the appropriate cross section type from LRFD Table 4.6.2.2.1-1. A precast I-beam with cast-in-place concrete deck corresponds to cross section k.
WSDOT deviates from the AASHTO LRFD BDS for exterior girders in type k sections as described in BDM 3.9.3.A.
Compute the longitudinal stiffness parameter Kg.
𝑔𝑔
𝐾𝐾𝑔𝑔 = 𝑠𝑠�𝐼𝐼 + 𝐴𝐴𝐴𝐴2�
where:
n | = | modular ratio between beam and deck material 𝑠𝑠 = 𝐸𝐸𝑡𝑡𝑒𝑒𝑏𝑏𝑏𝑏 𝐸𝐸𝑠𝑠𝑙𝑙𝑏𝑏𝑡𝑡
I | = | moment of inertia of the beam (in4)
A | = | area of beam (in2)
eg | = | distance between the centers of gravity of the basic beam and deck (in)
𝑠𝑠 =
5886.9891𝑠𝑠𝑠𝑠
4266.223𝑘𝑘𝑠𝑠𝑠𝑠
= 1.380
Yt
eg
ts/2
Figure 3-8: eg Detail
𝑓𝑓𝑠𝑠
𝐴𝐴𝑔𝑔 = 𝑌𝑌𝑑𝑑 + 2 = 38.343𝑠𝑠𝑠𝑠 +
7.0𝑠𝑠𝑠𝑠
2
= 41.843𝑠𝑠𝑠𝑠

## Slide 113
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝐾𝐾𝑔𝑔 = 1.380[734356.0𝑠𝑠𝑠𝑠2 + (923.531𝑠𝑠𝑠𝑠2)(41.843𝑠𝑠𝑠𝑠)2] = 3244494.4𝑠𝑠𝑠𝑠4
3.4.5.1 Number of Design Lanes
The number of design lanes is equal to the integer portion of the roadway width divided by 12 ft (LRFD 3.6.1.1.1).
39.833𝑓𝑓𝑓𝑓
12𝑓𝑓𝑓𝑓
𝑁𝑁𝐿𝐿 = � � = 3 𝐷𝐷𝐴𝐴𝑠𝑠𝑠𝑠𝑔𝑔𝑠𝑠 𝐿𝐿𝐴𝐴𝑠𝑠𝐴𝐴𝑠𝑠
      Distribution of Live Loads per Lane for Moments in Exterior Beams
LRFD Table 4.6.2.2.2d-1 gives the live load distribution factors for moments in exterior beams. For two or more loaded lanes the exterior beam distribution factor is a function of the interior beam distribution factor. The interior beam distribution factor is given in LRFD Table 4.6.2.2.2b-1.
        Compute Distribution Factor for Moment
Check the range of applicability for live load distribution factors.
Range Variable | Value | Status
3.5 ft  S  16 ft | S = 7.0 ft | OK
4.5 in  ts  12 in | ts = 7.0 in | OK
20 ft  L  240 ft | L =162.995 ft | OK
Nb  4 | Nb = 6 | OK
10,000in4 g  7,000,000 in4 | Kg =2288376 in4 | OK
−1.0 ≤ de ≤ 5.5 | de = 2.855ft | OK
3.4.5.2.1.1 One Design Lane Loaded
The live load distribution factor for one loaded lane is computed by the lever rule.
1
𝑒𝑒
𝑔𝑔𝑀𝑀 = (𝑚𝑚𝑘𝑘𝑓𝑓)
2
𝑃𝑃 ∑ 𝑑𝑑
𝑔𝑔
(𝑆𝑆)(𝑃𝑃)
Where mpf is the multiple presence factor, P is the axle load, di is the distance from the first interior girder (Girder B) to the wheel load, and S is the girder spacing.
Per the WSDOT BDM 3.9.3A, when the slab cantilever length exceeds 40% of the adjacent interior girder spacing a multiple presence factor of 1.0 is used in conjunction with the lever rule for computing the live load distribution for a single loaded lane.
AASHTO LRFD BDS 3.6.1.1.2 specifies a multiple presence factor of 1.2 for one loaded lane.
1
𝑒𝑒
𝑔𝑔𝑀𝑀 = 1.0
𝑃𝑃 (7.854𝑓𝑓𝑓𝑓 + 1.854𝑓𝑓𝑓𝑓)
2
(7.0𝑓𝑓𝑓𝑓)(𝑃𝑃)
= 0.694
3.4.5.2.1.2 Two or More Design Lanes Loaded
The live load distribution factor for two or more design lanes loaded is
𝑔𝑔𝑀𝑀𝑒𝑒 = 𝐴𝐴 𝑔𝑔𝑀𝑀𝑔𝑔
2+ 2+

## Slide 114
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝐴𝐴 = 0.77 +
𝑑𝑑𝑒𝑒
9.1
2+
0.6 𝑆𝑆 0.2
𝑔𝑔𝑀𝑀𝑔𝑔 = 0.075 + � � � � �
𝑆𝑆 𝐾𝐾𝑔𝑔
𝑠𝑠
9.5 𝐿𝐿 12.0𝐿𝐿𝑓𝑓3
0.1
�
2+
𝑔𝑔𝑀𝑀𝑔𝑔 = 0.075 + � � �
0.6 0.2
� �
7 7 3244494.4
0.1
� = 0.598
9.5 162.995 12.0 ∙ 162.995 ∙ 73
2.855
9.1
𝐴𝐴 = 0.77 + = 1.084
𝑔𝑔𝑀𝑀𝑒𝑒 = 1.084(0.598) = 0.648
2+
The girders are skewed with respect to end of the bridge. The skew correction factor is given in LRFD Table 4.6.2.2.2e-1.
𝑓𝑓 = 1 − 𝑐𝑐1(𝑓𝑓𝐴𝐴𝑠𝑠 𝜃𝜃) 1.5
𝑐𝑐1 = 0.0 𝑓𝑓𝑐𝑐𝐴𝐴 𝜃𝜃 < 30°
The skew correction factor is 1.0.
      Distribution of Live Loads per Lane for Shear in Exterior Beams
LRFD Table 4.6.2.2.3b-1 gives the live load distribution factors for shear in exterior beams. For two or more loaded lanes the exterior beam distribution factor is a function of the interior beam distribution factor. The interior beam distribution factor is given in LRFD Table 4.6.2.2.3a-1.
        Compute Distribution Factor for Shear
Check the range of applicability for live load distribution factors.
Range Variable | Value | Status
3.5 ft  S  16 ft | S = 7.0 ft | OK
4.5 in  ts  12 in | ts = 7.0 in | OK
20 ft  L  240 ft | L =162.995 ft | OK
Nb  4 | Nb = 6 | OK
−1.0 ≤ de ≤ 5.5 | de = 2.855ft | OK
3.4.5.3.1.1 One Design Lane Loaded
The live load distribution factor for one loaded lane is computed by the lever rule.
𝑔𝑔
𝑔𝑔𝑉𝑉𝑒𝑒 = 0.694
3.4.5.3.1.2 Two or More Design Lanes Loaded
The live load distribution factor for two or more loaded lanes is
𝑔𝑔𝑉𝑉𝑒𝑒 = 𝐴𝐴 𝑔𝑔𝑉𝑉𝑔𝑔
2+ 2+
𝐴𝐴 = 0.6 +
𝑑𝑑𝑒𝑒
10
2+
𝑆𝑆 𝑆𝑆
𝑔𝑔𝑉𝑉𝑔𝑔 = 0.2 + − � �
2.0
2+
7 7
12 35
𝑔𝑔𝑉𝑉𝑔𝑔 = 0.2 + − � �
12 35
2.0
= 0.743

## Slide 115
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝐴𝐴 = 0.6 +
2.855
10
= 0.889
The exterior beam cannot be designed for less load than the interior beam so 𝐴𝐴 = 1.0
𝑔𝑔𝑉𝑉𝑒𝑒 = 1.0(0.743) = 0.743
2+
The skew correction factor is given in LRFD Table 4.6.2.2.3c-1.
𝑓𝑓 = 1.0 + 0.2 �
𝐾𝐾𝑔𝑔
𝑠𝑠 �
12.0𝐿𝐿𝑓𝑓3 0.3
𝑓𝑓𝐴𝐴𝑠𝑠 𝜃𝜃
2
The average skew angle is 𝜃𝜃 = 0+1.57 = 0.79°
𝑓𝑓 = 1.0 + 0.2 �
3244494.4
12.0 ∙ 162.995 ∙ 73 0.3
� 𝑓𝑓𝐴𝐴𝑠𝑠(0.79) = 1.002
2+
𝑔𝑔𝑉𝑉𝑒𝑒 = 1.002(0.743) = 0.744
LRFD 4.6.2.2.3c - The skew correction factor is linearly interpolated between 1.0 at mid-span to its full value at the obtuse corner. Since the skew correction factor is 1.002, that level of detail will not be shown in these calculations. However, PGSuper does interpolate the skew correction factor as required by AASHTO LRFD.
3.4.5.4 Live Load Distribution Factor Summary
Distribution Factor Summary for Strength and Service Limit States
Distribution Factor | 1 Loaded Lane | 2+ Loaded Lanes | Controlling Factor
Moment (𝐠𝐠𝐠𝐠) | 0.694 | 0.648 | 0.694
Shear (𝐠𝐠𝐠𝐠) | 0.694 | 0.744 | 0.744
3.4.5.5 Live Load Distribution Factor for Fatigue Limit State
The fatigue live load distribution uses the factor for one loaded lane (LRFD 3.6.1.4.3b). The single lane distribution factors include a multiple presence factor of 1.2 when computed by the equations in LRFD Section 4. The multiple presence factor for fatigue loading is 1.0 (LRFD 3.6.1.1.2). Typically, the one loaded lane distribution factors are divided by 1.2 to get the fatigue distribution factors. However, in this case, the one loaded lane distribution factors are computed by the lever rule with a multiple presence factor of 1.0 per WSDOT policy so dividing by 1.2 is not needed.
Distribution Factor Summary for Fatigue Limit States
Distribution Factor | 1 Loaded Lane
Moment (𝐠𝐠𝐠𝐠) | 0.694
Shear (𝐠𝐠𝐠𝐠) | 0.694
4 Flexure Design
WSDOT and local girder fabricators developed the design methodology used by PGSuper. The concept is to design for optimized fabrication of precast, prestressed concrete bridge girders. The primary goal is to determine the least required concrete strength at release and initial lifting while simultaneously placing the least possible demand on the stressing system and achieving adequate stability of the girder during handling operations. A detailed description and numerical example of optimized fabrication design is available in the PCI Journal2. Figure 4-1 gives a high-level summary of the design procedure.

## Slide 116
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Girder stresses and stability at initial lifting and hauling are integral elements of the design process. Lifting and hauling conditions often govern the design.
Designing precast, prestressed concrete bridge girders for lateral stability ensures safety and constructability. AASHTO LRFD 5.5.4.3 requires buckling and stability of precast members during handling, transportation, and erection to be investigated. PCI’s Aspire Magazine3 presents WSDOT’s perspective on stability design.

## Slide 117
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Step 1 - Design for final service conditions
Determine precompression force
Step 2 - Design for lifting without temporary top strands
Determine optimum permanent strand arrangement
Determine lifting embedment locations for stability
This step determines highest concrete strength at lifting
Step 3 - Design for shipping
Estimate temporary top strand requirements
Estimate truck support locations
Estimate concrete strength required at shipping
Step 4 - Design for lifting with temporary top s
Determines lowest concrete strength at lift
Place lifting embedments as close to ends a maintaining adequate lateral stability
Temporary top strand required?
trands
ing
s possible while
orary top strands are
Step 6 – Check Erection Stresses
Check stresses in erected girder after temp removed but before additional dead load is placed
Check stresses in erected girder after additional dead load is placed
Step 7 – Check Final Conditions
Check stresses in final service conditions
Check strength conditions
Yes
No
Step 5 - Revise shipping design
Confirm temporary top strand requirements
Confirm truck support locations
Confirm concrete strength required at shipping
Figure 4-1: Optimized Fabrication Girder Design Procedure

## Slide 118
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
4.1 Step 1 Design for Final Service Conditions
Design for the Service III limit state for tensile stresses at the bottom of the girder at mid-span.
𝑓𝑓 =
4.1.1 Stresses due to loads on non-composite section
𝑀𝑀
𝑆𝑆
𝑆𝑆𝑑𝑑 = −19152.5𝑠𝑠𝑠𝑠3
𝑆𝑆𝑠𝑠 = 20594.8𝑠𝑠𝑠𝑠3
Load | Moment (k-ft) | 𝐞𝐞𝐭𝐭(𝐤𝐤𝐬𝐬𝐠𝐠) | 𝐞𝐞𝐬𝐬(𝐤𝐤𝐬𝐬𝐠𝐠)
Girder | 3368.43 | -2.110 | 1.963
Diaphragms | 140.17 | -0.088 | 0.082
Slab | 2465.61 | -1.545 | 1.437
Haunch | 760.28 | -0.476 | 0.443
    Stresses due to loads on the composite section
      Stress due to dead loads
𝑓𝑓 =
𝑀𝑀
𝑆𝑆
𝑆𝑆𝑑𝑑𝑔𝑔𝑐𝑐 = −49599.7𝑠𝑠𝑠𝑠3
𝑆𝑆𝑠𝑠𝑐𝑐 = 25509.6𝑠𝑠𝑠𝑠3
Load | Moment (k-ft) | 𝒇𝒇𝒕𝒕(𝒌𝒌𝒌𝒌𝒌𝒌) | 𝒇𝒇𝒃𝒃(𝒌𝒌𝒌𝒌𝒌𝒌)
Barrier | 732.12 | -0.177 | 0.344
Future Overlay | 739.63 | -0.179 | 0.348
4.1.2.2 Live Load Stresses
The live load moments computed above are for a full lane of load. These values must be scaled with the live load distribution factor to get a per girder moment
𝑓𝑓 = 𝑔𝑔
𝑀𝑀𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿
𝑆𝑆
𝑆𝑆𝑑𝑑𝑔𝑔𝑐𝑐 = −49599.7𝑠𝑠𝑠𝑠3
𝑆𝑆𝑠𝑠𝑐𝑐 = 25509.3𝑠𝑠𝑠𝑠3
Load | Moment (k-ft per lane) | g | Moment (k- ft per girder) | 𝒇𝒇𝒕𝒕(𝒌𝒌𝒌𝒌𝒌𝒌) Min | 𝒇𝒇𝒕𝒕(𝒌𝒌𝒌𝒌𝒌𝒌) Max | 𝒇𝒇𝒃𝒃(𝒌𝒌𝒌𝒌𝒌𝒌) Min | 𝒇𝒇𝒃𝒃(𝒌𝒌𝒌𝒌𝒌𝒌) Max
Design (HL93) | 5485.09 | 0.694 | 3804.05 | -0.920 | 0 | 0 | 1.789
Fatigue | 2686.86 | 0.694 | 1863.40 | -0.451 | 0 | 0 | 0.877

## Slide 119
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
4.1.2.3 Stress due to slab shrinkage
Girder stresses must include those due to slab shrinkage when gains due to slab shrinkage are included in the effective prestress force. The equivalent force is illustrated in Figure 4-2.
Pds
ed
Composite CG
Figure 4-2: Equivalent deck shrinkage force
∆𝑃𝑃𝑔𝑔𝑠𝑠 =
−𝜀𝜀𝑔𝑔𝑔𝑔𝑒𝑒𝐴𝐴𝑔𝑔 𝐸𝐸𝑐𝑐 𝑔𝑔𝑒𝑒𝑐𝑐𝑑𝑑
�1 + 0.7𝜓𝜓𝑔𝑔 �𝑓𝑓𝑒𝑒 , 𝑓𝑓𝑔𝑔 ��
𝑠𝑠𝑠𝑠 𝑔𝑔𝑠𝑠
1 𝐴𝐴𝑔𝑔
𝐴𝐴 𝑆𝑆
𝑐𝑐 𝑐𝑐
𝑓𝑓 = ∆𝑃𝑃 � − �
𝜀𝜀𝑔𝑔𝑔𝑔𝑒𝑒 = 𝐾𝐾𝑠𝑠ℎ 𝑘𝑘𝑠𝑠𝑘𝑘ℎ𝑠𝑠 𝑘𝑘𝑒𝑒 𝑘𝑘𝑑𝑑𝑔𝑔0.48 × 10−3
𝑉𝑉
𝑘𝑘𝑠𝑠 = 1.45 − 0.13 �𝑆𝑆� ≥ 1.0
PGSuper computes the volume of the deck slab by integrating the full bridge width cross-sectional area over the length of the slab, measured along the alignment curve. This is the most general solution and accounts for deck slabs that vary in width.
The surface area is twice the plan area (top and bottom of slab) less the common area with the girder top flanges plus the area
of exposed slab edges. PGSuper computes the volume to surface area ratio to be:
𝑉𝑉
𝑆𝑆
= 4.154𝑠𝑠𝑠𝑠
Use the gross slab depth when computing slab shrinkage effects. Shrinkage is an early age effect; therefore, the sacrificial depth is part of the deck slab that is shrinking.
𝑘𝑘𝑠𝑠 = 1.45 − 0.13(4.154) = 0.910 < 1.0 ∴ 1.0
𝑘𝑘ℎ𝑠𝑠 = 2.00 − 0.014𝐻𝐻 = 2.00 − 0.014(75) = 0.95
Slab concrete age at time of initial loading is 𝑓𝑓′ = 0.8𝑓𝑓′. (LRFD 5.4.2.3.1)
𝑐𝑐𝑔𝑔 𝑐𝑐
𝑓𝑓′ = 0.8𝑓𝑓′ = 0.8(4𝑘𝑘𝑠𝑠𝑠𝑠) = 3.2 𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐𝑔𝑔 𝑐𝑐
5 5
𝑘𝑘𝑒𝑒 = 1 + 𝑓𝑓′ = 1 + 3.2 = 1.19
𝑐𝑐𝑔𝑔
𝑓𝑓 = 𝑓𝑓𝑒𝑒 − 𝑓𝑓𝑔𝑔 = 2000 − 120 = 1880 𝑑𝑑𝐴𝐴𝑑𝑑𝑠𝑠
𝑘𝑘𝑑𝑑𝑔𝑔 =
12 �
100 − 4𝑓𝑓′
′
𝑓𝑓𝑐𝑐𝑔𝑔 + 20
=
𝑓𝑓 1880
𝑐𝑐𝑔𝑔 � + 𝑓𝑓 12 �
100 − 4(3.2)
3.2 + 20
� + 1880
= 0.977

## Slide 120
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝐾𝐾𝑠𝑠ℎ = 0.5 (BDM 5.1.4.3.D – use 50% slab shrinkage strain)
𝜀𝜀𝑔𝑔𝑔𝑔𝑒𝑒 = (0.5)(1.0)(0.95)(1.19)(0.978)(0.48 × 10−3) = 0.265 × 10−3
𝑔𝑔
𝜓𝜓𝑔𝑔 �𝑓𝑓𝑒𝑒 , 𝑓𝑓𝑔𝑔� = 1.9𝑘𝑘𝑠𝑠𝑘𝑘ℎ𝑐𝑐 𝑘𝑘𝑒𝑒 𝑘𝑘𝑑𝑑𝑔𝑔𝑓𝑓−0.118
𝑘𝑘ℎ𝑐𝑐 = 1.56 − 0.008𝐻𝐻 = 1.56 − 0.008(75) = 0.96
𝑓𝑓𝑔𝑔 = 1 𝑑𝑑𝐴𝐴𝑑𝑑𝑠𝑠
𝜓𝜓𝑔𝑔 �𝑓𝑓𝑒𝑒 , 𝑓𝑓𝑔𝑔� = 1.9(1.0)(0.96)(1.19)(0.978)(1)−0.118 = 2.12
The deck overhang varies along the length of the girder. At the mid-span section, the area of the deck that contributes to shrinkage is
𝐴𝐴𝑔𝑔 = 681.165𝑠𝑠𝑠𝑠2
The deck shrinkage force is
(−0.265 × 10−3)(681.165𝑠𝑠𝑠𝑠2)(4266.223𝑘𝑘𝑠𝑠𝑠𝑠)
[1 + 0.7(2.12)]
𝛥𝛥𝑃𝑃𝑔𝑔𝑠𝑠 = = −310.0 𝑘𝑘𝑠𝑠𝑘𝑘
The composite girder area is
𝐴𝐴𝑐𝑐 = 1349.614𝑠𝑠𝑠𝑠2
Recall that the effective overhang for section properties is limited to S/2.
The eccentricity of the center of the deck with respect to the composite section is
𝐴𝐴𝑔𝑔 = − �𝑌𝑌𝑑𝑑𝑐𝑐 +
𝑓𝑓𝑔𝑔𝑔𝑔𝑔𝑔𝑠𝑠𝑠𝑠 𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 𝑔𝑔𝑒𝑒𝑑𝑑𝑑𝑑ℎ
2
7.5𝑠𝑠𝑠𝑠
2
� = − �25.133 𝑠𝑠𝑠𝑠 + � = −28.883𝑠𝑠𝑠𝑠
𝑆𝑆𝑑𝑑𝑔𝑔𝑐𝑐 = −49599.7𝑠𝑠𝑠𝑠3
𝑆𝑆𝑠𝑠𝑐𝑐 = 25509.3𝑠𝑠𝑠𝑠3
𝑓𝑓𝑑𝑑𝑔𝑔𝑑𝑑 = (−310.0𝑘𝑘𝑠𝑠𝑘𝑘) �
2 +
1 −28.883𝑠𝑠𝑠𝑠
1349.614𝑠𝑠𝑠𝑠 −49599.7𝑠𝑠𝑠𝑠
3� = −0.410 𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠𝑔𝑔𝑑𝑑 = (−310.0𝑘𝑘𝑠𝑠𝑘𝑘) �
1 −28.883𝑠𝑠𝑠𝑠
1349.614𝑠𝑠𝑠𝑠 25509.3𝑠𝑠𝑠𝑠
2 + 3� = 0.121 𝑘𝑘𝑠𝑠𝑠𝑠
4.1.2.4 Estimate Prestressing
Typically, the governing limit state for final service conditions is Service III
𝑆𝑆𝐴𝐴𝐴𝐴𝑆𝑆𝑠𝑠𝑐𝑐𝐴𝐴 𝐼𝐼𝐼𝐼𝐼𝐼 = 1.0𝐷𝐷𝐷𝐷 + 1.0𝐷𝐷𝐻𝐻 + 0.8(𝐿𝐿𝐿𝐿 + 𝐼𝐼𝑀𝑀)
𝑓𝑓𝑠𝑠 = 1.963𝑘𝑘𝑠𝑠𝑠𝑠(𝑔𝑔𝑠𝑠𝐴𝐴𝑑𝑑𝐴𝐴𝐴𝐴) + 0.082𝑘𝑘𝑠𝑠𝑠𝑠(𝑑𝑑𝑠𝑠𝐴𝐴𝑘𝑘ℎ𝐴𝐴𝐴𝐴𝑔𝑔𝑚𝑚) + 1.437𝑘𝑘𝑠𝑠𝑠𝑠(𝑠𝑠𝑘𝑘𝐴𝐴𝑠𝑠) + 0.443𝑘𝑘𝑠𝑠𝑠𝑠(ℎ𝐴𝐴𝑎𝑎𝑠𝑠𝑐𝑐ℎ) + 0.344𝑘𝑘𝑠𝑠𝑠𝑠(𝑠𝑠𝐴𝐴𝐴𝐴𝐴𝐴𝑠𝑠𝐴𝐴𝐴𝐴)
+ 0.348𝑘𝑘𝑠𝑠𝑠𝑠(𝑓𝑓𝑎𝑎𝑓𝑓𝑎𝑎𝐴𝐴𝐴𝐴 𝑐𝑐𝑆𝑆𝐴𝐴𝐴𝐴𝑘𝑘𝐴𝐴𝑑𝑑) + 0.121𝑘𝑘𝑠𝑠𝑠𝑠(𝑠𝑠𝑘𝑘𝐴𝐴𝑠𝑠 𝑠𝑠ℎ𝐴𝐴𝑠𝑠𝑠𝑠𝑘𝑘𝐴𝐴𝑔𝑔𝐴𝐴) + (0.8)(1.789𝑘𝑘𝑠𝑠𝑠𝑠)(𝐷𝐷𝐴𝐴𝑠𝑠𝑠𝑠𝑔𝑔𝑠𝑠 𝐿𝐿𝐿𝐿𝐼𝐼𝑀𝑀)
= 6.169𝑘𝑘𝑠𝑠𝑠𝑠
The stress due to prestressing is
𝑃𝑃 𝑃𝑃𝐴𝐴
𝑓𝑓𝑑𝑑𝑠𝑠 = 𝐴𝐴 + 𝑆𝑆
The tension limit is 0.0 ksi per BDM 5.2.1.C.
𝑓𝑓𝑠𝑠 + 𝑓𝑓𝑑𝑑𝑠𝑠 = 0.0 𝑘𝑘𝑠𝑠𝑠𝑠
For load rating, use the tension stress limit from the LRFD Bridge Design Specifications (BDM 13.2.4)

## Slide 121
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Assume the resultant prestress force is 3” above the bottom of the girder.
𝐴𝐴 = 𝑌𝑌𝑠𝑠 − 3𝑠𝑠𝑠𝑠 = 35.657𝑠𝑠𝑠𝑠 − 3𝑠𝑠𝑠𝑠 = 33.657𝑠𝑠𝑠𝑠
𝑃𝑃 𝑃𝑃(33.657𝑠𝑠𝑠𝑠)
6.169𝑘𝑘𝑠𝑠𝑠𝑠 + + = 0.0𝑘𝑘𝑠𝑠𝑠𝑠
923.531𝑠𝑠𝑠𝑠2 20594.8𝑠𝑠𝑠𝑠3
𝑃𝑃 = −2270.5𝑘𝑘𝑠𝑠𝑘𝑘
Assume a final effective prestress of 85% of the initial prestress (15% prestress loss)
𝑃𝑃 = 𝑁𝑁(0.217𝑠𝑠𝑠𝑠2)(0.85)�0.75𝑓𝑓𝑑𝑑𝑎𝑎�
2270.5𝑘𝑘𝑠𝑠𝑘𝑘 = 𝑁𝑁(0.217𝑠𝑠𝑠𝑠2)(0.85)(0.75)(270𝑘𝑘𝑠𝑠𝑠𝑠)
𝑁𝑁 = 60.8
Use 61 strands.
𝑃𝑃 = 61(0.217𝑠𝑠𝑠𝑠2)(0.85)(0.75)(270𝑘𝑘𝑠𝑠𝑠𝑠) = 2278.4 𝑘𝑘𝑠𝑠𝑘𝑘
    Check Estimate of Final Concrete Strength
      Service limit state - compression with live load
Compression at the top of girder, Service I limit state with live load is limited to 0.6f’c.
Service I limit state for compression stresses at the top of the girder at mid-span.
𝑆𝑆𝐴𝐴𝐴𝐴𝑆𝑆𝑠𝑠𝑐𝑐𝐴𝐴 𝐼𝐼 = 1.0𝐷𝐷𝐷𝐷 + 1.0𝐷𝐷𝐻𝐻 + 1.0(𝐿𝐿𝐿𝐿 + 𝐼𝐼𝑀𝑀)
𝑓𝑓𝑑𝑑 = −2.110𝑘𝑘𝑠𝑠𝑠𝑠(𝑔𝑔𝑠𝑠𝐴𝐴𝑑𝑑𝐴𝐴𝐴𝐴) − 0.088𝑘𝑘𝑠𝑠𝑠𝑠(𝑑𝑑𝑠𝑠𝐴𝐴𝑘𝑘ℎ𝐴𝐴𝐴𝐴𝑔𝑔𝑚𝑚) − 1.545𝑘𝑘𝑠𝑠𝑠𝑠(𝑠𝑠𝑘𝑘𝐴𝐴𝑠𝑠) − 0.476𝑘𝑘𝑠𝑠𝑠𝑠(ℎ𝐴𝐴𝑎𝑎𝑠𝑠𝑐𝑐ℎ) − 0.177𝑘𝑘𝑠𝑠𝑠𝑠(𝑠𝑠𝐴𝐴𝐴𝐴𝐴𝐴𝑠𝑠𝐴𝐴𝐴𝐴)
− 0.179𝑘𝑘𝑠𝑠𝑠𝑠(𝑓𝑓𝑎𝑎𝑓𝑓𝑎𝑎𝐴𝐴𝐴𝐴 𝑐𝑐𝑆𝑆𝐴𝐴𝐴𝐴𝑘𝑘𝐴𝐴𝑑𝑑) − 0.410𝑘𝑘𝑠𝑠𝑠𝑠(𝑠𝑠𝑘𝑘𝐴𝐴𝑠𝑠 𝑠𝑠ℎ𝐴𝐴𝑠𝑠𝑠𝑠𝑘𝑘𝐴𝐴𝑔𝑔𝐴𝐴) − 0.920𝑘𝑘𝑠𝑠𝑠𝑠(𝐷𝐷𝐴𝐴𝑠𝑠𝑠𝑠𝑔𝑔𝑠𝑠 𝐿𝐿𝐿𝐿𝐼𝐼𝑀𝑀) = −5.905 𝑘𝑘𝑠𝑠𝑠𝑠
The stress due to prestressing is
𝑃𝑃 𝑃𝑃𝐴𝐴
𝑓𝑓𝑑𝑑𝑠𝑠 = 𝐴𝐴 + 𝑆𝑆
−2278.4𝑘𝑘𝑠𝑠𝑘𝑘 (−2278.4𝑘𝑘𝑠𝑠𝑘𝑘)(33.657𝑠𝑠𝑠𝑠)
𝑓𝑓𝑑𝑑𝑠𝑠 = 923.531𝑠𝑠𝑠𝑠2 + −20594.8𝑠𝑠𝑠𝑠3
= 1.256𝑘𝑘𝑠𝑠𝑠𝑠
Compute the required concrete strength
𝑐𝑐
−0.6𝑓𝑓′ = 1.256𝑘𝑘𝑠𝑠𝑠𝑠 − 5.905𝑘𝑘𝑠𝑠𝑠𝑠 = −4.649𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐
𝑓𝑓′ = 7.748𝑘𝑘𝑠𝑠𝑠𝑠
4.1.3.2 Service limit state - compression without live load
Compression at the top of girder, Service I limit state without live load is limited to 0.45f’c.
Service I limit state for compression stresses at the top of the girder at mid-span.
𝑆𝑆𝐴𝐴𝐴𝐴𝑆𝑆𝑠𝑠𝑐𝑐𝐴𝐴 𝐼𝐼 = 1.0𝐷𝐷𝐷𝐷 + 1.0𝐷𝐷𝐻𝐻
𝑓𝑓𝑑𝑑 = −2.110𝑘𝑘𝑠𝑠𝑠𝑠(𝑔𝑔𝑠𝑠𝐴𝐴𝑑𝑑𝐴𝐴𝐴𝐴) − 0.088𝑘𝑘𝑠𝑠𝑠𝑠(𝑑𝑑𝑠𝑠𝐴𝐴𝑘𝑘ℎ𝐴𝐴𝐴𝐴𝑔𝑔𝑚𝑚) − 1.545𝑘𝑘𝑠𝑠𝑠𝑠(𝑠𝑠𝑘𝑘𝐴𝐴𝑠𝑠) − 0.476𝑘𝑘𝑠𝑠𝑠𝑠(ℎ𝐴𝐴𝑎𝑎𝑠𝑠𝑐𝑐ℎ) − 0.177𝑘𝑘𝑠𝑠𝑠𝑠(𝑠𝑠𝐴𝐴𝐴𝐴𝐴𝐴𝑠𝑠𝐴𝐴𝐴𝐴)
− 0.179𝑘𝑘𝑠𝑠𝑠𝑠(𝑓𝑓𝑎𝑎𝑓𝑓𝑎𝑎𝐴𝐴𝐴𝐴 𝑐𝑐𝑆𝑆𝐴𝐴𝐴𝐴𝑘𝑘𝐴𝐴𝑑𝑑) − 0.410𝑘𝑘𝑠𝑠𝑠𝑠(𝑠𝑠𝑘𝑘𝐴𝐴𝑠𝑠 𝑠𝑠ℎ𝐴𝐴𝑠𝑠𝑠𝑠𝑘𝑘𝐴𝐴𝑔𝑔𝐴𝐴) = −4.985 𝑘𝑘𝑠𝑠𝑠𝑠
The stress due to prestressing is
𝑓𝑓𝑑𝑑𝑠𝑠 = 1.256 𝑘𝑘𝑠𝑠𝑠𝑠
Compute the required concrete strength
𝑐𝑐
−0.45𝑓𝑓′ = 1.256𝑘𝑘𝑠𝑠𝑠𝑠 − 4.985𝑘𝑘𝑠𝑠𝑠𝑠 = −3.729𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐
𝑓𝑓′ = 8.29𝑘𝑘𝑠𝑠𝑠𝑠

## Slide 122
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
4.1.3.3 Fatigue limit state
Compression at the top of girder, Fatigue I limit state. Stress is limited to 0.4f’c.
Fatigue I limit state for compression stresses at the top of the girder at mid-span.
𝐹𝐹𝐴𝐴𝑓𝑓𝑠𝑠𝑔𝑔𝑎𝑎𝐴𝐴 𝐼𝐼 = 0.5𝐷𝐷𝐷𝐷+ 0.5𝐷𝐷𝐻𝐻 + 1.5(𝐿𝐿𝐿𝐿 + 𝐼𝐼𝑀𝑀)
𝑓𝑓𝑑𝑑 = 0.5�−2.110𝑘𝑘𝑠𝑠𝑠𝑠(𝑔𝑔𝑠𝑠𝐴𝐴𝑑𝑑𝐴𝐴𝐴𝐴) − 0.088𝑘𝑘𝑠𝑠𝑠𝑠(𝑑𝑑𝑠𝑠𝐴𝐴𝑘𝑘ℎ𝐴𝐴𝐴𝐴𝑔𝑔𝑚𝑚) − 1.545𝑘𝑘𝑠𝑠𝑠𝑠(𝑠𝑠𝑘𝑘𝐴𝐴𝑠𝑠) − 0.476𝑘𝑘𝑠𝑠𝑠𝑠(ℎ𝐴𝐴𝑎𝑎𝑠𝑠𝑐𝑐ℎ) − 0.177𝑘𝑘𝑠𝑠𝑠𝑠(𝑠𝑠𝐴𝐴𝐴𝐴𝐴𝐴𝑠𝑠𝐴𝐴𝐴𝐴)
− 0.179𝑘𝑘𝑠𝑠𝑠𝑠(𝑓𝑓𝑎𝑎𝑓𝑓𝐴𝐴𝐴𝐴 𝑐𝑐𝑆𝑆𝐴𝐴𝐴𝐴𝑘𝑘𝐴𝐴𝑑𝑑) − 0.410𝑘𝑘𝑠𝑠𝑠𝑠(𝑠𝑠𝑘𝑘𝐴𝐴𝑠𝑠 𝑠𝑠ℎ𝐴𝐴𝑠𝑠𝑠𝑠𝑘𝑘𝐴𝐴𝑔𝑔𝐴𝐴)� + 1.75(−0.451𝑘𝑘𝑠𝑠𝑠𝑠)(𝐹𝐹𝐴𝐴𝑓𝑓𝑠𝑠𝑔𝑔𝑎𝑎𝐴𝐴 𝐿𝐿𝐿𝐿𝐼𝐼𝑀𝑀)
= −3.282 𝑘𝑘𝑠𝑠𝑠𝑠
The stress due to prestressing is
= 1.327𝑘𝑘𝑠𝑠𝑠𝑠
−2367.44𝑘𝑘𝑠𝑠𝑘𝑘 (−2367.44𝑘𝑘𝑠𝑠𝑘𝑘)(33.657𝑠𝑠𝑠𝑠)
𝑓𝑓𝑑𝑑𝑠𝑠 = 923.531𝑠𝑠𝑠𝑠2 + −20594.8𝑠𝑠𝑠𝑠3
𝑓𝑓𝑑𝑑𝑠𝑠 = 1.327 𝑘𝑘𝑠𝑠𝑠𝑠
Compute the required concrete strength
𝑐𝑐
−0.4𝑓𝑓′ = 0.5(1.327)𝑘𝑘𝑠𝑠𝑠𝑠 − 3.282𝑘𝑘𝑠𝑠𝑠𝑠 = −2.618𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓′ = 6.55𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐
The required concrete strength does not exceed our assumed value of 8.7 ksi. OK
  Step 2 - Design for Lifting without Temporary Top Strands
Temporary top strands are generally not required for lifting of girders. This step identifies the lifting locations that provide adequate lateral stability and the corresponding concrete strength. The optimum strand arrangement is also determined.
    Proportion Strands
The optimum exit location for the permanent pretensioning results in the compressive stress at the transfer point or lift point being approximately equal to the compressive stress at the harp point. This provides the lowest exit eccentricity that does not increase the required concrete strength at lifting. Finding this location is an iterative process. Experience has shown that a good starting point is a ratio of straight-to-harped strands of approximately 2:1. Manipulation of the harped strands varies the exit eccentricity.
The harped strand exit location can be manipulated in one of two ways: 1) by lowering a fixed number of harped strands at the girder ends or, 2) by leaving the harped strands at their highest exit location and reducing the number of harped strands by dropping pairs of strands from the harped strand group into the straight strand group. Minimizing the number of harped strands held at their highest position at the ends of the girder provides space over the height of the web for longitudinal reinforcement that may protrude from the end of the girder for making a connection with diaphragm concrete.
The optimal arrangement of strands for this girder is 44 straight stands with an eccentricity of 31.748 𝑠𝑠𝑠𝑠 and 17 harped strands with end eccentricity of −26.813 𝑠𝑠𝑠𝑠 and harp point eccentricity of 30.775 𝑠𝑠𝑠𝑠. The permanent strand eccentricity at 0.5L is 31.447 𝑠𝑠𝑠𝑠.
ee=-26.813in
eh=30.775in
CG Girder
Nh = 17
Ns = 44
es=31.748in
Figure 4-2: Optimum Strand Arrangement

## Slide 123
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
    Prestress losses
      Initial relaxation before transfer
Prior to the 2005 interim revisions to the LRFD 3rd Edition, relaxation before prestress transfer was included in prestress loss calculations. Since the 2005 interim revisions, this is no longer required based on the idea that fabricators can overstress strands to achieve an effective prestress of 0.75𝑓𝑓𝑑𝑑𝑎𝑎 at release. However, WSDOT retains the practice of including relaxation prior to prestress transfer because it reflects the production practices used by local fabricators.
∆𝑓𝑓𝑑𝑑𝑅𝑅0 =
40.0
𝑘𝑘𝑐𝑐𝑔𝑔 (24.0𝑓𝑓) 𝑓𝑓𝑑𝑑𝑝𝑝
𝑑𝑑𝑝𝑝
� − 0.55� 𝑓𝑓𝑑𝑑𝑝𝑝
𝑓𝑓
∆𝑓𝑓𝑑𝑑𝑅𝑅0 =
40
𝑓𝑓𝑑𝑑𝑝𝑝 = 0.75𝑓𝑓𝑑𝑑𝑎𝑎 = 0.75(270) = 202.5𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑑𝑑𝑝𝑝 = 0.9𝑓𝑓𝑑𝑑𝑎𝑎 = 243𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓 = 1 𝑑𝑑𝐴𝐴𝑑𝑑
𝑘𝑘𝑐𝑐𝑔𝑔 (24.0 ∙ 1𝑑𝑑𝐴𝐴𝑑𝑑) 202.5𝑘𝑘𝑠𝑠𝑠𝑠
� − 0.55� (202.5𝑘𝑘𝑠𝑠𝑠𝑠) = 1.980 𝑘𝑘𝑠𝑠𝑠𝑠
243.0𝑘𝑘𝑠𝑠𝑠𝑠
This calculation is for intrinsic relaxation of the strand. Intrinsic relaxation is associated with strand tensioned between two stationary points such as in a testing machine or between tensioning bulkheads.
4.2.2.2 Elastic Shortening
𝑑𝑑𝐸𝐸𝑆𝑆
∆𝑓𝑓 =
𝐸𝐸
𝐸𝐸𝑑𝑑
𝑐𝑐𝑔𝑔
𝑓𝑓𝑐𝑐𝑔𝑔𝑑𝑑
𝑓𝑓𝑐𝑐𝑔𝑔𝑑𝑑 = 𝐴𝐴 +
𝑃𝑃 𝑃𝑃𝐴𝐴2
𝐼𝐼
𝑀𝑀𝑔𝑔𝐴𝐴
−
𝐼𝐼
𝑃𝑃 = 𝑁𝑁�𝐴𝐴𝑑𝑑𝑠𝑠��𝑓𝑓𝑑𝑑𝑝𝑝 − ∆𝑓𝑓𝑑𝑑𝑅𝑅0 − ∆𝑓𝑓𝑑𝑑𝐸𝐸𝑆𝑆�
Solve this equation iteratively for P.
𝑐𝑐𝑔𝑔
Assume 10% initial loss and 𝑓𝑓′ = 7.4 𝑘𝑘𝑠𝑠𝑠𝑠.
𝐸𝐸𝑐𝑐𝑔𝑔 = 120000(1.0)(0.155)2(7.4)0.33 = 5580.731 𝑘𝑘𝑠𝑠𝑠𝑠
𝑃𝑃 = 61(0.217)(1 − 0.10)(202.5) = 2412.4 𝑘𝑘𝑠𝑠𝑘𝑘
−
1𝑓𝑓𝑓𝑓
12𝑠𝑠𝑠𝑠
(3514.22𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) � � (31.477𝑠𝑠𝑠𝑠)
2412.4 𝑘𝑘𝑠𝑠𝑘𝑘 (2412.4𝑘𝑘𝑠𝑠𝑘𝑘)(31.477𝑠𝑠𝑠𝑠)2
𝑓𝑓𝑐𝑐𝑔𝑔𝑑𝑑 = 923.531𝑠𝑠𝑠𝑠2 + 734356.0𝑠𝑠𝑠𝑠4 734356.0𝑠𝑠𝑠𝑠4
= 4.059 𝑘𝑘𝑠𝑠𝑠𝑠
28500𝑘𝑘𝑠𝑠𝑠𝑠
∆𝑓𝑓𝑑𝑑𝐸𝐸𝑆𝑆 = 5580.731𝑘𝑘𝑠𝑠𝑠𝑠 (4.059𝑘𝑘𝑠𝑠𝑠𝑠) = 20.68𝑘𝑘𝑠𝑠𝑠𝑠
𝑃𝑃 = (61)(0.217𝑠𝑠𝑠𝑠2)(202.5𝑘𝑘𝑠𝑠𝑠𝑠 − 1.98𝑘𝑘𝑠𝑠𝑠𝑠 − 20.68𝑘𝑘𝑠𝑠𝑠𝑠) = 2380.5 𝑘𝑘𝑠𝑠𝑘𝑘
PGSuper performs this calculation with a very small convergence tolerance. The calculations are also performed at many points along the girder because the center of the prestress force changes due to harped strand location and the girder dead load moment changes along the length of the girder. There is less elastic shortening effect at the ends of the girder than at mid-span. Since stability tends to govern the design, and temporary strands require extra effort by the fabricator and the contractor, this refinement in the analysis is used to minimize the required concrete strength and temporary strand usage. The effective prestress force at release and initial lifting for various points (as determined by PGSuper) are given below. The initial loss converges to 11%.

## Slide 124
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Location | Effective Prestress after release, 𝑷𝑷(𝒌𝒌𝒌𝒌𝒌𝒌) | ∆𝒇𝒇𝒌𝒌𝒑𝒑𝒑𝒑 (𝒌𝒌𝒌𝒌𝒌𝒌)
PSXFR | 2423.16 | 17.461
HP | 2380.27 | 20.701
0.5Lg | 2384.47 | 20.384
    Concrete strength for form stripping
This is not an essential design step; however, it helps to illustrate that the initial lifting case typically governs the initial concrete strength. Check the point of prestress transfer and the harp point.
      Stress due to Prestressing
𝑃𝑃 𝑃𝑃𝐴𝐴
𝑓𝑓𝑑𝑑𝑠𝑠 = 𝐴𝐴 + 𝑆𝑆
From PGSuper, the effective prestress force at the point of prestress transfer is 𝑃𝑃 = 2423.16 𝑘𝑘𝑠𝑠𝑘𝑘 with an eccentricity of
16.166 𝑠𝑠𝑠𝑠.
−(2423.16𝑘𝑘𝑠𝑠𝑘𝑘) (−2423.16𝑘𝑘𝑠𝑠𝑘𝑘)(16.166𝑠𝑠𝑠𝑠)
923.531𝑠𝑠𝑠𝑠2 −19152.5𝑠𝑠𝑠𝑠3
𝑓𝑓𝑑𝑑 = + = −0.578𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 =
−(2423.16𝑘𝑘𝑠𝑠𝑘𝑘) (−2423.16𝑘𝑘𝑠𝑠𝑘𝑘)(16.166𝑠𝑠𝑠𝑠)
923.531𝑠𝑠𝑠𝑠2 20594.8𝑠𝑠𝑠𝑠3
+ = −4.526𝑘𝑘𝑠𝑠𝑠𝑠
From PGSuper, the effective prestress force at the harp point is 𝑃𝑃 = 2380.27 𝑘𝑘𝑠𝑠𝑘𝑘 with an eccentricity of 31.477 𝑠𝑠𝑠𝑠.
−(2380.27𝑘𝑘𝑠𝑠𝑘𝑘) (−2380.27𝑘𝑘𝑠𝑠𝑘𝑘)(31.477𝑠𝑠𝑠𝑠)
923.531𝑠𝑠𝑠𝑠2 −19152.5𝑠𝑠𝑠𝑠3
𝑓𝑓𝑑𝑑 = + = 1.335𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 =
−(2380.27𝑘𝑘𝑠𝑠𝑘𝑘) (−2380.27𝑘𝑘𝑠𝑠𝑘𝑘)(31.477𝑠𝑠𝑠𝑠)
923.531𝑠𝑠𝑠𝑠2 20594.8𝑠𝑠𝑠𝑠3
+ = −6.215𝑘𝑘𝑠𝑠𝑠𝑠
4.2.3.2 Stress due to Girder self-weight
𝑤𝑤
𝑔𝑔
2
𝑔𝑔 𝑠𝑠
2
𝑀𝑀 = (𝐿𝐿 𝑤𝑤 − 𝑤𝑤 )
At the point of prestress transfer
𝑤𝑤 = 60𝑑𝑑𝑠𝑠 = 60(0.6𝑠𝑠𝑠𝑠) = 36𝑠𝑠𝑠𝑠 = 3𝑓𝑓𝑓𝑓
𝑔𝑔
2
(1.058𝑘𝑘𝑘𝑘𝑓𝑓)
𝑀𝑀 = �(162.995𝑓𝑓𝑓𝑓)(3𝑓𝑓𝑓𝑓) − (3𝑓𝑓𝑓𝑓)2� = 253.96𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
253.96𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 12𝑠𝑠𝑠𝑠
𝑓𝑓𝑑𝑑 = −19152.5𝑠𝑠𝑠𝑠3 � 1𝑓𝑓𝑓𝑓 � = −0.159𝑘𝑘𝑠𝑠𝑠𝑠
253.96𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 12𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 = 20594.8𝑠𝑠𝑠𝑠3 � 1𝑓𝑓𝑓𝑓 � = 0.148𝑘𝑘𝑠𝑠𝑠𝑠
At the harp point
𝑤𝑤 = 0.4𝐿𝐿𝑔𝑔 = 0.4(162.995𝑓𝑓𝑓𝑓) = 65.198𝑓𝑓𝑓𝑓
𝑔𝑔
2
(1.058𝑘𝑘𝑘𝑘𝑓𝑓)
𝑀𝑀 = �(162.995𝑓𝑓𝑓𝑓)(65.198𝑓𝑓𝑓𝑓) − (65.198𝑓𝑓𝑓𝑓)2� = 3373.66𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓

## Slide 125
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
3373.66𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 12𝑠𝑠𝑠𝑠
𝑓𝑓𝑑𝑑 = −19152.5𝑠𝑠𝑠𝑠3 � 1𝑓𝑓𝑓𝑓 � = −2.114𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 =
3373.66𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 12𝑠𝑠𝑠𝑠
20594.8𝑠𝑠𝑠𝑠3 � 1𝑓𝑓𝑓𝑓 � = 1.966𝑘𝑘𝑠𝑠𝑠𝑠
      Total stress
At the point of prestress transfer
𝑓𝑓𝑑𝑑 = −0.578 + −0.159 = −0.738 𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 = −4.526 + 0.148 = −4.378 𝑘𝑘𝑠𝑠𝑠𝑠
At the harp point
𝑓𝑓𝑑𝑑 = 1.335 − 2.114 = −0.779 𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 = −6.215 + 1.996 = −4.219 𝑘𝑘𝑠𝑠𝑠𝑠
      Required strength at form stripping
At the point of prestress transfer
𝑐𝑐𝑔𝑔
−0.65𝑓𝑓′ = −4.378𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐𝑔𝑔
𝑓𝑓′ = 6.74 𝑘𝑘𝑠𝑠𝑠𝑠
At the harp point
𝑐𝑐𝑔𝑔
−0.65𝑓𝑓′ = −4.219𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐𝑔𝑔
𝑓𝑓′ = 6.49 𝑘𝑘𝑠𝑠𝑠𝑠
Theoretically, the concrete curing system and forms can be removed, and the prestress force can be imparted into the girder at this concrete strength. This would allow crews to begin work and reduce the time until construction of the next girder can begin. However, there must be a high degree of confidence that the lifting and final concrete strength targets can be attained.
4.2.4 Check girder stability
PGSuper performs many iterations to converge on an adequate lifting configuration. The solution converges for lifting devices located 11 ft from the ends of the girder.
The PGSuper Fabrication Options Report gives the required lift point and initial concrete strength for lifting without temporary strands as well as lifting with pretensioned or post-tensioned temporary strands.

## Slide 126
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Figure 4-3: Equilibrium of Hanging Girder
      Vertical Location of Center of Gravity
The location of the center of gravity is critical to the stability analysis. Girder camber, sweep, and lift loop offset all factor into the location of the center of gravity with respect to the lifting roll axis.
        Estimate Camber
Compute camber for the girder in the hanging configuration. The stability analysis procedure needs the camber measured from a datum at the ends of the girder, not the lift points.
          Girder
The total girder deflection relative to the end of the girder is the sum of the deflection at the girder ends and the mid-span deflection.
g1
g2
Figure 4-4: Girder Self-Weight Deflection during Lifting
𝐿𝐿𝑠𝑠 = 𝐿𝐿𝑔𝑔 − 2𝐴𝐴 = 164.995𝑓𝑓𝑓𝑓 − 2(11𝑓𝑓𝑓𝑓) = 140.995𝑓𝑓𝑓𝑓
At girder ends
𝑔𝑔1
∆ =
𝑤𝑤𝑔𝑔𝐴𝐴
24𝐸𝐸𝑐𝑐𝑔𝑔 𝐼𝐼𝑥𝑥
𝑠𝑠 𝑠𝑠
[3𝐴𝐴2(𝐴𝐴 + 2𝐿𝐿 ) − 𝐿𝐿3]
=
(−1.058𝑘𝑘𝑘𝑘𝑓𝑓)(11𝑓𝑓𝑓𝑓)
24(5580.731𝑘𝑘𝑠𝑠𝑠𝑠)(734356.0𝑠𝑠𝑠𝑠4)
�3(11𝑓𝑓𝑓𝑓)2�11𝑓𝑓𝑓𝑓 + 2(140.995𝑓𝑓𝑓𝑓)� − (140.995𝑓𝑓𝑓𝑓)3� �
1728𝑠𝑠𝑠𝑠3
1𝑓𝑓𝑓𝑓3
�
= 0.551 𝑠𝑠𝑠𝑠
Mid-span
𝑔𝑔2
∆ =
𝑔𝑔 𝑠𝑠 𝑔𝑔
5𝑤𝑤 𝐿𝐿4 𝑤𝑤 𝐴𝐴2𝐿𝐿2 5(−1.058𝑘𝑘𝑘𝑘𝑓𝑓)(140.995𝑓𝑓𝑓𝑓)4
− 𝑠𝑠 = � − � �
(−1.058𝑘𝑘𝑘𝑘𝑓𝑓)(11𝑓𝑓𝑓𝑓)2(140.995𝑓𝑓𝑓𝑓)2 1728𝑠𝑠𝑠𝑠3
�
384𝐸𝐸𝑐𝑐𝑔𝑔 𝐼𝐼𝑥𝑥 16𝐸𝐸𝑐𝑐𝑔𝑔 𝐼𝐼𝑥𝑥 384(5580.731𝑘𝑘𝑠𝑠𝑠𝑠)(734356.0𝑠𝑠𝑠𝑠4) 16(5580.731𝑘𝑘𝑠𝑠𝑠𝑠)(734356.0𝑠𝑠𝑠𝑠4) 1𝑓𝑓𝑓𝑓3
= −2.296𝑠𝑠𝑠𝑠 + 0.067𝑠𝑠𝑠𝑠 = −2.229𝑠𝑠𝑠𝑠
4.2.4.1.1.2 Prestressing

## Slide 127
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Since the girder is unrestrained, the location of the supports does not affect the overall prestress deflection measured between the ends of the girder and the mid-point.
4.2.4.1.1.2.1 Straight Strands
44
𝑃𝑃 = � � (2384.47𝑘𝑘𝑠𝑠𝑘𝑘) = 1719.95𝑘𝑘𝑠𝑠𝑘𝑘
𝑠𝑠𝑠𝑠
∆ =
8𝐸𝐸 𝐼𝐼
𝑐𝑐𝑔𝑔 𝑥𝑥
=
8(5580.731𝑘𝑘𝑠𝑠𝑠𝑠)(734356.0𝑠𝑠𝑠𝑠4)
61
𝑃𝑃𝐴𝐴𝐿𝐿2 (1719.95𝑘𝑘𝑠𝑠𝑘𝑘)(31.447𝑠𝑠𝑠𝑠)(162.995𝑓𝑓𝑓𝑓)2 144𝑠𝑠𝑠𝑠2
� � = 6.308𝑠𝑠𝑠𝑠 1𝑓𝑓𝑓𝑓2
4.2.4.1.1.2.2 Harped Strands
17
𝑃𝑃 = � � (2384.47𝑘𝑘𝑠𝑠𝑘𝑘) = 664.52 𝑘𝑘𝑠𝑠𝑘𝑘
61
𝐴𝐴′ = 𝐴𝐴ℎ𝑑𝑑 − 𝐴𝐴𝑒𝑒 = 30.775𝑠𝑠𝑠𝑠 − (−26.813𝑠𝑠𝑠𝑠)) = 57.588 𝑠𝑠𝑠𝑠
𝑠𝑠 = 0.4
𝑠𝑠𝐿𝐿
𝑁𝑁 = =
𝑃𝑃𝐴𝐴′ (664.52𝑘𝑘𝑠𝑠𝑘𝑘)(57.588𝑠𝑠𝑠𝑠) 1𝑓𝑓𝑓𝑓
(0.4)(162.995𝑓𝑓𝑓𝑓) 12𝑠𝑠𝑠𝑠
� � = 48.91𝑘𝑘𝑠𝑠𝑘𝑘
∆ℎ𝑠𝑠=
𝑠𝑠(3 − 4𝑠𝑠2)𝑁𝑁𝐿𝐿3
𝑐𝑐𝑔𝑔 𝑥𝑥
𝑃𝑃𝐴𝐴𝑒𝑒 𝐿𝐿2
+
24𝐸𝐸 𝐼𝐼 8𝐸𝐸 𝐼𝐼
𝑐𝑐𝑔𝑔 𝑥𝑥
=
0.4(3 − 4(0.4)2)(48.91𝑘𝑘𝑠𝑠𝑘𝑘)(162.995𝑓𝑓𝑓𝑓)3 1728𝑠𝑠𝑠𝑠3
24(5580.731𝑘𝑘𝑠𝑠𝑠𝑠)(734356.0𝑠𝑠𝑠𝑠4) 1𝑓𝑓𝑓𝑓3
� �
+
8(5580.731𝑘𝑘𝑠𝑠𝑠𝑠)(734356𝑠𝑠𝑠𝑠4)
(664.52𝑘𝑘𝑠𝑠𝑘𝑘)(−26.813𝑠𝑠𝑠𝑠)(162.995𝑓𝑓𝑓𝑓)2 144𝑠𝑠𝑠𝑠2
� � = 3.513𝑠𝑠𝑠𝑠 − 1.973𝑠𝑠𝑠𝑠 = 1.540𝑠𝑠𝑠𝑠 1𝑓𝑓𝑓𝑓2
4.2.4.1.1.3 Camber at lifting
∆𝑑𝑑𝑠𝑠= 𝛥𝛥𝑠𝑠𝑠𝑠 + 𝛥𝛥ℎ𝑠𝑠 = 6.308𝑠𝑠𝑠𝑠 + 1.540𝑠𝑠𝑠𝑠 = 7.848𝑠𝑠𝑠𝑠
∆𝑐𝑐𝑠𝑠𝑐𝑐𝑠𝑠𝑒𝑒𝑔𝑔 = −∆𝑔𝑔1 + 𝛥𝛥𝑔𝑔2 + ∆𝑑𝑑𝑠𝑠= −0.551𝑠𝑠𝑠𝑠 − 2.229𝑠𝑠𝑠𝑠 + 7.848𝑠𝑠𝑠𝑠 = 5.068𝑠𝑠𝑠𝑠
        Location the roll axis above the top of girder
Lifting loops tend to be flexible laterally. Assume the rotation occurs at the top of the girder.
𝑑𝑑𝑔𝑔𝑐𝑐 = 0𝑠𝑠𝑠𝑠
        Offset factor
The offset factor locates the center of mass of the girder with respect to the roll axis.

## Slide 128
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
a
a
Ls=Lg-2a
Lg

/3
(Ls/Lg)2
Centroid of Girder (Parabolic Arc)
Center of Mass
Roll Axis
Inclined lift cable force, P
Vertical component of lift force Pv
Horizontal component of lift force Ph
Yt
op
yr = Ytop + yrc - (Ls/Lg)2 – 1/3]
Elevation View
yrc
Center of mass with respect to the roll axis
(Ls/Lg)2 – /3 = (Ls/Lg)2 – 1/3] Offset Factor = (Ls/Lg)2 – 1/3
Figure 4-5: Offset Factor
𝑔𝑔
𝐿𝐿
2
𝐹𝐹 = � 𝑠𝑠 � − = �
1 140.995𝑓𝑓𝑓𝑓 2 1
𝐿𝐿𝑔𝑔 3 162.995𝑓𝑓𝑓𝑓 3
� − = 0.415
4.2.4.1.4 Location of CG below roll axis
𝑑𝑑𝑔𝑔 = 𝑌𝑌𝑑𝑑𝑔𝑔𝑑𝑑 − 𝐹𝐹𝑔𝑔(∆𝑐𝑐𝑠𝑠𝑐𝑐𝑠𝑠𝑒𝑒𝑔𝑔 ) + 𝑑𝑑𝑔𝑔𝑐𝑐 = 38.343𝑠𝑠𝑠𝑠 − (0.415)(5.068𝑠𝑠𝑠𝑠) − 0𝑠𝑠𝑠𝑠 = 36.24𝑠𝑠𝑠𝑠
      Lateral Deflection Parameters
        Lateral Sweep
Sweep tolerance is 1/8” per 10 ft
𝛥𝛥𝑠𝑠𝑤𝑤𝑒𝑒𝑒𝑒𝑑𝑑 =
162.995𝑓𝑓𝑓𝑓 1
10𝑓𝑓𝑓𝑓 8
� 𝑠𝑠𝑠𝑠� = 2.037𝑠𝑠𝑠𝑠
        Initial Lateral Eccentricity
Initial lateral eccentricity of center of gravity of girder due to lateral sweep and eccentricity of lifting devices from CL girder
𝐴𝐴𝑠𝑠𝑔𝑔𝑒𝑒𝑑𝑑 = 0.25𝑠𝑠𝑠𝑠
𝐴𝐴𝑔𝑔 = 𝐹𝐹𝑔𝑔𝛥𝛥𝑠𝑠𝑤𝑤𝑒𝑒𝑒𝑒𝑑𝑑 + 𝐴𝐴𝑠𝑠𝑔𝑔𝑒𝑒𝑑𝑑 = (0.415)(2.037𝑠𝑠𝑠𝑠) + 0.25𝑠𝑠𝑠𝑠 = 1.095𝑠𝑠𝑠𝑠
        Lateral Deflection of CG
Lateral deflection of center of gravity due to total girder weight applied to weak axis
𝐻𝐻𝑔𝑔 = 𝑤𝑤𝑔𝑔𝐿𝐿𝑔𝑔 = (1.058𝑘𝑘𝑘𝑘𝑓𝑓)(162.995𝑓𝑓𝑓𝑓) = 172.45𝑘𝑘𝑠𝑠𝑘𝑘

## Slide 129
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝑔𝑔
𝑧𝑧 = �
𝐻𝐻𝑔𝑔
12𝐸𝐸 𝐼𝐼
𝑐𝑐𝑔𝑔 𝑝𝑝𝑝𝑝 𝑔𝑔
𝐿𝐿2
𝐿𝐿5
𝑠𝑠 𝑠𝑠
6𝐴𝐴5
10 5
� � 𝑠𝑠 − 𝐴𝐴2𝐿𝐿3 + 3𝐴𝐴4𝐿𝐿 + �
= �
172.45𝑘𝑘𝑠𝑠𝑘𝑘
12(5580.731𝑘𝑘𝑠𝑠𝑠𝑠)(72018.4𝑠𝑠𝑠𝑠4)(162.995𝑓𝑓𝑓𝑓)2
� �
(140.995𝑓𝑓𝑓𝑓)5
10
− (11𝑓𝑓𝑓𝑓)2(140.995𝑓𝑓𝑓𝑓)3
+ 3(11𝑓𝑓𝑓𝑓)4(140.995𝑓𝑓𝑓𝑓) + (11𝑓𝑓𝑓𝑓)5� �
6 1728𝑠𝑠𝑠𝑠3
5 1𝑓𝑓𝑓𝑓3
� = 12.187 𝑠𝑠𝑠𝑠
4.2.4.3 Equilibrium tilt angle
𝑒𝑒𝑒𝑒
𝜃𝜃 =
𝑔𝑔 𝑔𝑔
𝐴𝐴𝑔𝑔 1.095𝑠𝑠𝑠𝑠
= = 0.04552 𝐴𝐴𝐴𝐴𝑑𝑑
𝑑𝑑 − 𝑧𝑧 36.24𝑠𝑠𝑠𝑠 − 12.187𝑠𝑠𝑠𝑠
      Girder Stresses in Hanging Girder
        Direct stress at Lift Point and Harp Point
          Prestressing
𝑃𝑃 𝑃𝑃𝐴𝐴
𝑓𝑓𝑑𝑑𝑠𝑠 = 𝐴𝐴 + 𝑆𝑆
At Lift Point
From PGSuper, the effective prestress force at the lift point is 𝑃𝑃 = 1746.62 𝑘𝑘𝑠𝑠𝑘𝑘 straight strands and 𝑃𝑃 = 674.83𝑘𝑘𝑠𝑠𝑘𝑘 harped strands. The straight and harped strand eccentricities are 31.748𝑠𝑠𝑠𝑠 and −17.097𝑠𝑠𝑠𝑠, respectively.
−(1746.62𝑘𝑘𝑠𝑠𝑘𝑘 + 674.83𝑘𝑘𝑠𝑠𝑘𝑘) (−1746.62𝑘𝑘𝑠𝑠𝑘𝑘)(31.748𝑠𝑠𝑠𝑠) + (−674.83𝑘𝑘𝑠𝑠𝑘𝑘)(−17.097𝑠𝑠𝑠𝑠)
923.531𝑠𝑠𝑠𝑠2 −19152.5𝑠𝑠𝑠𝑠3
𝑓𝑓𝑑𝑑 = + = −0.329𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 =
−(1746.62𝑘𝑘𝑠𝑠𝑘𝑘 + 674.83𝑘𝑘𝑠𝑠𝑘𝑘) (−1746.62𝑘𝑘𝑠𝑠𝑘𝑘)(31.748𝑠𝑠𝑠𝑠) + (−674.83𝑘𝑘𝑠𝑠𝑘𝑘)(−17.097𝑠𝑠𝑠𝑠)
923.531𝑠𝑠𝑠𝑠2 20594.8𝑠𝑠𝑠𝑠3
+ = −4.754𝑘𝑘𝑠𝑠𝑠𝑠
At Harp Point
From PGSuper, the effective prestress force at the harp point is 𝑃𝑃 = 1716.91 𝑘𝑘𝑠𝑠𝑘𝑘 straight strands and 𝑃𝑃 = 663.35𝑘𝑘𝑠𝑠𝑘𝑘 harped strands. The straight and harped strand eccentricities are 31.748𝑠𝑠𝑠𝑠 and 30.775𝑠𝑠𝑠𝑠, respectively.
−(1716.91𝑘𝑘𝑠𝑠𝑘𝑘 + 663.35𝑘𝑘𝑠𝑠𝑘𝑘) (−1716.91𝑘𝑘𝑠𝑠𝑘𝑘)(31.748𝑠𝑠𝑠𝑠) + (−663.35𝑘𝑘𝑠𝑠𝑘𝑘)(30.775𝑠𝑠𝑠𝑠)
923.531𝑠𝑠𝑠𝑠2 −19152.5𝑠𝑠𝑠𝑠3
𝑓𝑓𝑑𝑑 = + = 1.335𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 =
−(1716.91𝑘𝑘𝑠𝑠𝑘𝑘 + 663.35𝑘𝑘𝑠𝑠𝑘𝑘) (−1716.91𝑘𝑘𝑠𝑠𝑘𝑘)(31.748𝑠𝑠𝑠𝑠) + (−663.35𝑘𝑘𝑠𝑠𝑘𝑘)(30.775𝑠𝑠𝑠𝑠)
923.531𝑠𝑠𝑠𝑠2 20594.8𝑠𝑠𝑠𝑠3
+ = −6.215𝑘𝑘𝑠𝑠𝑠𝑠
4.2.4.4.1.2 Girder self-weight
𝑤𝑤
𝑔𝑔
2
𝑔𝑔 𝑠𝑠
2
𝑀𝑀 = (𝐿𝐿 𝑤𝑤 − 𝑤𝑤 − 𝐴𝐴
2
)
At Lift Point
𝑤𝑤 = 𝑘𝑘𝑑𝑑 − 𝐴𝐴 = 11𝑓𝑓𝑓𝑓 − 11𝑓𝑓𝑓𝑓 = 0.0𝑓𝑓𝑓𝑓
𝑔𝑔
𝑀𝑀 =
(1.058𝑘𝑘𝑘𝑘𝑓𝑓)
2
�(140.995𝑓𝑓𝑓𝑓)(0𝑓𝑓𝑓𝑓) − (0𝑓𝑓𝑓𝑓)2 − (11𝑓𝑓𝑓𝑓)2� = −64.02𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
−64.02𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 12𝑠𝑠𝑠𝑠
𝑓𝑓𝑑𝑑 = −19152.5𝑠𝑠𝑠𝑠3 � 1𝑓𝑓𝑓𝑓 � = 0.040𝑘𝑘𝑠𝑠𝑠𝑠
−64.02𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 12𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 = 20594.8𝑠𝑠𝑠𝑠3 � 1𝑓𝑓𝑓𝑓 � = −0.037𝑘𝑘𝑠𝑠𝑠𝑠
At Harp Point

## Slide 130
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝑤𝑤 = 0.4𝐿𝐿𝑔𝑔 − 𝐴𝐴 = 0.4(162.995𝑓𝑓𝑓𝑓) − 11𝑓𝑓𝑓𝑓 = 54.198𝑓𝑓𝑓𝑓
𝑔𝑔
2
(1.058𝑘𝑘𝑘𝑘𝑓𝑓)
𝑀𝑀 = �(140.995𝑓𝑓𝑓𝑓)(54.198𝑓𝑓𝑓𝑓) − (54.198𝑓𝑓𝑓𝑓)2 − (11𝑓𝑓𝑓𝑓)2� = 2425.0𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
2425.0𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 12𝑠𝑠𝑠𝑠
𝑓𝑓𝑑𝑑 = −19152.5𝑠𝑠𝑠𝑠3 � 1𝑓𝑓𝑓𝑓 � = −1.519𝑘𝑘𝑠𝑠𝑠𝑠
2425.0𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 12𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 = 20594.8𝑠𝑠𝑠𝑠3 � 1𝑓𝑓𝑓𝑓 � = 1.413𝑘𝑘𝑠𝑠𝑠𝑠
4.2.4.4.1.3 Total Stress
At Lift Point
𝑓𝑓𝑑𝑑 = −0.329 𝑘𝑘𝑠𝑠𝑠𝑠 + 0.040𝑘𝑘𝑠𝑠𝑠𝑠 = −0.289 𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 = −4.754𝑘𝑘𝑠𝑠𝑠𝑠 − 0.037𝑘𝑘𝑠𝑠𝑠𝑠 = −4.792 𝑘𝑘𝑠𝑠𝑠𝑠
At Harp Point
𝑓𝑓𝑑𝑑 = 1.335𝑘𝑘𝑠𝑠𝑠𝑠 − 1.519𝑘𝑘𝑠𝑠𝑠𝑠 = −0.184𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 = −6.215𝑘𝑘𝑠𝑠𝑠𝑠 + 1.413𝑘𝑘𝑠𝑠𝑠𝑠 = −4.802 𝑘𝑘𝑠𝑠𝑠𝑠
4.2.4.4.2 Tilt induced stresses
At Lift Point
Top left flange tip at lift point
𝑓𝑓𝑑𝑑𝑠𝑠 =
𝑀𝑀𝑔𝑔𝐻𝐻𝑑𝑑𝑒𝑒
2𝐼𝐼
𝑝𝑝𝑝𝑝
𝜃𝜃𝑒𝑒𝑒𝑒
𝑓𝑓𝑑𝑑𝑠𝑠 =
(−64.02𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(49𝑠𝑠𝑠𝑠)
2(72018.4𝑠𝑠𝑠𝑠4)
12𝑠𝑠𝑠𝑠
(0.04452 𝐴𝐴𝐴𝐴𝑑𝑑) � � = −0.012𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
Bottom right flange tip at lift point
𝑓𝑓𝑠𝑠𝑔𝑔 = −
𝑀𝑀𝑔𝑔𝐻𝐻𝑠𝑠𝑒𝑒
2𝐼𝐼
𝑝𝑝𝑝𝑝
𝜃𝜃𝑒𝑒𝑒𝑒
𝑓𝑓𝑠𝑠𝑔𝑔 = −
(−64.02𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(38.375𝑠𝑠𝑠𝑠)
2(72018.4𝑠𝑠𝑠𝑠4)
12𝑠𝑠𝑠𝑠
(0.04452 𝐴𝐴𝐴𝐴𝑑𝑑) � � = 0.009𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
At Harp Point
Top left flange tip at Harp Point
𝑓𝑓𝑑𝑑𝑠𝑠 =
𝑀𝑀𝑔𝑔𝐻𝐻𝑑𝑑𝑒𝑒
2𝐼𝐼
𝑝𝑝𝑝𝑝
𝜃𝜃𝑒𝑒𝑒𝑒
𝑓𝑓𝑑𝑑𝑠𝑠 =
(2425.0𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(49𝑠𝑠𝑠𝑠)
2(72018.4𝑠𝑠𝑠𝑠4)
12𝑠𝑠𝑠𝑠
(0.04452 𝐴𝐴𝐴𝐴𝑑𝑑) � � = 0.451𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
Bottom right flange tip at Harp Point
𝑓𝑓𝑠𝑠𝑔𝑔 = −
𝑀𝑀𝑔𝑔𝐻𝐻𝑠𝑠𝑒𝑒
2𝐼𝐼
𝑝𝑝𝑝𝑝
𝜃𝜃𝑒𝑒𝑒𝑒
𝑓𝑓𝑠𝑠𝑔𝑔 = −
(2425.0𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(38.375𝑠𝑠𝑠𝑠)
2(72018.4𝑠𝑠𝑠𝑠4)
12𝑠𝑠𝑠𝑠
(0.04452 𝐴𝐴𝐴𝐴𝑑𝑑) � � = −0.353𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓

## Slide 131
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
4.2.4.4.3 Total stress
Top left flange tip at lift point
𝑓𝑓𝑑𝑑𝑠𝑠 = −0.329𝑘𝑘𝑠𝑠𝑠𝑠 + 0.040𝑘𝑘𝑠𝑠𝑠𝑠 − 0.012𝑘𝑘𝑠𝑠𝑠𝑠 = −0.576𝑘𝑘𝑠𝑠𝑠𝑠
Bottom left flange tip at lift point
𝑓𝑓𝑠𝑠𝑔𝑔 = −4.754𝑘𝑘𝑠𝑠𝑠𝑠 − 0.037𝑘𝑘𝑠𝑠𝑠𝑠 + 0.009𝑘𝑘𝑠𝑠𝑠𝑠 = −4.528𝑘𝑘𝑠𝑠𝑠𝑠
Top left flange tip at Harp Point
𝑓𝑓𝑑𝑑𝑠𝑠 = 1.335𝑘𝑘𝑠𝑠𝑠𝑠 − 1.519𝑘𝑘𝑠𝑠𝑠𝑠 + 0.451𝑘𝑘𝑠𝑠𝑠𝑠 = 0.266𝑘𝑘𝑠𝑠𝑠𝑠
Bottom left flange tip at Harp Point
𝑓𝑓𝑠𝑠𝑔𝑔 = −6.215𝑘𝑘𝑠𝑠𝑠𝑠 + 1.413𝑘𝑘𝑠𝑠𝑠𝑠 − 0.353𝑘𝑘𝑠𝑠𝑠𝑠 = −5.155𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐𝑔𝑔
4.2.4.4.4 Determine Concrete Strength at Lifting
For the general stress case, compression stress is limited to −0.65𝑓𝑓′ .
Bottom centerline at point of lift −0.65𝑓𝑓′ = −4.792𝑘𝑘𝑠𝑠𝑠𝑠, 𝑓𝑓′ = 7.37 𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐𝑔𝑔 𝑐𝑐𝑔𝑔
Bottom centerline at harp point −0.65𝑓𝑓′ = −4.802𝑘𝑘𝑠𝑠𝑠𝑠, 𝑓𝑓′ = 7.39 𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐𝑔𝑔 𝑐𝑐𝑔𝑔
𝑐𝑐𝑔𝑔
Peak compression stress at the extremities of the section is limited to −0.7𝑓𝑓′
Bottom left flange tip at point of lift point −0.70𝑓𝑓′ = −4.801𝑘𝑘𝑠𝑠𝑠𝑠, 𝑓𝑓′ = 6.85 𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐𝑔𝑔 𝑐𝑐𝑔𝑔
Bottom left flange time at harp point −0.70𝑓𝑓′ = −5.155𝑘𝑘𝑠𝑠𝑠𝑠, 𝑓𝑓′ = 7.36 𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐𝑔𝑔 𝑐𝑐𝑔𝑔
The controlling initial concrete strength matches our assumption.
The required concrete strength at the lift point and the harp point are the same. The shows the proportioning of the strands is optimal. If two fewer strands were to be harped (46 straight, 15 harped), the required strength at the lift point would increase to 7.6 ksi which has the potential to increase curing time and could delay construction of the next girder.
4.2.4.5 Factor of Safety Against Cracking
Lateral cracking moment
𝑀𝑀𝑐𝑐𝑔𝑔 = ±
(𝑓𝑓𝑔𝑔 − 𝑓𝑓𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑐𝑐𝑑𝑑 )2𝐼𝐼𝑝𝑝𝑝𝑝
𝐻𝐻
𝑑𝑑𝑔𝑔𝑑𝑑
Tilt angle at first crack
𝑐𝑐𝑔𝑔
𝑀𝑀𝑐𝑐𝑔𝑔
𝑀𝑀
𝑔𝑔
𝜃𝜃 = ≤ 0.4 𝐴𝐴𝐴𝐴𝑑𝑑
Cracking moment at lift point – cracking in top right corner
𝑓𝑓𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑐𝑐𝑑𝑑 = 𝑓𝑓𝑑𝑑𝑠𝑠 + 𝑓𝑓𝑔𝑔 = −0.329𝑘𝑘𝑠𝑠𝑠𝑠 + 0.040𝑘𝑘𝑠𝑠𝑠𝑠 = −0.289𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐𝑔𝑔
𝑓𝑓𝑔𝑔 = 0.24�𝑓𝑓′ = 0.24√7.4𝑘𝑘𝑠𝑠𝑠𝑠 = 0.653 𝑘𝑘𝑠𝑠𝑠𝑠
𝑀𝑀𝑐𝑐𝑔𝑔 = −
�0.653𝑘𝑘𝑠𝑠𝑠𝑠 − (−0.289𝑘𝑘𝑠𝑠𝑠𝑠)�2(72018.4𝑠𝑠𝑠𝑠4) 1𝑠𝑠𝑠𝑠
49𝑠𝑠𝑠𝑠 12𝑓𝑓𝑓𝑓
� � = −230.71 𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
Tilt angle at first crack at lift point

## Slide 132
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
−230.71𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝜃𝜃𝑐𝑐𝑔𝑔 = −64.02𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 = 3.6 𝐴𝐴𝐴𝐴𝑑𝑑 ∴ 0.4 𝐴𝐴𝐴𝐴𝑑𝑑
Factor of Safety against Cracking at lift point
𝑐𝑐𝑔𝑔
𝐹𝐹𝑆𝑆 =
𝑑𝑑𝑔𝑔 𝜃𝜃𝑐𝑐𝑔𝑔
𝑔𝑔 𝑔𝑔 𝑐𝑐𝑔𝑔
(36.24𝑠𝑠𝑠𝑠)(0.4)
= = 2.429
𝐴𝐴 + 𝑧𝑧 𝜃𝜃 1.095𝑠𝑠𝑠𝑠 + (12.187𝑠𝑠𝑠𝑠)(0.4)
𝐹𝐹𝑆𝑆𝑐𝑐𝑔𝑔 > 1.0 OK
𝑀𝑀𝑐𝑐𝑔𝑔 =
Cracking moment at Harp Point
�0.653𝑘𝑘𝑠𝑠𝑠𝑠 − (1.335𝑘𝑘𝑠𝑠𝑠𝑠 − 1.519𝑘𝑘𝑠𝑠𝑠𝑠)�2(72018.4𝑠𝑠𝑠𝑠4) 1𝑠𝑠𝑠𝑠
49𝑠𝑠𝑠𝑠 12𝑓𝑓𝑓𝑓
� � = 205.19 𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
Tilt angle at first crack at Harp Point
205.19𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝜃𝜃𝑐𝑐𝑔𝑔 = 2425.0𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 = 0.08461𝐴𝐴𝐴𝐴𝑑𝑑
Factor of Safety against Cracking at Harp Point
𝑐𝑐𝑔𝑔
𝐹𝐹𝑆𝑆 =
𝑑𝑑𝑔𝑔 𝜃𝜃𝑐𝑐𝑔𝑔
𝑔𝑔 𝑔𝑔 𝑐𝑐𝑔𝑔
(36.24𝑠𝑠𝑠𝑠)(0.08461)
= = 1.443
𝐴𝐴 + 𝑧𝑧 𝜃𝜃 1.095𝑠𝑠𝑠𝑠 + (12.187𝑠𝑠𝑠𝑠)(0.08461)
𝐹𝐹𝑆𝑆𝑐𝑐𝑔𝑔 > 1.0 OK
4.2.4.6 Factor of Safety against Failure
𝜃𝜃𝑐𝑐𝑠𝑠𝑥𝑥 = �
𝐴𝐴𝑔𝑔
2.5𝑧𝑧𝑔𝑔
≤ 0.4 𝐴𝐴𝐴𝐴𝑑𝑑 = �
1.095
2.5(12.187)
= 0.1896 𝐴𝐴𝐴𝐴𝑑𝑑
𝑒𝑒
𝐹𝐹𝑆𝑆 =
𝑑𝑑𝑔𝑔 𝜃𝜃𝑐𝑐𝑠𝑠𝑥𝑥
𝑔𝑔
𝐴𝐴 + (1 + 2.5𝜃𝜃
)(𝑧𝑧 𝜃𝜃
𝑐𝑐𝑠𝑠𝑥𝑥 𝑔𝑔 𝑐𝑐𝑠𝑠𝑥𝑥
(36.24𝑠𝑠𝑠𝑠)(0.1896)
) = 1.095𝑠𝑠𝑠𝑠 + �1 + 2.5(0.1896)�(12.187𝑠𝑠𝑠𝑠)(0.1896) = 1.527
𝐹𝐹𝑆𝑆𝑒𝑒 > 1.5 OK
4.3 Step 3 - Design for Shipping
Stresses and the factor of safety against cracking depend on, in part, the prestress force at the time of shipping. The prestress force is dependent on the strand configuration, including temporary top strands, and the initial concrete strength. The initial concrete strength is also dependent on the number of temporary top strands.
At this step in the design, the number of temporary top strands and the initial concrete strength for lifting with temporary top strands are unknown.
Using an assumed set of truck parameters and assuming the bunk points are located H (girder height) in from the ends of the girder, PGSuper uses the initial concrete strength determined in Step 2 and computes the factor of safety against rollover failure.
The location of the bunk points is iteratively moved inwards until the factor of safety against rollover failure is greater than
1.5. If an adequate factor of safety cannot be found, the truck parameters are revised, and the process starts over with bunk points at H from the end of the girder.
Once the factor of safety against rollover failure is satisfied, the factor of safety against cracking is evaluated. Temporary top strands are added until the factor of safety is greater than 1.0.
Finally, the compression stresses are evaluated and a concrete strength for shipping is estimated.
Recall that this analysis is based on the initial concrete strength for lifting without temporary top strands. If temporary top strands are required for shipping, it is advantageous to use them during initial lifting. Lift loops can be moved closer to the ends of the girder which reduces the initial concrete strength requirement. A lower initial concrete strength means the final steps in girder production can begin and production of the next girder can start sooner.

## Slide 133
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
The result of the design iterations described above are bunk points need to be at least 13’-8” from the end of the girder to satisfy the rollover stability criteria and 4 temporary top strands are needed to satisfy the cracking criteria. The estimated concrete strength for hauling is 7.8 ksi.
Step 5 of the design procedure will illustrate the details of the shipping stability analysis. The calculations shown in Step 5 are also performed in this step to estimate the bunk points, temporary top strand requirements, and shipping concrete strength.
The non-composite girder, after temporary top strands are removed, carrying the weight of the wet deck concrete is analyzed in Section 4.6.2. This case has a required 28-day design concrete strength of 8.7 ksi. PGSuper will use the 7.8 ksi strength to check shipping, then find the 8.7 ksi requirement, and then begin the design iterations again starting with updating section properties and estimating the prestressing requirements. Therefore the 28-day design concrete strength of 8.7 ksi is assumed in Section 3.3.2.
  Step 4 - Design for Lifting with Temporary Top Strands
Temporary top strands are generally not required for lifting of girders. However, if they are required for shipping it is advantageous to pretension them with the permanent strands as previously described.
From Step 3, 4 temporary top strands are required. These strands are located 2 inches below the top of the girder. Their eccentricity is -36.343 in.
    Prestress losses
∆𝑓𝑓𝑑𝑑𝑅𝑅0 =
40
4.4.1.1 Initial relaxation before transfer
𝑘𝑘𝑐𝑐𝑔𝑔 (24.0 ∙ 1𝑑𝑑𝐴𝐴𝑑𝑑) 202.5𝑘𝑘𝑠𝑠𝑠𝑠
� − 0.55� (202.5𝑘𝑘𝑠𝑠𝑠𝑠) = 1.980 𝑘𝑘𝑠𝑠𝑠𝑠
243.0𝑘𝑘𝑠𝑠𝑠𝑠
4.4.1.2 Elastic Shortening
The temporary and permanent strands are at significantly different locations in the cross section. For this reason, compute the elastic shortening loss in the permanent and temporary strands separately.
∆𝑓𝑓𝑑𝑑𝐸𝐸𝑆𝑆 =
𝐸𝐸
𝐸𝐸𝑑𝑑
𝑐𝑐𝑔𝑔
𝑓𝑓𝑐𝑐𝑔𝑔𝑑𝑑
𝑓𝑓𝑐𝑐𝑔𝑔𝑑𝑑−𝑑𝑑𝑒𝑒𝑔𝑔𝑐𝑐 = 𝐴𝐴 +
𝑃𝑃 𝑃𝑃𝐴𝐴 𝐴𝐴𝑑𝑑
−
𝑀𝑀𝑔𝑔𝐴𝐴𝑑𝑑
𝑃𝑃
𝑓𝑓𝑐𝑐𝑔𝑔𝑑𝑑−𝑑𝑑𝑒𝑒𝑐𝑐𝑑𝑑 = 𝐴𝐴 +
𝐼𝐼
𝑃𝑃𝐴𝐴 𝐴𝐴𝑑𝑑
−
𝐼𝐼
𝑀𝑀𝑔𝑔𝐴𝐴𝑑𝑑
𝐼𝐼 𝐼𝐼
𝑃𝑃 = 𝑁𝑁𝑑𝑑�𝐴𝐴𝑑𝑑𝑠𝑠��𝑓𝑓𝑑𝑑𝑝𝑝 − ∆𝑓𝑓𝑑𝑑𝑅𝑅0 − ∆𝑓𝑓𝑑𝑑𝐸𝐸𝑆𝑆−𝑑𝑑𝑒𝑒𝑔𝑔𝑐𝑐�+𝑁𝑁𝑑𝑑 �𝐴𝐴𝑑𝑑𝑠𝑠��𝑓𝑓𝑑𝑑𝑝𝑝 − ∆𝑓𝑓𝑑𝑑𝑅𝑅0 − ∆𝑓𝑓𝑑𝑑𝐸𝐸𝑆𝑆−𝑑𝑑𝑒𝑒𝑐𝑐𝑑𝑑 �
Solve this equation iteratively for P.
The eccentricity of the resultant prestress force at mid-span is 27.304 in.
𝑐𝑐𝑔𝑔
Assume 10% initial loss and 𝑓𝑓′ = 7.2 𝑘𝑘𝑠𝑠𝑠𝑠.
𝐸𝐸𝑐𝑐𝑔𝑔 = 120000(1.0)(0.155)2(7.2)0.33 = 5530.5 𝑘𝑘𝑠𝑠𝑠𝑠
𝑃𝑃 = (61 + 4)(0.217)(1 − 0.10)(202.5) = 2570.6 𝑘𝑘𝑠𝑠𝑘𝑘
At CG of permanent strands

## Slide 134
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
−
1𝑓𝑓𝑓𝑓
12𝑠𝑠𝑠𝑠
(3514.22𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) � � (31.477𝑠𝑠𝑠𝑠)
2570.6 𝑘𝑘𝑠𝑠𝑘𝑘 (2570.6𝑘𝑘𝑠𝑠𝑘𝑘)(27.304𝑠𝑠𝑠𝑠)(31.477𝑠𝑠𝑠𝑠)
𝑓𝑓𝑐𝑐𝑔𝑔𝑑𝑑−𝑑𝑑𝑒𝑒𝑔𝑔𝑐𝑐 = 923.531𝑠𝑠𝑠𝑠2 + 734356.0𝑠𝑠𝑠𝑠4 734356.0𝑠𝑠𝑠𝑠4
= 3.984 𝑘𝑘𝑠𝑠𝑠𝑠
28500𝑘𝑘𝑠𝑠𝑠𝑠
∆𝑓𝑓𝑑𝑑𝐸𝐸𝑆𝑆−𝑑𝑑𝑒𝑒𝑔𝑔𝑐𝑐 = 5530.5𝑘𝑘𝑠𝑠𝑠𝑠 (3.984𝑘𝑘𝑠𝑠𝑠𝑠) = 20.53𝑘𝑘𝑠𝑠𝑠𝑠
At CG of temporary strands
−
1𝑓𝑓𝑓𝑓
(3514.22𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) �12𝑠𝑠𝑠𝑠� (−36.343𝑠𝑠𝑠𝑠)
2570.6 𝑘𝑘𝑠𝑠𝑘𝑘 (2570.6𝑘𝑘𝑠𝑠𝑘𝑘)(27.304𝑠𝑠𝑠𝑠)(−36.343𝑠𝑠𝑠𝑠)
𝑓𝑓𝑐𝑐𝑔𝑔𝑑𝑑−𝑑𝑑𝑒𝑒𝑐𝑐𝑑𝑑 = 923.531𝑠𝑠𝑠𝑠2 + 734356.0𝑠𝑠𝑠𝑠4 734356.0𝑠𝑠𝑠𝑠4
= 1.397 𝑘𝑘𝑠𝑠𝑠𝑠
28500𝑘𝑘𝑠𝑠𝑠𝑠
∆𝑓𝑓𝑑𝑑𝐸𝐸𝑆𝑆−𝑑𝑑𝑒𝑒𝑐𝑐𝑑𝑑 = 5530.5𝑘𝑘𝑠𝑠𝑠𝑠 (1.397𝑘𝑘𝑠𝑠𝑠𝑠) = 7.20𝑘𝑘𝑠𝑠𝑠𝑠
𝑃𝑃 = (61)(0.217𝑠𝑠𝑠𝑠2)(202.5𝑘𝑘𝑠𝑠𝑠𝑠 − 1.98𝑘𝑘𝑠𝑠𝑠𝑠 − 20.53𝑘𝑘𝑠𝑠𝑠𝑠) + 4(0.217𝑠𝑠𝑠𝑠2)(202.5𝑘𝑘𝑠𝑠𝑠𝑠 − 1.98𝑘𝑘𝑠𝑠𝑠𝑠 − 7.20𝑘𝑘𝑠𝑠𝑠𝑠) = 2550.3 𝑘𝑘𝑠𝑠𝑘𝑘
PGSuper performs this calculation with a very small convergence tolerance. The calculations are also performed at many points along the girder because the center of the prestress force changes due to harped strand location and the girder dead load moment changes along the length of the girder. There is less elastic shortening effect at the ends of the girder than at mid-span. The effective prestress force at release and initial lifting for various points (as determined by PGSuper) are given below. The initial loss converges to 11%.
Location | Effective Prestress after release
PSXFR | 2585.89 kip
HP | 2549.04 kip
0.5Lg | 2552.99 kip
    Check girder stability
PGSuper performs many iterations to converge on an adequate lifting configuration. The solution converges for lifting devices located 8.25 ft from the ends of the girder when temporary top strands are used.
      Vertical Location of Center of Gravity
        Estimate Camber
The same calculations are made to estimate camber in the lifting without temporary top strand case. The differences are the
modulus of elasticity is reduced because 𝑓𝑓′ reduced from 7.4 ksi to 7.2 ksi, the lift points moved from 11 ft to 8.25 ft, and
𝑐𝑐𝑔𝑔
temporary top strands are included in the prestress deflection. The resulting camber is
∆𝑐𝑐𝑠𝑠𝑐𝑐𝑠𝑠𝑒𝑒𝑔𝑔 = 4.025 𝑠𝑠𝑠𝑠
The camber due to the temporary top strands is computed using the same equation as the straight strands. The temporary top strand eccentricity will be a negative value resulting in a negative, downward deflection
4.4.2.1.2 Offset factor
𝑔𝑔
𝐿𝐿𝑠𝑠 = 162.995 − 2(8.25) = 146.495 𝑓𝑓𝑓𝑓
2
𝐹𝐹 = � 𝑠𝑠 � − = �
𝐿𝐿 1 146.495𝑓𝑓𝑓𝑓 2 1
𝐿𝐿𝑔𝑔 3 162.995𝑓𝑓𝑓𝑓 3
� − = 0.474

## Slide 135
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
        Location the roll axis above the top of girder
𝑑𝑑𝑔𝑔𝑐𝑐 = 0𝑠𝑠𝑠𝑠
        Location of CG below roll axis
𝑑𝑑𝑔𝑔 = 𝑌𝑌𝑑𝑑𝑔𝑔𝑑𝑑 − 𝐹𝐹𝑔𝑔(∆𝑐𝑐𝑠𝑠𝑐𝑐𝑠𝑠𝑒𝑒𝑔𝑔 ) + 𝑑𝑑𝑔𝑔𝑐𝑐 = 38.343𝑠𝑠𝑠𝑠 − (0.474)(4.025𝑠𝑠𝑠𝑠) − 0𝑠𝑠𝑠𝑠 = 36.433𝑠𝑠𝑠𝑠
      Lateral Deflection Parameters
        Lateral Sweep
Sweep tolerance is 1/8” per 10 ft
𝐴𝐴𝑠𝑠𝑤𝑤𝑒𝑒𝑒𝑒𝑑𝑑 =
162.995𝑓𝑓𝑓𝑓 1
10𝑓𝑓𝑓𝑓 8
� 𝑠𝑠𝑠𝑠� = 2.037𝑠𝑠𝑠𝑠
        Initial Lateral Eccentricity
Initial lateral eccentricity of center of gravity of girder due to lateral sweep and eccentricity of lifting devices from CL girder
𝐴𝐴𝑠𝑠𝑔𝑔𝑒𝑒𝑑𝑑 = 0.25𝑠𝑠𝑠𝑠
𝐴𝐴𝑔𝑔 = 𝐹𝐹𝑔𝑔𝐴𝐴𝑠𝑠𝑤𝑤𝑒𝑒𝑒𝑒𝑑𝑑 + 𝐴𝐴𝑠𝑠𝑔𝑔𝑒𝑒𝑑𝑑 = (0.474)(2.037𝑠𝑠𝑠𝑠) + 0.25𝑠𝑠𝑠𝑠 = 1.217𝑠𝑠𝑠𝑠
        Lateral Deflection of CG
Lateral deflection of center of gravity due to total girder weight applied to weak axis
𝐻𝐻𝑔𝑔 = 𝑤𝑤𝑔𝑔𝐿𝐿𝑔𝑔 = (1.058𝑘𝑘𝑘𝑘𝑓𝑓)(162.995𝑓𝑓𝑓𝑓) = 172.45𝑘𝑘𝑠𝑠𝑘𝑘
𝑔𝑔
𝑧𝑧 = �
𝐻𝐻𝑔𝑔
12𝐸𝐸 𝐼𝐼
𝑐𝑐𝑔𝑔 𝑝𝑝𝑝𝑝 𝑔𝑔
𝐿𝐿2
𝐿𝐿5
𝑠𝑠 𝑠𝑠
6𝐴𝐴5
10 5
� � 𝑠𝑠 − 𝐴𝐴2𝐿𝐿3 + 3𝐴𝐴4𝐿𝐿 + �
= �
172.45𝑘𝑘𝑠𝑠𝑘𝑘
12(5530.5𝑘𝑘𝑠𝑠𝑠𝑠)(72018.4𝑠𝑠𝑠𝑠4)(162.995𝑓𝑓𝑓𝑓)2
� �
(146.495𝑓𝑓𝑓𝑓)5
10
− (8.25𝑓𝑓𝑓𝑓)2(146.495𝑓𝑓𝑓𝑓)3
+ 3(8.25𝑓𝑓𝑓𝑓)4(146.495𝑓𝑓𝑓𝑓) + (8.25𝑓𝑓𝑓𝑓)5� �
6 1728𝑠𝑠𝑠𝑠3
5 1𝑓𝑓𝑓𝑓3
� = 15.339 𝑠𝑠𝑠𝑠
4.4.2.3 Equilibrium tilt angle
𝑒𝑒𝑒𝑒
𝜃𝜃 =
𝑔𝑔 𝑔𝑔
𝐴𝐴𝑔𝑔 1.217𝑠𝑠𝑠𝑠
= = 0.05768 𝐴𝐴𝐴𝐴𝑑𝑑
𝑑𝑑 − 𝑧𝑧 36.433𝑠𝑠𝑠𝑠 − 15.339𝑠𝑠𝑠𝑠
      Girder Stresses in Hanging Girder
        Direct stress at Lift Point and Harp Point
          Prestressing
𝑓𝑓𝑑𝑑 =
𝑃𝑃 𝑃𝑃𝐴𝐴
𝑓𝑓𝑑𝑑𝑠𝑠 = 𝐴𝐴 + 𝑆𝑆
From PGSuper, the effective prestress force at the lift point is 𝑃𝑃 = 1743.87 𝑘𝑘𝑠𝑠𝑘𝑘 straight strands, 𝑃𝑃 = 673.64𝑘𝑘𝑠𝑠𝑘𝑘 harped strands and P = 167.83kip for temporary strands. The straight, harped, and temporary strand eccentricities are 31.748𝑠𝑠𝑠𝑠,−19.526𝑠𝑠𝑠𝑠, and −36.434𝑠𝑠𝑠𝑠, respectively.
−(1743.87𝑘𝑘𝑠𝑠𝑘𝑘 + 673.64𝑘𝑘𝑠𝑠𝑘𝑘 + 167.83𝑘𝑘𝑠𝑠𝑘𝑘)
+
923.531𝑠𝑠𝑠𝑠2
(−1743.87𝑘𝑘𝑠𝑠𝑘𝑘)(31.748𝑠𝑠𝑠𝑠) + (−673.64𝑘𝑘𝑠𝑠𝑘𝑘)(−19.526𝑠𝑠𝑠𝑠) + (−167.83𝑘𝑘𝑠𝑠𝑘𝑘)(−36.343𝑠𝑠𝑠𝑠)
−19152.5𝑠𝑠𝑠𝑠3
= −0.914𝑘𝑘𝑠𝑠𝑠𝑠

## Slide 136
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝑓𝑓𝑠𝑠 =
−(1743.87𝑘𝑘𝑠𝑠𝑘𝑘 + 673.64𝑘𝑘𝑠𝑠𝑘𝑘 + 167.83𝑘𝑘𝑠𝑠𝑘𝑘)
+
923.531𝑠𝑠𝑠𝑠2
(−1743.87𝑘𝑘𝑠𝑠𝑘𝑘)(31.748𝑠𝑠𝑠𝑠) + (−673.64𝑘𝑘𝑠𝑠𝑘𝑘)(−19.526𝑠𝑠𝑠𝑠) + (−167.83𝑘𝑘𝑠𝑠𝑘𝑘)(−36.343𝑠𝑠𝑠𝑠)
20594.8𝑠𝑠𝑠𝑠3
= −4.552𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑑𝑑 =
From PGSuper, the effective prestress force at the harp point is 𝑃𝑃 = 1717.36 𝑘𝑘𝑠𝑠𝑘𝑘 straight strands, 𝑃𝑃 = 663.53𝑘𝑘𝑠𝑠𝑘𝑘 harped strands, and 𝑃𝑃 = 168.15𝑘𝑘𝑠𝑠𝑘𝑘 temporary strands. The straight, harped, and temporary strand eccentricities are 31.748𝑠𝑠𝑠𝑠, 30.775𝑠𝑠𝑠𝑠, and −36.434 𝑠𝑠𝑠𝑠 respectively.
−(1717.36𝑘𝑘𝑠𝑠𝑘𝑘 + 663.53𝑘𝑘𝑠𝑠𝑘𝑘 + 168.15𝑘𝑘𝑠𝑠𝑘𝑘)
+
923.531𝑠𝑠𝑠𝑠2
(−1717.36𝑘𝑘𝑠𝑠𝑘𝑘)(31.748𝑠𝑠𝑠𝑠) + (−663.53𝑘𝑘𝑠𝑠𝑘𝑘)(−31.748𝑠𝑠𝑠𝑠) + (−168.15𝑘𝑘𝑠𝑠𝑘𝑘)(−36.343𝑠𝑠𝑠𝑠)
−19152.5𝑠𝑠𝑠𝑠3
= 0.834𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 =
−(1717.36𝑘𝑘𝑠𝑠𝑘𝑘 + 663.53𝑘𝑘𝑠𝑠𝑘𝑘 + 168.15𝑘𝑘𝑠𝑠𝑘𝑘)
+
923.531𝑠𝑠𝑠𝑠2
(−1717.36𝑘𝑘𝑠𝑠𝑘𝑘)(31.748𝑠𝑠𝑠𝑠) + (−663.53𝑘𝑘𝑠𝑠𝑘𝑘)(−31.748𝑠𝑠𝑠𝑠) + (−168.15𝑘𝑘𝑠𝑠𝑘𝑘)(−36.343𝑠𝑠𝑠𝑠)
20594.8𝑠𝑠𝑠𝑠3
= −6.102𝑘𝑘𝑠𝑠𝑠𝑠
4.4.2.4.1.2 Girder self-weight
𝑤𝑤
𝑔𝑔
2
𝑔𝑔 𝑠𝑠
2 2
𝑀𝑀 = (𝐿𝐿 𝑤𝑤 − 𝑤𝑤 − 𝐴𝐴 )
At Lift Point
𝑤𝑤 = 𝑘𝑘𝑑𝑑 − 𝐴𝐴 = 8.25𝑓𝑓𝑓𝑓 − 8.25𝑓𝑓𝑓𝑓 = 0.0𝑓𝑓𝑓𝑓
𝑔𝑔
𝑀𝑀 =
(1.058𝑘𝑘𝑘𝑘𝑓𝑓)
2
�(146.495𝑓𝑓𝑓𝑓)(0𝑓𝑓𝑓𝑓) − (0𝑓𝑓𝑓𝑓)2 − (11𝑓𝑓𝑓𝑓)2� = −36.01𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
−36.01𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 12𝑠𝑠𝑠𝑠
𝑓𝑓𝑑𝑑 = −19152.5𝑠𝑠𝑠𝑠3 � 1𝑓𝑓𝑓𝑓 � = 0.023𝑘𝑘𝑠𝑠𝑠𝑠
−36.01𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 12𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 = 20594.8𝑠𝑠𝑠𝑠3 � 1𝑓𝑓𝑓𝑓 � = −0.021𝑘𝑘𝑠𝑠𝑠𝑠
At Harp Point
𝑤𝑤 = 0.4𝐿𝐿𝑔𝑔 − 𝐴𝐴 = 0.4(162.995𝑓𝑓𝑓𝑓) − 8.25𝑓𝑓𝑓𝑓 = 56.948𝑓𝑓𝑓𝑓
𝑔𝑔
2
(1.058𝑘𝑘𝑘𝑘𝑓𝑓)
𝑀𝑀 = �(146.495𝑓𝑓𝑓𝑓)(56.948𝑓𝑓𝑓𝑓) − (56.948𝑓𝑓𝑓𝑓)2 − (8.25𝑓𝑓𝑓𝑓)2� = 2689.16𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
2689.16𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 12𝑠𝑠𝑠𝑠
𝑓𝑓𝑑𝑑 = −19152.5𝑠𝑠𝑠𝑠3 � 1𝑓𝑓𝑓𝑓 � = −1.685𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 =
2689.16𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 12𝑠𝑠𝑠𝑠
20594.8𝑠𝑠𝑠𝑠3 � 1𝑓𝑓𝑓𝑓 � = 1.567𝑘𝑘𝑠𝑠𝑠𝑠
4.4.2.4.2 Tilt induced stresses
Top left flange tip at lift point
𝑓𝑓𝑑𝑑𝑠𝑠 =
𝑀𝑀𝑔𝑔𝐻𝐻𝑑𝑑𝑒𝑒
2𝐼𝐼
𝑝𝑝𝑝𝑝
𝜃𝜃𝑒𝑒𝑒𝑒
𝑓𝑓𝑑𝑑𝑠𝑠 =
(−36.01𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(49𝑠𝑠𝑠𝑠)
2(72018.4𝑠𝑠𝑠𝑠4)
12𝑠𝑠𝑠𝑠
(0.05768 𝐴𝐴𝐴𝐴𝑑𝑑) � � = −0.008𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓

## Slide 137
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Bottom right flange tip at lift point
𝑓𝑓𝑠𝑠𝑔𝑔 = −
𝑀𝑀𝑔𝑔𝐻𝐻𝑠𝑠𝑒𝑒
2𝐼𝐼
𝑝𝑝𝑝𝑝
𝜃𝜃𝑒𝑒𝑒𝑒
𝑓𝑓𝑠𝑠𝑔𝑔 = −
(−36.01𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(38.375𝑠𝑠𝑠𝑠)
2(72018.4𝑠𝑠𝑠𝑠4)
12𝑠𝑠𝑠𝑠
(0.05768 𝐴𝐴𝐴𝐴𝑑𝑑) � � = 0.007𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
Top left flange tip at Harp Point
𝑓𝑓𝑑𝑑𝑠𝑠 =
𝑀𝑀𝑔𝑔𝐻𝐻𝑑𝑑𝑒𝑒
2𝐼𝐼
𝑝𝑝𝑝𝑝
𝜃𝜃𝑒𝑒𝑒𝑒
𝑓𝑓𝑑𝑑𝑠𝑠 =
(2662.16𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(49𝑠𝑠𝑠𝑠)
2(72018.4𝑠𝑠𝑠𝑠4)
12𝑠𝑠𝑠𝑠
(0.05768 𝐴𝐴𝐴𝐴𝑑𝑑) � � = 0.627𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
Bottom right flange tip at Harp Point
𝑓𝑓𝑠𝑠𝑔𝑔 = −
𝑀𝑀𝑔𝑔𝐻𝐻𝑠𝑠𝑒𝑒
2𝐼𝐼
𝑝𝑝𝑝𝑝
𝜃𝜃𝑒𝑒𝑒𝑒
𝑓𝑓𝑠𝑠𝑔𝑔 = −
(2662.16𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(38.375𝑠𝑠𝑠𝑠)
2(72018.4𝑠𝑠𝑠𝑠4)
12𝑠𝑠𝑠𝑠
(0.05768 𝐴𝐴𝐴𝐴𝑑𝑑) � � = −0.491𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
4.4.2.4.3 Total stress
Top left flange tip at lift point
𝑓𝑓𝑑𝑑𝑠𝑠 = −0.914𝑘𝑘𝑠𝑠𝑠𝑠 + 0.023𝑘𝑘𝑠𝑠𝑠𝑠 − 0.008𝑘𝑘𝑠𝑠𝑠𝑠 = −0.900𝑘𝑘𝑠𝑠𝑠𝑠
Bottom left flange tip at lift point
𝑓𝑓𝑠𝑠𝑔𝑔 = −4.401𝑘𝑘𝑠𝑠𝑠𝑠 − 0.021𝑘𝑘𝑠𝑠𝑠𝑠 + 0.007𝑘𝑘𝑠𝑠𝑠𝑠 = −4.566𝑘𝑘𝑠𝑠𝑠𝑠
Top left flange tip at Harp Point
𝑓𝑓𝑑𝑑𝑠𝑠 = 0.834𝑘𝑘𝑠𝑠𝑠𝑠 − 1.668𝑘𝑘𝑠𝑠𝑠𝑠 + 0.627𝑘𝑘𝑠𝑠𝑠𝑠 = −0.207𝑘𝑘𝑠𝑠𝑠𝑠
Bottom left flange tip at Harp Point
𝑓𝑓𝑠𝑠𝑔𝑔 = −6.102𝑘𝑘𝑠𝑠𝑠𝑠 + 1.551𝑘𝑘𝑠𝑠𝑠𝑠 − 0.491𝑘𝑘𝑠𝑠𝑠𝑠 = −5.042𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐𝑔𝑔
4.4.2.4.4 Determine Concrete Strength at Lifting
For the general stress case, compression stress is limited to −0.65𝑓𝑓′ .
Bottom centerline at point of lift −0.65𝑓𝑓′ = −4.573𝑘𝑘𝑠𝑠𝑠𝑠, 𝑓𝑓′ = 7.04 𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐𝑔𝑔 𝑐𝑐𝑔𝑔
Bottom centerline at harp point −0.65𝑓𝑓′ = −4.551𝑘𝑘𝑠𝑠𝑠𝑠, 𝑓𝑓′ = 7.00 𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐𝑔𝑔 𝑐𝑐𝑔𝑔
𝑐𝑐𝑔𝑔
Peak compression stress at the extremities of the section is limited to−0.7𝑓𝑓′
Bottom left flange tip at point of lift point −0.70𝑓𝑓′ = −4.580𝑘𝑘𝑠𝑠𝑠𝑠, 𝑓𝑓′ = 6.54𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐𝑔𝑔 𝑐𝑐𝑔𝑔
Bottom left flange time at harp point −0.70𝑓𝑓′ = −5.042𝑘𝑘𝑠𝑠𝑠𝑠, 𝑓𝑓′ = 7.2 𝑘𝑘𝑠𝑠𝑠𝑠  Controls
𝑐𝑐𝑔𝑔 𝑐𝑐𝑔𝑔
The controlling concrete strength matches the assumed value.
4.4.2.5 Factor of Safety Against Cracking
Lateral cracking moment

## Slide 138
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝑀𝑀𝑐𝑐𝑔𝑔 = ±
(𝑓𝑓𝑔𝑔 − 𝑓𝑓𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑐𝑐𝑑𝑑 )2𝐼𝐼𝑝𝑝𝑝𝑝
𝐻𝐻
𝑑𝑑𝑔𝑔𝑑𝑑
Tilt angle at first crack
𝑐𝑐𝑔𝑔
𝑀𝑀𝑐𝑐𝑔𝑔
𝑀𝑀
𝑔𝑔
𝜃𝜃 = ≤ 0.4 𝐴𝐴𝐴𝐴𝑑𝑑
Cracking moment at lift point – cracking in top right corner
𝑓𝑓𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑐𝑐𝑑𝑑 = 𝑓𝑓𝑑𝑑𝑠𝑠 + 𝑓𝑓𝑔𝑔 = −0.914𝑘𝑘𝑠𝑠𝑠𝑠 + 0.023𝑘𝑘𝑠𝑠𝑠𝑠 = −0.892𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐𝑔𝑔
𝑓𝑓𝑔𝑔 = 0.24�𝑓𝑓′ = 0.24√7.2𝑘𝑘𝑠𝑠𝑠𝑠 = 0.644 𝑘𝑘𝑠𝑠𝑠𝑠
𝑀𝑀𝑐𝑐𝑔𝑔 = −
�0.644𝑘𝑘𝑠𝑠𝑠𝑠 − (−0.892𝑘𝑘𝑠𝑠𝑠𝑠)�2(72018.4𝑠𝑠𝑠𝑠4) 1𝑠𝑠𝑠𝑠
49𝑠𝑠𝑠𝑠 12𝑓𝑓𝑓𝑓
� � = −376.15 𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
Tilt angle at first crack at lift point
𝜃𝜃𝑐𝑐𝑔𝑔 =
−376.151𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
−36.01𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
= 10.44 𝐴𝐴𝐴𝐴𝑑𝑑 ∴ 0.4 𝐴𝐴𝐴𝐴𝑑𝑑
Factor of Safety against Cracking at lift point
𝑐𝑐𝑔𝑔
𝐹𝐹𝑆𝑆 =
𝑑𝑑𝑔𝑔 𝜃𝜃𝑐𝑐𝑔𝑔
𝑔𝑔 𝑔𝑔 𝑐𝑐𝑔𝑔
(36.433𝑠𝑠𝑠𝑠)(0.4)
= = 1.98
𝐴𝐴 + 𝑧𝑧 𝜃𝜃 1.217𝑠𝑠𝑠𝑠 + (15.339𝑠𝑠𝑠𝑠)(0.4)
𝐹𝐹𝑆𝑆𝑐𝑐𝑔𝑔 > 1.0 OK
𝑀𝑀𝑐𝑐𝑔𝑔 =
Cracking moment at Harp Point
�0.644𝑘𝑘𝑠𝑠𝑠𝑠 − (0.834𝑘𝑘𝑠𝑠𝑠𝑠 − 1.685𝑘𝑘𝑠𝑠𝑠𝑠)�2(72018.4𝑠𝑠𝑠𝑠4) 1𝑠𝑠𝑠𝑠
49𝑠𝑠𝑠𝑠 12𝑓𝑓𝑓𝑓
� � = 362.09 𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
Tilt angle at first crack at Harp Point
362.09𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝜃𝜃𝑐𝑐𝑔𝑔 = 2662.16𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 = 0.13601𝐴𝐴𝐴𝐴𝑑𝑑
Factor of Safety against Cracking at Harp Point
𝑐𝑐𝑔𝑔
𝐹𝐹𝑆𝑆 =
𝑑𝑑𝑔𝑔 𝜃𝜃𝑐𝑐𝑔𝑔
𝑔𝑔 𝑔𝑔 𝑐𝑐𝑔𝑔
(36.433𝑠𝑠𝑠𝑠)(0.13601)
= = 1.5
𝐴𝐴 + 𝑧𝑧 𝜃𝜃 1.217𝑠𝑠𝑠𝑠 + (15.339𝑠𝑠𝑠𝑠)(0.13601)
𝐹𝐹𝑆𝑆𝑐𝑐𝑔𝑔 > 1.0 OK
4.4.2.6 Factor of Safety against Failure
𝑐𝑐𝑠𝑠𝑥𝑥
𝜃𝜃 = �
𝐴𝐴𝑔𝑔
2.5𝑧𝑧𝑔𝑔
≤ 0.4 𝐴𝐴𝐴𝐴𝑑𝑑 = �
1.217
2.5(15.339)
= 0.17812 𝐴𝐴𝐴𝐴𝑑𝑑
𝑒𝑒
𝐹𝐹𝑆𝑆 =
𝑑𝑑𝑔𝑔 𝜃𝜃𝑐𝑐𝑠𝑠𝑥𝑥
𝑔𝑔
𝐴𝐴 + (1 + 2.5𝜃𝜃
)(𝑧𝑧 𝜃𝜃
𝑐𝑐𝑠𝑠𝑥𝑥 𝑔𝑔 𝑐𝑐𝑠𝑠𝑥𝑥
(36.433𝑠𝑠𝑠𝑠)(0.17812)
) = 1.217𝑠𝑠𝑠𝑠 + �1 + 2.5(0.17812)�(165.339𝑠𝑠)(0.17812) = 1.256
When 𝐹𝐹𝑆𝑆𝑒𝑒 < 𝐹𝐹𝑆𝑆𝑐𝑐𝑔𝑔 , 𝐹𝐹𝑆𝑆𝑒𝑒 = 𝐹𝐹𝑆𝑆𝑐𝑐𝑔𝑔 ∴ 𝐹𝐹𝑆𝑆𝑒𝑒 = 1.5
𝐹𝐹𝑆𝑆𝑒𝑒 ≥ 1.5 OK

## Slide 139
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
  Step 5 – Revise Shipping Design
Up to this point initial concrete strength, final concrete strength, and temporary strand requirements have been estimated based on assumed values. This design step verifies the shipping stability design.
Per the WSDOT Standard Specifications, WF girders can be shipped as soon as 10 days and as late as 90 days. The effective prestress force and camber vary during this time range. The analysis is conservative when using the effective prestress force at 10 days and the camber at 90 days (BDM 5.6.3.D.6).
    Estimate Prestress Losses at Shipping
Assume hauling to occur as soon as possible (10 days)
      Initial Relaxation
See 4.4.1.1
      Elastic Shortening
See 4.4.1.2
      Shrinkage of Girder Concrete
∆𝑓𝑓𝑆𝑆𝑅𝑅𝑆𝑆 = 𝜀𝜀𝑠𝑠𝑔𝑔ℎ𝐸𝐸𝑑𝑑𝐾𝐾𝑔𝑔ℎ
𝜀𝜀𝑠𝑠𝑔𝑔ℎ = 𝑘𝑘𝑠𝑠𝑘𝑘ℎ𝑠𝑠𝑘𝑘𝑒𝑒 𝑘𝑘𝑑𝑑𝑔𝑔0.48 × 10−3
𝐾𝐾𝑔𝑔ℎ (𝑃𝑃𝐴𝐴𝐴𝐴𝑚𝑚𝐴𝐴𝑠𝑠𝐴𝐴𝑠𝑠𝑓𝑓 𝑆𝑆𝑓𝑓𝐴𝐴𝐴𝐴𝑠𝑠𝑑𝑑𝑠𝑠) = 𝐾𝐾𝑔𝑔ℎ−𝑑𝑑𝑒𝑒𝑔𝑔𝑐𝑐 =
1
𝐸𝐸 𝐴𝐴
𝐸𝐸𝑐𝑐𝑔𝑔 𝐴𝐴𝑔𝑔
𝐴𝐴 𝐴𝐴 𝐴𝐴
𝐼𝐼𝑔𝑔
𝑠𝑠 𝑒𝑒 𝑔𝑔
1 + 𝑑 𝑑 𝑑𝑑𝑠𝑠 �1 + 𝑔 𝑔 𝑑𝑑𝑠 𝑠 𝑑𝑑� �1 + 0.7𝜓𝜓 �𝑓𝑓 , 𝑓𝑓 ��
𝐾𝐾𝑔𝑔ℎ (𝑇𝑇𝐴𝐴𝑚𝑚𝑘𝑘𝑐𝑐𝐴𝐴𝐴𝐴𝐴𝐴𝑑𝑑 𝑆𝑆𝑓𝑓𝐴𝐴𝐴𝐴𝑠𝑠𝑑𝑑𝑠𝑠) = 𝐾𝐾𝑔𝑔ℎ−𝑑𝑑𝑒𝑒𝑐𝑐𝑑𝑑 =
1
𝐸𝐸 𝐴𝐴
𝐸𝐸𝑐𝑐𝑔𝑔 𝐴𝐴𝑔𝑔
𝐴𝐴 𝐴𝐴 𝐴𝐴
𝐼𝐼𝑔𝑔
𝑠𝑠 𝑒𝑒 𝑔𝑔
1 + 𝑑 𝑑 𝑑𝑑𝑠𝑠 �1 + 𝑔 𝑔 𝑑𝑑𝑠 𝑠 𝑑𝑑 � �1 + 0.7𝜓𝜓 �𝑓𝑓 , 𝑓𝑓 ��
𝑔𝑔
𝜓𝜓𝑠𝑠 �𝑓𝑓𝑒𝑒 , 𝑓𝑓𝑔𝑔� = 1.9𝑘𝑘𝑠𝑠𝑘𝑘ℎ𝑐𝑐 𝑘𝑘𝑒𝑒 𝑘𝑘𝑑𝑑𝑔𝑔𝑓𝑓−0.118
𝑉𝑉
𝑘𝑘𝑠𝑠 = 1.45 − 0.13 �𝑆𝑆� ≥ 1.0
=
𝑉𝑉 𝐴𝐴𝐿𝐿
𝑔𝑔
𝑆𝑆 𝑃𝑃𝐿𝐿𝑔𝑔 + 2𝐴𝐴
=
1𝑓𝑓𝑓𝑓
(923.531𝑠𝑠𝑠𝑠2)(162.995𝑓𝑓𝑓𝑓)(12𝑠𝑠𝑠𝑠)
(289.284𝑠𝑠𝑠𝑠)(162.995𝑓𝑓𝑓𝑓) �12𝑠𝑠𝑠𝑠� + 2(923.531𝑠𝑠𝑠𝑠2)
= 3.182𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
𝑘𝑘𝑠𝑠 = 1.45 − 0.13(3.187) = 1.04
𝑘𝑘ℎ𝑠𝑠 = 2.00 − 0.014𝐻𝐻 = 2.00 − 0.014(75) = 0.95
𝑘𝑘ℎ𝑐𝑐 = 1.56 − 0.008𝐻𝐻 = 1.56 − 0.005(75) = 0.96
5 5
𝑘𝑘𝑒𝑒 = 1 + 𝑓𝑓′ = 1 + 7.2 = 0.61
𝑘𝑘𝑑𝑑𝑔𝑔(𝑓𝑓 = 9𝑑𝑑𝐴𝐴𝑑𝑑𝑠𝑠) =
𝑐𝑐𝑔𝑔
𝑓𝑓𝑔𝑔 = 1 𝑑𝑑𝐴𝐴𝑑𝑑, 𝑓𝑓ℎ = 10 𝑑𝑑𝐴𝐴𝑑𝑑𝑠𝑠, 𝑓𝑓 = 𝑓𝑓ℎ − 𝑓𝑓𝑔𝑔 = 9 𝑑𝑑𝐴𝐴𝑑𝑑𝑠𝑠
9
12 �
100 − 4(7.2)
7.2 + 20
� + 9
= 0.223
𝑓𝑓𝑔𝑔 = 1 𝑑𝑑𝐴𝐴𝑑𝑑, 𝑓𝑓𝑒𝑒 = 2000 𝑑𝑑𝐴𝐴𝑑𝑑𝑠𝑠, 𝑓𝑓 = 𝑓𝑓𝑒𝑒 − 𝑓𝑓𝑔𝑔 = 1999 𝑑𝑑𝐴𝐴𝑑𝑑𝑠𝑠

## Slide 140
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝑘𝑘𝑑𝑑𝑔𝑔(𝑓𝑓 = 1999𝑑𝑑𝐴𝐴𝑑𝑑𝑠𝑠) =
1999
12 �
100 − 4(7.2)
7.2 + 20
� + 1999
= 0.985
𝐾𝐾𝑔𝑔ℎ−𝑑𝑑𝑒𝑒𝑔𝑔𝑐𝑐 =
𝜓𝜓𝑠𝑠 �𝑓𝑓𝑒𝑒 , 𝑓𝑓𝑔𝑔� = 1.9(1.04)(0.96)(0.61)(0.985)(1)−0.118 = 1.135
𝜀𝜀𝑠𝑠𝑔𝑔ℎ = (1.04)(0.95)(0.61)(0.223)(0.48 × 10−3) = 0.000064
𝐴𝐴𝑑𝑑𝑠𝑠 = (61 + 4)(0.217𝑠𝑠𝑠𝑠2) = 14.105𝑠𝑠𝑠𝑠2
1
28500𝑘𝑘𝑠𝑠𝑠𝑠 14.105𝑠𝑠𝑠𝑠2
1 + 5530.5𝑘𝑘𝑠𝑠𝑠𝑠 923.531𝑠𝑠𝑠𝑠3 �1 +
923.531𝑠𝑠𝑠𝑠2(27.304𝑠𝑠𝑠𝑠)(31.447𝑠𝑠𝑠𝑠)
734356.0𝑠𝑠𝑠𝑠4
� [1 + 0.7(1.135)]
= 0.773
𝐾𝐾𝑔𝑔ℎ−𝑑𝑑𝑒𝑒𝑐𝑐𝑑𝑑 =
1
28500𝑘𝑘𝑠𝑠𝑠𝑠 14.105𝑠𝑠𝑠𝑠2
923.531𝑠𝑠𝑠𝑠2(27.304𝑠𝑠𝑠𝑠)(−36.343𝑠𝑠𝑠𝑠)
1 + 5530.5𝑘𝑘𝑠𝑠𝑠𝑠 923.531𝑠𝑠𝑠𝑠3 �1 + 734356.0𝑠𝑠𝑠𝑠4
� [1 + 0.7(1.135)]
= 1.04
∆𝑓𝑓𝑑𝑑𝑆𝑆𝑅𝑅𝑆𝑆 (𝑃𝑃𝐴𝐴𝐴𝐴𝑚𝑚𝐴𝐴𝑠𝑠𝐴𝐴𝑠𝑠𝑓𝑓 𝑆𝑆𝑓𝑓𝐴𝐴𝐴𝐴𝑠𝑠𝑑𝑑𝑠𝑠) = (0.000064)(28500𝑘𝑘𝑠𝑠𝑠𝑠)(0.773) = 1.414𝑘𝑘𝑠𝑠𝑠𝑠
∆𝑓𝑓𝑑𝑑𝑆𝑆𝑅𝑅𝑆𝑆 (𝑇𝑇𝐴𝐴𝑚𝑚𝑘𝑘𝑐𝑐𝐴𝐴𝐴𝐴𝐴𝐴𝑑𝑑 𝑆𝑆𝑓𝑓𝐴𝐴𝐴𝐴𝑠𝑠𝑑𝑑𝑠𝑠) = (0.000064)(28500𝑘𝑘𝑠𝑠𝑠𝑠)(1.04) = 1.895𝑘𝑘𝑠𝑠𝑠𝑠
4.5.1.4 Creep of Girder Concrete
𝐸𝐸𝑃𝑃
∆𝑓𝑓 = 𝑓𝑓 𝜓𝜓 (𝑓𝑓 , 𝑓𝑓 )𝐾𝐾
𝑑𝑑𝑝𝑝𝑅𝑅𝑆𝑆 𝐸𝐸𝑐𝑐𝑔𝑔 𝑐𝑐𝑔𝑔𝑑𝑑 𝑠𝑠 ℎ 𝑔𝑔 𝑔𝑔ℎ
𝜓𝜓𝑠𝑠 (𝑓𝑓ℎ, 𝑓𝑓𝑔𝑔) = 1.9(1.04)(0.96)(0.61)(0.223)(1)−0.118 = 0.257
From the elastic shortening loss calculated in 4.4.1.2
𝑓𝑓𝑐𝑐𝑔𝑔𝑑𝑑−𝑑𝑑𝑒𝑒𝑔𝑔𝑐𝑐 = 3.984 𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑐𝑐𝑔𝑔𝑑𝑑−𝑑𝑑𝑒𝑒𝑐𝑐𝑑𝑑 = 1.397 𝑘𝑘𝑠𝑠𝑠𝑠
After multiple iterations in PGSuper
𝑓𝑓𝑐𝑐𝑔𝑔𝑑𝑑−𝑑𝑑𝑒𝑒𝑔𝑔𝑐𝑐 = 3.945 𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑐𝑐𝑔𝑔𝑑𝑑−𝑑𝑑𝑒𝑒𝑐𝑐𝑑𝑑 = 1.402 𝑘𝑘𝑠𝑠𝑠𝑠
28500𝑘𝑘𝑠𝑠𝑠𝑠
𝛥𝛥𝑓𝑓𝑝𝑝𝑅𝑅𝑆𝑆−𝑑𝑑𝑒𝑒𝑔𝑔𝑐𝑐 = 5530.5𝑘𝑘𝑠𝑠𝑠𝑠 (3.945𝑘𝑘𝑠𝑠𝑠𝑠)(0.257)(0.773) = 4.033𝑘𝑘𝑠𝑠𝑠𝑠
28500𝑘𝑘𝑠𝑠𝑠𝑠
𝛥𝛥𝑓𝑓𝑝𝑝𝑅𝑅𝑆𝑆−𝑑𝑑𝑒𝑒𝑐𝑐𝑑𝑑 = 5530.5𝑘𝑘𝑠𝑠𝑠𝑠 (1.402𝑘𝑘𝑠𝑠𝑠𝑠)(0.257)(1.04) = 1.921𝑘𝑘𝑠𝑠𝑠𝑠
4.5.1.5 Relaxation of Prestressing Strands
The girder concrete holds the prestressing strand in tension. The concrete undergoes creep and shrinkage deformations. The strands are between two points that move toward one another. Relaxation occurs at a reduced rate compared to intrinsic relaxation. The relaxation equations given by the AASHTO LRFD BDS are for reduced relaxation.
𝛥𝛥𝑓𝑓𝑑𝑑𝑅𝑅1𝑆𝑆 = �
𝐿𝐿
′
𝑓𝑓𝑑𝑑𝑑𝑑 𝑘𝑘𝑐𝑐𝑔𝑔 (24𝑓𝑓ℎ)
𝐾𝐾 𝑘𝑘𝑐𝑐𝑔𝑔(24𝑓𝑓 ) 𝑓𝑓
𝑔𝑔 𝑑𝑑𝑝𝑝
� − 0.55�� �1 −
𝑓𝑓𝑑𝑑𝑑𝑑 3�𝛥𝛥𝑓𝑓𝑑𝑑𝑆𝑆𝑅𝑅𝑆𝑆 + 𝛥𝛥𝑓𝑓𝑑𝑑𝑝𝑝𝑅𝑅𝑆𝑆 �
𝑓𝑓
𝑑𝑑𝑑𝑑
� 𝐾𝐾𝑔𝑔ℎ
𝐿𝐿
𝐾𝐾′ = 45
𝑓𝑓𝑑𝑑𝑑𝑑 = 𝑓𝑓𝑑𝑑𝑝𝑝 − ∆𝑓𝑓𝑑𝑑𝑅𝑅0 − ∆𝑓𝑓𝑑𝑑𝐸𝐸𝑆𝑆
𝑓𝑓𝑑𝑑𝑑𝑑−𝑑𝑑𝑒𝑒𝑔𝑔𝑐𝑐 = 202.5 𝑘𝑘𝑠𝑠𝑠𝑠 − 1.98𝑘𝑘𝑠𝑠𝑠𝑠 − 20.33𝑘𝑘𝑠𝑠𝑠𝑠 = 180.19𝑘𝑘𝑠𝑠𝑠𝑠

## Slide 141
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝑓𝑓𝑑𝑑𝑑𝑑−𝑑𝑑𝑒𝑒𝑐𝑐𝑑𝑑 = 202.5 𝑘𝑘𝑠𝑠𝑠𝑠 − 1.98𝑘𝑘𝑠𝑠𝑠𝑠 − 7.22𝑘𝑘𝑠𝑠𝑠𝑠 = 193.3𝑘𝑘𝑠𝑠𝑠𝑠
𝛥𝛥𝑓𝑓𝑑𝑑𝑅𝑅1𝑆𝑆−𝑑𝑑𝑒𝑒𝑔𝑔𝑐𝑐 = �
180.19𝑘𝑘𝑠𝑠𝑠𝑠 𝑘𝑘𝑐𝑐𝑔𝑔 (24 ∙ 10) 180.19𝑘𝑘𝑠𝑠𝑠𝑠
�
45 𝑘𝑘𝑐𝑐𝑔𝑔 (24 ∙ 1) 243𝑘𝑘𝑠𝑠𝑠𝑠
− 0.55�� �1−
3(1.414𝑘𝑘𝑠𝑠𝑠𝑠 + 4.098𝑘𝑘𝑠𝑠𝑠𝑠)
180.19𝑘𝑘𝑠𝑠𝑠𝑠
� (0.773) = 0.920 𝑘𝑘𝑠𝑠𝑠𝑠
𝛥𝛥𝑓𝑓𝑑𝑑𝑅𝑅1𝑆𝑆−𝑑𝑑𝑒𝑒𝑐𝑐𝑑𝑑 = �
193.3𝑘𝑘𝑠𝑠𝑠𝑠 𝑘𝑘𝑐𝑐𝑔𝑔 (24 ∙ 10) 193.3𝑘𝑘𝑠𝑠𝑠𝑠
� − 0.55�� �1−
45 𝑘𝑘𝑐𝑐𝑔𝑔 (24 ∙ 1) 243𝑘𝑘𝑠𝑠𝑠𝑠
3(1.895𝑘𝑘𝑠𝑠𝑠𝑠 + 1.921𝑘𝑘𝑠𝑠𝑠𝑠)
193.3𝑘𝑘𝑠𝑠𝑠𝑠
� (1.04) = 1.773 𝑘𝑘𝑠𝑠𝑠𝑠
PGSuper supports all three methods of computing relaxation described in the AASHTO LRFD BDS (LRFD 5.9.3.4.2c, C5.9.3.4.2c)
4.5.1.6 Losses at Shipping
∆𝑓𝑓𝑑𝑑𝑆𝑆 = ∆𝑓𝑓𝑑𝑑𝑅𝑅0 + ∆𝑓𝑓𝑑𝑑𝐸𝐸𝑆𝑆 + ∆𝑓𝑓𝑑𝑑𝐿𝐿𝑝𝑝𝑆𝑆
∆𝑓𝑓𝑑𝑑𝐿𝐿𝑝𝑝𝑆𝑆 = ∆𝑓𝑓𝑑𝑑𝑆𝑆𝑅𝑅𝑆𝑆 + ∆𝑓𝑓𝑑𝑑𝑝𝑝𝑅𝑅𝑆𝑆 + ∆𝑓𝑓𝑑𝑑𝑅𝑅1𝑆𝑆
∆𝑓𝑓𝑑𝑑𝐿𝐿𝑝𝑝𝑆𝑆−𝑑𝑑𝑒𝑒𝑔𝑔𝑐𝑐 = 1.414𝑘𝑘𝑠𝑠𝑠𝑠 + 4.098𝑘𝑘𝑠𝑠𝑠𝑠 + 0.920𝑘𝑘𝑠𝑠𝑠𝑠 = 6.376𝑘𝑘𝑠𝑠𝑠𝑠
∆𝑑𝑑𝑆𝑆−𝑑𝑑𝑒𝑒𝑔𝑔𝑐𝑐 = 1.98𝑘𝑘𝑠𝑠𝑠𝑠 + 20.654𝑘𝑘𝑠𝑠𝑠𝑠 + 6.376𝑘𝑘𝑠𝑠𝑠𝑠 = 28.683𝑘𝑘𝑠𝑠𝑠𝑠
∆𝑓𝑓𝑑𝑑𝐿𝐿𝑝𝑝𝑆𝑆−𝑑𝑑𝑒𝑒𝑐𝑐𝑑𝑑 = 1.895𝑘𝑘𝑠𝑠𝑠𝑠 + 1.921𝑘𝑘𝑠𝑠𝑠𝑠 + 1.773𝑘𝑘𝑠𝑠𝑠𝑠 = 5.589𝑘𝑘𝑠𝑠𝑠𝑠
∆𝑑𝑑𝑆𝑆−𝑑𝑑𝑒𝑒𝑐𝑐𝑑𝑑 = 1.98𝑘𝑘𝑠𝑠𝑠𝑠 + 7.223𝑘𝑘𝑠𝑠𝑠𝑠 + 5.589𝑘𝑘𝑠𝑠𝑠𝑠 = 14.792𝑘𝑘𝑠𝑠𝑠𝑠
4.5.2 Check Girder Stability
Assume bunk points at 13’-8”.
Per WSDOT BDM 5.6.3 the hauling stability design is based on the least stiff haul truck from BDM Table 5.6.3-1 that allows the stress and stability factors of safety to be achieved.
Assume shipping support parameters for 40,000 kip-in/radian rotational spring constant. That equals to the HT40-72 haul truck configuration in PGSuper.

## Slide 142
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Figure 4-6: Equilibrium during Hauling
4.5.2.1 Stability Analysis Parameters
Parameter
Value
Rotational Stiffness
k ∙ in Kθ = 40000 rad
Center-to-center wheel spacing Wcc = 72 in
Height of the roll center above the roadway surface Hrc = 24in
Height of the bottom of the girder above roadway Hbg = 72 in
Bunk placement tolerance ebunk = 1.0 in
Normal Crown Slope
α = 0.02
ft ft
Maximum Superelevation
ft
α = 0.06
ft
Impact for Normal Crown Slope Case IM = ±20%
Impact for Superelevation Case IM = 0%
Modulus of Rupture
𝑐𝑐
𝑓𝑓𝑔𝑔 = 0.24𝜆𝜆�𝑓𝑓′ = (0.24)(1.0)√8.7𝑘𝑘𝑠𝑠𝑠𝑠 = 0.708𝑘𝑘𝑠𝑠𝑠𝑠
      Vertical Location of Center of Gravity
        Camber at Hauling
Assume girder transportation occurs as late as possible to maximum camber grown while in storage. Assume transportation occurs at 90 days.
The camber at hauling is equal to the camber at the end of storage plus the change in dead load deflection due to the different support conditions between storage and hauling.
From before, the prestress deflection measured from the ends of the girder is
∆𝑑𝑑𝑠𝑠= 7.160𝑠𝑠𝑠𝑠

## Slide 143
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Changing the datum to the storage support location
𝛥𝛥𝑑𝑑𝑠𝑠1 = 6.897𝑠𝑠𝑠𝑠 at mid-span
𝛥𝛥𝑑𝑑𝑠𝑠2 = −0.263𝑠𝑠𝑠𝑠 at girder end
ps 1
ps2
ps
Storage datum
Release datum
Figure 4-7: Prestress induced Deflection based on Storage Datum
The dead load deflection at mid-span during storage is
𝐿𝐿𝑠𝑠 = 𝐿𝐿𝑔𝑔 − 2𝐴𝐴 = 162.995𝑓𝑓𝑓𝑓 − 2(1.708𝑓𝑓𝑓𝑓) = 159.578𝑓𝑓𝑓𝑓
The dead load deflection at the girder ends during storage is
𝑔𝑔1
∆ =
𝑤𝑤𝑔𝑔𝐴𝐴
24𝐸𝐸𝑐𝑐𝑔𝑔 𝐼𝐼𝑥𝑥
𝑠𝑠 𝑠𝑠
[3𝐴𝐴2(𝐴𝐴 + 2𝐿𝐿 ) − 𝐿𝐿3 ]
=
(−1.058𝑘𝑘𝑘𝑘𝑓𝑓)(1.708𝑓𝑓𝑓𝑓)
24(5530.5𝑘𝑘𝑠𝑠𝑠𝑠)(734356.0𝑠𝑠𝑠𝑠4)
�3(1.708𝑓𝑓𝑓𝑓)2�1.708𝑓𝑓𝑓𝑓 + 2(159.578𝑓𝑓𝑓𝑓)� − (159.578𝑓𝑓𝑓𝑓)3� �
1728𝑠𝑠𝑠𝑠3
1𝑓𝑓𝑓𝑓3
�
= 0.130 𝑠𝑠𝑠𝑠
At mid span
𝑔𝑔2
∆ =
𝑔𝑔 𝑠𝑠 𝑔𝑔
− 𝑠𝑠 = � − � �
5𝑤𝑤 𝐿𝐿4 𝑤𝑤 𝐴𝐴2𝐿𝐿2 5(−1.058𝑘𝑘𝑘𝑘𝑓𝑓)(159.578𝑓𝑓𝑓𝑓)4 (−1.058𝑘𝑘𝑘𝑘𝑓𝑓)(1.708𝑓𝑓𝑓𝑓)2(159.578𝑓𝑓𝑓𝑓)2 1728𝑠𝑠𝑠𝑠3
16(5530.5𝑘𝑘𝑠𝑠𝑠𝑠)(734356.0𝑠𝑠𝑠𝑠4) 1𝑓𝑓𝑓𝑓3
�
384𝐸𝐸𝑐𝑐𝑔𝑔 𝐼𝐼𝑥𝑥 16𝐸𝐸𝑐𝑐𝑔𝑔 𝐼𝐼𝑥𝑥 384(5530.5𝑘𝑘𝑠𝑠𝑠𝑠)(734356.0𝑠𝑠𝑠𝑠4)
= −3.80𝑠𝑠𝑠𝑠
g1
g2
Figure 4-8: Girder Self-Weight Deflection during Storage
Creep deflection during storage is
∆𝑐𝑐𝑔𝑔𝑒𝑒𝑒𝑒𝑑𝑑 = 𝜓𝜓𝑠𝑠 (𝑓𝑓ℎ, 𝑓𝑓𝑔𝑔 )(𝛥𝛥𝑑𝑑𝑠𝑠 + 𝛥𝛥𝑔𝑔)
89
12 �
100 − 4(7.2)
7.2 + 20
� + 89
𝑘𝑘𝑑𝑑𝑔𝑔(𝑓𝑓 = 89𝑑𝑑𝐴𝐴𝑑𝑑𝑠𝑠) = = 0.738
𝜓𝜓𝑠𝑠 (𝑓𝑓ℎ, 𝑓𝑓𝑔𝑔) = 1.9(1.04)(0.96)(0.61)(0.738)(1)−0.118 = 0.852
At mid-span
𝛥𝛥𝑐𝑐𝑔𝑔𝑒𝑒𝑒𝑒𝑑𝑑 = (0.852)(6.897𝑠𝑠𝑠𝑠 − 3.80𝑠𝑠𝑠𝑠) = 2.639𝑠𝑠𝑠𝑠
At end of girder

## Slide 144
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝛥𝛥𝑐𝑐𝑔𝑔𝑒𝑒𝑒𝑒𝑑𝑑 = (0.852)(−0.263𝑠𝑠𝑠𝑠 + 0. .130𝑠𝑠𝑠𝑠) = −0.113𝑠𝑠𝑠𝑠
Girder deflection in the hauling configuration
𝐿𝐿𝑠𝑠 = 162.995𝑓𝑓𝑓𝑓 − 2(13.67𝑓𝑓𝑓𝑓) = 135.66𝑓𝑓𝑓𝑓
Mid-span deflection
𝑔𝑔
∆ =
𝑔𝑔 𝑠𝑠 − 𝑔𝑔
5𝑤𝑤 𝐿𝐿4 𝑤𝑤 𝐴𝐴2𝐿𝐿2
𝑠𝑠 = � − � �
5(−1.058𝑘𝑘𝑘𝑘𝑓𝑓)(135.66𝑓𝑓𝑓𝑓)4 (−1.058𝑘𝑘𝑘𝑘𝑓𝑓)(13.67𝑓𝑓𝑓𝑓)2(135.66𝑓𝑓𝑓𝑓)2 1728𝑠𝑠𝑠𝑠3
�
384𝐸𝐸𝑐𝑐 𝐼𝐼𝑥𝑥 16𝐸𝐸𝑐𝑐 𝐼𝐼𝑥𝑥 384(5886.891𝑘𝑘𝑠𝑠𝑠𝑠)(734356.0𝑠𝑠𝑠𝑠4) 16(5886.891𝑘𝑘𝑠𝑠𝑠𝑠)(734356.0𝑠𝑠𝑠𝑠4) 1𝑓𝑓𝑓𝑓3
= −1.864𝑠𝑠𝑠𝑠 + 0.091𝑠𝑠𝑠𝑠 = −1.773𝑠𝑠𝑠𝑠
Deflection at girder ends
𝑔𝑔
∆ =
𝑤𝑤𝑔𝑔𝐴𝐴
24𝐸𝐸𝑐𝑐 𝐼𝐼𝑥𝑥
𝑠𝑠 𝑠𝑠
[3𝐴𝐴2(𝐴𝐴 + 2𝐿𝐿 ) − 𝐿𝐿3]
=
(−1.058𝑘𝑘𝑘𝑘𝑓𝑓)(13.67𝑓𝑓𝑓𝑓)
24(5886.891𝑘𝑘𝑠𝑠𝑠𝑠)(734356.0𝑠𝑠𝑠𝑠4)
�3(13.67𝑓𝑓𝑓𝑓)2�13.67𝑓𝑓𝑓𝑓 + 2(135.66𝑓𝑓𝑓𝑓)� − (135.66𝑓𝑓𝑓𝑓)3� �
1728𝑠𝑠𝑠𝑠3
1𝑓𝑓𝑓𝑓3
�
= 0.563 𝑠𝑠𝑠𝑠
We want the total camber measured between the girder ends and mid-span
∆𝑐𝑐𝑠𝑠𝑐𝑐𝑠𝑠𝑒𝑒𝑔𝑔 = �𝛥𝛥𝑔𝑔 + 𝛥𝛥𝑑𝑑𝑠𝑠 + 𝛥𝛥𝑐𝑐𝑔𝑔𝑒𝑒𝑒𝑒𝑑𝑑 � − �𝛥𝛥𝑔𝑔 + 𝛥𝛥𝑑𝑑𝑠𝑠 + 𝛥𝛥𝑐𝑐𝑔𝑔𝑒𝑒𝑒𝑒𝑑𝑑 �
𝑐𝑐𝑔𝑔𝑔𝑔−𝑠𝑠𝑑𝑑𝑠𝑠𝑖𝑖 𝑒𝑒𝑖𝑖𝑔𝑔
= (−1.864𝑠𝑠𝑠𝑠 + 6.897𝑠𝑠𝑠𝑠 + 2.639𝑠𝑠𝑠𝑠) − (0.563𝑠𝑠𝑠𝑠 − 0.263𝑠𝑠𝑠𝑠 − 0.113𝑠𝑠𝑠𝑠) = 7.485𝑠𝑠𝑠𝑠
PGSuper computes ∆𝑐𝑐𝑠𝑠𝑐𝑐𝑠𝑠𝑒𝑒𝑔𝑔 = 7.338 𝑠𝑠𝑠𝑠. Use this value going forward.
4.5.2.2.2 Offset Factor
𝑔𝑔
𝐿𝐿
2
𝐹𝐹 = � 𝑠𝑠 � − = �
1 135.66𝑓𝑓𝑓𝑓
2
1
𝐿𝐿𝑔𝑔 3 162.995𝑓𝑓𝑓𝑓 3
� − = 0.359
        Location of roll axis below top of girder
𝑑𝑑𝑔𝑔𝑐𝑐 = 𝐻𝐻𝑠𝑠𝑔𝑔 + 𝐻𝐻𝑔𝑔 − 𝐻𝐻𝑔𝑔𝑐𝑐 = 72.0𝑠𝑠𝑠𝑠 + 74.0𝑠𝑠𝑠𝑠 − 24.0𝑠𝑠𝑠𝑠 = 122.0𝑠𝑠𝑠𝑠
        Location of center of gravity above roll axis
𝑑𝑑𝑔𝑔 = 𝑑𝑑𝑔𝑔𝑐𝑐 − 𝑌𝑌𝑑𝑑𝑔𝑔𝑑𝑑 + 𝐹𝐹𝑔𝑔(∆𝑐𝑐𝑠𝑠𝑐𝑐𝑠𝑠𝑒𝑒𝑔𝑔 ) = 122.0𝑠𝑠𝑠𝑠 − 38.343𝑠𝑠𝑠𝑠 + 0.359(7.338𝑠𝑠𝑠𝑠) = 86.295𝑠𝑠𝑠𝑠
      Lateral Deflection Parameters
        Lateral Sweep
Sweep tolerance = 1/8” per 10 ft
𝛥𝛥𝑠𝑠𝑤𝑤𝑒𝑒𝑒𝑒𝑑𝑑 = �
10𝑓𝑓𝑓𝑓
162.995𝑓𝑓𝑓𝑓 1
� � 𝑠𝑠𝑠𝑠� = 2.037𝑠𝑠𝑠𝑠 8
        Initial Lateral Eccentricity
Initial lateral eccentricity of center of gravity of girder due to lateral sweep and eccentricity of bunking devices from CL girder
𝐴𝐴𝑔𝑔 = 𝐹𝐹𝑔𝑔𝛥𝛥𝑠𝑠𝑤𝑤𝑒𝑒𝑒𝑒𝑑𝑑 + 𝐴𝐴𝑠𝑠𝑎𝑎𝑖𝑖𝑑𝑑 = (0.359)(2.037𝑠𝑠𝑠𝑠) + 1.000𝑠𝑠𝑠𝑠 = 1.732𝑠𝑠𝑠𝑠
        Lateral Deflection of CG
Lateral deflection of center of gravity due to total weight of girder applied to the weak axis
𝑔𝑔
𝑧𝑧 =
𝐻𝐻𝑔𝑔
𝑐𝑐 𝑝𝑝 𝑔𝑔
𝐿𝐿5
12𝐸𝐸 𝐼𝐼 𝐿𝐿2 10
𝑠𝑠 𝑠𝑠
6
5
� 𝑠𝑠 − 𝐴𝐴2𝐿𝐿3 + 3𝐴𝐴4𝐿𝐿 + 𝐴𝐴5�

## Slide 145
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝑧𝑧𝑔𝑔 =
172.48𝑘𝑘𝑠𝑠𝑘𝑘
12(5886.891𝑘𝑘𝑠𝑠𝑠𝑠)(72018.4𝑠𝑠𝑠𝑠4)(162.995𝑓𝑓𝑓𝑓)2
�
(135.66𝑓𝑓𝑓𝑓)5
10
− (13.67𝑓𝑓𝑓𝑓)2(135.66𝑓𝑓𝑓𝑓)3 + 3(13.67𝑓𝑓𝑓𝑓)4(135.66𝑓𝑓𝑓𝑓)
+ (13.67𝑓𝑓𝑓𝑓)5� �
6 1728𝑠𝑠𝑠𝑠3
5 1𝑓𝑓𝑓𝑓3
� = 9.137𝑠𝑠𝑠𝑠
Impact up
𝑧𝑧𝑔𝑔 = (0.8)(9.137𝑠𝑠𝑠𝑠) = 7.309𝑠𝑠𝑠𝑠
Impact down
𝑧𝑧𝑔𝑔 = (1.2)(9.137𝑠𝑠𝑠𝑠) = 10.964𝑠𝑠𝑠𝑠
4.5.2.3.4 Girder Stresses at Harping Point
𝑓𝑓𝑑𝑑 =
4.5.2.3.4.1 Stress due to prestressing
−(1655.95𝑘𝑘𝑠𝑠𝑘𝑘 + 640.23𝑘𝑘𝑠𝑠𝑘𝑘 + 163.38𝑘𝑘𝑠𝑠𝑘𝑘)
+
923.531𝑠𝑠𝑠𝑠2
(−1655.95𝑘𝑘𝑠𝑠𝑘𝑘)(31.748𝑠𝑠𝑠𝑠) + (−640.23𝑘𝑘𝑠𝑠𝑘𝑘)(30.775𝑠𝑠𝑠𝑠) + (−163.38𝑘𝑘𝑠𝑠𝑘𝑘)(−36.343𝑠𝑠𝑠𝑠)
−19152.5𝑠𝑠𝑠𝑠3
= 0.800𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 =
−(1655.95𝑘𝑘𝑠𝑠𝑘𝑘 + 640.23𝑘𝑘𝑠𝑠𝑘𝑘 + 163.38𝑘𝑘𝑠𝑠𝑘𝑘)
+
923.531𝑠𝑠𝑠𝑠2
(−1655.95𝑘𝑘𝑠𝑠𝑘𝑘)(31.748𝑠𝑠𝑠𝑠) + (−640.23𝑘𝑘𝑠𝑠𝑘𝑘)(30.775𝑠𝑠𝑠𝑠) + (−163.38𝑘𝑘𝑠𝑠𝑘𝑘)(−36.343𝑠𝑠𝑠𝑠)
20594.85𝑠𝑠𝑠𝑠3
= −5.883𝑘𝑘𝑠𝑠𝑠𝑠
4.5.2.3.4.2 Stress due to girder self-weight (without impact)
𝑤𝑤
𝑔𝑔
2
𝑔𝑔 𝑠𝑠
2 2
𝑀𝑀 = (𝐿𝐿 𝑤𝑤 − 𝑤𝑤 − 𝐴𝐴 )
𝑤𝑤 = 0.4𝐿𝐿𝑔𝑔 − 𝐴𝐴 = 0.4(162.995𝑓𝑓𝑓𝑓) − 13.67𝑓𝑓𝑓𝑓 = 54.265𝑓𝑓𝑓𝑓
𝑔𝑔
2
1.058𝑘𝑘𝑘𝑘𝑓𝑓
𝑀𝑀 = �(135.66𝑓𝑓𝑓𝑓)(54.265𝑓𝑓𝑓𝑓) − (54.265𝑓𝑓𝑓𝑓)2 − (13.67𝑓𝑓𝑓𝑓)2� = 2195.02𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
2195.02𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 12𝑠𝑠𝑠𝑠
𝑓𝑓𝑑𝑑 = −19152.5𝑠𝑠𝑠𝑠3 � 1𝑓𝑓𝑓𝑓 � = −1.375𝑘𝑘𝑠𝑠𝑠𝑠
2195.02𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 12𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 = 20594.85𝑠𝑠𝑠𝑠3 � 1𝑓𝑓𝑓𝑓 � = 1.279𝑘𝑘𝑠𝑠𝑠𝑠
      Analyze normal crown slope, no impact case
        Equilibrium tilt angle
𝑒𝑒𝑒𝑒
𝜃𝜃 =
�𝐾𝐾𝜃𝜃 𝛼𝛼 + (𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔𝐴𝐴𝑔𝑔 �
=
𝑔𝑔𝑠𝑠𝑔𝑔
𝑓𝑓𝑓𝑓
��40000𝑑𝑑∙𝑔𝑔𝑖𝑖� �0.02 𝑓𝑓𝑓𝑓� + (1.0)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)(1.732𝑠𝑠𝑠𝑠)�
𝑑𝑑∙𝑔𝑔𝑖𝑖
𝑔𝑔𝑠𝑠𝑔𝑔
𝐾𝐾𝜃𝜃 − (𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔(𝑑𝑑𝑔𝑔 + 𝑧𝑧𝑔𝑔) �40000 � − (1.0)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)(86.295𝑠𝑠𝑠𝑠 + 9.137𝑠𝑠𝑠𝑠)
= 0.04668 𝐴𝐴𝐴𝐴𝑑𝑑
4.5.2.4.2 Stress due to lateral loading from tilt
Top left flange tip
𝑓𝑓𝑑𝑑𝑠𝑠 =
2𝐼𝐼
𝑝𝑝
=
(2)(72018.4𝑠𝑠𝑠𝑠4)
(𝐼𝐼𝑀𝑀)�𝑀𝑀𝑔𝑔�𝜃𝜃𝑒𝑒𝑒𝑒 𝐻𝐻𝑑𝑑𝑔𝑔𝑑𝑑 (1.0)(2195.02𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(0.04668)(49𝑠𝑠𝑠𝑠) 12𝑠𝑠𝑠𝑠
� � = 0.418 𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
Bottom right flange tip

## Slide 146
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
(𝐼𝐼𝑀𝑀)�𝑀𝑀𝑔𝑔�𝜃𝜃𝑒𝑒𝑒𝑒 𝐻𝐻𝑠𝑠𝑔𝑔𝑑𝑑
𝑝𝑝
𝑓𝑓𝑠𝑠𝑔𝑔 = − = −
2𝐼𝐼 (2)(72018.4𝑠𝑠𝑠𝑠4)
(1.0)(2195.02𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(0.04668)(38.375𝑠𝑠𝑠𝑠) 12𝑠𝑠𝑠𝑠
� � = −0.328 𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
4.5.2.4.3 Factor of Safety against Cracking
Lateral cracking moment
𝑓𝑓𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑐𝑐𝑑𝑑 = 𝑓𝑓𝑑𝑑𝑠𝑠 + (𝐼𝐼𝑀𝑀)𝑓𝑓𝑔𝑔 = 0.800𝑘𝑘𝑠𝑠𝑠𝑠 + (1.0)(−1.375𝑘𝑘𝑠𝑠𝑠𝑠) = −0.575𝑘𝑘𝑠𝑠𝑠𝑠
𝑀𝑀𝑐𝑐𝑔𝑔 =
(𝑓𝑓𝑔𝑔 − 𝑓𝑓𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑐𝑐𝑑𝑑 )2𝐼𝐼𝑝𝑝
𝐻𝐻
𝑑𝑑𝑔𝑔𝑑𝑑
=
�0.708𝑘𝑘𝑠𝑠𝑠𝑠 − (−0.575𝑘𝑘𝑠𝑠𝑠𝑠)�(2)(72018.4𝑠𝑠𝑠𝑠4) 1𝑓𝑓𝑓𝑓
49𝑠𝑠𝑠𝑠 12𝑠𝑠𝑠𝑠
� � = 314.26𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
Tilt angle at first crack
𝑐𝑐𝑔𝑔
𝜃𝜃 =
𝑀𝑀𝑐𝑐𝑔𝑔
(𝐼𝐼𝑀𝑀)𝑀𝑀
𝑔𝑔
≤ 0.4
314.26 𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝜃𝜃𝑐𝑐𝑔𝑔 = (1.0)(2195.02 𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) = 0.14323 𝐴𝐴𝐴𝐴𝑑𝑑
Factor of Safety against Cracking
𝑐𝑐𝑔𝑔
𝐹𝐹𝑆𝑆 =
𝐾𝐾𝜃𝜃 (𝜃𝜃𝑐𝑐𝑔𝑔 − 𝛼𝛼)
(𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔[((𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔 + 𝑑𝑑𝑔𝑔 )𝜃𝜃𝑐𝑐𝑔𝑔 + 𝐴𝐴𝑔𝑔 ]
𝑔𝑔𝑠𝑠𝑔𝑔
𝑓𝑓𝑓𝑓
��40000 𝑑𝑑∙𝑔𝑔𝑖𝑖� �0.14323 𝐴𝐴𝐴𝐴𝑑𝑑 − 0.02 𝑓𝑓𝑓𝑓��
𝐹𝐹𝑆𝑆𝑐𝑐𝑔𝑔 = (1.0)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)[((1.0)9.137𝑠𝑠𝑠𝑠 + 86.295𝑠𝑠𝑠𝑠)(0.14323𝐴𝐴𝐴𝐴𝑑𝑑) + 1.732𝑠𝑠𝑠𝑠] = 1.86
𝐹𝐹𝑆𝑆𝑐𝑐𝑔𝑔 > 1.0 OK
4.5.2.4.4 Factor of Safety against Failure
𝑐𝑐𝑠𝑠𝑥𝑥
2.5(𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔
𝐴𝐴𝑔𝑔 + �(𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔 + 𝑑𝑑𝑔𝑔 �𝛼𝛼
𝜃𝜃 = 𝛼𝛼 + �𝛼𝛼2 + ≤ 0.4 𝐴𝐴𝐴𝐴𝑑𝑑
�
𝑓𝑓𝑓𝑓 𝑓𝑓𝑓𝑓 2
𝜃𝜃𝑐𝑐𝑠𝑠𝑥𝑥 = 0.02 𝑓𝑓𝑓𝑓 + �0.02 𝑓𝑓𝑓𝑓� +
𝑓𝑓𝑓𝑓
1.732𝑠𝑠𝑠𝑠 + �(1.0)(9.137𝑠𝑠𝑠𝑠) + (86.295𝑠𝑠𝑠𝑠)� �0.02 𝑓𝑓𝑓𝑓�
2.5(1.0)(9.137𝑠𝑠𝑠𝑠)
= 0.399 𝐴𝐴𝐴𝐴𝑑𝑑
𝑒𝑒
𝐹𝐹𝑆𝑆 =
𝐾𝐾𝜃𝜃 (𝜃𝜃𝑐𝑐𝑠𝑠𝑥𝑥 − 𝛼𝛼)
(𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔[(𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔 𝜃𝜃𝑐𝑐𝑠𝑠𝑥𝑥 (1 + 2.5𝜃𝜃
𝑐𝑐𝑠𝑠𝑥𝑥 𝑔𝑔 𝑐𝑐𝑠𝑠𝑥𝑥 𝑔𝑔
) + 𝑑𝑑 𝜃𝜃 + 𝐴𝐴 ]
𝑔𝑔𝑠𝑠𝑔𝑔
𝑓𝑓𝑓𝑓
�40000 𝑑𝑑∙𝑔𝑔𝑖𝑖� �0.399 − 0.02 𝑓𝑓𝑓𝑓�
𝐹𝐹𝑆𝑆𝑒𝑒 = (1.0)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)[(1.0)(9.137𝑠𝑠𝑠𝑠)(0.399)�1 + 2.5(0.4)� + (86.295𝑠𝑠𝑠𝑠)(0.4) + 1.732𝑠𝑠𝑠𝑠 = 2.023
If 𝐹𝐹𝑆𝑆𝑒𝑒 < 𝐹𝐹𝑆𝑆𝑐𝑐𝑔𝑔 , 𝐹𝐹𝑆𝑆𝑒𝑒 = 𝐹𝐹𝑆𝑆𝑐𝑐𝑔𝑔
𝐹𝐹𝑆𝑆𝑒𝑒 = 2.023
𝐹𝐹𝑆𝑆𝑒𝑒 > 1.5 OK
4.5.2.4.5 Factor of Safety against Rollover
𝑔𝑔𝑔𝑔
𝜃𝜃 =
𝑔𝑔
𝐻𝐻
𝑐𝑐𝑐𝑐
2
(𝐼𝐼𝑀𝑀)𝐻𝐻 � − 𝐻𝐻 𝛼𝛼 − 𝐴𝐴
𝑔𝑔𝑐𝑐 𝑠𝑠𝑎𝑎𝑖𝑖𝑑𝑑
�
𝐾𝐾𝜃𝜃
+ 𝛼𝛼

## Slide 147
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
(1.0)(172.48𝑘𝑘𝑠𝑠𝑘𝑘) �72𝑠𝑠𝑠𝑠 − (24𝑠𝑠𝑠𝑠)(0.02) − 1.0𝑠𝑠𝑠𝑠�
𝑔𝑔𝑠𝑠𝑔𝑔
�40000 𝑑𝑑∙𝑔𝑔𝑖𝑖�
𝜃𝜃𝑔𝑔𝑔𝑔 = 2 + 0.02 = 0.17316 𝐴𝐴𝐴𝐴𝑑𝑑
𝑔𝑔
𝐹𝐹𝑆𝑆 =
𝐾𝐾𝜃𝜃 (𝜃𝜃𝑔𝑔𝑔𝑔 − 𝛼𝛼)
(𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔[((𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔(1 + 2.5𝜃𝜃𝑔𝑔𝑔𝑔) + 𝑑𝑑𝑔𝑔 )𝜃𝜃𝑔𝑔𝑔𝑔 + 𝐴𝐴𝑔𝑔]
�40000 𝑑𝑑∙𝑔𝑔𝑖𝑖�(0.17316 − 0.02)
𝐹𝐹𝑆𝑆𝑔𝑔 = 𝑔𝑔𝑠𝑠𝑔 𝑔 = 1.875
(1.0)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)��(1.0)(9.137𝑠𝑠𝑠𝑠)�1 + 2.5(0.17316)� + 86.295𝑠𝑠𝑠𝑠�(0.17316) + 1.732𝑠𝑠𝑠𝑠�
𝐹𝐹𝑆𝑆𝑔𝑔 > 1.5 OK
4.5.2.5 Analyze normal crown slope, impact up
4.5.2.5.1.1 Equilibrium tilt angle
𝑒𝑒𝑒𝑒
𝜃𝜃 =
�𝐾𝐾𝜃𝜃 𝛼𝛼 + (𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔𝐴𝐴𝑔𝑔�
=
𝑔𝑔𝑠𝑠𝑔𝑔
𝑓𝑓𝑓𝑓
��40000𝑑𝑑∙𝑔𝑔𝑖𝑖� �0.02 𝑓𝑓𝑓𝑓� + (0.8)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)(1.732𝑠𝑠𝑠𝑠)�
𝑑𝑑∙𝑔𝑔𝑖𝑖
𝑔𝑔𝑠𝑠𝑔𝑔
𝐾𝐾𝜃𝜃 − (𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔(𝑑𝑑𝑔𝑔 + 𝑧𝑧𝑔𝑔 ) �40000 � − (0.8)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)(86.295𝑠𝑠𝑠𝑠 + (0.8)(9.137𝑠𝑠𝑠𝑠))
= 0.03836 𝐴𝐴𝐴𝐴𝑑𝑑
4.5.2.5.1.2 Stress due to lateral loading from tilt
Top left flange tip
𝑓𝑓𝑑𝑑𝑠𝑠 =
2𝐼𝐼
𝑝𝑝
=
(2)(72018.4𝑠𝑠𝑠𝑠4)
(𝐼𝐼𝑀𝑀)�𝑀𝑀𝑔𝑔�𝜃𝜃𝑒𝑒𝑒𝑒 𝐻𝐻𝑑𝑑𝑔𝑔𝑑𝑑 (0.8)(2195.02𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(0.03836)(49𝑠𝑠𝑠𝑠) 12𝑠𝑠𝑠𝑠
� � = 0.275 𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
Bottom right flange tip
𝑓𝑓𝑠𝑠𝑔𝑔 = −
(𝐼𝐼𝑀𝑀)�𝑀𝑀𝑔𝑔�𝜃𝜃𝑒𝑒𝑒𝑒 𝐻𝐻𝑠𝑠𝑔𝑔𝑑𝑑
2𝐼𝐼
𝑝𝑝
= −
(2)(72018.4𝑠𝑠𝑠𝑠4)
(0.8)(2195.02𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(0.03836)(38.375𝑠𝑠𝑠𝑠) 12𝑠𝑠𝑠𝑠
� � = −0.215 𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
𝑀𝑀𝑐𝑐𝑔𝑔 =
(𝑓𝑓𝑔𝑔 − 𝑓𝑓𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑐𝑐𝑑𝑑 )2𝐼𝐼𝑝𝑝
𝐻𝐻
𝑑𝑑𝑔𝑔𝑑𝑑
49𝑠𝑠𝑠𝑠
4.5.2.5.2 Factor of Safety against Cracking
Cracking moment
𝑓𝑓𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑐𝑐𝑑𝑑 = 𝑓𝑓𝑑𝑑𝑠𝑠 + (𝐼𝐼𝑀𝑀)𝑓𝑓𝑔𝑔 = 0.800𝑘𝑘𝑠𝑠𝑠𝑠 + (0.8)(−1.375𝑘𝑘𝑠𝑠𝑠𝑠) = −0.300𝑘𝑘𝑠𝑠𝑠𝑠
�0.708𝑘𝑘𝑠𝑠𝑠𝑠 − (−0.300𝑠𝑠𝑠𝑠)�(2)(72018.4𝑠𝑠𝑠𝑠4) 1𝑓𝑓𝑓𝑓
12𝑠𝑠𝑠𝑠
= � � = 246.88𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
Tilt angle at first crack
𝑐𝑐𝑔𝑔
𝜃𝜃 =
𝑀𝑀𝑐𝑐𝑔𝑔
(𝐼𝐼𝑀𝑀)𝑀𝑀
𝑔𝑔
≤ 0.4
246.88 𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝜃𝜃𝑐𝑐𝑔𝑔 = (0.8)2195.02 𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 = 0.14059 𝐴𝐴𝐴𝐴𝑑𝑑
Factor of Safety against Cracking
𝑐𝑐𝑔𝑔
𝐹𝐹𝑆𝑆 =
𝐾𝐾𝜃𝜃 (𝜃𝜃𝑐𝑐𝑔𝑔 − 𝛼𝛼)
(𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔[((𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔 + 𝑑𝑑𝑔𝑔 )𝜃𝜃𝑐𝑐𝑔𝑔 + 𝐴𝐴𝑔𝑔 ]
𝑔𝑔𝑠𝑠𝑔𝑔
𝑓𝑓𝑓𝑓
��40000 𝑑𝑑∙𝑔𝑔𝑖𝑖� �0.14059 𝐴𝐴𝐴𝐴𝑑𝑑 − 0.02 𝑓𝑓𝑓𝑓��
𝐹𝐹𝑆𝑆𝑐𝑐𝑔𝑔 = (0.8)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)[((0.8)(9.137𝑠𝑠𝑠𝑠) + 86.295𝑠𝑠𝑠𝑠)(0.14059𝐴𝐴𝐴𝐴𝑑𝑑) + 1.732𝑠𝑠𝑠𝑠] = 2.35
𝐹𝐹𝑆𝑆𝑐𝑐𝑔𝑔 > 1.0 OK

## Slide 148
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
4.5.2.5.3 Factor of Safety against Failure
𝑐𝑐𝑠𝑠𝑥𝑥
2.5𝑧𝑧𝑔𝑔
𝐴𝐴𝑔𝑔 + �(𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔 + 𝑑𝑑𝑔𝑔 �𝛼𝛼
𝜃𝜃 = 𝛼𝛼 + �𝛼𝛼2 + ≤ 0.4 𝐴𝐴𝐴𝐴𝑑𝑑
𝑓𝑓𝑓𝑓 𝑓𝑓𝑓𝑓 2
𝜃𝜃′𝑐𝑐𝑠𝑠𝑥𝑥 = 0.02 𝑓𝑓𝑓𝑓 + ��0.02 𝑓𝑓𝑓𝑓� +
1.732𝑠𝑠𝑠𝑠 + �(0.8)(9.137𝑠𝑠𝑠𝑠) + 86.295𝑠𝑠𝑠𝑠�0.02
2.5(0.8)(9.317𝑠𝑠𝑠𝑠)
= 0.46024 𝐴𝐴𝐴𝐴𝑑𝑑 ∴ 0.4 𝐴𝐴𝐴𝐴𝑑𝑑
𝑒𝑒
𝐹𝐹𝑆𝑆 =
𝐾𝐾𝜃𝜃 (𝜃𝜃′𝑐𝑐𝑠𝑠𝑥𝑥 − 𝛼𝛼)
𝑔𝑔
(𝐼𝐼𝑀𝑀)𝐻𝐻[(𝐼𝐼𝑀𝑀)𝑧𝑧 𝜃𝜃′
𝑔𝑔 𝑐𝑐𝑠𝑠𝑥𝑥 𝑐𝑐𝑠𝑠𝑥𝑥 𝑔𝑔 𝑐𝑐𝑠𝑠𝑥𝑥 𝑔𝑔
(1 + 2.5𝜃𝜃′ ) + 𝑑𝑑 𝜃𝜃′ + 𝐴𝐴 ]
𝑔𝑔𝑠𝑠𝑔𝑔
𝑓𝑓𝑓𝑓
�40000 𝑑𝑑∙𝑖𝑖 � �0.4 − 0.02 𝑓𝑓𝑓𝑓�
𝐹𝐹𝑆𝑆𝑒𝑒 = (0.8)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)[(0.8)(9.317𝑠𝑠𝑠𝑠)(0.4)�1 + 2.5(0.4)� + (86.295𝑠𝑠𝑠𝑠)(0.4) + 1.732𝑠𝑠𝑠𝑠 = 2.617
𝐹𝐹𝑆𝑆𝑒𝑒 > 1.5 OK
4.5.2.5.4 Factor of Safety against Rollover
𝑔𝑔𝑔𝑔
𝜃𝜃 =
𝑔𝑔
𝐻𝐻
𝑐𝑐𝑐𝑐
2
𝑔𝑔𝑐𝑐
(𝐼𝐼𝑀𝑀)𝐻𝐻 � − 𝐻𝐻 𝛼𝛼�
𝐾𝐾𝜃𝜃
+ 𝛼𝛼
𝜃𝜃𝑔𝑔𝑔𝑔 =
2
(0.8)(172.48𝑘𝑘𝑠𝑠𝑘𝑘) �72𝑠𝑠𝑠𝑠 − (24𝑠𝑠𝑠𝑠)(0.02)�
𝑔𝑔𝑠𝑠𝑔𝑔
�40000 𝑑𝑑−𝑔𝑔𝑖𝑖�
+ 0.02 = 0.14253 𝐴𝐴𝐴𝐴𝑑𝑑
𝑔𝑔
𝐹𝐹𝑆𝑆 =
𝐾𝐾𝜃𝜃 (𝜃𝜃𝑔𝑔𝑔𝑔 − 𝛼𝛼)
(𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔[((𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔(1 + 2.5𝜃𝜃𝑔𝑔𝑔𝑔) + 𝑑𝑑𝑔𝑔 )𝜃𝜃𝑔𝑔𝑔𝑔 + 𝐴𝐴𝑔𝑔]
�40000 𝑑𝑑∙𝑔𝑔𝑖𝑖�(0.14253 − 0.02)
𝐹𝐹𝑆𝑆𝑔𝑔 = 𝑔𝑔𝑠𝑠𝑔 𝑔 = 2.30
(0.8)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)��(0.8)(9.317𝑠𝑠𝑠𝑠)�1 + 2.5(0.14253)� + 86.295𝑠𝑠𝑠𝑠�(0.14253) + 1.732𝑠𝑠𝑠𝑠�
𝐹𝐹𝑆𝑆𝑔𝑔 > 1.5 OK
4.5.2.6 Analyze normal crown slope, impact down
4.5.2.6.1.1 Equilibrium tilt angle
𝑒𝑒𝑒𝑒
𝜃𝜃 =
�𝐾𝐾𝜃𝜃 𝛼𝛼 + (𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔𝐴𝐴𝑔𝑔�
=
𝑔𝑔𝑠𝑠𝑔𝑔
𝑓𝑓𝑓𝑓
��40000𝑑𝑑∙𝑔𝑔𝑖𝑖� �0.02 𝑓𝑓𝑓𝑓� + (1.2)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)(1.732𝑠𝑠𝑠𝑠)�
𝑑𝑑∙𝑔𝑔𝑖𝑖
𝑔𝑔𝑠𝑠𝑔𝑔
𝐾𝐾𝜃𝜃 − (𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔(𝑑𝑑𝑔𝑔 + 𝑧𝑧𝑔𝑔 ) �40000 � − (1.2)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)(86.295𝑠𝑠𝑠𝑠 + (1.2)(9.137𝑠𝑠𝑠𝑠))
= 0.05831 𝐴𝐴𝐴𝐴𝑑𝑑
4.5.2.6.1.2 Stress due to lateral loading from tilt
Top left flange tip
𝑓𝑓𝑑𝑑𝑠𝑠 =
2𝐼𝐼
𝑝𝑝
=
(2)(72018.4𝑠𝑠𝑠𝑠4)
(𝐼𝐼𝑀𝑀)�𝑀𝑀𝑔𝑔�𝜃𝜃𝑒𝑒𝑒𝑒 𝐻𝐻𝑑𝑑𝑔𝑔𝑑𝑑 (1.2)(2195.02𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(0.05831)(49𝑠𝑠𝑠𝑠) 12𝑠𝑠𝑠𝑠
� � = 0.627 𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
Bottom right flange tip
𝑓𝑓𝑠𝑠𝑔𝑔 = −
(𝐼𝐼𝑀𝑀)�𝑀𝑀𝑔𝑔�𝜃𝜃𝑒𝑒𝑒𝑒 𝐻𝐻𝑠𝑠𝑔𝑔𝑑𝑑
2𝐼𝐼
𝑝𝑝
= −
(2)(72018.4𝑠𝑠𝑠𝑠4)
(1.2)(2195.02𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(0.05831)(38.375𝑠𝑠𝑠𝑠) 12𝑠𝑠𝑠𝑠
� � = −0.491 𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
4.5.2.6.2 Factor of Safety against Cracking

## Slide 149
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Cracking moment
𝑓𝑓𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑐𝑐𝑑𝑑 = 𝑓𝑓𝑑𝑑𝑠𝑠 + (𝐼𝐼𝑀𝑀)𝑓𝑓𝑔𝑔 = 0.800𝑘𝑘𝑠𝑠𝑠𝑠 + (1.2)(−1.375𝑘𝑘𝑠𝑠𝑠𝑠) = −0.850𝑘𝑘𝑠𝑠𝑠𝑠
𝑀𝑀𝑐𝑐𝑔𝑔 =
(𝑓𝑓𝑔𝑔 − 𝑓𝑓𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑐𝑐𝑑𝑑 )2𝐼𝐼𝑝𝑝
𝐻𝐻
𝑑𝑑𝑔𝑔𝑑𝑑
=
�0.708𝑘𝑘𝑠𝑠𝑠𝑠 − (−0.850𝑠𝑠𝑠𝑠)�(2)(72018.4𝑠𝑠𝑠𝑠4) 1𝑓𝑓𝑓𝑓
49𝑠𝑠𝑠𝑠 12𝑠𝑠𝑠𝑠
� � = 381.64𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
Tilt angle at first crack
𝑐𝑐𝑔𝑔
𝜃𝜃 =
𝑀𝑀𝑐𝑐𝑔𝑔
(𝐼𝐼𝑀𝑀)𝑀𝑀
𝑔𝑔
≤ 0.4
381.64 𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝜃𝜃𝑐𝑐𝑔𝑔 = (1.2)2195.02 𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 = 0.14489 𝐴𝐴𝐴𝐴𝑑𝑑
Factor of Safety against Cracking
𝑐𝑐𝑔𝑔
𝐹𝐹𝑆𝑆 =
𝐾𝐾𝜃𝜃 (𝜃𝜃𝑐𝑐𝑔𝑔 − 𝛼𝛼)
(𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔[((𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔 + 𝑑𝑑𝑔𝑔 )𝜃𝜃𝑐𝑐𝑔𝑔 + 𝐴𝐴𝑔𝑔 ]
𝑔𝑔𝑠𝑠𝑔𝑔
𝑓𝑓𝑓𝑓
��40000 𝑑𝑑∙𝑔𝑔𝑖𝑖� �0.14489 𝐴𝐴𝐴𝐴𝑑𝑑 − 0.02 𝑓𝑓𝑓𝑓��
𝐹𝐹𝑆𝑆𝑐𝑐𝑔𝑔 = (1.2)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)[((1.2)(9.137𝑠𝑠𝑠𝑠) + 86.295𝑠𝑠𝑠𝑠)(0.14489𝐴𝐴𝐴𝐴𝑑𝑑) + 1.732𝑠𝑠𝑠𝑠] = 1.53
𝐹𝐹𝑆𝑆𝑐𝑐𝑔𝑔 > 1.0 OK
4.5.2.6.3 Factor of Safety against Failure
𝑐𝑐𝑠𝑠𝑥𝑥
2.5𝑧𝑧𝑔𝑔
𝐴𝐴𝑔𝑔 + �(𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔 + 𝑑𝑑𝑔𝑔 �𝛼𝛼
𝜃𝜃 = 𝛼𝛼 + �𝛼𝛼2 + ≤ 0.4 𝐴𝐴𝐴𝐴𝑑𝑑
𝑓𝑓𝑓𝑓 𝑓𝑓𝑓𝑓 2
𝜃𝜃′𝑐𝑐𝑠𝑠𝑥𝑥 = 0.02 𝑓𝑓𝑓𝑓 + ��0.02 𝑓𝑓𝑓𝑓� +
1.732𝑠𝑠𝑠𝑠 + �(1.2)(9.137𝑠𝑠𝑠𝑠) + 86.295𝑠𝑠𝑠𝑠�0.02
2.5(1.2)(9.317𝑠𝑠𝑠𝑠)
= 0.38683 𝐴𝐴𝐴𝐴𝑑𝑑
𝑒𝑒
𝐹𝐹𝑆𝑆 =
𝐾𝐾𝜃𝜃 (𝜃𝜃′𝑐𝑐𝑠𝑠𝑥𝑥 − 𝛼𝛼)
(𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔[(𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔𝜃𝜃′𝑐𝑐𝑠𝑠𝑥𝑥 (1 + 2.5𝜃𝜃′
𝑐𝑐𝑠𝑠𝑥𝑥 𝑔𝑔 𝑐𝑐𝑠𝑠𝑥𝑥 𝑔𝑔
) + 𝑑𝑑 𝜃𝜃′ + 𝐴𝐴 ]
𝑔𝑔𝑠𝑠𝑔𝑔
𝑓𝑓𝑓𝑓
�40000 𝑑𝑑∙𝑖𝑖 � �0.38683 − 0.02 𝑓𝑓𝑓𝑓�
𝐹𝐹𝑆𝑆𝑒𝑒 = (1.2)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)[(1.2)(9.317𝑠𝑠𝑠𝑠)(0.38683)�1 + 2.5(0.38683)� + (86.295𝑠𝑠𝑠𝑠)(0.38683) + 1.732𝑠𝑠𝑠𝑠 = 1.631
𝐹𝐹𝑆𝑆𝑒𝑒 > 1.5 OK
4.5.2.6.4 Factor of Safety against Rollover
𝑔𝑔𝑔𝑔
𝜃𝜃 =
𝑔𝑔
𝐻𝐻
𝑐𝑐𝑐𝑐
2
𝑔𝑔𝑐𝑐
(𝐼𝐼𝑀𝑀)𝐻𝐻 � − 𝐻𝐻 𝛼𝛼�
𝐾𝐾𝜃𝜃
+ 𝛼𝛼
𝜃𝜃𝑔𝑔𝑔𝑔 =
2
(1.2)(172.48𝑘𝑘𝑠𝑠𝑘𝑘) �72𝑠𝑠𝑠𝑠 − (24𝑠𝑠𝑠𝑠)(0.02)�
𝑔𝑔𝑠𝑠𝑔𝑔
�40000 𝑑𝑑−𝑔𝑔𝑖𝑖�
+ 0.02 = 0.20380 𝐴𝐴𝐴𝐴𝑑𝑑
𝑔𝑔
𝐹𝐹𝑆𝑆 =
𝐾𝐾𝜃𝜃 (𝜃𝜃𝑔𝑔𝑔𝑔 − 𝛼𝛼)
(𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔[((𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔(1 + 2.5𝜃𝜃𝑔𝑔𝑔𝑔) + 𝑑𝑑𝑔𝑔 )𝜃𝜃𝑔𝑔𝑔𝑔 + 𝐴𝐴𝑔𝑔]

## Slide 150
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
�40000 𝑑𝑑∙𝑔𝑔𝑖𝑖�(0.20380 − 0.02)
𝐹𝐹𝑆𝑆𝑔𝑔 = 𝑔𝑔𝑠𝑠𝑔 𝑔 = 1.565
(1.2)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)��(1.2)(9.317𝑠𝑠𝑠𝑠)�1 + 2.5(0.20380)� + 86.295𝑠𝑠𝑠𝑠�(0.20380) + 1.732𝑠𝑠𝑠𝑠�
𝐹𝐹𝑆𝑆𝑔𝑔 > 1.5 OK
4.5.2.7 Analyze at maximum superelevation, no impact
4.5.2.7.1 Equilibrium tilt angle
𝑒𝑒𝑒𝑒
𝜃𝜃 =
�𝐾𝐾𝜃𝜃 𝛼𝛼 + (𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔𝐴𝐴𝑔𝑔�
=
𝑔𝑔𝑠𝑠𝑔𝑔
𝑓𝑓𝑓𝑓
��40000𝑑𝑑∙𝑔𝑔𝑖𝑖� �0.06 𝑓𝑓𝑓𝑓� + (1.0)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)(1.732𝑠𝑠𝑠𝑠)�
𝑑𝑑∙𝑔𝑔𝑖𝑖
𝑔𝑔𝑠𝑠𝑔𝑔
𝐾𝐾𝜃𝜃 − (𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔(𝑑𝑑𝑔𝑔 + (𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔 ) �40000 � − (1.0)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)�86.295𝑠𝑠𝑠𝑠 + (1.0)(9.317𝑠𝑠𝑠𝑠)�
= 0.11465 𝐴𝐴𝐴𝐴𝑑𝑑
4.5.2.7.2 Stress due to lateral loading from tilt
Top left flange tip
𝑓𝑓𝑑𝑑𝑠𝑠 =
2𝐼𝐼
𝑝𝑝
=
(2)(72018.4𝑠𝑠𝑠𝑠4)
(𝐼𝐼𝑀𝑀)�𝑀𝑀𝑔𝑔�𝜃𝜃𝑒𝑒𝑒𝑒 𝐻𝐻𝑑𝑑𝑔𝑔𝑑𝑑 (1.0)(2195.02𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(0.11465)(49𝑠𝑠𝑠𝑠) 12𝑠𝑠𝑠𝑠
� � = 1.027 𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
Bottom right flange tip
(𝐼𝐼𝑀𝑀)�𝑀𝑀𝑔𝑔�𝜃𝜃𝑒𝑒𝑒𝑒 𝐻𝐻𝑠𝑠𝑔𝑔𝑑𝑑
𝑝𝑝
𝑓𝑓𝑠𝑠𝑔𝑔 = − = −
2𝐼𝐼 (2)(72018.4𝑠𝑠𝑠𝑠4)
(1.0)(2195.02𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(0.11465)(38.375𝑠𝑠𝑠𝑠) 12𝑠𝑠𝑠𝑠
� � = −0.856 𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
4.5.2.7.3 Factor of Safety against Cracking
Cracking moment
𝑓𝑓𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑐𝑐𝑑𝑑 = 𝑓𝑓𝑑𝑑𝑠𝑠 + (𝐼𝐼𝑀𝑀)𝑓𝑓𝑔𝑔 = 0.800𝑘𝑘𝑠𝑠𝑠𝑠 + (1.0)(−1.375𝑘𝑘𝑠𝑠𝑠𝑠) = −0.575𝑘𝑘𝑠𝑠𝑠𝑠
𝑀𝑀𝑐𝑐𝑔𝑔 =
(𝑓𝑓𝑔𝑔 − 𝑓𝑓𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑐𝑐𝑑𝑑 )2𝐼𝐼𝑝𝑝
𝐻𝐻
𝑑𝑑𝑔𝑔𝑑𝑑
=
�0.708𝑘𝑘𝑠𝑠𝑠𝑠 − (−0.575𝑠𝑠𝑠𝑠)�(2)(72018.4𝑠𝑠𝑠𝑠4) 1𝑓𝑓𝑓𝑓
49𝑠𝑠𝑠𝑠 12𝑠𝑠𝑠𝑠
� � = 314.26𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
Tilt angle at first crack
𝑀𝑀𝑐𝑐𝑔𝑔
𝜃𝜃𝑐𝑐𝑔𝑔 = (𝐼𝐼𝑀𝑀)𝑀𝑀
𝑔𝑔
≤ 0.4
314.26 𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝜃𝜃𝑐𝑐𝑔𝑔 = (1.0)2195.02 𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 = 0.14317 𝐴𝐴𝐴𝐴𝑑𝑑
Factor of Safety against Cracking
𝑐𝑐𝑔𝑔
𝐹𝐹𝑆𝑆 =
𝐾𝐾𝜃𝜃 (𝜃𝜃𝑐𝑐𝑔𝑔 − 𝛼𝛼)
(𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔[((𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔 + 𝑑𝑑𝑔𝑔 )𝜃𝜃𝑐𝑐𝑔𝑔 + 𝐴𝐴𝑔𝑔 ]
𝑔𝑔𝑠𝑠𝑔𝑔
𝑓𝑓𝑓𝑓
��40000 𝑑𝑑∙𝑔𝑔𝑖𝑖� �0.14317 𝐴𝐴𝐴𝐴𝑑𝑑 − 0.06 𝑓𝑓𝑓𝑓��
𝐹𝐹𝑆𝑆𝑐𝑐𝑔𝑔 = (1.0)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)[((1.0)(9.137𝑠𝑠𝑠𝑠) + 86.295𝑠𝑠𝑠𝑠)(0.14317𝐴𝐴𝐴𝐴𝑑𝑑) + 1.732𝑠𝑠𝑠𝑠] = 1.253
𝐹𝐹𝑆𝑆𝑐𝑐𝑔𝑔 > 1.0 OK
4.5.2.7.4 Factor of Safety against Failure
𝑐𝑐𝑠𝑠𝑥𝑥
2.5(𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔
𝐴𝐴𝑔𝑔 + �(𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔 + 𝑑𝑑𝑔𝑔 �𝛼𝛼
𝜃𝜃 = 𝛼𝛼 + �𝛼𝛼2 + ≤ 0.4 𝐴𝐴𝐴𝐴𝑑𝑑

## Slide 151
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
�
𝑓𝑓𝑓𝑓 𝑓𝑓𝑓𝑓 2
𝜃𝜃𝑐𝑐𝑠𝑠𝑥𝑥 = 0.06 𝑓𝑓𝑓𝑓 + �0.06 𝑓𝑓𝑓𝑓� +
𝑓𝑓𝑓𝑓
1.732𝑠𝑠𝑠𝑠 + �(1.0)(9.137𝑠𝑠𝑠𝑠) + (86.295𝑠𝑠𝑠𝑠)� �0.06 𝑓𝑓𝑓𝑓�
2.5(1.0)(9.137𝑠𝑠𝑠𝑠)
= 0.634 𝐴𝐴𝐴𝐴𝑑𝑑 ∴ 0.4 𝐴𝐴𝐴𝐴𝑑𝑑
𝑒𝑒
𝐹𝐹𝑆𝑆 =
𝐾𝐾𝜃𝜃 (𝜃𝜃𝑐𝑐𝑠𝑠𝑥𝑥 − 𝛼𝛼)
(𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔[(𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔 𝜃𝜃𝑐𝑐𝑠𝑠𝑥𝑥 (1 + 2.5𝜃𝜃
𝑐𝑐𝑠𝑠𝑥𝑥 𝑔𝑔 𝑐𝑐𝑠𝑠𝑥𝑥 𝑔𝑔
) + 𝑑𝑑 𝜃𝜃 + 𝐴𝐴 ]
𝑔𝑔𝑠𝑠𝑔𝑔
𝑓𝑓𝑓𝑓
�40000 𝑑𝑑∙𝑔𝑔𝑖𝑖� �0.4 − 0.06 𝑓𝑓𝑓𝑓�
𝐹𝐹𝑆𝑆𝑒𝑒 = (1.0)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)[(1.0)(9.137𝑠𝑠𝑠𝑠)(0.4)�1 + 2.5(0.4)� + (86.295𝑠𝑠𝑠𝑠)(0.4) + 1.732𝑠𝑠𝑠𝑠 = 1.810
𝐹𝐹𝑆𝑆𝑒𝑒 > 1.5 OK
4.5.2.7.5 Factor of Safety against Rollover
𝑔𝑔𝑔𝑔
𝜃𝜃 =
𝑔𝑔
𝐻𝐻
𝑐𝑐𝑐𝑐
2
(𝐼𝐼𝑀𝑀)𝐻𝐻 � − 𝐻𝐻 𝛼𝛼 − 𝐴𝐴
𝑔𝑔𝑐𝑐 𝑠𝑠𝑎𝑎𝑖𝑖𝑑𝑑
�
𝐾𝐾𝜃𝜃
+ 𝛼𝛼
(1.0)(172.48𝑘𝑘𝑠𝑠𝑘𝑘) �72𝑠𝑠𝑠𝑠 − (24𝑠𝑠𝑠𝑠)(0.06) − 1.0𝑠𝑠𝑠𝑠�
𝑔𝑔𝑠𝑠𝑔𝑔
�40000 𝑑𝑑∙𝑔𝑔𝑖𝑖�
𝜃𝜃𝑔𝑔𝑔𝑔 = 2 + 0.06 = 0.20903 𝐴𝐴𝐴𝐴𝑑𝑑
𝑔𝑔
𝐹𝐹𝑆𝑆 =
𝐾𝐾𝜃𝜃 (𝜃𝜃𝑔𝑔𝑔𝑔 − 𝛼𝛼)
(𝐼𝐼𝑀𝑀)𝐻𝐻𝑔𝑔[((𝐼𝐼𝑀𝑀)𝑧𝑧𝑔𝑔(1 + 2.5𝜃𝜃𝑔𝑔𝑔𝑔) + 𝑑𝑑𝑔𝑔 )𝜃𝜃𝑔𝑔𝑔𝑔 + 𝐴𝐴𝑔𝑔]
�40000 𝑑𝑑∙𝑔𝑔𝑖𝑖�(0.20903 − 0.06)
𝐹𝐹𝑆𝑆𝑔𝑔 = 𝑔𝑔𝑠𝑠𝑔 𝑔 = 1.52
(1.0)(172.48𝑘𝑘𝑠𝑠𝑘𝑘)��(1.0)(9.137𝑠𝑠𝑠𝑠)�1 + 2.5(0.20903)� + 86.295𝑠𝑠𝑠𝑠�(0.20903) + 1.732𝑠𝑠𝑠𝑠�
𝐹𝐹𝑆𝑆𝑔𝑔 > 1.5 OK
Case 𝒇𝒇𝒌𝒌𝒌𝒌(𝒌𝒌𝒌𝒌𝒌𝒌) IM 𝒇𝒇𝒈𝒈(𝒌𝒌𝒌𝒌𝒌𝒌) 𝒇𝒇𝒅𝒅𝒌𝒌𝒅𝒅𝒅𝒅𝒅𝒅𝒕𝒕 𝒇𝒇′ |  |  |  |  | 𝒇𝒇𝒕𝒕𝒌𝒌𝒕𝒕𝒕𝒕(𝒌𝒌𝒌𝒌𝒌𝒌) 𝒇𝒇′ 𝒅𝒅 |  | 
= 𝒇𝒇𝒌𝒌𝒌𝒌 = |  |  |  |  | 𝒇𝒇𝒅𝒅𝒌𝒌𝒅𝒅𝒅𝒅𝒅𝒅𝒕𝒕 (𝒌𝒌𝒌𝒌𝒌𝒌) = 𝒇𝒇𝒅𝒅𝒌𝒌𝒅𝒅𝒅𝒅𝒅𝒅𝒕𝒕 + 𝒇𝒇𝒕𝒕𝒌𝒌𝒕𝒕𝒕𝒕 (𝒌𝒌𝒌𝒌𝒌𝒌) |  | 
 |  |  |  | + (𝑰𝑰𝑰𝑰)𝒇𝒇𝒈𝒈 (𝒌𝒌𝒌𝒌𝒌𝒌) | 𝟎𝟎. 𝟔𝟔𝟔𝟔 |  | 𝟎𝟎. 𝟕𝟕𝟎𝟎
2% slope, no impact | -5.886 | 1.0 | 1.279 | -4.607 | 7.1 | -0.318 | 7.1
2% slope, impact up | -5.886 | 0.8 | 1.279 | -4.863 | 7.5 | -0.215 | 7.3
2% slope, impact down | -5.886 | 1.2 | 1.279 | -4.351 | 6.2 | -0.491 | 6.9
6% slope, | -5.886 | 1.0 | 1.279 | -4.607 | 7.1 | -0.856 | 7.8
no impact |  |  |  |  |  |  | Controls
    Check concrete strength
      Compression
Compression stress is limited to −0.65𝑓𝑓′ when tilt is not considered and −0.70𝑓𝑓′ when tilt is considered.
𝑐𝑐 𝑐𝑐
𝒅𝒅
4.5.3.2 Tension
Check tension stress limit
Maximum tension stress occurs at harp point top left corner of girder on with superelevated slope of 6%

## Slide 152
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝑓𝑓𝑑𝑑 = 0.800𝑘𝑘𝑠𝑠𝑠𝑠 − 1.375𝑘𝑘𝑠𝑠𝑠𝑠 + 1.027𝑘𝑘𝑠𝑠𝑠𝑠 = 0.452 𝑘𝑘𝑠𝑠𝑠𝑠
Stress limit
0.24𝜆𝜆�𝑓𝑓′ = 0.24(1.0)√8.7𝑘𝑘𝑠𝑠𝑠𝑠 = 0.708 𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐
Tension stress is within limit. However, use of this tensile stress limit requires reinforcement sufficient to resist the tensile force in the concrete computed assuming an uncracked section, where reinforcement is proportioned using a stress of 0.5𝑓𝑓𝑝𝑝 , no exceeding 30 ksi (LRFD Table 5.9.2.3.1b-1).
  Step 6 – Check Erection Stresses
Evaluate the stress in the girder after the temporary strands are removed and the wet deck is cast. This is the maximum loading condition for the bare girder.
This check is not specified in the AASHTO LRFD BDS. This check is a WSDOT design policy. See WSDOT BDM Table 5.2.1-1
    Losses between Transfer to Deck Placement
      Temporary strand removal
Removing the temporary strands changes the state of stress in the girder and causes and additional elastic shortening loss in the permanent strands.
Assuming the temporary strands are removed shortly after erection, the force in the temporary strands at time of removal is
𝑃𝑃𝑑𝑑𝑔𝑔 = 𝐴𝐴𝑑𝑑 �𝑓𝑓𝑑𝑑𝑝𝑝 − ∆𝑓𝑓𝑑𝑑𝑆𝑆 �
The change of stress in the concrete at the level of the permanent strand due to the removal of the temporary strands is
𝑑𝑑𝑑𝑑𝑔𝑔
𝑓𝑓 = − −
𝑃𝑃𝑑𝑑𝑔𝑔 𝑃𝑃𝑑𝑑𝑔𝑔 𝐴𝐴𝑑𝑑 𝐴𝐴𝑑𝑑
𝐴𝐴 𝐼𝐼
𝑔𝑔 𝑔𝑔
The change in stress in the permanent strands is
∆𝑓𝑓
𝑑𝑑𝑑𝑑𝑔𝑔
𝐸𝐸𝑑𝑑
𝐸𝐸
𝑐𝑐
= 𝑓𝑓
𝑑𝑑𝑑𝑑𝑔𝑔
At the mid-span section
𝑃𝑃𝑑𝑑𝑔𝑔 = 4(0.217𝑠𝑠𝑠𝑠2)(202.5𝑘𝑘𝑠𝑠𝑠𝑠 − 7.569𝑘𝑘𝑠𝑠𝑠𝑠) = 162.93 𝑘𝑘𝑠𝑠𝑘𝑘
162.93𝑘𝑘𝑠𝑠𝑘𝑘 (162.93𝑘𝑘𝑠𝑠𝑘𝑘)(−36.343𝑠𝑠𝑠𝑠)(31.477𝑠𝑠𝑠𝑠)
𝑓𝑓𝑑𝑑𝑑𝑑𝑔𝑔 = − 923.531𝑠𝑠𝑠𝑠2 − 734356.0𝑠𝑠𝑠𝑠4
= 0.077𝑘𝑘𝑠𝑠𝑠𝑠
28500𝑘𝑘𝑠𝑠𝑠𝑠
∆𝑓𝑓𝑑𝑑𝑑𝑑𝑔𝑔 = 5886.891𝑘𝑘𝑠𝑠𝑠𝑠 (0.077𝑘𝑘𝑠𝑠𝑠𝑠) = 0.375 𝑘𝑘𝑠𝑠𝑠𝑠
4.6.1.2 Shrinkage of Girder Concrete
𝐾𝐾𝑔𝑔𝑔𝑔 =
𝛥𝛥𝑓𝑓𝑑𝑑𝑆𝑆𝑅𝑅 = 𝜀𝜀𝑠𝑠𝑔𝑔𝑔𝑔 𝐸𝐸𝑑𝑑𝐾𝐾𝑔𝑔𝑔𝑔
𝜀𝜀𝑠𝑠𝑔𝑔𝑔𝑔 = 𝑘𝑘𝑠𝑠𝑘𝑘ℎ𝑠𝑠𝑘𝑘𝑒𝑒 𝑘𝑘𝑑𝑑𝑔𝑔0.48 × 10−3
1
𝐸𝐸𝑐𝑐𝑔𝑔 𝐴𝐴𝑔𝑔
𝐸𝐸 𝐴𝐴 𝐴𝐴 𝐴𝐴 𝐴𝐴
𝐼𝐼𝑔𝑔
𝑠𝑠 𝑒𝑒 𝑔𝑔
1 + 𝑑 𝑑 𝑑𝑑𝑠𝑠 �1 + 𝑔 𝑔 𝑑𝑑� �1 + 0.7𝜓𝜓 �𝑓𝑓 , 𝑓𝑓 ��
𝑔𝑔
𝜓𝜓𝑠𝑠 �𝑓𝑓𝑒𝑒 , 𝑓𝑓𝑔𝑔� = 1.9𝑘𝑘𝑠𝑠𝑘𝑘ℎ𝑐𝑐 𝑘𝑘𝑒𝑒 𝑘𝑘𝑑𝑑𝑔𝑔𝑓𝑓−0.118

## Slide 153
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝑉𝑉
𝑘𝑘𝑠𝑠 = 1.45 − 0.13 �𝑆𝑆� ≥ 1.0 = 1.04
𝑘𝑘ℎ𝑠𝑠 = 2.00 − 0.014𝐻𝐻 = 0.95
𝑘𝑘ℎ𝑐𝑐 = 1.56 − 0.008𝐻𝐻 = 0.96 1
𝑘𝑘𝑒𝑒 = 1 + 𝑓𝑓′ = 0.61
𝑘𝑘𝑑𝑑𝑔𝑔 =
𝑓𝑓
12 �
100 − 4𝑓𝑓′
′
𝑓𝑓𝑐𝑐𝑔𝑔 + 20
𝑐𝑐𝑔𝑔 � + 𝑓𝑓
𝑐𝑐𝑔𝑔
0.791 𝑤𝑤𝑠𝑠𝑓𝑓ℎ 𝑓𝑓 = (𝑓𝑓𝑔𝑔 − 𝑓𝑓𝑔𝑔 ) = 119 𝑑𝑑𝐴𝐴𝑑𝑑
𝑒𝑒 𝑔𝑔
= 0.985 𝑤𝑤𝑠𝑠𝑓𝑓ℎ 𝑓𝑓 = �𝑓𝑓 − 𝑓𝑓 � = 1999 𝑑𝑑𝐴𝐴𝑑𝑑
𝐾𝐾𝑔𝑔𝑔𝑔 =
𝑓𝑓𝑔𝑔 = 1 𝑑𝑑𝐴𝐴𝑑𝑑
𝑓𝑓𝑔𝑔 = 120 𝑑𝑑𝐴𝐴𝑑𝑑
𝑓𝑓𝑒𝑒 = 2000 𝑑𝑑𝐴𝐴𝑑𝑑
𝜀𝜀𝑠𝑠𝑔𝑔𝑔𝑔 = (1.04)(0.95)(0.61)(0.791)(0.48 × 10−3) = 0.000228
𝜓𝜓𝑠𝑠 �𝑓𝑓𝑒𝑒 , 𝑓𝑓𝑔𝑔� = 1.9(1.04)(0.96)(0.61)(0.985)(1)−0.118 = 1.135
1
28500𝑘𝑘𝑠𝑠𝑠𝑠
1 + �5530.5𝑘𝑘𝑠𝑠𝑠𝑠� �
14.105𝑠𝑠𝑠𝑠2 (923.531𝑠𝑠𝑠𝑠2)(27.304𝑠𝑠𝑠𝑠)(31.477𝑠𝑠𝑠𝑠)
923.531𝑠𝑠𝑠𝑠 734356.0𝑠𝑠𝑠𝑠
4
2� �1 + � �1 + 0.7(1.135)�
= 0.773
𝛥𝛥𝑓𝑓𝑑𝑑𝑆𝑆𝑅𝑅 = (0.000228)(28500𝑘𝑘𝑠𝑠𝑠𝑠)(0.773) = 5.022 𝑘𝑘𝑠𝑠𝑠𝑠
4.6.1.3 Creep of Girder Concrete
𝐸𝐸𝑑𝑑
𝛥𝛥𝑓𝑓 = 𝑓𝑓 𝜓𝜓 (𝑓𝑓 , 𝑓𝑓 )𝐾𝐾
𝑑𝑑𝑝𝑝𝑅𝑅 𝐸𝐸𝑐𝑐𝑔𝑔 𝑐𝑐𝑔𝑔𝑑𝑑 𝑠𝑠 𝑔𝑔 𝑔𝑔 𝑔𝑔𝑔𝑔
𝜓𝜓𝑠𝑠 (𝑓𝑓𝑔𝑔 , 𝑓𝑓𝑔𝑔) = 1.9(1.04)(0.96)(0.61)(0.791)(1)−0.118 = 0.912 28500𝑘𝑘𝑠𝑠𝑠𝑠
𝛥𝛥𝑓𝑓𝑑𝑑𝑝𝑝𝑅𝑅 = 4935.632𝑘𝑘𝑠𝑠𝑠𝑠 (3.945𝑘𝑘𝑠𝑠𝑠𝑠)(0.912)(0.773) = 14.327 𝑘𝑘𝑠𝑠𝑠𝑠
4.6.1.4 Relaxation of Prestressing Strands
𝛥𝛥𝑓𝑓𝑑𝑑𝑅𝑅1 = �
′
𝑓𝑓𝑑𝑑𝑑𝑑 𝑘𝑘𝑐𝑐𝑔𝑔 (24𝑓𝑓𝑔𝑔)
𝑓𝑓𝑑𝑑𝑑𝑑
𝐾𝐾 𝑘𝑘𝑐𝑐𝑔𝑔(24𝑓𝑓 ) 𝑓𝑓
� − 0.55�� �1 −
3�𝛥𝛥𝑓𝑓𝑑𝑑𝑆𝑆𝑅𝑅 + 𝛥𝛥𝑓𝑓𝑑𝑑𝑝𝑝𝑅𝑅 �
𝑓𝑓
𝐿𝐿 𝑔𝑔 𝑑𝑑𝑝𝑝 𝑑𝑑𝑑𝑑
� 𝐾𝐾𝑔𝑔𝑔𝑔
𝑓𝑓𝑑𝑑𝑑𝑑 = 𝑓𝑓𝑑𝑑𝑝𝑝 − ∆𝑓𝑓𝑑𝑑𝑅𝑅0 − ∆𝑓𝑓𝑑𝑑𝐸𝐸𝑆𝑆 = 202.5𝑘𝑘𝑠𝑠𝑠𝑠 − 1.98𝑘𝑘𝑠𝑠𝑠𝑠 − 20.328𝑘𝑘𝑠𝑠𝑠𝑠 = 180.193𝑘𝑘𝑠𝑠𝑠𝑠
𝛥𝛥𝑓𝑓𝑑𝑑𝑅𝑅1 = �
45 𝑘𝑘𝑐𝑐𝑔𝑔 (24 ∙ 1) 243𝑘𝑘𝑠𝑠𝑠𝑠
180.193 𝑘𝑘𝑠𝑠𝑠𝑠 𝑘𝑘𝑐𝑐𝑔𝑔 (24 ∙ 120) 180.193𝑘𝑘𝑠𝑠𝑠𝑠 3(5.022𝑘𝑘𝑠𝑠𝑠𝑠 + 14.327𝑘𝑘𝑠𝑠𝑠𝑠)
180.193 𝑘𝑘𝑠𝑠𝑠𝑠
� − 0.55�� �1 − � (0.773) = 1.007 𝑘𝑘𝑠𝑠𝑠𝑠
      Time dependent losses
∆𝑓𝑓𝑑𝑑𝐿𝐿𝑝𝑝𝑟𝑟𝑒𝑒 = ∆𝑓𝑓𝑑𝑑𝑆𝑆𝑅𝑅 + ∆𝑓𝑓𝑑𝑑𝑝𝑝𝑅𝑅 + ∆𝑓𝑓𝑑𝑑𝑅𝑅1
∆𝑓𝑓𝑑𝑑𝐿𝐿𝑝𝑝𝑟𝑟𝑒𝑒 = 5.022𝑘𝑘𝑠𝑠𝑠𝑠 + 14.327𝑘𝑘𝑠𝑠𝑠𝑠 + 1.007𝑘𝑘𝑠𝑠𝑠𝑠 = 20.355 𝑘𝑘𝑠𝑠𝑠𝑠
      Elastic gains
Added dead load on noncomposite section
𝑀𝑀𝑠𝑠𝑔𝑔𝑠𝑠 = 𝑀𝑀𝑔𝑔𝑔𝑔𝑠𝑠𝑑𝑑ℎ𝑔𝑔𝑠𝑠𝑔𝑔𝑐𝑐 + 𝑀𝑀𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 + 𝑀𝑀ℎ𝑠𝑠𝑎𝑎𝑖𝑖𝑐𝑐ℎ
𝑀𝑀𝑠𝑠𝑔𝑔𝑠𝑠 = 140.17𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 + 2465.61𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 + 760.28𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 = 3366.05𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓

## Slide 154
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝑐𝑐𝑔𝑔
′
∆𝑓𝑓 =
𝑠𝑠𝑔𝑔𝑠𝑠
𝑀𝑀 𝐴𝐴
𝐼𝐼𝑔𝑔
𝑐𝑐𝑔𝑔
′
(
∆𝑓𝑓 = 3366.05𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 �
1𝑓𝑓𝑓𝑓
12𝑠𝑠𝑠𝑠 31.477𝑠𝑠𝑠𝑠
) � � � = 1.731 𝑘𝑘𝑠𝑠𝑠𝑠
734356.0𝑠𝑠𝑠𝑠4
𝑑𝑑𝐸𝐸𝑝𝑝
𝐸𝐸
𝑑𝑑
𝐸𝐸𝑐𝑐
∆𝑓𝑓 = ∆𝑓𝑓
𝑐𝑐𝑔𝑔
′
∆𝑓𝑓𝑑𝑑𝐸𝐸𝑝𝑝 = �
28500𝑘𝑘𝑠𝑠𝑠𝑠
5886.891𝑘𝑘𝑠𝑠𝑠𝑠
� (1.731𝑘𝑘𝑠𝑠𝑠𝑠) = 8.382 𝑘𝑘𝑠𝑠𝑠𝑠
4.6.2 Stresses
Effective prestress
𝑃𝑃 = 𝐴𝐴𝑑𝑑𝑠𝑠�𝑓𝑓𝑑𝑑𝑝𝑝 − ∆𝑓𝑓𝑑𝑑𝑅𝑅0 − ∆𝑓𝑓𝑑𝑑𝐸𝐸𝑆𝑆 − ∆𝑓𝑓𝑑𝑑𝐿𝐿𝑝𝑝𝑟𝑟𝑒𝑒 − ∆𝑓𝑓𝑑𝑑𝑑𝑑𝑔𝑔 + ∆𝑓𝑓𝑑𝑑𝐸𝐸𝑝𝑝�
𝑃𝑃 = 13.237𝑠𝑠𝑠𝑠2(202.5𝑘𝑘𝑠𝑠𝑠𝑠 − 1.98𝑘𝑘𝑠𝑠𝑠𝑠 − 20.328𝑘𝑘𝑠𝑠𝑠𝑠 − 20.355𝑘𝑘𝑠𝑠𝑠𝑠 − 0.375𝑘𝑘𝑠𝑠𝑠𝑠 + 8.382𝑘𝑘𝑠𝑠𝑠𝑠) = 2221.8 𝑘𝑘𝑠𝑠𝑘𝑘
Stress in girder due to effective prestress
𝑃𝑃 𝑃𝑃𝐴𝐴
𝑓𝑓𝑑𝑑𝑠𝑠 = 𝐴𝐴 + 𝑆𝑆
−2221.8𝑘𝑘𝑠𝑠𝑘𝑘 (−2221.8𝑘𝑘𝑠𝑠𝑘𝑘)(31.447𝑠𝑠𝑠𝑠)
𝑓𝑓𝑑𝑑 = 923.531𝑠𝑠𝑠𝑠2 + −19152.5𝑠𝑠𝑠𝑠3
= 1.246𝑘𝑘𝑠𝑠𝑠𝑠
−2221.8𝑘𝑘𝑠𝑠𝑘𝑘 (−2221.8𝑘𝑘𝑠𝑠𝑘𝑘)(31.447𝑠𝑠𝑠𝑠)
𝑓𝑓𝑠𝑠 = 923.531𝑠𝑠𝑠𝑠2 + 20594.8𝑠𝑠𝑠𝑠3
= −5.801𝑘𝑘𝑠𝑠𝑠𝑠
Stress due to loading
𝑓𝑓 =
𝑀𝑀𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 + 𝑀𝑀𝑔𝑔𝑔𝑔𝑠𝑠𝑑𝑑ℎ𝑔𝑔𝑠𝑠𝑔𝑔𝑐𝑐 + 𝑀𝑀𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 + 𝑀𝑀ℎ𝑠𝑠𝑎𝑎𝑖𝑖𝑐𝑐ℎ
𝑆𝑆
𝑓𝑓𝑑𝑑 =
−19152.5𝑠𝑠𝑠𝑠3
(3368.43𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 + 140.17𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 + 2465.61𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 + 760.28𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) 12𝑠𝑠𝑠𝑠
� � = −4.219 𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
𝑓𝑓𝑠𝑠 =
20594.8𝑠𝑠𝑠𝑠3
(3368.43𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 + 140.17𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 + 2465.61𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 + 760.28𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) 12𝑠𝑠𝑠𝑠
� � = 3.924 𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
Stress Limits Compression
𝑐𝑐
−0.45𝑓𝑓′ = −0.45(8.7𝑘𝑘𝑠𝑠𝑠𝑠) = −3.915𝑘𝑘𝑠𝑠𝑠𝑠
Tension
𝑐𝑐
0.19𝜆𝜆�𝑓𝑓′ = 0.19(1.0)√8.7 𝑘𝑘𝑠𝑠𝑠𝑠 = 0.560𝑘𝑘𝑠𝑠𝑠𝑠
Stress Demand
𝑓𝑓𝑑𝑑 = 1.246𝑘𝑘𝑠𝑠𝑠𝑠 − 4.219𝑘𝑘𝑠𝑠𝑠𝑠 = −2.974 𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 = −5.801𝑘𝑘𝑠𝑠𝑠𝑠 + 3.924𝑘𝑘𝑠𝑠𝑠𝑠 = −1.877 𝑘𝑘𝑠𝑠𝑠𝑠
Stresses at mid-span satisfy the limit state.
These calculations are repeated at the point of prestress transfer. The results are
𝑓𝑓𝑑𝑑 = −0.648 𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 = −3.892 𝑘𝑘𝑠𝑠𝑠𝑠
The required concrete strength is

## Slide 155
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝑐𝑐
−0.45𝑓𝑓′ = −3.892𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓′ = 8.65 𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐
This is the overall governing 28-day design concrete strength.
  Step 7 – Check Final Conditions
    Losses from Deck Placement to Final
      Shrinkage of Girder Concrete
𝐾𝐾𝑔𝑔𝑒𝑒 =
𝛥𝛥𝑓𝑓𝑑𝑑𝑆𝑆𝑝𝑝 = 𝜀𝜀𝑠𝑠𝑔𝑔𝑒𝑒𝐸𝐸𝑑𝑑 𝐾𝐾𝑔𝑔𝑒𝑒
𝜀𝜀𝑠𝑠𝑔𝑔𝑒𝑒 = 𝜀𝜀𝑠𝑠𝑔𝑔𝑒𝑒 − 𝜀𝜀𝑠𝑠𝑔𝑔𝑔𝑔
𝜀𝜀 = 𝑘𝑘𝑠𝑠𝑘𝑘ℎ𝑠𝑠𝑘𝑘𝑒𝑒 𝑘𝑘𝑑𝑑𝑔𝑔0.48 × 10−3
1
𝐸𝐸 𝐴𝐴
𝐸𝐸𝑐𝑐𝑔𝑔 𝐴𝐴𝑐𝑐
𝐴𝐴 𝐴𝐴2
𝐼𝐼𝑐𝑐
𝑠𝑠 𝑒𝑒 𝑔𝑔
1 + 𝑑 𝑑 𝑑𝑑𝑠𝑠 �1 + 𝑐 𝑐 𝑐𝑐 � �1.0 + 0.7𝜓𝜓 �𝑓𝑓 , 𝑓𝑓 ��
From before
𝐾𝐾𝑔𝑔𝑒𝑒 =
𝑘𝑘𝑠𝑠 = 1.04
𝑘𝑘ℎ𝑠𝑠 = 0.95
𝑘𝑘ℎ𝑐𝑐 = 0.96
𝑘𝑘𝑒𝑒 = 0.61
𝜓𝜓𝑠𝑠 �𝑓𝑓𝑒𝑒 , 𝑓𝑓𝑔𝑔 � = 1.135
𝜀𝜀𝑠𝑠𝑔𝑔𝑔𝑔 = 0.000228
𝑘𝑘𝑑𝑑𝑔𝑔�𝑓𝑓 = 𝑓𝑓𝑒𝑒 − 𝑓𝑓𝑔𝑔 � = 0.985
𝜀𝜀𝑠𝑠𝑔𝑔𝑒𝑒 = (1.04)(0.95)(0.61)(0.985)(0.48 × 10−3) = 0.000284
𝜀𝜀𝑠𝑠𝑔𝑔𝑒𝑒 = 0.000284 − 0.000228 = 0.000056
𝐴𝐴𝑐𝑐 = 𝐴𝐴 + 𝑑𝑑𝑠𝑠𝑐𝑐 − 𝑑𝑑𝑠𝑠 = 31.477𝑠𝑠𝑠𝑠 + 48.867𝑠𝑠𝑠𝑠 − 35.657𝑠𝑠𝑠𝑠 = 44.687𝑠𝑠𝑠𝑠 1
28500𝑘𝑘𝑠𝑠𝑠𝑠 13.237𝑠𝑠𝑠𝑠2
1 + �5530.5𝑘𝑘𝑠𝑠𝑠𝑠� �1349.614𝑠𝑠𝑠𝑠2� �1 +
(1349.614𝑠𝑠𝑠𝑠2)(44.687𝑠𝑠𝑠𝑠)2 1246570.6𝑠𝑠𝑠𝑠4
� �1 + 0.7(1.135)�
= 0.777
∆𝑓𝑓𝑑𝑑𝑆𝑆𝑝𝑝 = (0.000056)(28500𝑘𝑘𝑠𝑠𝑠𝑠)(0.777) = 1.234 𝑘𝑘𝑠𝑠𝑠𝑠
4.7.1.2 Creep of Girder Concrete
𝑑𝑑𝑝𝑝𝑝𝑝 𝐸𝐸𝑐𝑐𝑔𝑔 𝑐𝑐𝑔𝑔𝑑𝑑 𝑠𝑠 𝑒𝑒 𝑔𝑔 𝑠𝑠 𝑔𝑔 𝑔𝑔 𝑔𝑔𝑒𝑒
𝐸𝐸
𝑑𝑑
𝐸𝐸𝑐𝑐
𝐸𝐸𝑑𝑑
∆𝑓𝑓 = 𝑓𝑓 �𝜓𝜓 �𝑓𝑓 , 𝑓𝑓 � − 𝜓𝜓 (𝑓𝑓 , 𝑓𝑓 )�𝐾𝐾 + (𝛥𝛥𝑓𝑓 )𝜓𝜓 �𝑓𝑓 , 𝑓𝑓 �𝐾𝐾
𝑐𝑐𝑔𝑔 𝑠𝑠 𝑒𝑒 𝑔𝑔 𝑔𝑔𝑒𝑒
𝐴𝐴𝑑𝑑𝑠𝑠
𝐴𝐴𝑔𝑔
𝐴𝐴𝑔𝑔𝐴𝐴2
𝐼𝐼𝑔𝑔
𝑐𝑐𝑔𝑔 𝑐𝑐𝑔𝑔
𝛥𝛥𝑓𝑓𝑐𝑐𝑔𝑔 = −�𝛥𝛥𝑓𝑓𝑑𝑑𝑆𝑆𝑅𝑅 + 𝛥𝛥𝑓𝑓𝑑𝑑𝑝𝑝𝑅𝑅 + 𝛥𝛥𝑓𝑓𝑑𝑑𝑅𝑅1� � � �1 + � − (𝛥𝛥𝑓𝑓′ + 𝛥𝛥𝑓𝑓′′ )
𝑐𝑐𝑔𝑔
′
𝛥𝛥𝑓𝑓 =
𝑠𝑠𝑔𝑔𝑠𝑠
𝑀𝑀 𝐴𝐴
𝐼𝐼𝑔𝑔
= 1.731 𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐𝑔𝑔
′′
𝛥𝛥𝑓𝑓 =
𝑠𝑠𝑔𝑔𝑔𝑔𝑠𝑠 𝑠𝑠𝑐𝑐 𝑠𝑠𝑔𝑔
𝑀𝑀 �𝑌𝑌 − 𝑌𝑌 + 𝐴𝐴�
𝐼𝐼𝑐𝑐

## Slide 156
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝑀𝑀𝑠𝑠𝑔𝑔𝑔𝑔𝑠𝑠 = 𝑀𝑀𝑠𝑠𝑠𝑠𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 + 𝑀𝑀𝑔𝑔𝑜𝑜𝑒𝑒𝑔𝑔𝑠𝑠𝑠𝑠𝑝𝑝
𝑀𝑀𝑠𝑠𝑔𝑔𝑔𝑔𝑠𝑠 = 732.83𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 + 739.63𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 = 1471.75𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑐𝑐𝑔𝑔
′′
𝛥𝛥𝑓𝑓 =
1246570.6𝑠𝑠𝑠𝑠4
(1471.75𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(48.867𝑠𝑠𝑠𝑠 − 35.657𝑠𝑠𝑠𝑠 + 31.477𝑠𝑠𝑠𝑠) 12𝑠𝑠𝑠𝑠
� � = 0.633𝑘𝑘𝑠𝑠𝑠𝑠 1𝑓𝑓𝑓𝑓
14.105𝑠𝑠𝑠𝑠2
𝛥𝛥𝑓𝑓𝑐𝑐𝑔𝑔 = −(5.022 + 14.732 + 1.007 𝑘𝑘𝑠𝑠𝑠𝑠) �923.531𝑠𝑠𝑠𝑠3� �1 +
(923.531𝑠𝑠𝑠𝑠2)(31.477𝑠𝑠𝑠𝑠)2
734356.0𝑠𝑠𝑠𝑠4
� − (1.731𝑘𝑘𝑠𝑠𝑠𝑠 + 0.633𝑘𝑘𝑠𝑠𝑠𝑠)
= −3.020 𝑘𝑘𝑠𝑠𝑠𝑠
𝑘𝑘𝑑𝑑𝑔𝑔 =
𝑓𝑓
12 �
100 − 4𝑓𝑓′
′
𝑓𝑓𝑐𝑐𝑔𝑔 + 20
𝑐𝑐𝑔𝑔 � + 𝑓𝑓
= 0.984 𝑤𝑤𝑠𝑠𝑓𝑓ℎ 𝑓𝑓 = �𝑓𝑓𝑒𝑒 − 𝑓𝑓𝑔𝑔� = 2000 − 120 = 1880 𝑑𝑑𝐴𝐴𝑑𝑑
𝛥𝛥𝑓𝑓𝑑𝑑𝑝𝑝𝑝𝑝 = �
28500𝑘𝑘𝑠𝑠𝑠𝑠
𝜓𝜓𝑠𝑠 �𝑓𝑓𝑒𝑒 , 𝑓𝑓𝑔𝑔 � = 1.9(1.04)(0.96)(0.61)(0.984)(120)−0.118 = 0.644
28500𝑘𝑘𝑠𝑠𝑠𝑠
5530.5𝑘𝑘𝑠𝑠𝑠𝑠 5886.891𝑘𝑘𝑠𝑠𝑠𝑠
� (3.945𝑘𝑘𝑠𝑠𝑠𝑠)(1.135 − 0.912)(0.777) + � � (−3.020𝑘𝑘𝑠𝑠𝑠𝑠)(0.644)(0.777) = −2.892 𝑘𝑘𝑠𝑠𝑠𝑠
      Relaxation of Prestressing Strands
𝛥𝛥𝑓𝑓𝑑𝑑𝑅𝑅2 = 𝛥𝛥𝑓𝑓𝑑𝑑𝑅𝑅1 = 1.007 𝑘𝑘𝑠𝑠𝑠𝑠
      Shrinkage of Deck Concrete
𝑑𝑑𝑆𝑆𝑆𝑆
𝐸𝐸𝑑𝑑
𝐸𝐸
𝑐𝑐
𝛥𝛥𝑓𝑓 = 𝛥𝛥𝑓𝑓
𝑐𝑐𝑔𝑔𝑒𝑒 𝑔𝑔𝑒𝑒 𝑠𝑠 𝑒𝑒 𝑔𝑔
𝐾𝐾 �1 + 0.7𝜓𝜓 �𝑓𝑓 , 𝑓𝑓 ��
𝛥𝛥𝑓𝑓𝑐𝑐𝑔𝑔𝑒𝑒 =
𝜀𝜀𝑔𝑔𝑔𝑔𝑒𝑒𝐴𝐴𝑔𝑔 𝐸𝐸𝑐𝑐 𝑔𝑔𝑒𝑒𝑐𝑐𝑑𝑑
1
�1 + 0.7𝜓𝜓𝑔𝑔�𝑓𝑓𝑒𝑒 , 𝑓𝑓𝑔𝑔�� 𝐴𝐴𝑐𝑐
𝐴𝐴𝑐𝑐 𝐴𝐴𝑔𝑔
� − �
𝛥𝛥𝑓𝑓𝑐𝑐𝑔𝑔𝑒𝑒 =
(−0.000265)(681.165𝑠𝑠𝑠𝑠2)(4266.223𝑘𝑘𝑠𝑠𝑠𝑠) 1
� 2 −
𝐼𝐼𝑐𝑐
(44.687𝑠𝑠𝑠𝑠)(28.883𝑠𝑠𝑠𝑠)
1349.614𝑠𝑠𝑠𝑠 1246570.6𝑠𝑠𝑠𝑠
4
� = 0.091 𝑘𝑘𝑠𝑠𝑠𝑠
𝛥𝛥𝑓𝑓𝑑𝑑𝑆𝑆𝑆𝑆 = �
1 + 0.7(2.12)
28500𝑘𝑘𝑠𝑠𝑠𝑠
5886.891𝑘𝑘𝑠𝑠𝑠𝑠
� (0.091𝑘𝑘𝑠𝑠𝑠𝑠)(0.777)�1 + 0.7(0.644)� = 0.498 𝑘𝑘𝑠𝑠𝑠𝑠
      Time Dependent Losses
𝛥𝛥𝑓𝑓𝑑𝑑𝐿𝐿𝑝𝑝𝑒𝑒𝑡𝑡 = 𝛥𝛥𝑓𝑓𝑑𝑑𝑆𝑆𝑝𝑝 + 𝛥𝛥𝑓𝑓𝑑𝑑𝑝𝑝𝑝𝑝 + 𝛥𝛥𝑓𝑓𝑑𝑑𝑅𝑅1 − 𝛥𝛥𝑓𝑓𝑑𝑑𝑆𝑆𝑆𝑆 = 1.234𝑘𝑘𝑠𝑠𝑠𝑠 − 2.892𝑘𝑘𝑠𝑠𝑠𝑠 + 1.007𝑘𝑘𝑠𝑠𝑠𝑠 − 0.498𝑘𝑘𝑠𝑠𝑠𝑠 = −1.149 𝑘𝑘𝑠𝑠𝑠𝑠
∆𝑓𝑓𝑑𝑑𝐿𝐿𝑝𝑝 = ∆𝑓𝑓𝑑𝑑𝐿𝐿𝑝𝑝𝑟𝑟𝑒𝑒 + ∆𝑓𝑓𝑑𝑑𝐿𝐿𝑝𝑝𝑒𝑒𝑡𝑡 = 20.355𝑘𝑘𝑠𝑠𝑠𝑠 − 1.149𝑘𝑘𝑠𝑠𝑠𝑠 = 19.206𝑘𝑘𝑠𝑠𝑠𝑠
∆𝑓𝑓𝑑𝑑𝑝𝑝 = ∆𝑓𝑓𝑑𝑑𝑅𝑅0 + ∆𝑓𝑓𝑑𝑑𝐸𝐸𝑆𝑆 + 𝑓𝑓𝑑𝑑𝑑𝑑𝑔𝑔 + ∆𝑓𝑓𝑑𝑑𝐿𝐿𝑝𝑝 − ∆𝑓𝑓𝑑𝑑𝐸𝐸𝑝𝑝 − ∆𝑓𝑓𝑑𝑑𝑆𝑆𝐿𝐿𝑝𝑝𝐿𝐿
= 1.98𝑘𝑘𝑠𝑠𝑠𝑠 + 20.328𝑘𝑘𝑠𝑠𝑠𝑠 + 0.375𝑘𝑘𝑠𝑠𝑠𝑠 + 19.206𝑘𝑘𝑠𝑠𝑠𝑠 − 8.382𝑘𝑘𝑠𝑠𝑠𝑠 − 3.065𝑘𝑘𝑠𝑠𝑠𝑠 = 30.441𝑘𝑘𝑠𝑠𝑠𝑠
      Elastic Gains
        Superimposed dead loads
𝐸𝐸
𝑑𝑑
𝐸𝐸𝑐𝑐
𝑑𝑑𝑆𝑆𝐿𝐿𝑝𝑝𝐿𝐿 𝑐𝑐𝑔𝑔
′′
𝛥𝛥𝑓𝑓 = 𝛥𝛥𝑓𝑓 = �
28500𝑘𝑘𝑠𝑠𝑠 𝑠
5886.891𝑘𝑘𝑠𝑠𝑠𝑠
� (0.633𝑘𝑘𝑠𝑠𝑠𝑠) = 3.065 𝑘𝑘𝑠𝑠𝑠𝑠
4.7.1.6.2 Live Loads
𝑑𝑑𝐿𝐿𝐿𝐿
𝐸𝐸
𝑃𝑃
𝐸𝐸𝑐𝑐
𝛥𝛥𝑓𝑓 = 𝛥𝛥𝑓𝑓
𝑐𝑐𝑔𝑔
′′′
𝑐𝑐𝑔𝑔
′′′
𝛥𝛥𝑓𝑓 =
𝑀𝑀
𝑠𝑠𝑠𝑠𝑔𝑔𝑐𝑐 𝑠𝑠𝑐𝑐 𝑠𝑠𝑔𝑔
�𝑌𝑌 − 𝑌𝑌 + 𝐴𝐴�
𝐼𝐼𝑐𝑐
59

## Slide 157
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝑐𝑐𝑔𝑔
𝛥𝛥𝑓𝑓′′′ =
⎩
1243570.6𝑠𝑠𝑠𝑠4
(3804.05𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(48.867𝑠𝑠𝑠𝑠 − 35.657𝑠𝑠𝑠𝑠 + 31.477𝑠𝑠𝑠𝑠) 12𝑠𝑠𝑠𝑠
� � = 1.636 𝑘𝑘𝑠𝑠𝑠𝑠 (𝐷𝐷𝐴𝐴𝑠𝑠𝑠𝑠𝑔𝑔𝑠𝑠 𝐿𝐿𝑠𝑠𝑆𝑆𝐴𝐴 𝐿𝐿𝑐𝑐𝐴𝐴𝑑𝑑) 1𝑓𝑓𝑓𝑓
1243570.6𝑠𝑠𝑠𝑠4
(1863.4𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(48.867𝑠𝑠𝑠𝑠 − 35.657𝑠𝑠𝑠𝑠 + 31.477𝑠𝑠𝑠𝑠) 12𝑠𝑠𝑠𝑠
� � = 0.802 𝑘𝑘𝑠𝑠𝑠𝑠 (𝐹𝐹𝐴𝐴𝑓𝑓𝑠𝑠𝑔𝑔𝑎𝑎𝐴𝐴 𝐿𝐿𝑠𝑠𝑆𝑆𝐴𝐴 𝐿𝐿𝑐𝑐𝐴𝐴𝑑𝑑) 1𝑓𝑓𝑓𝑓
𝛥𝛥𝑓𝑓𝑑𝑑𝐿𝐿𝐿𝐿 = �
�
28500𝑘𝑘𝑠𝑠𝑠𝑠
5886.891𝑘𝑘𝑠𝑠𝑠𝑠
� (1.636𝑘𝑘𝑠𝑠𝑠𝑠) = 7.922𝑘𝑘𝑠𝑠𝑠𝑠 (𝐷𝐷𝐴𝐴𝑠𝑠𝑠𝑠𝑔𝑔𝑠𝑠 𝐿𝐿𝑠𝑠𝑆𝑆𝐴𝐴 𝐿𝐿𝑐𝑐𝐴𝐴𝑑𝑑)
�
28500𝑘𝑘𝑠𝑠𝑠𝑠
5886.891𝑘𝑘𝑠𝑠𝑠𝑠
� (0.802𝑘𝑘𝑠𝑠𝑠𝑠) = 3.881𝑘𝑘𝑠𝑠𝑠𝑠 (𝐹𝐹𝐴𝐴𝑓𝑓𝑠𝑠𝑔𝑔𝑎𝑎𝐴𝐴 𝐿𝐿𝑠𝑠𝑆𝑆𝐴𝐴 𝐿𝐿𝑐𝑐𝐴𝐴𝑑𝑑)
    Stresses
      Final Stresses without Live Load
This analysis is for the Service I limit state.
Effective Prestress
𝑃𝑃 = 𝐴𝐴𝑑𝑑𝑠𝑠�𝑓𝑓𝑑𝑑𝑝𝑝 − 𝛥𝛥𝑓𝑓𝑑𝑑𝑅𝑅0 − 𝛥𝛥𝑓𝑓𝑑𝑑𝐸𝐸𝑆𝑆 − ∆𝑓𝑓𝑑𝑑𝑑𝑑𝑔𝑔 − 𝛥𝛥𝑓𝑓𝑑𝑑𝐿𝐿𝑝𝑝 + 𝛥𝛥𝑓𝑓𝑑𝑑𝐸𝐸𝑝𝑝 + 𝛥𝛥𝑓𝑓𝑑𝑑𝑆𝑆𝐿𝐿𝑝𝑝𝐿𝐿 �
𝑃𝑃 = 13.237𝑠𝑠𝑠𝑠2(202.5𝑘𝑘𝑠𝑠𝑠𝑠 − 1.98𝑘𝑘𝑠𝑠𝑠𝑠 − 20.328𝑘𝑘𝑠𝑠𝑠𝑠 − 0.375𝑘𝑘𝑠𝑠𝑠𝑠 − 19.206𝑘𝑘𝑠𝑠𝑠𝑠 + 8.382𝑘𝑘𝑠𝑠𝑠𝑠 + 3.065𝑘𝑘𝑠𝑠𝑠𝑠)
= (13.237𝑠𝑠𝑠𝑠2)(172.059𝑘𝑘𝑠𝑠𝑠𝑠) = 2277.5 𝑘𝑘𝑠𝑠𝑘𝑘
Stress in girder due to effective prestress
𝑃𝑃 𝑃𝑃𝐴𝐴
𝑓𝑓𝑑𝑑𝑠𝑠 = 𝐴𝐴 + 𝑆𝑆
−2277.5𝑘𝑘𝑠𝑠𝑘𝑘
𝑓𝑓𝑑𝑑 = 923.531𝑠𝑠𝑠𝑠2 +
(−2277.5𝑘𝑘𝑠𝑠𝑘𝑘)(31.477𝑠𝑠𝑠𝑠)
−19152.5𝑠𝑠𝑠𝑠3
= 1.277𝑘𝑘𝑠𝑠𝑠𝑠
−2277.5𝑘𝑘𝑠𝑠𝑘𝑘
𝑓𝑓𝑠𝑠 = 923.531𝑠𝑠𝑠𝑠2 +
(−2277.5𝑘𝑘𝑠𝑠𝑘𝑘)(31.477𝑠𝑠𝑠𝑠)
20594.8𝑠𝑠𝑠𝑠3
= −5.947𝑘𝑘𝑠𝑠𝑠𝑠
Stress due to loading
𝑓𝑓 =
(𝑀𝑀𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 + 𝑀𝑀𝑔𝑔𝑔𝑔𝑠𝑠𝑑𝑑ℎ𝑔𝑔𝑠𝑠𝑔𝑔𝑐𝑐 + 𝑀𝑀𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 + 𝑀𝑀ℎ𝑠𝑠𝑎𝑎𝑖𝑖𝑐𝑐ℎ ) �𝑀𝑀𝑠𝑠𝑠𝑠𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 + 𝑀𝑀𝑔𝑔𝑜𝑜𝑒𝑒𝑔𝑔𝑠𝑠𝑠𝑠𝑝𝑝 �
𝑆𝑆 𝑆𝑆
𝑐𝑐
+ + 𝑓𝑓𝑠𝑠𝑠𝑠
𝑓𝑓𝑑𝑑 =
(3368.43 + 140.17 + 2465.61 + 760.28𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) 12𝑠𝑠𝑠𝑠
� � +
1𝑓𝑓𝑓𝑓
−49599.7𝑠𝑠𝑠𝑠3
(732.12 + 739.63𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) 12𝑠𝑠𝑠𝑠
� � − 0.410𝑘𝑘𝑠𝑠𝑠𝑠 1𝑓𝑓𝑓𝑓
−19152.5𝑠𝑠𝑠𝑠3
= −4.986 𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 =
20594.8𝑠𝑠𝑠𝑠3
(3368.43 + 140.17 + 2465.61 + 760.28𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) 12𝑠𝑠𝑠𝑠
� � +
1𝑓𝑓𝑓𝑓
25509.3𝑠𝑠𝑠𝑠3
(732.12 + 0.0𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) 12𝑠𝑠𝑠𝑠
� � + 0.121𝑘𝑘𝑠𝑠𝑠𝑠 = 4.390 𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
This limit state evaluation is for compression stress. Minimize the stress at the bottom of the girder by considering the case before future overlay installation.
Stress Limits Compression
𝑐𝑐
−0.45𝑓𝑓′ = −0.45(8.7𝑘𝑘𝑠𝑠𝑠𝑠) = −3.915𝑘𝑘𝑠𝑠𝑠𝑠
Stress Demand
𝑓𝑓𝑑𝑑 = 1.277𝑘𝑘𝑠𝑠𝑠𝑠 − 4.986𝑘𝑘𝑠𝑠𝑠𝑠 = −3.709 𝑘𝑘𝑠𝑠𝑠𝑠

## Slide 158
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Stresses satisfy the limit state criteria.
      Final Stresses with Live Load
        Service I Limit State
This is a compression stress limit state.
Effective Prestress with Service I live load
𝑃𝑃 = 𝐴𝐴𝑑𝑑𝑠𝑠�𝑓𝑓𝑑𝑑𝑝𝑝 − 𝛥𝛥𝑓𝑓𝑑𝑑𝑅𝑅0 − 𝛥𝛥𝑓𝑓𝑑𝑑𝐸𝐸𝑆𝑆 − ∆𝑓𝑓𝑑𝑑𝑑𝑑𝑔𝑔 − 𝛥𝛥𝑓𝑓𝑑𝑑𝐿𝐿𝑝𝑝 + 𝛥𝛥𝑓𝑓𝑑𝑑𝐸𝐸𝑝𝑝 + 𝛥𝛥𝑓𝑓𝑑𝑑𝑆𝑆𝐿𝐿𝑝𝑝𝐿𝐿 + 𝛥𝛥𝑓𝑓𝑑𝑑𝐿𝐿𝐿𝐿 �
𝑃𝑃 = 13.237𝑠𝑠𝑠𝑠2(202.5𝑘𝑘𝑠𝑠𝑠𝑠 − 1.98𝑘𝑘𝑠𝑠𝑠𝑠 − 20.328𝑘𝑘𝑠𝑠𝑠𝑠 − 0.375𝑘𝑘𝑠𝑠𝑠𝑠 − 19.206𝑘𝑘𝑠𝑠𝑠𝑠 + 8.382𝑘𝑘𝑠𝑠𝑠𝑠 + 3.065𝑘𝑘𝑠𝑠𝑠𝑠 + 7.922 𝑘𝑘𝑠𝑠𝑠𝑠)
= (13.237𝑠𝑠𝑠𝑠2)(179.98𝑘𝑘𝑠𝑠𝑠𝑠) = 2382.4 𝑘𝑘𝑠𝑠𝑘𝑘
Stress in girder due to effective prestress
𝑃𝑃 𝑃𝑃𝐴𝐴
𝑓𝑓𝑑𝑑𝑠𝑠 = 𝐴𝐴 + 𝑆𝑆
−2382.4𝑘𝑘𝑠𝑠𝑘𝑘 (−2382.4𝑘𝑘𝑠𝑠𝑘𝑘)(31.477𝑠𝑠𝑠𝑠)
𝑓𝑓𝑑𝑑 = 923.531𝑠𝑠𝑠𝑠2 + −19152.5𝑠𝑠𝑠𝑠3
= 1.324𝑘𝑘𝑠𝑠𝑠𝑠
Stress due to loading
𝑓𝑓 =
(𝑀𝑀𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 + 𝑀𝑀𝑔𝑔𝑔𝑔𝑠𝑠𝑑𝑑ℎ𝑔𝑔𝑠𝑠𝑔𝑔𝑐𝑐 + 𝑀𝑀𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 + 𝑀𝑀ℎ𝑠𝑠𝑎𝑎𝑖𝑖𝑐𝑐ℎ ) �𝑀𝑀𝑠𝑠𝑠𝑠𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 + 𝑀𝑀𝑔𝑔𝑜𝑜𝑒𝑒𝑔𝑔𝑠𝑠𝑠𝑠𝑝𝑝 + 𝑀𝑀𝑠𝑠𝑠𝑠𝑔𝑔𝑐𝑐 �
𝑆𝑆 𝑆𝑆
𝑐𝑐
+ + 𝑓𝑓𝑠𝑠𝑠𝑠
𝑓𝑓𝑑𝑑 =
(3368.43 + 140.17 + 2465.61 + 760.28𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) 12𝑠𝑠𝑠𝑠
� � +
1𝑓𝑓𝑓𝑓
−49599.7𝑠𝑠𝑠𝑠3
(732.12 + 739.63 + 3804.05𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) 12𝑠𝑠𝑠𝑠
� � − 0.410𝑘𝑘𝑠𝑠𝑠𝑠 1𝑓𝑓𝑓𝑓
−19152.5𝑠𝑠𝑠𝑠3
= −5.906 𝑘𝑘𝑠𝑠𝑠𝑠
This limit state evaluation is for compression stress. Minimize the stress at the bottom of the girder by considering the case before future overlay installation and live load not on the structure.
Stress Limits Compression
𝑐𝑐
−0.6𝑓𝑓′ = −0.6(8.7𝑘𝑘𝑠𝑠𝑠𝑠) = −5.220𝑘𝑘𝑠𝑠𝑠𝑠
Stress Demand
𝑓𝑓𝑑𝑑 = (1.325𝑘𝑘𝑠𝑠𝑠𝑠 − 5.906𝑘𝑘𝑠𝑠𝑠𝑠) = −4.570 𝑘𝑘𝑠𝑠𝑠𝑠
Stresses are within limits
4.7.2.2.2 Service III Limit State
This is a tension stress limit state.
Effective Prestress with Service III live load
𝑃𝑃 = 𝐴𝐴𝑑𝑑𝑠𝑠�𝑓𝑓𝑑𝑑𝑝𝑝 − 𝛥𝛥𝑓𝑓𝑑𝑑𝑅𝑅0 − 𝛥𝛥𝑓𝑓𝑑𝑑𝐸𝐸𝑆𝑆 − ∆𝑓𝑓𝑑𝑑𝑑𝑑𝑔𝑔 − 𝛥𝛥𝑓𝑓𝑑𝑑𝐿𝐿𝑝𝑝 + 𝛥𝛥𝑓𝑓𝑑𝑑𝐸𝐸𝑝𝑝 + 𝛥𝛥𝑓𝑓𝑑𝑑𝑆𝑆𝐿𝐿𝑝𝑝𝐿𝐿 + 0.8𝛥𝛥𝑓𝑓𝑑𝑑𝐿𝐿𝐿𝐿�
𝑃𝑃 = 13.237𝑠𝑠𝑠𝑠2(202.5𝑘𝑘𝑠𝑠𝑠𝑠 − 1.98𝑘𝑘𝑠𝑠𝑠𝑠 − 20.328𝑘𝑘𝑠𝑠𝑠𝑠 − 0.375𝑘𝑘𝑠𝑠𝑠𝑠 − 19.206𝑘𝑘𝑠𝑠𝑠𝑠 + 8.382𝑘𝑘𝑠𝑠𝑠𝑠 + 3.065𝑘𝑘𝑠𝑠𝑠𝑠 + (0.8)7.922 𝑘𝑘𝑠𝑠𝑠𝑠)
= (13.237𝑠𝑠𝑠𝑠2)(178.397𝑘𝑘𝑠𝑠𝑠𝑠) = 2361.4 𝑘𝑘𝑠𝑠𝑘𝑘
Stress in girder due to effective prestress
𝑃𝑃 𝑃𝑃𝐴𝐴
𝑓𝑓𝑑𝑑𝑠𝑠 = 𝐴𝐴 + 𝑆𝑆

## Slide 159
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
−2361.4𝑘𝑘𝑠𝑠𝑘𝑘
𝑓𝑓𝑠𝑠 = 923.531𝑠𝑠𝑠𝑠2 +
(−2361.4𝑘𝑘𝑠𝑠𝑘𝑘)(31.477𝑠𝑠𝑠𝑠)
20594.8𝑠𝑠𝑠𝑠3
= −6.166𝑘𝑘𝑠𝑠𝑠𝑠
Stress due to loading
𝑓𝑓 =
(𝑀𝑀𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 + 𝑀𝑀𝑔𝑔𝑔𝑔𝑠𝑠𝑑𝑑ℎ𝑔𝑔𝑠𝑠𝑔𝑔𝑐𝑐 + 𝑀𝑀𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 + 𝑀𝑀ℎ𝑠𝑠𝑎𝑎𝑖𝑖𝑐𝑐ℎ ) �𝑀𝑀𝑠𝑠𝑠𝑠𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 + 𝑀𝑀𝑔𝑔𝑜𝑜𝑒𝑒𝑔𝑔𝑠𝑠𝑠𝑠𝑝𝑝 + 0.8𝑀𝑀𝑠𝑠𝑠𝑠𝑔𝑔𝑐𝑐 �
𝑆𝑆 𝑆𝑆
𝑐𝑐
+ + 𝑓𝑓𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 =
(3368.43 + 140.17 + 2465.61 + 760.28𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) 12𝑠𝑠𝑠𝑠
� � +
1𝑓𝑓𝑓𝑓 25509.3𝑠𝑠𝑠𝑠3
(732.12 + 0.0 + (0.8)3804.05𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) 12𝑠𝑠𝑠𝑠
� � + 0.121𝑘𝑘𝑠𝑠𝑠𝑠 1𝑓𝑓𝑓𝑓
20594.8𝑠𝑠𝑠𝑠3
= 6.169 𝑘𝑘𝑠𝑠𝑠𝑠
Stress Limits
The tension stress limit is 0.0 ksi per WSDOT BDM Stress Demand
𝑓𝑓𝑑𝑑 = (−6.166𝑘𝑘𝑠𝑠𝑠𝑠 − 6.169𝑘𝑘𝑠𝑠𝑠𝑠) = 0.003 𝑘𝑘𝑠𝑠𝑠𝑠 ≈ 0𝑘𝑘𝑠𝑠𝑠𝑠
Stresses are within limits
Check the assumed effective prestress of 85% (15% loss).
𝑓𝑓𝑑𝑑𝑒𝑒
𝑓𝑓𝑑𝑑𝑝𝑝
=
178.397
202.5
= 0.88 = 88% ≈ 85%
𝑓𝑓𝑑𝑑𝑒𝑒
𝐿𝐿𝑐𝑐𝑠𝑠𝑠𝑠 = 1 − = 1 − 0.88 = 0.12 = 12% ≈ 15%
𝑓𝑓𝑑𝑑𝑝𝑝
4.7.2.2.3 Fatigue I Limit State
Effective Prestress with Fatigue I live load
𝑃𝑃 = 𝐴𝐴𝑑𝑑𝑠𝑠�𝑓𝑓𝑑𝑑𝑝𝑝 − 𝛥𝛥𝑓𝑓𝑑𝑑𝑅𝑅0 − 𝛥𝛥𝑓𝑓𝑑𝑑𝐸𝐸𝑆𝑆 − ∆𝑓𝑓𝑑𝑑𝑑𝑑𝑔𝑔 − 𝛥𝛥𝑓𝑓𝑑𝑑𝐿𝐿𝑝𝑝 + 𝛥𝛥𝑓𝑓𝑑𝑑𝐸𝐸𝑝𝑝 + 𝛥𝛥𝑓𝑓𝑑𝑑𝑆𝑆𝐿𝐿𝑝𝑝𝐿𝐿 + 1.5𝛥𝛥𝑓𝑓𝑑𝑑𝐿𝐿𝐿𝐿�
𝑃𝑃 = 13.237𝑠𝑠𝑠𝑠2(202.5𝑘𝑘𝑠𝑠𝑠𝑠 − 1.98𝑘𝑘𝑠𝑠𝑠𝑠 − 20.328𝑘𝑘𝑠𝑠𝑠𝑠 − 0.375𝑘𝑘𝑠𝑠𝑠𝑠 − 19.206𝑘𝑘𝑠𝑠𝑠𝑠 + 8.382𝑘𝑘𝑠𝑠𝑠𝑠 + 3.065𝑘𝑘𝑠𝑠𝑠𝑠 + (1.5)3.881 𝑘𝑘𝑠𝑠𝑠𝑠)
= (13.237𝑠𝑠𝑠𝑠2)(177.88𝑘𝑘𝑠𝑠𝑠𝑠) = 2354.6 𝑘𝑘𝑠𝑠𝑘𝑘
Stress in girder due to effective prestress
𝑃𝑃 𝑃𝑃𝐴𝐴
𝑓𝑓𝑑𝑑𝑠𝑠 = 𝐴𝐴 + 𝑆𝑆
−2354.6𝑘𝑘𝑠𝑠𝑘𝑘 (−2354.6𝑘𝑘𝑠𝑠𝑘𝑘)(31.477𝑠𝑠𝑠𝑠)
𝑓𝑓𝑑𝑑 = 923.531𝑠𝑠𝑠𝑠2 + −19152.5𝑠𝑠𝑠𝑠3
= 1.327𝑘𝑘𝑠𝑠𝑠𝑠
Stress due to loading
𝑓𝑓 =
+
0.5(𝑀𝑀𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 + 𝑀𝑀𝑔𝑔𝑔𝑔𝑠𝑠𝑑𝑑ℎ𝑔𝑔𝑠𝑠𝑔𝑔𝑐𝑐 + 𝑀𝑀𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 + 𝑀𝑀ℎ𝑠𝑠𝑎𝑎𝑖𝑖𝑐𝑐ℎ ) 0.5�𝑀𝑀𝑠𝑠𝑠𝑠𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 + 𝑀𝑀𝑔𝑔𝑜𝑜𝑒𝑒𝑔𝑔𝑠𝑠𝑠𝑠𝑝𝑝 �
𝑆𝑆 𝑆𝑆
+ 0.5𝑓𝑓𝑠𝑠𝑠𝑠 +
1.5𝑀𝑀𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿
𝑆𝑆
𝑐𝑐 𝑐𝑐
𝑓𝑓𝑑𝑑 =
0.5(3368.43 + 140.17 + 2465.61 + 760.28𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) 12𝑠𝑠𝑠𝑠
� � +
1𝑓𝑓𝑓𝑓 −49599.7𝑠𝑠𝑠𝑠3
0.5(732.12 + 739.63𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) 12𝑠𝑠𝑠𝑠
� �
1𝑓𝑓𝑓𝑓
−19152.5𝑠𝑠𝑠𝑠3
+ (0.5)(−0.410𝑘𝑘𝑠𝑠𝑠𝑠) +
−49599.7𝑠𝑠𝑠𝑠3
1.5(1863.4𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) 12𝑠𝑠𝑠𝑠
� � = −3.282 𝑘𝑘𝑠𝑠𝑠𝑠
1𝑓𝑓𝑓𝑓
Stress Demand
𝑓𝑓𝑑𝑑 = 0.5(1.327 𝑘𝑘𝑠𝑠𝑠𝑠) − 3.282𝑘𝑘𝑠𝑠𝑠𝑠 = −2.619 𝑘𝑘𝑠𝑠𝑠𝑠
Stress limit
𝑐𝑐
−0.4𝑓𝑓′ = −0.4(8.7𝑘𝑘𝑠𝑠𝑠𝑠) = −3.480𝑘𝑘𝑠𝑠𝑠𝑠
Stresses are within limits

## Slide 160
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
    Moment Capacity
      Compute Nominal Moment Capacity at 0.5Lg.
Strength I limit state
𝑆𝑆𝑓𝑓𝐴𝐴𝐴𝐴𝑠𝑠𝑔𝑔𝑓𝑓ℎ 𝐼𝐼 = 1.25𝐷𝐷𝐷𝐷 + 1.5𝐷𝐷𝐻𝐻 + 1.75(𝐿𝐿𝐿𝐿 + 𝐼𝐼𝑀𝑀)
𝑀𝑀𝑎𝑎 = 1.25(3368.43 + 140.17 + 2465.61 + 760.28 + 732.12) + 1.50(739.63) + 1.75(3804.05) = 17099.8𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑐𝑐 =
𝐴𝐴𝑑𝑑𝑠𝑠𝑓𝑓𝑑𝑑𝑎𝑎 − 𝛼𝛼1𝑓𝑓′(𝑠𝑠 − 𝑠𝑠 )ℎ
𝑐𝑐 𝑤𝑤 𝑒𝑒
′
𝛼𝛼 𝑓𝑓 𝛽𝛽 𝑠𝑠 + 𝑘𝑘𝐴𝐴
1 𝑐𝑐 1 𝑤𝑤 𝑑𝑑𝑠𝑠
𝑓𝑓𝑑𝑑𝑎𝑎
𝑑𝑑
𝑑𝑑
𝑓𝑓𝑑𝑑𝑝𝑝
𝑓𝑓𝑑𝑑𝑎𝑎
243
270
𝑘𝑘 = 2 �1.04 − � = 2 �1.04 − � = 0.28
𝑑𝑑𝑠𝑠 𝑑𝑑𝑎𝑎
𝑐𝑐
𝑑𝑑
𝑑𝑑
𝑓𝑓 = 𝑓𝑓 �1 − 𝑘𝑘 �
𝑐𝑐 =
𝛼𝛼1 = 0.85
𝑑𝑑𝑑𝑑 = 𝑌𝑌𝑑𝑑 + 𝐴𝐴 + 𝑓𝑓𝑠𝑠 = 38.343𝑠𝑠𝑠𝑠 + 31.477𝑠𝑠𝑠𝑠 + 7𝑠𝑠𝑠𝑠 = 76.82𝑠𝑠𝑠𝑠 (13.237𝑠𝑠𝑠𝑠2)(270𝑘𝑘𝑠𝑠𝑠𝑠) − 0.85(4𝑘𝑘𝑠𝑠𝑠𝑠)(84𝑠𝑠𝑠𝑠 − 6.125𝑠𝑠𝑠𝑠)(7𝑠𝑠𝑠𝑠) 1720.565𝑘𝑘𝑠𝑠𝑘𝑘
270𝑘𝑘𝑠𝑠𝑠𝑠 𝑘𝑘
0.85(4𝑘𝑘𝑠𝑠𝑠𝑠)(0.85)(6.125𝑠𝑠𝑠𝑠) + (0.28)(13.237𝑠𝑠𝑠𝑠2) �76.82𝑠𝑠𝑠𝑠� 17.7 𝑠𝑠𝑠𝑠 + 13.0 𝑠𝑠𝑠𝑠
= 𝑘𝑘 = 56.04𝑠𝑠𝑠𝑠
56.04𝑠𝑠𝑠𝑠
𝑓𝑓𝑑𝑑𝑠𝑠 = 270𝑘𝑘𝑠𝑠𝑠𝑠 �1 − 0.28 76.82𝑠𝑠𝑠𝑠� = 214.85𝑘𝑘𝑠𝑠𝑠𝑠
𝐴𝐴 = 𝛽𝛽1𝑐𝑐 = 0.85(56.04𝑠𝑠𝑠𝑠) = 47.63𝑠𝑠𝑠𝑠
2
𝑖𝑖 𝑑𝑑𝑠𝑠 𝑑𝑑𝑠𝑠 𝑑𝑑 1 𝑐𝑐
′
𝑤𝑤 𝑒𝑒
𝐴𝐴 𝐴𝐴 ℎ
𝑒𝑒
2 2
𝑀𝑀 = 𝐴𝐴 𝑓𝑓 �𝑑𝑑 − � + 𝛼𝛼 𝑓𝑓 (𝑠𝑠 − 𝑠𝑠 )ℎ � − �
𝑖𝑖
47.63𝑠𝑠𝑠𝑠
𝑀𝑀 = (13.237𝑠𝑠𝑠𝑠2)(214.85𝑘𝑘𝑠𝑠𝑠𝑠) �76.82𝑠𝑠𝑠𝑠 − � + 0.85(4𝑘𝑘𝑠𝑠𝑠𝑠)(
84𝑠𝑠𝑠𝑠 − 6.125𝑠𝑠𝑠𝑠
7𝑠𝑠𝑠𝑠 �
2 2
47.63𝑠𝑠𝑠𝑠 7𝑠𝑠𝑠𝑠
)( ) − �
2
= 188396.9𝑘𝑘 ∙ 𝑠𝑠𝑠𝑠 = 15699.7𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑑𝑑𝑑𝑑 = 74𝑠𝑠𝑠𝑠 + 7𝑠𝑠𝑠𝑠 − 2𝑠𝑠𝑠𝑠 = 79𝑠𝑠𝑠𝑠
𝜀𝜀𝑑𝑑 = 0.003
𝑑𝑑𝑑𝑑 − 𝑐𝑐 79 − 56.04
𝑐𝑐 56.04
= 0.003 = 0.00123
(𝜀𝜀𝑑𝑑 − 𝜀𝜀𝑐𝑐𝑠𝑠 )
0.75 ≤ 𝜙𝜙 = 0.75 + 0.25 (𝜀𝜀 − 𝜀𝜀 ) ≤ 1.0
𝜙𝜙 = 0.75 +
𝑑𝑑𝑠𝑠 𝑐𝑐𝑠𝑠
0.25(0.00123 − 0.002)
(0.005 − 0.002)
= 0.686, 𝑎𝑎𝑠𝑠𝐴𝐴 0.75
𝑀𝑀𝑔𝑔 = 𝜙𝜙𝑀𝑀𝑖𝑖 = 0.75(15699.7𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) = 11774.8𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀𝑔𝑔 < 𝑀𝑀𝑎𝑎 No Good
The AASHTO method for computing moment capacity does not account for the large compression flange in the girder or the higher strength of the girder concrete. See Reference 7 for more information. PGSuper uses strain compatibility analysis to compute the moment capacity.
Stress-strain relationship for prestressing strands:

## Slide 161
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
⎢
⎣
⎡
𝑓𝑓𝑑𝑑𝑠𝑠 = 𝜀𝜀𝑑𝑑𝑠𝑠 ⎢877 +
27,613
�1 + �112.4𝜀𝜀
𝑑𝑑𝑠𝑠
⎦
7.36 7.36⎥
� �
⎤
1 ⎥ ≤ 270𝑘𝑘𝑠𝑠𝑠𝑠
Stress-strain relationship for concrete:
𝑓𝑓 = 𝑓𝑓
𝑐𝑐 𝑐𝑐
′ 𝑐 𝑐
𝜀𝜀′
𝜀𝜀𝑐𝑐𝑒𝑒
𝑠𝑠 � �
𝜀𝜀
𝑐𝑐
′
𝑠𝑠 − 1 + � �
𝜀𝜀𝑐𝑐𝑒𝑒 𝑖𝑖𝑑𝑑
where
𝑠𝑠 = 0.8 +
𝑐𝑐
𝑓𝑓′
2500
𝑘𝑘 = 0.67 +
𝑐𝑐
𝑓𝑓′
9000
𝜀𝜀𝑐𝑐𝑒𝑒
𝜀𝜀
𝑐𝑐
′
𝑠𝑠𝑓𝑓 < 1.0, 𝑘𝑘 = 1.0
𝑐𝑐
𝐸𝐸 =
𝑐𝑐
40,000�𝑓𝑓′ + 1,000,000
1000
𝑐𝑐
𝜀𝜀′ 𝑤𝑤1000 = 𝑐𝑐
𝑓𝑓′
𝑠𝑠
𝐸𝐸𝑐𝑐 𝑠𝑠 − 1
Effective prestress, 𝑓𝑓𝑑𝑑𝑒𝑒 = 𝑓𝑓𝑑𝑑𝑝𝑝 − 𝛥𝛥𝑓𝑓𝑑𝑑𝑝𝑝 = 202.5𝑘𝑘𝑠𝑠𝑠𝑠 − 30.441𝑘𝑘𝑠𝑠𝑠𝑠 = 172.059𝑘𝑘𝑠𝑠𝑠𝑠
Initial strain in prestressing strand, sometimes referred to as the decompression strain, is, 𝜀𝜀
𝑑𝑑𝑠𝑠𝑔𝑔
𝐸𝐸𝑝𝑝 28500𝑑𝑑𝑠𝑠𝑔𝑔
𝑒𝑒𝑝𝑝𝑒𝑒
= = 172.059𝑑𝑑𝑠𝑠𝑔𝑔 =
6.037𝑤𝑤10−3
Discretize the composite girder section into “slices”. Compute the strain at the centroid of each slice. The stress in the slice is determined from the stress-strain relationship for the slice material. Finally, compute the axial force and moment contribution for each slice. Sum the contribution of each slice to determine the capacity of the section.

## Slide 162
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Figure 4-9: Discretized Girder Section for Strain Compatibility Analysis Table 4-1: Strain compatibility analysis details
Slice | Piece | Area (in2) | Ytop (in) | Ybot (in) | Ycg (in) | fpe (KSI) | Initial Strain | Incremental Strain | Total Strain | Stress (Fg - Bg) (KSI) | dF = (Area)(Stress) (kip) | dM = (dF)(Ycg) (kip-ft)
1 | Deck | 340.168 | 7.000 | 2.950 | 4.975 |  | 0 | -0.00259832 | -0.00259832 | -3.590 | -1221.16 | -506.27
2 | Deck | 247.777 | 2.950 | 0.000 | 1.475 |  | 0 | -0.00190406 | -0.00190406 | -3.999 | -990.83 | -121.79
3 | Girder | 98.000 | 0.000 | -2.000 | -1.000 |  | 0 | -0.00141312 | -0.00141312 | -6.481 | -635.09 | 52.92
4 | Girder | 159.696 | -2.000 | -7.850 | -3.995 |  | 0 | -0.000818991 | -0.000818991 | -3.863 | -616.87 | 205.38
5 | Girder | 2.233 | -7.850 | -8.124 | -7.985 |  | 0 | -2.748e-05 | -2.748e-05 | -0.130 | -0.29 | 0.19
6 | Girder | 40.433 | -8.124 | -14.600 | -11.306 |  | 0 | 0.000631199 | 0.000631199 | 0.000 | 0.00 | 0.00
7 | Girder | 46.856 | -14.600 | -22.250 | -18.425 |  | 0 | 0.00204331 | 0.00204331 | 0.000 | 0.00 | 0.00
8 | Girder | 52.369 | -22.250 | -30.800 | -26.525 |  | 0 | 0.00365003 | 0.00365003 | 0.000 | 0.00 | 0.00
9 | Girder | 57.881 | -30.800 | -40.250 | -35.525 |  | 0 | 0.00543527 | 0.00543527 | 0.000 | 0.00 | 0.00
10 | Girder | 63.394 | -40.250 | -50.600 | -45.425 |  | 0 | 0.00739903 | 0.00739903 | 0.000 | 0.00 | 0.00
11 | Girder | 69.132 | -50.600 | -61.850 | -56.243 |  | 0 | 0.00954486 | 0.00954486 | 0.000 | 0.00 | 0.00
12 | Straight Strand 44 | 0.217 | -66.000 | -66.000 | -66.000 | 172.059 | 0.00603715 | 0.0114803 | 0.0175174 | 260.978 | 56.63 | -311.48
13 | Straight Strand 43 | 0.217 | -66.000 | -66.000 | -66.000 | 172.059 | 0.00603715 | 0.0114803 | 0.0175174 | 260.978 | 56.63 | -311.48
14 | Harped Strand 15 | 0.217 | -67.000 | -67.000 | -67.000 | 172.059 | 0.00603715 | 0.0116787 | 0.0177158 | 261.172 | 56.67 | -316.43
15 | Harped Strand 14 | 0.217 | -67.000 | -67.000 | -67.000 | 172.059 | 0.00603715 | 0.0116787 | 0.0177158 | 261.172 | 56.67 | -316.43
16 | Harped Strand 13 | 0.217 | -67.000 | -67.000 | -67.000 | 172.059 | 0.00603715 | 0.0116787 | 0.0177158 | 261.172 | 56.67 | -316.43
17 | Harped Strand 16 | 0.217 | -67.000 | -67.000 | -67.000 | 172.059 | 0.00603715 | 0.0116787 | 0.0177158 | 261.172 | 56.67 | -316.43
18 | Harped Strand 17 | 0.217 | -67.000 | -67.000 | -67.000 | 172.059 | 0.00603715 | 0.0116787 | 0.0177158 | 261.172 | 56.67 | -316.43
19 | Straight Strand 35 | 0.217 | -68.000 | -68.000 | -68.000 | 172.059 | 0.00603715 | 0.011877 | 0.0179142 | 261.364 | 56.72 | -321.39
20 | Straight Strand 34 | 0.217 | -68.000 | -68.000 | -68.000 | 172.059 | 0.00603715 | 0.011877 | 0.0179142 | 261.364 | 56.72 | -321.39
21 | Straight Strand 37 | 0.217 | -68.000 | -68.000 | -68.000 | 172.059 | 0.00603715 | 0.011877 | 0.0179142 | 261.364 | 56.72 | -321.39

## Slide 163
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Slice | Piece | Area (in2) | Ytop (in) | Ybot (in) | Ycg (in) | fpe (KSI) | Initial Strain | Incremental Strain | Total Strain | Stress (Fg - Bg) (KSI) | dF = (Area)(Stress) (kip) | dM = (dF)(Ycg) (kip-ft)
22 | Straight Strand 33 | 0.217 | -68.000 | -68.000 | -68.000 | 172.059 | 0.00603715 | 0.011877 | 0.0179142 | 261.364 | 56.72 | -321.39
23 | Straight Strand 42 | 0.217 | -68.000 | -68.000 | -68.000 | 172.059 | 0.00603715 | 0.011877 | 0.0179142 | 261.364 | 56.72 | -321.39
24 | Straight Strand 41 | 0.217 | -68.000 | -68.000 | -68.000 | 172.059 | 0.00603715 | 0.011877 | 0.0179142 | 261.364 | 56.72 | -321.39
25 | Straight Strand 40 | 0.217 | -68.000 | -68.000 | -68.000 | 172.059 | 0.00603715 | 0.011877 | 0.0179142 | 261.364 | 56.72 | -321.39
26 | Straight Strand 39 | 0.217 | -68.000 | -68.000 | -68.000 | 172.059 | 0.00603715 | 0.011877 | 0.0179142 | 261.364 | 56.72 | -321.39
27 | Straight Strand 38 | 0.217 | -68.000 | -68.000 | -68.000 | 172.059 | 0.00603715 | 0.011877 | 0.0179142 | 261.364 | 56.72 | -321.39
28 | Straight Strand 36 | 0.217 | -68.000 | -68.000 | -68.000 | 172.059 | 0.00603715 | 0.011877 | 0.0179142 | 261.364 | 56.72 | -321.39
29 | Girder | 333.537 | -61.850 | -74.000 | -69.327 |  | 0 | 0.0121403 | 0.0121403 | 0.000 | 0.00 | 0.00
30 | Straight Strand 8 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
31 | Straight Strand 21 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
32 | Straight Strand 22 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
33 | Straight Strand 23 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
34 | Straight Strand 24 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
35 | Straight Strand 25 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
36 | Straight Strand 26 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
37 | Straight Strand 27 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
38 | Straight Strand 28 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
39 | Straight Strand 29 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
40 | Straight Strand 30 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
41 | Straight Strand 31 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
42 | Straight Strand 32 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
43 | Harped Strand 2 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
44 | Harped Strand 3 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
45 | Harped Strand 4 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
46 | Harped Strand 5 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
47 | Harped Strand 6 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
48 | Harped Strand 7 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
49 | Harped Strand 8 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
50 | Harped Strand 9 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
51 | Harped Strand 1 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
52 | Harped Strand 11 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
53 | Harped Strand 12 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
54 | Straight Strand 1 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
55 | Straight Strand 2 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
56 | Straight Strand 7 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
57 | Harped Strand 10 | 0.217 | -70.000 | -70.000 | -70.000 | 172.059 | 0.00603715 | 0.0122737 | 0.0183109 | 261.745 | 56.80 | -331.33
58 | Straight Strand 17 | 0.217 | -72.000 | -72.000 | -72.000 | 172.059 | 0.00603715 | 0.0126705 | 0.0187076 | 262.121 | 56.88 | -341.28
59 | Straight Strand 16 | 0.217 | -72.000 | -72.000 | -72.000 | 172.059 | 0.00603715 | 0.0126705 | 0.0187076 | 262.121 | 56.88 | -341.28
60 | Straight Strand 19 | 0.217 | -72.000 | -72.000 | -72.000 | 172.059 | 0.00603715 | 0.0126705 | 0.0187076 | 262.121 | 56.88 | -341.28
61 | Straight Strand 15 | 0.217 | -72.000 | -72.000 | -72.000 | 172.059 | 0.00603715 | 0.0126705 | 0.0187076 | 262.121 | 56.88 | -341.28
62 | Straight Strand 14 | 0.217 | -72.000 | -72.000 | -72.000 | 172.059 | 0.00603715 | 0.0126705 | 0.0187076 | 262.121 | 56.88 | -341.28
63 | Straight Strand 13 | 0.217 | -72.000 | -72.000 | -72.000 | 172.059 | 0.00603715 | 0.0126705 | 0.0187076 | 262.121 | 56.88 | -341.28
64 | Straight Strand 12 | 0.217 | -72.000 | -72.000 | -72.000 | 172.059 | 0.00603715 | 0.0126705 | 0.0187076 | 262.121 | 56.88 | -341.28
65 | Straight Strand 11 | 0.217 | -72.000 | -72.000 | -72.000 | 172.059 | 0.00603715 | 0.0126705 | 0.0187076 | 262.121 | 56.88 | -341.28
66 | Straight Strand 10 | 0.217 | -72.000 | -72.000 | -72.000 | 172.059 | 0.00603715 | 0.0126705 | 0.0187076 | 262.121 | 56.88 | -341.28
67 | Straight Strand 5 | 0.217 | -72.000 | -72.000 | -72.000 | 172.059 | 0.00603715 | 0.0126705 | 0.0187076 | 262.121 | 56.88 | -341.28
68 | Straight Strand 4 | 0.217 | -72.000 | -72.000 | -72.000 | 172.059 | 0.00603715 | 0.0126705 | 0.0187076 | 262.121 | 56.88 | -341.28
69 | Straight Strand 3 | 0.217 | -72.000 | -72.000 | -72.000 | 172.059 | 0.00603715 | 0.0126705 | 0.0187076 | 262.121 | 56.88 | -341.28

## Slide 164
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Slice | Piece | Area (in2) | Ytop (in) | Ybot (in) | Ycg (in) | fpe (KSI) | Initial Strain | Incremental Strain | Total Strain | Stress (Fg - Bg) (KSI) | dF = (Area)(Stress) (kip) | dM = (dF)(Ycg) (kip-ft)
70 | Straight Strand 9 | 0.217 | -72.000 | -72.000 | -72.000 | 172.059 | 0.00603715 | 0.0126705 | 0.0187076 | 262.121 | 56.88 | -341.28
71 | Straight Strand 6 | 0.217 | -72.000 | -72.000 | -72.000 | 172.059 | 0.00603715 | 0.0126705 | 0.0187076 | 262.121 | 56.88 | -341.28
72 | Straight Strand 20 | 0.217 | -72.000 | -72.000 | -72.000 | 172.059 | 0.00603715 | 0.0126705 | 0.0187076 | 262.121 | 56.88 | -341.28
73 | Straight Strand 18 | 0.217 | -72.000 | -72.000 | -72.000 | 172.059 | 0.00603715 | 0.0126705 | 0.0187076 | 262.121 | 56.88 | -341.28
Resultant Force = (F) = 0.00 kip
Resultant Moment = (M) = -20526.2 kip-ft Depth to neutral axis, c = 15.124 in
Compression Resultant, C = -3464.24 kip
Depth to Compression Resultant, dc =5.720 in
Tension Resultant, T = 3464.24 kip
Depth to Tension Resultant, de = 76.822 in Net tensile strain, εt = 12.7x10−3 Nominal Capacity, Mn = 20526.2 kip-ft Moment Arm, de - dc = Mn/T = 71.102 in
(𝜀𝜀𝑑𝑑 − 𝜀𝜀𝑐𝑐𝑠𝑠 )
0.75 ≤ 𝜙𝜙 = 0.75 + 0.25 (𝜀𝜀 − 𝜀𝜀 ) ≤ 1.0
𝜙𝜙 = 0.75 +
𝑑𝑑𝑠𝑠 𝑐𝑐𝑠𝑠
0.25(0.0127 − 0.002)
(0.005 − 0.002)
= 1.64, 𝑎𝑎𝑠𝑠𝐴𝐴 1.0
𝑀𝑀𝑔𝑔 = 1.0(20526.2)𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 ≥ 𝑀𝑀𝑎𝑎 = 17099.8𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 OK
The Moment Capacity Detail report from PGSuper provides the details of the moment capacity strain compatibility analysis.
The total strain in the reinforcement is the sum of the net tensile strain = 12.7x10−3 and the initial strain 6.037x10−3. The total strain is 18.7x10−3 = 1.87%. This is less than the minimum required elongation of 3.5% for A416 strand.
4.7.3.2 Minimum Reinforcement and the Cracking Moment
To insure there is sufficient reinforcement in the section to achieve ductile behavior, a minimum amount of reinforcement is required. The minimum reinforcement is such that any section in the girder shall have adequate prestressed reinforcement to develop a factored flexural resistance, Mr, which is at least the lesser of the cracking strength or 133% of the ultimate moment. (LRFD 5.6.3.3)
𝑀𝑀𝑔𝑔 𝑐𝑐𝑔𝑔𝑖𝑖 = 𝑘𝑘𝐴𝐴𝑠𝑠𝑠𝑠𝐴𝐴𝐴𝐴 𝑐𝑐𝑓𝑓 �
𝑀𝑀𝑐𝑐𝑔𝑔
1.33𝑀𝑀𝑎𝑎
The cracking moment is
𝑆𝑆𝑐𝑐
𝑆𝑆𝑠𝑠
𝑀𝑀𝑐𝑐𝑔𝑔 = 𝛾𝛾3 ��𝛾𝛾1𝑓𝑓𝑔𝑔 + 𝛾𝛾2𝑓𝑓𝑐𝑐𝑑𝑑𝑒𝑒 �𝑆𝑆𝑐𝑐 − 𝑀𝑀𝑔𝑔𝑖𝑖𝑐𝑐 � − 1��
where:
fr | = | Modulus of rupture
fcpe | = | Compressive stress due to prestressing at the bottom of the girder
Sc | = | Bottom section modulus of the composite section

## Slide 165
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Sb | = | Bottom section modulus of the non-composite section
Mdnc | = | Dead load moment resisted by the non-composite section
γ1 | = | Flexural cracking variability factor = 1.6
γ2 | = | Prestress variability factor = 1.0
γ3 | = | Ratio of specified minimum yield strength to ultimate tensile strength of the reinforcement = 1.0 for prestressed concrete
4.7.3.2.1 Compute cracking moment at 0.5Lg.
𝑐𝑐
𝑓𝑓𝑔𝑔 = 0.24𝜆𝜆�𝑓𝑓′ = 0.24(1.0)√8.7𝑘𝑘𝑠𝑠𝑠𝑠 = 0.708𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑐𝑐𝑑𝑑𝑒𝑒 = 5.947𝑘𝑘𝑠𝑠𝑠𝑠
𝑆𝑆𝑐𝑐 = 25509.3𝑠𝑠𝑠𝑠3
𝑆𝑆𝑠𝑠 = 20594.8𝑠𝑠𝑠𝑠3
𝑀𝑀𝑔𝑔𝑖𝑖𝑐𝑐 = 𝑀𝑀𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 + 𝑀𝑀𝑔𝑔𝑔𝑔𝑠𝑠𝑑𝑑ℎ𝑔𝑔𝑠𝑠𝑔𝑔𝑐𝑐𝑠𝑠 + 𝑀𝑀𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 + 𝑀𝑀ℎ𝑠𝑠𝑎𝑎𝑖𝑖𝑐𝑐ℎ = 6734.48𝑘𝑘 ⋅ 𝑓𝑓𝑓𝑓
1𝑓𝑓𝑓𝑓
12𝑠𝑠𝑠𝑠
𝑀𝑀𝑐𝑐𝑔𝑔 = 1.0 �(1.6 ∙ 0.708𝑘𝑘𝑠𝑠𝑠𝑠 + 1.0 ∙ 5.947𝑘𝑘𝑠𝑠𝑠𝑠)(25509.3𝑠𝑠𝑠𝑠3) � � − (6734.48𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) �
25509.3𝑠𝑠𝑠𝑠3
20594.8𝑠𝑠𝑠𝑠3
− 1��
= 14707.1 𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
4.7.3.2.2 Evaluate Minimum Reinforcement Requirement
𝑀𝑀𝑎𝑎 = 17099.8𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀𝑔𝑔 𝑐𝑐𝑔𝑔𝑖𝑖 = 𝑘𝑘𝐴𝐴𝑠𝑠𝑠𝑠𝐴𝐴𝐴𝐴 𝑐𝑐𝑓𝑓 �
𝑀𝑀𝑐𝑐𝑔𝑔 = 14707.1𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
1.33𝑀𝑀𝑎𝑎 = 1.33 ∙ 17099.8𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 = 22742.7𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
= 14707.1𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀𝑔𝑔 = 20526.2𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 ≥ 𝑀𝑀𝑔𝑔 𝑐𝑐𝑔𝑔𝑖𝑖 = 14707.1𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 OK
4.8 Check Splitting Resistance
Compute the splitting resistance of the pretensioned anchorage zone provided by the vertical reinforcement in the ends of the girder at the service limit states as 𝑃𝑃𝑔𝑔 = 𝑓𝑓𝑠𝑠𝐴𝐴𝑠𝑠 (5.9.4.4.1) where,
fs = the stress in the steel not exceeding 20 ksi
As = total area of vertical reinforcement located within the distance h/4 from the end of the beam (in2) h = overall depth of the girder (in)
The resistance shall not be less than 4% of the prestressing force at transfer.
The splitting force at the point of prestress transfer is the total of the permanent and temporary strand forces.
𝑃𝑃 = 0.04𝐴𝐴𝑑𝑑𝑠𝑠�𝑓𝑓𝑑𝑑𝑝𝑝 − 𝛥𝛥𝑓𝑓𝑑𝑑𝑅𝑅0 − 𝛥𝛥𝑓𝑓𝑑𝑑𝐸𝐸𝑆𝑆�
Permanent strands
𝑃𝑃 = 0.04(13.237𝑠𝑠𝑠𝑠2)(202.5 − 19.858𝑘𝑘𝑠𝑠𝑠𝑠) = 96.71 𝑘𝑘𝑠𝑠𝑘𝑘
Temporary strands
𝑃𝑃 = 0.04(0.868𝑠𝑠𝑠𝑠2)(202.5 − 8.656𝑘𝑘𝑠𝑠𝑠𝑠) = 6.73 𝑘𝑘𝑠𝑠𝑘𝑘
Total splitting force
𝑃𝑃 = 96.71 + 6.73 = 103.44 𝑘𝑘𝑠𝑠𝑘𝑘
4 4 12𝑔𝑔𝑖𝑖
The splitting zone is ℎ = 74𝑔𝑔𝑖𝑖 � 1𝑒𝑒𝑑𝑑 � = 1.542𝑓𝑓𝑓𝑓.

## Slide 166
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Splitting resistance is 𝑃𝑃𝑔𝑔 = 𝑓𝑓𝑠𝑠𝐴𝐴𝑠𝑠
The required area of splitting reinforcement is
103.44𝑘𝑘𝑠𝑠𝑘𝑘 = (20𝑘𝑘𝑠𝑠𝑠𝑠)𝐴𝐴𝑠𝑠
𝐴𝐴𝑠𝑠 = 5.172 𝑠𝑠𝑠𝑠2
5.172𝑠𝑠𝑠𝑠2
1.542𝑓𝑓𝑓𝑓
= 3.62
𝑠𝑠𝑠𝑠2
𝑓𝑓𝑓𝑓
The standard stirrup layout has 2-legs #5 at 3.5” for the end 1’-9” of the beam.
2(0.31𝑠𝑠𝑠𝑠2)
�
3.5𝑠𝑠𝑠 𝑠
12 𝑠𝑠𝑠𝑠⁄𝑓𝑓𝑓𝑓
�
𝑠𝑠𝑠𝑠2
= 2.126
𝑓𝑓𝑓𝑓
Try 2-legs #5 at 2.5”.
2(0.31𝑠𝑠𝑠𝑠2)
�
2.5𝑠𝑠𝑠 𝑠
12 𝑠𝑠𝑠𝑠⁄𝑓𝑓𝑓𝑓
�
𝑠𝑠𝑠𝑠2
= 2.976
𝑓𝑓𝑓𝑓
WSDOT BDM 5.6.2F permits the total splitting reinforcement to extend beyond H/4 at a spacing not greater than 2.5”.
𝑠𝑠𝑠𝑠2
𝑓𝑓𝑓𝑓
5.172𝑠𝑠𝑠𝑠2 = 2.976 𝑋𝑋
𝑋𝑋 = 1.74 𝑓𝑓𝑓𝑓
Use 2-legs #5 at 2.5” for 1’-9”
PGSuper does not currently apply the provisions of WSDOT BDM 5.6.2F.
4.9 Check Confinement Zone Reinforcement
For the distance of 1.5d from the ends of the girder, reinforcement shall be placed to confine the prestressing steel in the bottom flange (LRFD 5.9.4.4.2). The reinforcement shall not be less than #3 deformed bars with spacing not exceeding 6 in.
The length of the confinement zone is 1.5𝑑𝑑 = 1.5(74 𝑠𝑠𝑠𝑠) = 111 𝑠𝑠𝑠𝑠 = 9.25 𝑓𝑓𝑓𝑓.
Provide #3 bars spaced at 6” for the end 9.25ft of the girder.
Shear Design
Ensure the girder has sufficient capacity to resist shear in the Strength I limit state. Verify that shear reinforcement is adequately detailed.
These computations and checks demonstrate shear design at the critical section (LRFD 5.7.3.2 and 5.7.3.3). A complete design will also evaluate shear at locations where abrupt changes to the shear force diagram occur and at changes in reinforcement size and spacing.
  Locate Critical Section for Shear
The critical section for shear is located at dv from the face of support where dv is determined based on critical section. For purposes of design, the ultimate shear between the support and the critical section is equal to the shear at the critical section.
Determining the location of the critical section can be challenging because dv varies with position along the girder. To find the critical section plot dv along the length of the girder and draw a 45° line from the face of support towards the center of the girder. The intersection of the 45° line and the dv curve is the location of the critical section. Figure 5-1 illustrates this technique.

## Slide 167
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Figure 5-1: Graphical method to Determine Critical Section Location
For this girder, the critical section is located 5.782 ft from the face of support. The table that follows show the details for finding the critical sections.
Table 5-1: Critical Section Calculation Details for Abutment 1
Location from Left Support (ft) | Assumed C.S. Location (in) | dv (in) | CS Intersects?
(FoS) 0.500 | 0.000 | 69.382 | No
(Bar Develop.) 0.834 | 4.011 | 69.382 | No
(PSXFR) 1.292 | 9.498 | 69.382 | No
4.625 | 49.500 | 69.384 | No
6.282 | 69.384 | 69.384 | *Yes
6.542 | 72.498 | 69.384 | No
(H) 6.667 | 74.000 | 69.384 | No
(1.5H) 9.750 | 111.000 | 69.384 | No
11.958 | 137.498 | 69.384 | No
(SZB) 12.170 | 140.037 | 69.384 | No
(SZB) 12.920 | 149.037 | 69.384 | No
14.591 | 169.092 | 69.384 | No
* - Intersection values are linearly interpolated
  Check Ultimate Shear Capacity
    Compute Nominal Shear Resistance
The nominal shear resistance, Vn, is the lesser of:
𝑉𝑉𝑖𝑖 = 𝑉𝑉𝑐𝑐 + 𝑉𝑉𝑑𝑑 + 𝑉𝑉𝑠𝑠
𝑉𝑉𝑖𝑖 = 0.25𝑓𝑓′𝑠𝑠 𝑑𝑑 + 𝑉𝑉
𝑐𝑐 𝑜𝑜 𝑜𝑜 𝑑𝑑
for which

## Slide 168
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝑉𝑉𝑐𝑐 = 0.0316𝛽𝛽�𝑓𝑓′𝑠𝑠 𝑑𝑑
𝑐𝑐 𝑜𝑜 𝑜𝑜
𝑉𝑉𝑠𝑠 =
𝐴𝐴𝑜𝑜 𝑓𝑓𝑝𝑝𝑑𝑑𝑜𝑜 𝑐𝑐𝑐𝑐𝑓𝑓 𝜃𝜃
𝑠𝑠
where
bv | = | Effective web width taken as the minimum web width within the depth dv.
dv | = | Effective shear depth
s | = | Stirrup spacing
 | = | Factor indicating ability of diagonally cracked concrete to transmit tension
 | = | Angle of inclination of diagonal compressive stresses
Av | = | Area of shear reinforcement within a distance s
Vp | = | Component in the direction of the applied shear of the effective prestressing force, positive if resisting the applied shear.
5.2.1.1 Determination of  and 
Step 1: Determine bv
bv is the effective web width. For this girder 𝑠𝑠𝑜𝑜 = 6.125𝑠𝑠𝑠𝑠.
Step 2: Determine dv
dv is the distance measured perpendicular to the neutral axis, between the resultants of the tensile and compressive forces due to flexure (internal moment arm), but it need not be taken less than the greater of 0.9de or 0.72h.
From a flexural capacity analysis at the critical section the Moment Arm =59.470 in, de =77.094 in, and h =81 in.
𝑀𝑀𝑐𝑐𝑚𝑚𝐴𝐴𝑠𝑠𝑓𝑓 𝐴𝐴𝐴𝐴𝑚𝑚 = 59.470𝑠𝑠𝑠𝑠
𝑑𝑑𝑜𝑜 = 𝑔𝑔𝐴𝐴𝐴𝐴𝐴𝐴𝑓𝑓𝐴𝐴𝑠𝑠𝑓𝑓 𝑐𝑐𝑓𝑓 �0.9𝑑𝑑𝑒𝑒 = 0.9(77.094𝑠𝑠𝑠𝑠) = 69.384𝑠𝑠𝑠𝑠
0.72ℎ = 0.72(81𝑠𝑠𝑠𝑠) = 58.32𝑠𝑠𝑠𝑠
Step 3: Compute stress in prestrssing steel when the stress in the surrounding concrete is 0.0 ksi
𝑓𝑓𝑑𝑑𝑔𝑔 = 0.70𝑓𝑓𝑑𝑑𝑎𝑎 = 189𝑘𝑘𝑠𝑠𝑠𝑠
Step 4: Compute the longitudinal strain on the flexural tension side of the beam
𝑠𝑠
𝜀𝜀 =
𝑔𝑔
𝑣 𝑣
�|𝐿𝐿𝑢𝑢|+0.5𝑁𝑁𝑢𝑢+�𝑉𝑉𝑢𝑢−𝑉𝑉𝑝𝑝�−𝐴𝐴𝑝𝑝𝑠𝑠𝑒𝑒𝑝𝑝𝑝𝑝�
𝐸𝐸𝑠𝑠 𝐴𝐴𝑠𝑠 + 𝐸𝐸𝑑𝑑𝐴𝐴𝑑𝑑𝑠𝑠 + 𝐸𝐸𝑐𝑐 𝐴𝐴𝑐𝑐𝑑𝑑
𝑠𝑠
𝑓𝑓𝑐𝑐𝐴𝐴 𝜀𝜀 < 0
At the critical section the flexural tension side is the bottom half of the beam. The area of concrete and area of steel on the flexural tension side are identified in Figure 5-2.

## Slide 169
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
h/2
Flexural Tension Side
Act
Aps
Figure 5-2: Flexural Tension Side of Beam with Area of Concrete and Area of Steel Identified
The longitudinal strain parameters are:
𝑀𝑀𝑎𝑎 = 2603.98 𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑁𝑁𝑎𝑎 = 0 𝑘𝑘𝑠𝑠𝑘𝑘
𝑉𝑉𝑎𝑎 = 413.73 𝑘𝑘𝑠𝑠𝑘𝑘
𝑉𝑉𝑑𝑑 = 43.18 𝑘𝑘𝑠𝑠𝑘𝑘
�𝑉𝑉𝑎𝑎 – 𝑉𝑉𝑑𝑑 � = 370.54 𝑘𝑘𝑠𝑠𝑘𝑘
𝑑𝑑𝑜𝑜 = 69.384 𝑠𝑠𝑠𝑠
𝐴𝐴𝑠𝑠 = 0 𝑠𝑠𝑠𝑠2
𝐸𝐸𝑠𝑠 = 29000 𝑘𝑘𝑠𝑠𝑠𝑠
𝐴𝐴𝑑𝑑𝑠𝑠 = 9.143 𝑠𝑠𝑠𝑠2
𝐸𝐸𝑑𝑑𝑠𝑠 = 28500 𝑘𝑘𝑠𝑠𝑠𝑠
𝐴𝐴𝑐𝑐𝑑𝑑 = 507.406 𝑠𝑠𝑠𝑠2

## Slide 170
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝐸𝐸𝑐𝑐 = 5886.891𝑘𝑘𝑠𝑠𝑠𝑠
12𝑔𝑔𝑖𝑖
|2603.98𝑑𝑑∙𝑒𝑒𝑑𝑑|� �
� 1𝑒𝑒𝑑 𝑑 +0.5(0)+370.54𝑑𝑑𝑔𝑔𝑑𝑑−�9.143𝑔𝑔𝑖𝑖2�(189𝑑𝑑𝑠𝑠𝑔𝑔)�
69.384𝑔𝑔𝑖𝑖
−3
𝜀𝜀𝑠𝑠 = (29000𝑘𝑘𝑠𝑠𝑠𝑠)(0𝑠𝑠𝑠𝑠2) + (28500𝑘𝑘𝑠𝑠𝑠𝑠)(9.143𝑠𝑠𝑠𝑠2) + (5886.891𝑘𝑘𝑠𝑠𝑠𝑠)(507.406𝑠𝑠𝑠𝑠2) = −0.279𝑤𝑤10 < 0
Step 5: Compute  and 
𝛽𝛽 =
4.8
4.8
(1 + 750𝜀𝜀𝑠𝑠) �1 + (750)(−0.279𝑤𝑤10−3)�
= = 6.07
𝜃𝜃 = 29 + 3500𝜀𝜀𝑠𝑠 = 29 + (3500)(−0.279𝑤𝑤10−3) = 28.02°
5.2.1.2 Compute Shear Capacity of Concrete
Vc = 0.0316βλ�f′b d = 0.0316(6.07)(1.0)√8.7ksi(6.125in)(69.384in) = 240.51 kip
c v v
𝑉𝑉𝑠𝑠 =
𝐴𝐴𝑜𝑜 𝑓𝑓𝑝𝑝𝑑𝑑𝑜𝑜 𝑐𝑐𝑐𝑐𝑓𝑓 𝜃𝜃
𝜆𝜆𝑔𝑔𝑎𝑎𝑐𝑐𝑑𝑑 =
5.2.1.3 Compute Shear Capacity of Transverse Reinforcement
For #5 stirrups at 6”, 𝐴𝐴𝑜𝑜 = 0.62 𝑠𝑠𝑠𝑠2.
(0.62 𝑠𝑠𝑠𝑠2)(60 𝑘𝑘𝑠𝑠𝑠𝑠)(69.384𝑠𝑠𝑠𝑠) 𝑐𝑐𝑐𝑐𝑓𝑓 28.02
𝑠𝑠 6 𝑠𝑠𝑠𝑠
(1.0) = 808.29 𝑘𝑘𝑠𝑠𝑘𝑘
5.2.1.4 Compute Nominal Shear Capacity of Section
𝑉𝑉𝑖𝑖 = 𝑉𝑉𝑐𝑐 + 𝑉𝑉𝑑𝑑 + 𝑉𝑉𝑠𝑠 = 240.51 𝑘𝑘𝑠𝑠𝑘𝑘 + 43.18 𝑘𝑘𝑠𝑠𝑘𝑘 + 808.29 𝑘𝑘𝑠𝑠𝑘𝑘 = 1091.99 𝑘𝑘𝑠𝑠𝑘𝑘
𝑐𝑐 𝑜𝑜 𝑜𝑜 𝑑𝑑
𝑉𝑉𝑖𝑖 = 0.25𝑓𝑓′𝑠𝑠 𝑑𝑑 + 𝑉𝑉 = 0.25(8.7 𝑘𝑘𝑠𝑠𝑠𝑠)(6.125 𝑠𝑠𝑠𝑠)(69.384 𝑠𝑠𝑠𝑠) + 43.18 𝑘𝑘𝑠𝑠𝑘𝑘 = 967.51𝑘𝑘𝑠𝑠𝑘𝑘
𝑉𝑉𝑔𝑔 = 𝜙𝜙𝑉𝑉𝑖𝑖 = 0.9(967.51 𝑘𝑘𝑠𝑠𝑘𝑘) = 870.76 𝑘𝑘𝑠𝑠𝑘𝑘
5.2.1.5 Check Ultimate Shear Capacity
𝑉𝑉𝑎𝑎 = 413.73 𝑘𝑘𝑠𝑠𝑘𝑘 ≤ 𝑉𝑉𝑔𝑔 = 870.76 𝑘𝑘𝑠𝑠𝑘𝑘 OK
Repeat these calculations at all locations where stirrup size or spacing changes or where the applied shear abruptly changes.
    Check Requirement for Transverse Reinforcement
Transverse reinforcement is required when 𝑉𝑉𝑎𝑎 > 0.5𝜙𝜙�𝑉𝑉𝑐𝑐 + 𝑉𝑉𝑑𝑑 �. (LRFD 5.8.2.4)
0.5𝜙𝜙�𝑉𝑉𝑐𝑐 + 𝑉𝑉𝑑𝑑� = 0.5(0.9)(240.51 𝑘𝑘𝑠𝑠𝑘𝑘 + 43.18 𝑘𝑘𝑠𝑠𝑘𝑘) = 127.66 𝑘𝑘𝑠𝑠𝑘𝑘 < 413.73 𝑘𝑘𝑠𝑠𝑘𝑘
Vu exceeds the limiting value; therefore, transverse reinforcement is required at this section. Transverse reinforcement is provided. OK
    Check Minimum Transverse Reinforcement
Where transverse reinforcement is required, as specified in LRFD 5.8.2.4, the area of steel shall not be less than 𝐴𝐴𝑜𝑜 𝑐𝑐𝑔𝑔𝑖𝑖 =
𝑐𝑐 𝑒𝑒𝑦𝑦
60 𝑑𝑑𝑠𝑠𝑔𝑔
0.0316�𝑓𝑓′ 𝑠𝑠𝑣𝑣𝑠𝑠 = 0.0316√8.7 𝑘𝑘𝑠𝑠𝑠𝑠 (6.125 𝑔𝑔𝑖𝑖)(6 𝑔𝑔𝑖𝑖) = 0.057 𝑠𝑠𝑠𝑠2 < 0.62 𝑠𝑠𝑠𝑠2
OK
𝑐𝑐 𝑒𝑒𝑦𝑦
𝑠𝑠 60 𝑑𝑑𝑠𝑠𝑔𝑔 𝑔𝑔𝑖𝑖 𝑒𝑒𝑑𝑑
2 2
This can also be represented as 𝐴𝐴𝑣𝑣 𝑚𝑚𝑠𝑠𝑠𝑠 = 0.0316�𝑓𝑓′ 𝑠𝑠𝑣𝑣 = 0.0316√8.7 𝑘𝑘𝑠𝑠𝑠𝑠 6.125 𝑔𝑔𝑖𝑖 = 0.0095 𝑔𝑔𝑖𝑖 = 0.114 𝑔𝑔𝑖𝑖 .
    Check Maximum Spacing of Transverse Reinforcement
The spacing of the transverse reinforcement shall not exceed the following:
      If 𝑆𝑆𝑎𝑎 < 0.125𝑓𝑓′ then 𝑠𝑠 ≤ 0.8𝑑𝑑 ≤ 24 𝑠𝑠𝑠𝑠
𝑐𝑐 𝑜𝑜

## Slide 171
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
If 𝑆𝑆𝑎𝑎 ≥ 0.125𝑓𝑓′ then 𝑠𝑠 ≤ 0.4𝑑𝑑 ≤ 12 𝑠𝑠𝑠𝑠
𝑐𝑐 𝑜𝑜
𝑆𝑆𝑎𝑎 =
�𝑉𝑉𝑎𝑎 − 𝜙𝜙𝑉𝑉𝑑𝑑 �
𝜙𝜙𝑠𝑠 𝑑𝑑
𝑜𝑜 𝑜𝑜
=
|413.73 − 0.9(43.18)|
0.9(6.125)(69.384)
= 0.98 𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐
0.125𝑓𝑓′ = 0.125(8.7 𝑘𝑘𝑠𝑠𝑠𝑠) = 1.09 𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐
𝑆𝑆𝑎𝑎 = 0.98 𝑘𝑘𝑠𝑠𝑠𝑠 < 0.125𝑓𝑓′ = 1.09 𝑘𝑘𝑠𝑠𝑠𝑠
𝑠𝑠𝑐𝑐𝑠𝑠𝑥𝑥 = 0.8𝑑𝑑𝑜𝑜 = 0.8(69.384 𝑠𝑠𝑠𝑠) = 55.5 𝑠𝑠𝑠𝑠 ≤ 24 𝑠𝑠𝑠𝑠 (18 𝑠𝑠𝑠𝑠 𝑘𝑘𝐴𝐴𝐴𝐴 𝐻𝐻𝑆𝑆𝐷𝐷𝑊𝑊𝑇𝑇) → 𝑠𝑠𝑐𝑐𝑠𝑠𝑥𝑥 = 18 𝑠𝑠𝑠𝑠
The actual spacing is 6.0 in. OK
Per WSDOT BDM 5.2.2.B.4, the maximum spacing of transverse reinforcement is limited to 18 inches
5.3 Check Longitudinal Reinforcement for Shear
At each section, the tensile capacity of the longitudinal reinforcement on the flexural tension side of the member shall be proportioned to satisfy:
𝑑𝑑 𝜙𝜙
𝑀𝑀𝑎𝑎 𝑁𝑁𝑎𝑎 𝑉𝑉𝑎𝑎
𝜙𝜙 𝜙𝜙
𝑜𝑜 𝑒𝑒 𝑠𝑠 𝑜𝑜
𝑠𝑠 𝑝𝑝 𝑑𝑑𝑠𝑠 𝑑𝑑𝑠𝑠 𝑑𝑑
𝑠𝑠
𝐴𝐴 𝑓𝑓 + 𝐴𝐴 𝑓𝑓 ≥ � + 0.5 + �� − 𝑉𝑉 � − 0.5𝑉𝑉 � 𝑐𝑐𝑐𝑐𝑓𝑓 𝜃𝜃�
At the inside edge of the bearing area of simple end supports to the section of critical shear, the longitudinal reinforcement on the flexural tension side of the member shall satisfy:
𝑉𝑉𝑎𝑎
𝐴𝐴𝑠𝑠𝑓𝑓𝑝𝑝 + 𝐴𝐴𝑑𝑑𝑠𝑠𝑓𝑓𝑑𝑑𝑠𝑠 ≥ � − 0.5𝑉𝑉𝑠𝑠 − 𝑉𝑉𝑑𝑑� 𝑐𝑐𝑐𝑐𝑓𝑓 𝜃𝜃
𝜙𝜙𝑜𝑜
At the critical section, all the harped strands are above the mid-height of the girder. The harped strands are not on the flexural tension side (See LRFD Figure 5.7.3.4.2-2)
𝐴𝐴𝑑𝑑𝑠𝑠 = (44)(0.217𝑠𝑠𝑠𝑠2) = 9.548𝑠𝑠𝑠𝑠2
From the moment capacity analysis, 𝑓𝑓𝑑𝑑𝑠𝑠,𝑠𝑠𝑜𝑜𝑔𝑔 = 126.855𝑘𝑘𝑠𝑠𝑠𝑠 which takes into account the lack of full development per LRFD
5.9.4.3.2. Do not apply the reduction again in these calculations.
𝑑𝑑𝑜𝑜 = 69.382𝑠𝑠𝑠𝑠
𝑉𝑉𝑎𝑎 = 413.73𝑘𝑘𝑠𝑠𝑘𝑘
𝑉𝑉𝑠𝑠 = 459.70𝑠𝑠𝑘𝑘
𝑉𝑉𝑑𝑑 = 43.18𝑘𝑘𝑠𝑠𝑘𝑘
𝜃𝜃 = 28.02°
𝜙𝜙
𝑜𝑜
𝑠𝑠 𝑑𝑑
� − 0.5𝑉𝑉 − 𝑉𝑉 � 𝑐𝑐𝑐𝑐𝑓𝑓 𝜃𝜃 = �
𝑉𝑉𝑎𝑎 413.73𝑘𝑘𝑠𝑠𝑘𝑘
0.9
− 0.5(459.7𝑘𝑘𝑠𝑠𝑘𝑘) − 43.18𝑘𝑘𝑠𝑠𝑘𝑘� 𝑐𝑐𝑐𝑐𝑓𝑓 28.02° = 350.7𝑘𝑘𝑠𝑠𝑘𝑘
𝐴𝐴𝑑𝑑𝑠𝑠𝑓𝑓𝑑𝑑𝑠𝑠 = (9.548𝑠𝑠𝑠𝑠2)(126.885𝑘𝑘𝑠𝑠𝑠𝑠) = 1211.5𝑘𝑘𝑠𝑠𝑘𝑘 1211.5kip ≥ 350.7kip
OK
5.4 Check Horizontal Interface Shear
This entire design assumes that the slab and girder work together to form a composite section. Verify the slab-girder interface has adequate capacity to develop this composite action.

## Slide 172
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
    Check Nominal Capacity
The critical section for shear location is used to demonstrate these calculations. A complete design will verify the slab-girder interface capacity at various sections along the girder.
      Compute Nominal Capacity
The nominal shear resistance at the slab-girder interface is 𝑉𝑉𝑖𝑖𝑔𝑔 = 𝑐𝑐𝐴𝐴𝑐𝑐𝑜𝑜 + 𝜇𝜇�𝐴𝐴𝑜𝑜𝑒𝑒 𝑓𝑓𝑝𝑝 + 𝑃𝑃𝑐𝑐 � ≤ 𝑚𝑚𝑠𝑠𝑠𝑠𝑠𝑠𝑚𝑚𝑎𝑎𝑚𝑚 � 1 𝑐𝑐
𝐾𝐾 𝑓𝑓′𝐴𝐴
𝑐𝑐𝑜𝑜
𝐾𝐾2𝐴𝐴𝑐𝑐𝑜𝑜
where
Vni | = | Nominal shear resistance (kip)
Acv | = | Area of concrete engaged in shear transfer (in2)
Avf | = | Area of shear reinforcement crossing the shear plane (in2)
fy | = | Yield strength of reinforcement (ksi)
c | = | Cohesion factor
 | = | Friction factor
Pc | = | Permanent net compressive force normal to the shear plane, or 0.0 kip if tensile (kip)
f’c | = | Specified 28-day strength of the weaker concrete (ksi)
K1 | = | 0.3
K2 | = | 1.8
The top flange of the girder, which is a roughened surface, supports the deck slab. For this situation c = 0.280 ksi and  = 1.0.
The area of concrete engaged in the shear transfer: 𝐴𝐴𝑐𝑐𝑜𝑜 = 𝑠𝑠𝑜𝑜𝑔𝑔 𝐿𝐿𝑜𝑜𝑔𝑔 = (49 𝑠𝑠𝑠𝑠) �1
� = 49
𝑔𝑔𝑖𝑖
𝑔𝑔𝑖𝑖 𝑔𝑔𝑖𝑖
𝑔𝑔𝑖𝑖2.
The area of shear reinforcement consists of the stirrups extending from the web into the slab (#5 @ 3.5 in): 𝐴𝐴
𝑜𝑜𝑒𝑒
3.5 𝑔𝑔𝑖𝑖
2
= 0.62 𝑔𝑔𝑖𝑖 =
2 2
0.177 𝑔𝑔𝑖𝑖 = 2.126 𝑔𝑔𝑖𝑖 .
𝑔𝑔𝑖𝑖 𝑒𝑒𝑑𝑑
It is conservative to take 𝑃𝑃𝑐𝑐 = 0 𝑘𝑘𝑘𝑘𝑓𝑓.
𝑉𝑉𝑖𝑖𝑔𝑔 = 𝑐𝑐𝐴𝐴𝑐𝑐𝑜𝑜 + 𝜇𝜇�𝐴𝐴𝑜𝑜𝑒𝑒 𝑓𝑓𝑝𝑝 + 𝑃𝑃𝑐𝑐 � = (0.280 𝑘𝑘𝑠𝑠𝑠𝑠) �49
2
𝑔𝑔𝑖𝑖 12𝑔𝑔𝑖𝑖
𝑔𝑔𝑖𝑖 1𝑒𝑒𝑑𝑑
𝑔𝑔𝑖𝑖
2
𝑒𝑒𝑑𝑑
� + 1.0 ��2.126 � (60𝑘𝑘𝑠𝑠𝑠𝑠) + 0 𝑘𝑘𝑘𝑘𝑓𝑓� = 292.183 𝑘𝑘𝑠𝑠𝑘𝑘⁄𝑓𝑓𝑓𝑓
1 𝑐𝑐 𝑐𝑐𝑜𝑜
𝑔𝑔𝑖𝑖 𝑡𝑡𝑡𝑡
2
𝐾𝐾 𝑓𝑓′𝐴𝐴 = 0.3(4𝑘𝑘𝑠𝑠𝑠𝑠) �49𝑔𝑔𝑖𝑖 12𝑟𝑟𝑖𝑖� = 705.6 𝑘𝑘𝑠𝑠𝑘𝑘⁄𝑓𝑓𝑓𝑓
2 𝑐𝑐𝑜𝑜
𝑔𝑔𝑖𝑖 𝑡𝑡𝑡𝑡
2
𝐾𝐾 𝐴𝐴 = 1.8 �49𝑔𝑔𝑖𝑖 12𝑟𝑟𝑖𝑖� = 1058.4 𝑘𝑘𝑠𝑠𝑘𝑘⁄𝑓𝑓𝑓𝑓
𝑉𝑉𝑖𝑖𝑔𝑔 = 292.183 𝑘𝑘𝑠𝑠𝑘𝑘⁄𝑓𝑓𝑓𝑓
𝑉𝑉𝑔𝑔 = 𝜙𝜙𝑉𝑉𝑖𝑖𝑔𝑔 = 0.9(292.183 𝑘𝑘𝑠𝑠𝑘𝑘⁄𝑓𝑓𝑓𝑓) = 262.965 𝑘𝑘𝑠𝑠𝑘𝑘/𝑓𝑓𝑓𝑓
𝑎𝑎𝑔𝑔
𝑠𝑠𝑣𝑣𝑟𝑟𝑔𝑔𝑣𝑣𝑟𝑟
5.4.1.2 Compute Demand
The factored interface shear stress for a concrete girder/slab bridge may be determined as 𝑆𝑆 = 𝑉𝑉𝑢 𝑢 . The factored interface
shear force for a concrete girder/slab bridge may be determined as 𝑉𝑉𝑎𝑎𝑔𝑔 = 𝑆𝑆𝑎𝑎𝑔𝑔 𝐴𝐴𝑐𝑐𝑜𝑜 . Substituting Equation 5.8.4.2-1 into 5.8.4.2-
𝑎𝑎ℎ
𝑔𝑔𝑣𝑣𝑟𝑟
2 the interface shear force is 𝑉𝑉 = 𝑉𝑉𝑢𝑢 .
At the critical section, Vu = 413.73 kip.
𝐼𝐼
𝑉𝑉𝑎𝑎ℎ = =
𝑉𝑉𝑎𝑎 𝑄𝑄 (413.73𝑘𝑘𝑠𝑠𝑘𝑘)(12199.9𝑠𝑠𝑠𝑠3)
𝑘𝑘
= 48.589
𝑓𝑓𝑓𝑓
(1246570.6𝑠𝑠𝑠𝑠4)
𝑉𝑉𝑎𝑎ℎ ≤ 𝑉𝑉𝑔𝑔

## Slide 173
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
OK
5.4.2 Check Minimum Reinforcement
The LRFD specification requires a minimum amount of shear reinforcement in the slab-girder interface. Check to make sure this requirement is satisfied.
𝑒𝑒𝑦𝑦
The cross-sectional area, Avf, of the reinforcement per unit length should not be less than0.05𝑠𝑠𝑣𝑣.
For a cast-in-place concrete slab on clean concrete girder surface free of laitance:
The minimum interface shear reinforcement need not exceed the lessor of the amount determined using Eqn.
5.8.4.4-1 and the amount needed to resist 1.33𝑉𝑉𝑢𝑢𝑟𝑟 as determined using Eqn 5.8.4.1-3
𝜙𝜙
The minimum reinforcement provisions shall be waived for girder/slab interfaces with surface roughened to an amplitude of 0.25 in where the factored interface shear stress, 𝑆𝑆𝑎𝑎𝑔𝑔 of Eqn 5.8.4.2-1 is less than 0.210 ksi, and all vertical (transverse) shear reinforcement required by the provisions of Article 5.8.1.1 is extended across the interface and adequately anchored into the slab.
𝜐𝜐
𝑎𝑎𝑔𝑔
𝑉𝑉
= 𝑎𝑎𝑔𝑔 =
𝐴𝐴𝑐𝑐𝑜𝑜
48.589 𝑘𝑘𝑠𝑠𝑘𝑘
49 𝑠𝑠𝑠𝑠 1𝑓𝑓𝑓𝑓
𝑠𝑠𝑠𝑠2 12𝑠𝑠𝑠𝑠 𝑓𝑓𝑓𝑓
𝑓𝑓𝑓𝑓 𝑘𝑘𝑠𝑠𝑠𝑠
= 0.083 < 0.210
𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑓𝑓
This requirement is waived.
OK
The maximum allowable spacing of the transverse reinforcement is 24.0 in. The actual spacing at this section is 3.5 in. The maximum spacing along the length of the girder is 18.0 in. OK
Check the “A” Dimension
The slab offset, or “A” dimension in WSDOT terminology, was assumed to be 12.5in. Verify the haunch is large enough to accommodate the camber, but not too large that the girder has to carry unnecessary dead load. For such a large girder, an extra inch of concrete over the top flange can add up to a considerable amount of weight.
The haunch depth is to be such that at the mid-span the distance between the bottom of the slab and the top of the girder is equal to the slab fillet dimension, 0.75in. Account for geometric effects due to the roadway and camber. The haunch depth at the bearing is Ahaunch = Aslab+fillet + Aprofile effect + Agirder orientation effect + Aexcess camber.
  Slab and Fillet
The slab and fillet is the gross slab depth plus the fillet dimension. If the actual camber is exactly equal to the predicted value, and all deflections are as predicted, the top of the girder will be exactly tfillet below the bottom of the deck at its closest point.

## Slide 174
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Figure 6-1: Slab + Fillet Effect
𝐴𝐴𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠+𝑒𝑒𝑔𝑔𝑠𝑠𝑠𝑠𝑒𝑒𝑑𝑑 = 7.5 𝑠𝑠𝑠𝑠 + 0.75 𝑠𝑠𝑠𝑠 = 8.25𝑠𝑠𝑠𝑠
6.2 Profile Effect
PGSuper uses a general approach to determine the profile effect. Draw a chord line from the point where a vertical line passing through the CL Bearings intersect the deck. Then the profile effect is the maximum difference in elevation between this chord line and the roadway surface.
Figure 6-2: General Method for Profile Effect

## Slide 175
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
The entire bridge is within the limits of the horizontal and vertical curves. Also, there are no superelevation transitions within the limits of the bridge. Therefore, the simplified method of computing the profile effect can be used as described in WSDOT BDM Appendix 5-B1.
6.2.1 Vertical Curve
Figure 6-3: Vertical Curve Effect
𝑜𝑜𝑐𝑐
𝐴𝐴 =
1.5(𝑔𝑔2 − 𝑔𝑔1)𝐿𝐿2
100𝐿𝐿𝑜𝑜𝑐𝑐
𝑔𝑔 (𝑠𝑠𝑠𝑠) =
1.5�−1.5% − (−2%)�(124.58𝑓𝑓𝑓𝑓)2
100(600𝑓𝑓𝑓𝑓)
= 0.194 𝑠𝑠𝑠𝑠

## Slide 176
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
6.2.2 Horizontal Curve
Figure 6-4: Horizontal Curve Effect
𝐴𝐴ℎ𝑐𝑐 =
1.5𝑆𝑆2𝑚𝑚
𝑅𝑅
(𝑠𝑠𝑠𝑠) =
𝑓𝑓𝑓𝑓
1.5(827.42 − 702.71𝑓𝑓𝑓𝑓)2 �0.04 𝑓𝑓𝑓𝑓�
6000 𝑓𝑓𝑓𝑓
= 0.156𝑠𝑠𝑠𝑠
6.2.3 Profile Effect
𝐴𝐴𝑑𝑑𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔𝑠𝑠𝑒𝑒 = 𝐴𝐴𝑜𝑜𝑐𝑐 + 𝐴𝐴ℎ𝑐𝑐 = 0.194𝑠𝑠𝑠𝑠 + 0.156𝑠𝑠𝑠𝑠 = 0.350𝑠𝑠𝑠𝑠
6.3 Girder Orientation Effect
The girder orientation effect accounts for the crown slope and the orientation of the girder. 𝐴𝐴
𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑖𝑖𝑑𝑑𝑠𝑠𝑑𝑑𝑔𝑔𝑔𝑔𝑖𝑖 𝑒𝑒𝑒𝑒𝑒𝑒𝑒𝑒𝑐𝑐𝑑𝑑
2
𝑤𝑤𝑡𝑡𝑡𝑡
= 𝑚𝑚 .

## Slide 177
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Figure 6-5: Top Flange Effect
𝐴𝐴𝑑𝑑𝑔𝑔𝑑𝑑 𝑒𝑒𝑠𝑠𝑠𝑠𝑖𝑖𝑔𝑔𝑒𝑒 𝑒𝑒𝑒𝑒𝑒𝑒𝑒𝑒𝑐𝑐𝑑𝑑 = 0.04
49𝑠𝑠𝑠𝑠
2
= 0.980𝑠𝑠𝑠𝑠
6.4 Excess Camber
The excess camber is the camber that remains in the girder after all of the loads are applied.
Figure 6-6: Camber Effect
The graphic below illustrates how the girder deflects over time.

## Slide 178
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Figure 6-7: Camber Diagram
Assume time-dependent deformations end after deck casting
𝛥𝛥𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 = 𝑑𝑑𝐴𝐴𝑓𝑓𝑘𝑘𝐴𝐴𝑐𝑐𝑓𝑓𝑠𝑠𝑐𝑐𝑠𝑠 𝑑𝑑𝑎𝑎𝐴𝐴 𝑓𝑓𝑐𝑐 𝑔𝑔𝑠𝑠𝐴𝐴𝑑𝑑𝐴𝐴𝐴𝐴 𝑠𝑠𝐴𝐴𝑘𝑘𝑓𝑓
𝛥𝛥𝑑𝑑𝑠𝑠 = 𝑑𝑑𝐴𝐴𝑓𝑓𝑘𝑘𝐴𝐴𝑐𝑐𝑓𝑓𝑠𝑠𝑐𝑐𝑠𝑠 𝑑𝑑𝑎𝑎𝐴𝐴 𝑓𝑓𝑐𝑐 𝑘𝑘𝐴𝐴𝐴𝐴𝑚𝑚𝐴𝐴𝑠𝑠𝐴𝐴𝑠𝑠𝑓𝑓 𝑘𝑘𝐴𝐴𝐴𝐴𝑠𝑠𝑓𝑓𝐴𝐴𝐴𝐴𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑔𝑔, 𝑠𝑠𝐴𝐴𝑠𝑠𝐴𝐴𝑑𝑑 𝑐𝑐𝑠𝑠 𝑠𝑠𝑠𝑠𝑘𝑘𝑘𝑘𝐴𝐴𝑐𝑐𝐴𝐴 𝑠𝑠𝑘𝑘𝐴𝐴𝑠𝑠 𝑘𝑘𝐴𝐴𝑠𝑠𝑔𝑔𝑓𝑓ℎ
𝛥𝛥𝑐𝑐𝑔𝑔𝑒𝑒𝑒𝑒𝑑𝑑1 = 𝜓𝜓(𝑓𝑓𝑒𝑒 , 𝑓𝑓𝑔𝑔)�𝛥𝛥𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 + 𝛥𝛥𝑑𝑑𝑠𝑠�
𝛥𝛥𝑔𝑔𝑔𝑔𝑠𝑠𝑑𝑑ℎ𝑔𝑔𝑠𝑠𝑔𝑔𝑐𝑐 = 𝑑𝑑𝐴𝐴𝑓𝑓𝑘𝑘𝐴𝐴𝑐𝑐𝑓𝑓𝑠𝑠𝑐𝑐𝑠𝑠 𝑑𝑑𝑎𝑎𝐴𝐴 𝑓𝑓𝑐𝑐 𝑑𝑑𝑠𝑠𝐴𝐴𝑘𝑘ℎ𝐴𝐴𝐴𝐴𝑔𝑔𝑚𝑚 𝑠𝑠𝐴𝐴𝑘𝑘𝑓𝑓 𝑤𝑤𝐴𝐴𝑠𝑠𝑔𝑔ℎ𝑓𝑓
𝛿𝛿𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 = 𝑠𝑠𝑠𝑠𝑐𝑐𝐴𝐴𝐴𝐴𝑚𝑚𝐴𝐴𝑠𝑠𝑓𝑓𝐴𝐴𝑘𝑘 𝑔𝑔𝑠𝑠𝐴𝐴𝑑𝑑𝐴𝐴𝐴𝐴 𝑑𝑑𝐴𝐴𝑓𝑓𝑘𝑘𝐴𝐴𝑐𝑐𝑓𝑓𝑠𝑠𝑐𝑐𝑠𝑠 𝑑𝑑𝑎𝑎𝐴𝐴 𝑓𝑓𝑐𝑐 𝑐𝑐ℎ𝐴𝐴𝑠𝑠𝑔𝑔𝐴𝐴 𝑠𝑠𝑠𝑠 𝑠𝑠𝑎𝑎𝑘𝑘𝑘𝑘𝑐𝑐𝐴𝐴𝑓𝑓 𝑘𝑘𝑐𝑐𝑐𝑐𝐴𝐴𝑓𝑓𝑠𝑠𝑐𝑐𝑠𝑠 𝑠𝑠𝐴𝐴𝑓𝑓𝑤𝑤𝐴𝐴𝐴𝐴𝑠𝑠 𝑠𝑠𝑓𝑓𝑐𝑐𝐴𝐴𝐴𝐴𝑔𝑔𝐴𝐴 𝐴𝐴𝑠𝑠𝑑𝑑 𝐴𝐴𝐴𝐴𝐴𝐴𝑐𝑐𝑓𝑓𝑠𝑠𝑐𝑐𝑠𝑠
𝛥𝛥𝑐𝑐𝑔𝑔𝑒𝑒𝑒𝑒𝑑𝑑2 = [𝜓𝜓(𝑓𝑓𝑔𝑔, 𝑓𝑓𝑔𝑔) − 𝜓𝜓(𝑓𝑓𝑒𝑒, 𝑓𝑓𝑔𝑔 )]�𝛥𝛥𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 + 𝛥𝛥𝑑𝑑𝑠𝑠� + 𝜓𝜓(𝑓𝑓𝑔𝑔, 𝑓𝑓𝑒𝑒 )�𝛥𝛥𝑑𝑑𝑑𝑑𝑔𝑔 + 𝛥𝛥𝑔𝑔𝑔𝑔𝑠𝑠𝑑𝑑ℎ𝑔𝑔𝑠𝑠𝑔𝑔𝑐𝑐 + 𝛿𝛿𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 �
𝛥𝛥𝑑𝑑𝑑𝑑𝑔𝑔 = 𝑓𝑓𝐴𝐴𝑚𝑚𝑘𝑘𝑐𝑐𝐴𝐴𝐴𝐴𝐴𝐴𝑑𝑑 𝑘𝑘𝐴𝐴𝐴𝐴𝑠𝑠𝑓𝑓𝐴𝐴𝐴𝐴𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑔𝑔 𝑠𝑠𝑓𝑓𝐴𝐴𝐴𝐴𝑠𝑠𝑑𝑑 𝐴𝐴𝐴𝐴𝑚𝑚𝑐𝑐𝑆𝑆𝐴𝐴𝑘𝑘
𝛥𝛥𝑔𝑔𝑒𝑒𝑐𝑐𝑑𝑑 = 𝑑𝑑𝐴𝐴𝑓𝑓𝑘𝑘𝐴𝐴𝑐𝑐𝑓𝑓𝑠𝑠𝑐𝑐𝑠𝑠 𝑑𝑑𝑎𝑎𝐴𝐴 𝑓𝑓𝑐𝑐 𝑑𝑑𝐴𝐴𝑐𝑐𝑘𝑘 𝑠𝑠𝐴𝐴𝑘𝑘𝑓𝑓 𝑤𝑤𝐴𝐴𝑠𝑠𝑔𝑔ℎ𝑓𝑓
𝛥𝛥ℎ𝑠𝑠𝑎𝑎𝑖𝑖𝑐𝑐ℎ = 𝑑𝑑𝐴𝐴𝑓𝑓𝑘𝑘𝐴𝐴𝑐𝑐𝑓𝑓𝑠𝑠𝑐𝑐𝑠𝑠 𝑑𝑑𝑎𝑎𝐴𝐴 𝑓𝑓𝑐𝑐 ℎ𝐴𝐴𝑎𝑎𝑠𝑠𝑐𝑐ℎ 𝑠𝑠𝐴𝐴𝑘𝑘𝑓𝑓 𝑤𝑤𝐴𝐴𝑠𝑠𝑔𝑔ℎ𝑓𝑓
𝛥𝛥𝑠𝑠𝑠𝑠𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 = 𝑑𝑑𝐴𝐴𝑓𝑓𝑘𝑘𝐴𝐴𝑐𝑐𝑓𝑓𝑠𝑠𝑐𝑐𝑠𝑠 𝑑𝑑𝑎𝑎𝐴𝐴 𝑓𝑓𝑐𝑐 𝑓𝑓𝐴𝐴𝐴𝐴𝑓𝑓𝑓𝑓𝑠𝑠𝑐𝑐 𝑠𝑠𝐴𝐴𝐴𝐴𝐴𝐴𝑠𝑠𝐴𝐴𝐴𝐴 𝑠𝑠𝐴𝐴𝑘𝑘𝑓𝑓 𝑤𝑤𝐴𝐴𝑠𝑠𝑔𝑔ℎ𝑓𝑓
𝛥𝛥𝑒𝑒𝑥𝑥𝑐𝑐𝑒𝑒𝑠𝑠𝑠𝑠 = 𝐴𝐴𝑤𝑤𝑐𝑐𝐴𝐴𝑠𝑠𝑠𝑠 𝑐𝑐𝐴𝐴𝑚𝑚𝑠𝑠𝐴𝐴𝐴𝐴
𝛥𝛥1 = �𝛥𝛥𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 + 𝛥𝛥𝑑𝑑𝑠𝑠�
𝛥𝛥2 = 𝛥𝛥1 + 𝛥𝛥𝑐𝑐𝑔𝑔𝑒𝑒𝑒𝑒𝑑𝑑1
𝛥𝛥3 = 𝛥𝛥2 + 𝛥𝛥𝑑𝑑𝑑𝑑𝑔𝑔 + 𝛥𝛥𝑔𝑔𝑔𝑔𝑠𝑠𝑑𝑑ℎ𝑔𝑔𝑠𝑠𝑔𝑔𝑐𝑐
𝛥𝛥4 = 𝛥𝛥3 + 𝛥𝛥𝑐𝑐𝑔𝑔𝑒𝑒𝑒𝑒𝑑𝑑2
𝛥𝛥5 = 𝛥𝛥4 + 𝛥𝛥𝑔𝑔𝑒𝑒𝑐𝑐𝑑𝑑 + ∆ℎ𝑠𝑠𝑎𝑎𝑖𝑖𝑐𝑐ℎ
𝛥𝛥6 = 𝛥𝛥𝑒𝑒𝑥𝑥𝑐𝑐𝑒𝑒𝑠𝑠𝑠𝑠 = 𝛥𝛥5 + 𝛥𝛥𝑠𝑠𝑠𝑠𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔

## Slide 179
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
6.4.1 Compute Creep Coefficients
The creep coefficients for release until erection and deck casting are computed above.
Prestress release until erection 𝜓𝜓(𝑓𝑓ℎ = 90, 𝑓𝑓𝑔𝑔 = 1) = 𝜓𝜓(𝑓𝑓𝑒𝑒 = 90, 𝑓𝑓𝑔𝑔 = 1) = 0.852
Prestress release until deck casting 𝜓𝜓(𝑓𝑓𝑔𝑔 = 120, 𝑓𝑓𝑒𝑒 = 1) = 0.912
Compute creep coefficient for erection to deck casting
𝑐𝑐𝑔𝑔
𝑓𝑓′ = 7.4 𝑘𝑘𝑠𝑠𝑠𝑠
5
𝑘𝑘𝑒𝑒 = 1 + 7.4 = 0.610
𝑘𝑘𝑑𝑑𝑔𝑔 =
(120 − 90)
12 �
100 − 4(7.4)
7.4 + 20
� + (120 − 90)
= 0.488
𝜓𝜓(𝑓𝑓𝑔𝑔 = 120, 𝑓𝑓𝑒𝑒 = 90) = 1.9(1.04)(0.96)(0.610)(0.488)(90)−0.118 = 0.331
𝑔𝑔
∆ =
6.4.2 Compute Deflections
Girder Deflection, for the erected girder
5𝑤𝑤𝐿𝐿4
𝑐𝑐𝑔𝑔 𝑥𝑥
=
384𝐸𝐸 𝐼𝐼 384(5530.5𝑘𝑘𝑠𝑠𝑠𝑠)(734356.0𝑠𝑠𝑠𝑠
4
5(−1.058𝑘𝑘𝑘𝑘𝑓𝑓)(159.578𝑓𝑓𝑓𝑓)4 1728𝑠𝑠𝑠𝑠3
) 1𝑓𝑓𝑓𝑓3
� � = −3.802𝑠𝑠𝑠𝑠
Prestress Deflection, 𝛥𝛥𝑑𝑑𝑠𝑠 = 7.161𝑠𝑠𝑠𝑠. This is the deflection measured relative to the ends of the girder. The deflection at the CL Bearing based on the release datum is 𝛥𝛥𝑑𝑑𝑠𝑠𝑠𝑠𝑔𝑔𝑔𝑔 = 0.263𝑠𝑠𝑠𝑠. The prestress deflection measured relative to the bearings is
𝛥𝛥𝑑𝑑𝑠𝑠 = 7.161𝑠𝑠𝑠𝑠 − 0.263𝑠𝑠𝑠𝑠 = 6.897𝑠𝑠𝑠𝑠
Creep Deflection during Storage, ∆𝑐𝑐𝑔𝑔𝑒𝑒𝑒𝑒𝑑𝑑1= 0.852(6.897𝑠𝑠𝑠𝑠 − 3.802𝑠𝑠𝑠𝑠) = 2.639𝑠𝑠𝑠𝑠
Diaphragm Deflection, ∆𝑔𝑔𝑔𝑔𝑠𝑠𝑑𝑑ℎ𝑔𝑔𝑠𝑠𝑔𝑔𝑐𝑐 = −0.141𝑠𝑠𝑠𝑠
Slab Deflection, ∆𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠 = −2.610𝑠𝑠𝑠𝑠
Haunch Deflection, ∆ℎ𝑠𝑠𝑎𝑎𝑖𝑖𝑐𝑐ℎ = −0.808𝑠𝑠𝑠𝑠
Creep Deflection between diaphragm and deck casting, ∆𝑐𝑐𝑔𝑔𝑒𝑒𝑒𝑒𝑑𝑑2= (0.912 − 0.852)(6.897𝑠𝑠𝑠𝑠 − 3.802𝑠𝑠𝑠𝑠) + (0.331)(−0.141𝑠𝑠𝑠𝑠) = 0.347𝑠𝑠𝑠𝑠. Since the girder is stored at the locations of the bearings 𝛿𝛿𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 = 0 𝑠𝑠𝑠𝑠
Traffic Barrier Deflection, ∆𝑠𝑠𝑠𝑠𝑔𝑔𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔 = −0.457𝑠𝑠𝑠𝑠
Because the girder concrete has gained strength, not all of the deflection due to the installation of the temporary top strands is recoverable. The elastic rebound due to temporary strand removal is
𝑃𝑃 = 162.93𝑘𝑘𝑠𝑠𝑘𝑘
𝑑𝑑𝑑𝑑𝑠𝑠𝑔𝑔
∆ =
8𝐸𝐸 𝐼𝐼
𝑐𝑐 𝑥𝑥
=
8(5886.891𝑘𝑘𝑠𝑠𝑠𝑠)(734356.0𝑠𝑠𝑠𝑠4)
𝑃𝑃𝐴𝐴𝐿𝐿2 (162.93𝑘𝑘𝑠𝑠𝑘𝑘)(−36.343𝑠𝑠𝑠𝑠)(162.995𝑓𝑓𝑓𝑓)2 144𝑠𝑠𝑠𝑠2
� � = 0.655𝑠𝑠𝑠𝑠 1𝑓𝑓𝑓𝑓2
Measured relative to the bearings, 𝛥𝛥𝑑𝑑𝑑𝑑𝑠𝑠𝑔𝑔 = 0.628 𝑠𝑠𝑠𝑠
∆1= −3.802𝑠𝑠𝑠𝑠 + 6.897𝑠𝑠𝑠𝑠 = 3.096𝑠𝑠𝑠𝑠
∆2= 3.096𝑠𝑠𝑠𝑠 + 2.639𝑠𝑠𝑠𝑠 = 5.735𝑠𝑠𝑠𝑠
∆3= 5.735 − 0.141𝑠𝑠𝑠𝑠 + 0.628𝑠𝑠𝑠𝑠 = 6.222𝑠𝑠𝑠𝑠
∆4= 6.222𝑠𝑠𝑠𝑠 + 0.347𝑠𝑠𝑠𝑠 = 6.569𝑠𝑠𝑠𝑠 = 𝐷𝐷120
∆5= 6.569𝑠𝑠𝑠𝑠 − 2.610𝑠𝑠𝑠𝑠 − 0.808𝑠𝑠𝑠𝑠 = 3.150𝑠𝑠𝑠𝑠
∆6= 3.150 − 0.457𝑠𝑠𝑠𝑠 = 2.693𝑠𝑠𝑠𝑠 = ∆𝑒𝑒𝑥𝑥𝑐𝑐𝑒𝑒𝑠𝑠𝑠𝑠

## Slide 180
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
The screed camber, 𝐷𝐷 = 𝛥𝛥4 − 𝛥𝛥6 = 3.876 𝑠𝑠𝑠𝑠
  Check Required Haunch
The required haunch is 𝛢𝛢ℎ𝑠𝑠𝑎𝑎𝑖𝑖𝑐𝑐ℎ = 𝛢𝛢𝑠𝑠𝑠𝑠𝑠𝑠𝑠𝑠+𝑒𝑒𝑔𝑔𝑠𝑠𝑠𝑠𝑒𝑒𝑑𝑑 + 𝛢𝛢𝑑𝑑𝑔𝑔𝑑𝑑 𝑒𝑒𝑠𝑠𝑠𝑠𝑖𝑖𝑔𝑔𝑒𝑒 𝑒𝑒𝑒𝑒𝑒𝑒𝑒𝑒𝑐𝑐𝑑𝑑 + + 𝐴𝐴𝑑𝑑𝑔𝑔𝑔𝑔𝑒𝑒𝑔𝑔𝑠𝑠𝑒𝑒 𝑒𝑒𝑒𝑒𝑒𝑒𝑒𝑒𝑐𝑐𝑑𝑑 + 𝛢𝛢𝑒𝑒𝑥𝑥𝑐𝑐𝑒𝑒𝑠𝑠𝑠𝑠 𝑐𝑐𝑠𝑠𝑐𝑐𝑠𝑠𝑒𝑒𝑔𝑔
𝛢𝛢ℎ𝑠𝑠𝑎𝑎𝑖𝑖𝑐𝑐ℎ = 8.25𝑠𝑠𝑠𝑠 + 0.98𝑠𝑠𝑠𝑠 + 0.35𝑠𝑠𝑠𝑠 + 2.693𝑠𝑠𝑠𝑠 = 12.27 𝑠𝑠𝑠𝑠
The provided haunch is 12.5 in. OK
  Compute Lower Bound Camber at 40 days
    Creep Coefficients
Creep coefficients are computed the same as before, assuming erection at 10 days and deck casting at 40 days.
𝜓𝜓𝑠𝑠 (𝑓𝑓𝑔𝑔 = 10, 𝑓𝑓𝑔𝑔 = 1) = 0.257
𝜓𝜓𝑠𝑠 �𝑓𝑓𝑒𝑒 = 40, 𝑓𝑓1 = 1� = 0.638
𝜓𝜓𝑠𝑠 (𝑓𝑓𝑔𝑔 = 40, 𝑓𝑓𝑒𝑒 = 10) = 0.429
    Compute Deflections
Creep Deflection during Storage, ∆𝑐𝑐𝑔𝑔𝑒𝑒𝑒𝑒𝑑𝑑1= 0.638(6.897𝑠𝑠𝑠𝑠 − 3.802𝑠𝑠𝑠𝑠) = 0.795𝑠𝑠𝑠𝑠
Creep Deflection between diaphragm and deck casting, ∆𝑐𝑐𝑔𝑔𝑒𝑒𝑒𝑒𝑑𝑑2= (0.638 − 0.257)(6.897𝑠𝑠𝑠𝑠 − 3.802𝑠𝑠𝑠𝑠) + (0.429)(−0.141𝑠𝑠𝑠𝑠) = 1.391𝑠𝑠𝑠𝑠
∆1= 3.096𝑠𝑠𝑠𝑠
∆2= 3.891𝑠𝑠𝑠𝑠
∆3= 4.378𝑠𝑠𝑠𝑠
∆4= 5.769𝑠𝑠𝑠𝑠 = 𝐷𝐷40
This is an upper bound value for camber at 40 days. There is a ±25% natural variation in camber from the mean value. Therefore, lower bound camber at 40 days = 0.5𝐷𝐷40 = 2.884 𝑠𝑠𝑠𝑠
6.7 Check for Possible Girder Sag
When the screed camber, C, exceeds the deflection at slab casting, D, the girder will have a net downward deflection, also known as sag. The sag condition is most likely to occur for rapidly constructed bridges.
Compare the screed camber to the average value of camber at 40 days to determine the potential for sag. The average value is
75% ∆40= (0.75)(5.769in) = 4.327in
Δexcess = D − C
∆5= 5.769 − 2.610 − 0.808 = 2.351in
∆6= 2.351 − 0.457 = 1.894in = ∆excess C = ∆4 − ∆6= 5.769 − 1.894 = 3.875in C < 75%∆40 OK
7 Bearing Seat Elevations
From the PGSuper Bridge Geometry Report, the roadway surface elevations at the CL Bearing points for Girder A are:
Abutment 1, Sta. 7+02.70, Offset 17.463ft L, Elev. 104.688ft Abutment 2, Sta. 8+61.82, Offset 17.457ft L, Elev. 101.748ft

## Slide 181
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
The slope of the girder is 104.688𝑒𝑒𝑑𝑑−101.748𝑒𝑒𝑑𝑑 = −0.0184 𝑒𝑒𝑑𝑑
159.578𝑒𝑒𝑑𝑑 𝑒𝑒𝑑𝑑
The slope-adjusted height of the girder is74𝑠𝑠𝑠𝑠 ��(−0.0184)2 + (1)2� = 74.013𝑠𝑠𝑠𝑠
Deduct the sloped adjusted girder height and the slab offset from the roadway surface elevation to get the bottom of girder elevation.
Bottom of girder elevation at Abutment 1: Elev = 104.688𝑓𝑓𝑓𝑓 − 74.013𝑠𝑠𝑠𝑠 � 1𝑒𝑒𝑑𝑑 � − 12.5𝑠𝑠𝑠𝑠 � 1𝑒𝑒𝑑𝑑 � = 97.479𝑓𝑓𝑓𝑓
12𝑔𝑔𝑖𝑖 12𝑔𝑔𝑖𝑖
Bottom of girder elevation at Abutment 2: Elev = 101.748𝑓𝑓𝑓𝑓 − 74.013𝑠𝑠𝑠𝑠 � 1𝑒𝑒𝑑𝑑 � − 12.5𝑠𝑠𝑠𝑠 � 1𝑒𝑒𝑑𝑑 � = 94.538𝑓𝑓𝑓𝑓
12𝑔𝑔𝑖𝑖 12𝑔𝑔𝑖𝑖
After designing the bearings, add the bearing recess (typically ½”) and deduct the bearing depth from the bottom of girder elevation to get the bearing seat elevation.
8 Design Summary
𝑐𝑐𝑔𝑔
𝑓𝑓′ = 7.2𝑘𝑘𝑠𝑠𝑠𝑠
𝑐𝑐
𝑓𝑓′ = 8.7𝑘𝑘𝑠𝑠𝑠𝑠
𝐻𝐻𝐴𝐴𝑎𝑎𝑘𝑘 𝑇𝑇𝐴𝐴𝑎𝑎𝑐𝑐𝑘𝑘 𝐷𝐷𝑐𝑐𝑠𝑠𝑓𝑓𝑠𝑠𝑔𝑔𝑎𝑎𝐴𝐴𝐴𝐴𝑓𝑓𝑠𝑠𝑐𝑐𝑠𝑠 = 40,000
# 𝑃𝑃𝐴𝐴𝐴𝐴𝑚𝑚𝐴𝐴𝑠𝑠𝐴𝐴𝑠𝑠𝑓𝑓 𝑆𝑆𝑓𝑓𝐴𝐴𝐴𝐴𝑠𝑠𝑑𝑑𝑠𝑠 = 61 (44 𝑆𝑆𝑓𝑓𝐴𝐴𝐴𝐴𝑠𝑠𝑔𝑔ℎ𝑓𝑓, 17 𝐻𝐻𝐴𝐴𝐴𝐴𝑘𝑘𝐴𝐴𝑑𝑑) # 𝑇𝑇𝐴𝐴𝑚𝑚𝑘𝑘𝑐𝑐𝐴𝐴𝐴𝐴𝐴𝐴𝑑𝑑 𝑇𝑇𝑐𝑐𝑘𝑘 𝑆𝑆𝑓𝑓𝐴𝐴𝐴𝐴𝑠𝑠𝑑𝑑𝑠𝑠 = 4
𝑆𝑆𝑘𝑘𝐴𝐴𝑠𝑠 𝑊𝑊𝑓𝑓𝑓𝑓𝑠𝑠𝐴𝐴𝑓𝑓 ("A" 𝐷𝐷𝑠𝑠𝑚𝑚𝐴𝐴𝑠𝑠𝑠𝑠𝑠𝑠𝑐𝑐𝑠𝑠) = 12.5𝑠𝑠𝑠𝑠
𝑃𝑃𝑠𝑠𝑐𝑐𝑘𝑘 𝑃𝑃𝑐𝑐𝑠𝑠𝑠𝑠𝑓𝑓 = 8′3"
𝐵𝐵𝑎𝑎𝑠𝑠𝑘𝑘 𝑃𝑃𝑐𝑐𝑠𝑠𝑠𝑠𝑓𝑓 = 13′8"
𝑘𝑘𝑠𝑠𝑘𝑘 − 𝑠𝑠𝑠𝑠
𝐴𝐴𝐴𝐴𝑑𝑑
𝑤𝑤𝑠𝑠𝑓𝑓ℎ 72" 𝑤𝑤ℎ𝐴𝐴𝐴𝐴𝑘𝑘 𝑠𝑠𝐴𝐴𝑠𝑠𝐴𝐴 (𝐻𝐻𝑇𝑇40 − 72)
𝑈𝑈𝑠𝑠𝐴𝐴 𝑠𝑠𝑓𝑓𝑠𝑠𝐴𝐴𝐴𝐴𝑎𝑎𝑘𝑘𝑠𝑠 𝑘𝑘𝐴𝐴𝐴𝐴 𝐻𝐻𝑆𝑆𝐷𝐷𝑊𝑊𝑇𝑇 𝑠𝑠𝑓𝑓𝐴𝐴𝑠𝑠𝑑𝑑𝐴𝐴𝐴𝐴𝑑𝑑
Load Rating
The bridge opens for traffic without the future overlay installed. For this reason, take the DW force effects associated with the overlay as zero. Installing the overlay necessitates updating the load rating analysis.
  Inventory Rating
    Moment
𝑅𝑅𝐹𝐹 =
𝜙𝜙𝑐𝑐𝜙𝜙𝑠𝑠𝜙𝜙𝑖𝑖𝐾𝐾𝑀𝑀𝑖𝑖 − 𝛾𝛾𝑝𝑝𝑝𝑝 𝑀𝑀𝑝𝑝𝑝𝑝 − 𝛾𝛾𝑝𝑝𝑊𝑊𝑀𝑀𝑝𝑝𝑊𝑊
𝛾𝛾𝐿𝐿𝐿𝐿 𝑀𝑀𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿
𝜙𝜙𝑐𝑐 𝜙𝜙𝑠𝑠 ≥ 0.85
𝑀𝑀𝑔𝑔
𝑀𝑀𝑐𝑐𝑔𝑔𝑖𝑖
𝐾𝐾 = ≤ 1.0
At 0.5L
𝜙𝜙𝑐𝑐 = 𝜙𝜙𝑠𝑠 = 𝜙𝜙𝑖𝑖 = 1.0
𝑀𝑀𝑖𝑖 = 20526.2𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀𝑝𝑝𝑝𝑝 = 7466.6𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀𝑝𝑝𝑊𝑊 = 0.0𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿 = 3804.05 𝑔𝑔𝑠𝑠𝐴𝐴𝑑𝑑𝐴𝐴𝐴𝐴

## Slide 182
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝑀𝑀𝑐𝑐𝑔𝑔 = 14707.13𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀𝑎𝑎 = 17099.79𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀
𝑐𝑐𝑔𝑔𝑖𝑖
= 𝑚𝑚𝑠𝑠𝑠𝑠 �
𝑀𝑀𝑐𝑐𝑔𝑔
1.33𝑀𝑀𝑎𝑎
= 14707.13𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝐾𝐾 =
(1.0)(20526.2𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)
14707.13𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
= 1.39 ∴ 1.0
𝑅𝑅𝐹𝐹 =
𝛾𝛾𝑝𝑝𝑝𝑝 = 1.25, 𝛾𝛾𝑝𝑝𝑊𝑊 = 1.50, 𝛾𝛾𝐿𝐿𝐿𝐿 = 1.75 (1)(1)(1)(1)(20526.2𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) − (1.25)(7466.6𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) − (1.5)(0𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)
(1.75)(3804.05𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)
= 1.68
9.1.2 Shear
𝑅𝑅𝐹𝐹 =
𝜙𝜙𝑐𝑐𝜙𝜙𝑠𝑠𝜙𝜙𝑖𝑖𝑉𝑉𝑖𝑖 − 𝛾𝛾𝑝𝑝𝑝𝑝 𝑉𝑉𝑝𝑝𝑝𝑝 − 𝛾𝛾𝑝𝑝𝑊𝑊𝑉𝑉𝑝𝑝𝑊𝑊
𝛾𝛾𝐿𝐿𝐿𝐿 𝑉𝑉𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿
At 10.388ft and 142.908ft (location where stirrup spacing increases)
𝜙𝜙𝑐𝑐 = 𝜙𝜙𝑠𝑠 = 1.0, 𝜙𝜙𝑖𝑖 = 0.9
𝑉𝑉𝑖𝑖 = 518.10𝑘𝑘𝑠𝑠𝑘𝑘
𝑉𝑉𝑝𝑝𝑝𝑝 = 147.84𝑘𝑘𝑠𝑠𝑘𝑘
𝑉𝑉𝑝𝑝𝑊𝑊 = 0.0𝑘𝑘
𝑘𝑘𝑠𝑠𝑘𝑘
𝑉𝑉𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿 = 90.13 𝑔𝑔𝑠𝑠𝐴𝐴𝑑𝑑𝐴𝐴𝐴𝐴
𝑅𝑅𝐹𝐹 =
𝛾𝛾𝑝𝑝𝑝𝑝 = 1.25, 𝛾𝛾𝑝𝑝𝑊𝑊 = 1.50, 𝛾𝛾𝐿𝐿𝐿𝐿 = 1.75 (1)(1)(0.9)(518.10𝑘𝑘𝑠𝑠𝑘𝑘) − (1.25)(147.84𝑘𝑘𝑠𝑠𝑘𝑘) − (1.5)(0𝑘𝑘𝑠𝑠𝑘𝑘)
(1.75)(90.13𝑘𝑘𝑠𝑠𝑘𝑘)
= 1.78
9.1.3 Bending Stress – Service III limit state
𝑅𝑅𝐹𝐹 =
𝑓𝑓𝑅𝑅 − 𝛾𝛾𝑝𝑝𝑝𝑝 𝑓𝑓𝑝𝑝𝑝𝑝 − 𝛾𝛾𝑝𝑝𝑊𝑊𝑓𝑓𝑝𝑝𝑊𝑊
𝛾𝛾𝐿𝐿𝐿𝐿 𝑓𝑓𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿
Per WSDOT BDM 13.2.4, use the AASHTO LRFD specifications tension stress limit and live load factor for load rating purposes.
𝑐𝑐
𝑓𝑓𝑅𝑅 = 𝑓𝑓𝑠𝑠𝑔𝑔𝑐𝑐𝑔𝑔𝑑𝑑 − 𝑓𝑓𝑑𝑑𝑠𝑠 = 0.19𝜆𝜆�𝑓𝑓′ − 𝑓𝑓𝑑𝑑𝑠𝑠
𝑓𝑓𝑅𝑅 = 0.19(1.0)√8.7𝑘𝑘𝑠𝑠𝑠𝑠 − (−6.221𝑘𝑘𝑠𝑠𝑠𝑠) = 0.560𝑘𝑘𝑠𝑠𝑠𝑠 − (−6.221𝑘𝑘𝑠𝑠𝑠𝑠) = 6.781𝑘𝑘𝑠𝑠𝑠𝑠
Since we are using refined losses and elastic gains, the live load factor is 1.0 (See AASHTO LRFD Table 3.4.1-4).
𝛾𝛾𝐿𝐿𝐿𝐿 = 1.0
6.781𝑘𝑘𝑠𝑠𝑠𝑠 − (1.0)(4.268𝑘𝑘𝑠𝑠𝑠𝑠) − 1.0(0𝑘𝑘𝑠𝑠𝑠𝑠)
(1.0)(1.789𝑘𝑘𝑠𝑠𝑠𝑠)
𝑅𝑅𝐹𝐹 = = 1.40
  Operating Rating
    Moment
𝑅𝑅𝐹𝐹 =
𝜙𝜙𝑐𝑐𝜙𝜙𝑠𝑠𝜙𝜙𝑖𝑖𝐾𝐾𝑀𝑀𝑖𝑖 − 𝛾𝛾𝑝𝑝𝑝𝑝 𝑀𝑀𝑝𝑝𝑝𝑝 − 𝛾𝛾𝑝𝑝𝑊𝑊𝑀𝑀𝑝𝑝𝑊𝑊
𝛾𝛾𝐿𝐿𝐿𝐿 𝑀𝑀𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿
𝜙𝜙𝑐𝑐 𝜙𝜙𝑠𝑠 ≥ 0.85

## Slide 183
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝐾𝐾 =
𝑀𝑀𝑔𝑔
𝑀𝑀𝑐𝑐𝑔𝑔𝑖𝑖
≤ 1.0
At 0.5L
𝜙𝜙𝑐𝑐 = 𝜙𝜙𝑠𝑠 = 𝜙𝜙𝑖𝑖 = 1.0
𝑀𝑀𝑖𝑖 = 20526.2𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀𝑝𝑝𝑝𝑝 = 7466.6𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀𝑝𝑝𝑊𝑊 = 0.0𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿 = 3804.05 𝑔𝑔𝑠𝑠𝐴𝐴𝑑𝑑𝐴𝐴𝐴𝐴
𝑀𝑀𝑐𝑐𝑔𝑔 = 14707.13𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀𝑎𝑎 = 17099.79𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀
𝑐𝑐𝑔𝑔𝑖𝑖
= 𝑚𝑚𝑠𝑠𝑠𝑠 �
𝑀𝑀𝑐𝑐𝑔𝑔
1.33𝑀𝑀𝑎𝑎
= 14707.13𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝐾𝐾 =
(1.0)(20526.2𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)
14707.13𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
= 1.39 ∴ 1.0
𝑅𝑅𝐹𝐹 =
𝛾𝛾𝑝𝑝𝑝𝑝 = 1.25, 𝛾𝛾𝑝𝑝𝑊𝑊 = 1.50, 𝛾𝛾𝐿𝐿𝐿𝐿 = 1.35 (1)(1)(1)(1)(20526.2𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) − (1.25)(7466.6𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) − (1.5)(0𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)
(1.35)(3804.05𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)
= 2.18
9.2.2 Shear
𝑅𝑅𝐹𝐹 =
𝜙𝜙𝑐𝑐𝜙𝜙𝑠𝑠𝜙𝜙𝑖𝑖𝑉𝑉𝑖𝑖 − 𝛾𝛾𝑝𝑝𝑝𝑝 𝑉𝑉𝑝𝑝𝑝𝑝 − 𝛾𝛾𝑝𝑝𝑊𝑊𝑉𝑉𝑝𝑝𝑊𝑊
𝛾𝛾𝐿𝐿𝐿𝐿 𝑉𝑉𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿
At 10.388ft and 142.908ft (location where stirrup spacing increases)
𝜙𝜙𝑐𝑐 = 𝜙𝜙𝑠𝑠 = 1.0, 𝜙𝜙𝑖𝑖 = 0.9
𝑉𝑉𝑖𝑖 = 518.10𝑘𝑘𝑠𝑠𝑘𝑘
𝑉𝑉𝑝𝑝𝑝𝑝 = 147.84𝑘𝑘𝑠𝑠𝑘𝑘
𝑉𝑉𝑝𝑝𝑊𝑊 = 0.0𝑘𝑘
𝑘𝑘𝑠𝑠𝑘𝑘
𝑉𝑉𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿 = 90.13 𝑔𝑔𝑠𝑠𝐴𝐴𝑑𝑑𝐴𝐴𝐴𝐴
𝑅𝑅𝐹𝐹 =
𝛾𝛾𝑝𝑝𝑝𝑝 = 1.25, 𝛾𝛾𝑝𝑝𝑊𝑊 = 1.50, 𝛾𝛾𝐿𝐿𝐿𝐿 = 1.35 (1)(1)(0.9)(518.10𝑘𝑘𝑠𝑠𝑘𝑘) − (1.25)(147.84𝑘𝑘𝑠𝑠𝑘𝑘) − (1.5)(0𝑘𝑘𝑠𝑠𝑘𝑘)
(1.35)(90.13𝑘𝑘𝑠𝑠𝑘𝑘)
= 2.38
9.3 Legal Loads
Type 3, MLLIM = 1404.25k ∙ ft
Type 3S2, MLLIM = 1826.63k ∙ ft
Type 3-3, MLLIM = 1931.27k ∙ ft
Type 3-3 rating will govern so we will show calculations of the rating factors for this loading. The rating factor calculations for the other loadings will be similar. The rating factor calculations for NRL, EV2 and EV3 are similar.

## Slide 184
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
9.3.1 Moment
𝑅𝑅𝐹𝐹 =
𝜙𝜙𝑐𝑐𝜙𝜙𝑠𝑠𝜙𝜙𝑖𝑖𝐾𝐾𝑀𝑀𝑖𝑖 − 𝛾𝛾𝑝𝑝𝑝𝑝 𝑀𝑀𝑝𝑝𝑝𝑝 − 𝛾𝛾𝑝𝑝𝑊𝑊𝑀𝑀𝑝𝑝𝑊𝑊
𝛾𝛾𝐿𝐿𝐿𝐿 𝑀𝑀𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿
𝜙𝜙𝑐𝑐 𝜙𝜙𝑠𝑠 ≥ 0.85
𝑀𝑀𝑔𝑔
𝑀𝑀𝑐𝑐𝑔𝑔𝑖𝑖
𝐾𝐾 = ≤ 1.0
At 0.5L
𝜙𝜙𝑐𝑐 = 𝜙𝜙𝑠𝑠 = 𝜙𝜙𝑖𝑖 = 1.0
𝑀𝑀𝑖𝑖 = 20526.2𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀𝑝𝑝𝑝𝑝 = 7466.6𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀𝑝𝑝𝑊𝑊 = 0.0𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿 = 1931.27 𝑔𝑔𝑠𝑠𝐴𝐴𝑑𝑑𝐴𝐴𝐴𝐴
𝑀𝑀𝑐𝑐𝑔𝑔 = 14707.13𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀𝑎𝑎 = 17099.79𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝑀𝑀
𝑐𝑐𝑔𝑔𝑖𝑖
= 𝑚𝑚𝑠𝑠𝑠𝑠 �
𝑀𝑀𝑐𝑐𝑔𝑔
1.33𝑀𝑀𝑎𝑎
= 14707.13𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
𝐾𝐾 =
(1.0)(20526.2𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)
14707.13𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
= 1.39 ∴ 1.0
𝑅𝑅𝐹𝐹 =
𝛾𝛾𝑝𝑝𝑝𝑝 = 1.25, 𝛾𝛾𝑝𝑝𝑊𝑊 = 1.50, 𝛾𝛾𝐿𝐿𝐿𝐿 = 1.45 (1)(1)(1)(1)(20526.2𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) − (1.25)(7466.6𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) − (1.5)(0𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)
(1.45)(1931.27𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)
= 4.0
9.3.2 Shear
𝑅𝑅𝐹𝐹 =
𝜙𝜙𝑐𝑐𝜙𝜙𝑠𝑠𝜙𝜙𝑖𝑖𝑉𝑉𝑖𝑖 − 𝛾𝛾𝑝𝑝𝑝𝑝 𝑉𝑉𝑝𝑝𝑝𝑝 − 𝛾𝛾𝑝𝑝𝑊𝑊𝑉𝑉𝑝𝑝𝑊𝑊
𝛾𝛾𝐿𝐿𝐿𝐿 𝑉𝑉𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿
At 10.388ft and 142.908ft (location where stirrup spacing increases)
𝜙𝜙𝑐𝑐 = 𝜙𝜙𝑠𝑠 = 1.0, 𝜙𝜙𝑖𝑖 = 0.9
𝑉𝑉𝑖𝑖 = 518.10𝑘𝑘𝑠𝑠𝑘𝑘
𝑉𝑉𝑝𝑝𝑝𝑝 = 147.84𝑘𝑘𝑠𝑠𝑘𝑘
𝑉𝑉𝑝𝑝𝑊𝑊 = 0.0𝑘𝑘
𝑘𝑘𝑠𝑠𝑘𝑘
𝑉𝑉𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿 = 90.13 𝑔𝑔𝑠𝑠𝐴𝐴𝑑𝑑𝐴𝐴𝐴𝐴
𝑅𝑅𝐹𝐹 =
𝛾𝛾𝑝𝑝𝑝𝑝 = 1.25, 𝛾𝛾𝑝𝑝𝑊𝑊 = 1.50, 𝛾𝛾𝐿𝐿𝐿𝐿 = 1.45 (1)(1)(0.9)(518.10𝑘𝑘𝑠𝑠𝑘𝑘) − (1.25)(147.84𝑘𝑘𝑠𝑠𝑘𝑘) − (1.5)(0𝑘𝑘𝑠𝑠𝑘𝑘)
(1.45)(90.13𝑘𝑘𝑠𝑠𝑘𝑘)
= 4.29
9.3.3 Bending Stress – Service III limit state
In accordance with WSDOT BDM 13.1.1 Service III ratings for legal loads can be ignored at the discretion of the state Load Rating Engineer. Without a variance for this structure, the Service III rating factor will be computed.

## Slide 185
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
𝑅𝑅𝐹𝐹 =
𝑓𝑓𝑅𝑅 − 𝛾𝛾𝑝𝑝𝑝𝑝 𝑓𝑓𝑝𝑝𝑝𝑝 − 𝛾𝛾𝑝𝑝𝑊𝑊𝑓𝑓𝑝𝑝𝑊𝑊
𝛾𝛾𝐿𝐿𝐿𝐿 𝑓𝑓𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿
For load rating we use the AASHTO specified tension limit and live load factor
𝑐𝑐
𝑓𝑓𝑅𝑅 = 𝑓𝑓𝑠𝑠𝑔𝑔𝑐𝑐𝑔𝑔𝑑𝑑 − 𝑓𝑓𝑑𝑑𝑠𝑠 = 0.19𝜆𝜆�𝑓𝑓′ − 𝑓𝑓𝑑𝑑𝑠𝑠
Before we can compute the stress in the girder due to the prestressing, we must compute the effective prestress accounting for the elastic gain for to the Type 3-3 loading.
∆𝑓𝑓𝑑𝑑𝐿𝐿𝐿𝐿 =
𝐸𝐸𝑑𝑑 𝑀𝑀𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿�𝑌𝑌𝑠𝑠𝑐𝑐 − 𝑌𝑌𝑠𝑠𝑔𝑔 + 𝐴𝐴�
𝐸𝐸 𝐼𝐼
𝑐𝑐 𝑐𝑐
=
5886.891 𝑘𝑘𝑠𝑠𝑠𝑠 1243580.6𝑠𝑠𝑠𝑠4
28500𝑘𝑘𝑠𝑠𝑠𝑠 (1931.27𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(48.867𝑠𝑠𝑠𝑠 − 35.657𝑠𝑠𝑠𝑠 + 31.477𝑠𝑠𝑠𝑠) 12𝑠𝑠𝑠𝑠
� �
1𝑓𝑓𝑓𝑓
= 4.032𝑘𝑘𝑠𝑠𝑠𝑠
𝑃𝑃 = (13.237𝑠𝑠𝑠𝑠2)(172.059𝑘𝑘𝑠𝑠𝑠𝑠 + 4.032𝑘𝑘𝑠𝑠𝑠𝑠) = 2330.92𝑘𝑘𝑠𝑠𝑘𝑘
−2330.92𝑘𝑘𝑠𝑠𝑘𝑘 (−2330.92𝑘𝑘𝑠𝑠𝑘𝑘)(31.477𝑠𝑠𝑠𝑠)
𝑓𝑓𝑑𝑑𝑠𝑠 = 923.531𝑠𝑠𝑠𝑠2 + 20594.8𝑠𝑠𝑠𝑠3
= −6.086𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑅𝑅 = 0.19(1.0)√8.7𝑘𝑘𝑠𝑠𝑠𝑠 − (−6.086𝑘𝑘𝑠𝑠𝑠𝑠) = 0.560𝑘𝑘𝑠𝑠𝑠𝑠 − (−6.086𝑘𝑘𝑠𝑠𝑠𝑠) = 6.647𝑘𝑘𝑠𝑠𝑠𝑠
𝛾𝛾𝐿𝐿𝐿𝐿 = 1.0
6.647𝑘𝑘𝑠𝑠𝑠𝑠 − (1.0)(4.268𝑘𝑘𝑠𝑠𝑠𝑠) − 1.0(0𝑘𝑘𝑠𝑠𝑠𝑠)
(1.0)(0.909𝑘𝑘𝑠𝑠𝑠𝑠)
𝑅𝑅𝐹𝐹 = = 2.62
9.3.4 Special Hauling Vehicles (SHV)
WSDOT policy (BDM 13.2.19) requires bridges to be load rated for SHVs if the rating factor for Type 3, Type 3S2, or Type3-3 are less than 1.35. The legal load rating factors exceed this threshold, so the additional load rating analysis is not required.
9.4 Permit Loads
WSDOT load rates bridges for two standard overload vehicles, Overload 1 (OL1) and Overload 2 (OL2). The vehicle details are presented in WSDOT BDM 13.1.5.
The load ratings for the permit loads are the same as the legal loads (with the obvious exception of the live load effects and load factors being different).
In accordance with WSDOT BDM 13.1.1 Service III ratings for permit loads can be ignored at the discretion of the state Load Rating Engineer. Without a variance for this structure, the Service III rating factor is computed.
The rating factors are summarized in Table 9-1.
Table 9-1: Load rating summary for permit vehicles.
Permit Vehicle | Moment Rating | Shear Rating | Service III Stress Rating
OL1 | 3.58 | 3.98 | 1.98
OL2 | 1.95 | 2.18 | 1.15
WSDOT also evaluates the optional reinforcement yielding check (MBE 6A.5.4.2.2b). The stress in the prestressing steel nearest the extreme tension fiber should not exceed 0.9𝑓𝑓𝑝𝑝 . The analysis method used by PGSuper follows MBE A3.13.4.2b.
𝑓𝑓𝑔𝑔 = 0.9𝑓𝑓𝑝𝑝 = (0.9)(0.9)𝑓𝑓𝑑𝑑𝑎𝑎 = (0.9)(0.9)(270𝑘𝑘𝑠𝑠𝑠𝑠) = 218.7𝑘𝑘𝑠𝑠𝑠𝑠
Moment beyond cracking
𝑀𝑀𝑠𝑠𝑐𝑐𝑔𝑔 = 𝛾𝛾𝑝𝑝𝑝𝑝 𝑀𝑀𝑝𝑝𝑝𝑝 + 𝛾𝛾𝑝𝑝𝑊𝑊𝑀𝑀𝑝𝑝𝑊𝑊 + 𝛾𝛾𝐿𝐿𝐿𝐿 𝑀𝑀𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿 − 𝑀𝑀𝑐𝑐𝑔𝑔

## Slide 186
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
Unlike the other permit rating cases where the one loaded lane live load distribution factor is used (MBE 6A.4.5.4.2b), use the governing of one loaded lane and two or more loaded lanes for these calculations (MBE C6A.5.4.2.2b).
For OL1, 𝑀𝑀𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿 = 2605.89𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 per girder. For OL2, 𝑀𝑀𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿 = 4794.03𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 per girder
𝑀𝑀𝑠𝑠𝑐𝑐𝑔𝑔 = (1.0)(7466.6𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) + (1.0)(0) + (1.0)(4794.03𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓) − 14707.13𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓 = −2446.5𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
Because 𝑀𝑀𝑠𝑠𝑐𝑐𝑔𝑔 < 0, the loads aren’t enough to cause cracking, so take 𝑀𝑀𝑠𝑠𝑐𝑐𝑔𝑔 = 0.0𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓
The additional stress transferred to the reinforcement due to cracking is
fbcr = E
Es Mbcr(ds − c)
I
g cr
= 0.0ksi
fs = fpe + fbcr
Compute the effective prestress For OL1
∆𝑓𝑓𝑑𝑑𝐿𝐿𝐿𝐿 =
𝐸𝐸𝑑𝑑 𝑀𝑀𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿�𝑌𝑌𝑠𝑠𝑐𝑐 − 𝑌𝑌𝑠𝑠𝑔𝑔 + 𝐴𝐴�
𝐸𝐸 𝐼𝐼
𝑐𝑐 𝑐𝑐
=
5886.891 𝑘𝑘𝑠𝑠𝑠𝑠 1243580.6𝑠𝑠𝑠𝑠4
28500𝑘𝑘𝑠𝑠𝑠𝑠 (2065.89𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(48.867𝑠𝑠𝑠𝑠 − 35.657𝑠𝑠𝑠𝑠 + 31.477𝑠𝑠𝑠𝑠) 12𝑠𝑠𝑠𝑠
� �
1𝑓𝑓𝑓𝑓
= 4.312𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑑𝑑𝑒𝑒 = 172.056𝑘𝑘𝑠𝑠𝑠𝑠 + 4.312𝑘𝑘𝑠𝑠𝑠𝑠 = 176.37 𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 = 𝑓𝑓𝑑𝑑𝑒𝑒 + 𝑓𝑓𝑠𝑠𝑔𝑔𝑐𝑐 = 176.37𝑘𝑘𝑠𝑠𝑠𝑠 + 0𝑘𝑘𝑠𝑠𝑠𝑠 = 176.37𝑘𝑘𝑠𝑠𝑠𝑠
For OL2
𝑑𝑑𝐿𝐿𝐿𝐿
∆𝑓𝑓 =
𝐸𝐸𝑑𝑑 𝑀𝑀𝐿𝐿𝐿𝐿𝐿𝐿𝐿𝐿�𝑌𝑌𝑠𝑠𝑐𝑐 − 𝑌𝑌𝑠𝑠𝑔𝑔 + 𝐴𝐴�
𝐸𝐸 𝐼𝐼
𝑐𝑐 𝑐𝑐
=
5886.891 𝑘𝑘𝑠𝑠𝑠𝑠 1243580.6𝑠𝑠𝑠𝑠4
28500𝑘𝑘𝑠𝑠𝑠𝑠 (4794.03𝑘𝑘 ∙ 𝑓𝑓𝑓𝑓)(48.867𝑠𝑠𝑠𝑠 − 35.657𝑠𝑠𝑠𝑠 + 31.477𝑠𝑠𝑠𝑠) 12𝑠𝑠𝑠𝑠
� �
1𝑓𝑓𝑓𝑓
= 10.01𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑑𝑑𝑒𝑒 = 172.056𝑘𝑘𝑠𝑠𝑠𝑠 + 10.01𝑘𝑘𝑠𝑠𝑠𝑠 = 182.07 𝑘𝑘𝑠𝑠𝑠𝑠
𝑓𝑓𝑠𝑠 = 182.07𝑘𝑘𝑠𝑠𝑠𝑠
Yield stress ratio
𝑆𝑆𝑅𝑅 =
𝑓𝑓𝑔𝑔
𝑓𝑓𝑠𝑠
OL1
𝑆𝑆𝑅𝑅 =
218.7𝑘𝑘𝑠𝑠𝑠𝑠
176.37𝑘𝑘𝑠𝑠𝑠𝑠
= 1.24
OL2
𝑆𝑆𝑅𝑅 =
218.7𝑘𝑘𝑠𝑠𝑠𝑠
182.07𝑘𝑘𝑠𝑠𝑠𝑠
= 1.20
10 Software
PGSuper is precast-prestressed girder design, analysis, and load rating software. PGSuper is part of the BridgeLink Bridge Engineering Application Suite jointly developed by the Washington State and Texas Departments of Transportation.
Download from http://www.wsdot.wa.gov/eesc/bridge/software This design example is based on version 7.0.

## Slide 187
Precast, Prestressed Girder Design Example – PGSuper Training (11/16/2022)
11 References
AASHTO, LRFD Bridge Design Specifications, Ninth Edition 2020, American Association of State Highway and Transportation Officials, Washington, D.C., 2020
Brice, R., Khaleghi, B., Seguirant, S., “Design optimization for fabrication of pretensioned concrete bridge girders: An example problem”, PCI JOURNAL, Prestressed Concrete Institute, Chicago, IL, Vol. 54, No. 4, Fall 2009, pp.73-111
Brice, R. “Designing Precast, Prestressed Concrete Bridge Girders for Lateral Stability: An Owner’s Perspective”, Aspire, (PCI) Winter 2018, pp.10-12
PCI (Precast/Prestressed Concrete Institute). 2016. Recommended Practice for Lateral Stability of Precast, Prestressed Concrete Bridge Girders. CB-02-16-E. Chicago, IL: PCI
PCI, Precast Prestressed Concrete Bridge Design Manual, Vol 1 & 2, Precast Concrete Institute, Chicago, Illinois, 1997
Seguirant, S. J., "New Deep WSDOT Standard Sections Extend Spans of Prestressed Concrete Girders," PCI JOURNAL, Prestressed Concrete Institute, Chicago, IL, Vol. 43, No. 4, July-August 1998, pp. 92-119
Seguirant, S. J., R. Brice, and B. Khaleghi. 2005, “Flexural Strength of Reinforced and Prestressed Concrete T-Beams,” PCI JOURNAL, Prestressed Concrete Institute, Chicago, IL, Vol. 50, No. 1, January-February 2005, pp. 44-73.
WSDOT, Bridge Design Manual, Washington State Department of Transportation
WSDOT, PGSuper Technical Guide, Washington State Department of Transportation